Table 1.  Crystal data and structure refinement for 2008sjc0003.

Identification code 	2008sjc0003 (SF5)

Empirical formula 	C20 H20 Cu F6 N4 P

Formula weight 	524.91

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Tetragonal

Space group 	I-4

Unit cell dimensions	a = 12.50090(10) Å	a= 90º.

b = 12.50090(10) Å	b= 90º.

c = 6.91330(10) Å	g = 90º.

Volume	1080.36(2) Å3

Z	2

Density (calculated)	1.614 Mg/m3

Absorption coefficient	1.151 mm-1

F(000)	532

Crystal size	0.60 x 0.15 x 0.12 mm3

Theta range for data collection	3.26 to 27.46º.

Index ranges	-16<=h<=16, -16<=k<=16, -8<=l<=8

Reflections collected	9784

Independent reflections	1236 [R(int) = 0.0331]

Completeness to theta = 27.46º	99.7 %

Absorption correction	Semi-empirical from equivalents

Max. and min. transmission	0.8742 and 0.5450

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	1236 / 0 / 73

Goodness-of-fit on F2	1.116

Final R indices [I>2sigma(I)]	R1 = 0.0250, wR2 = 0.0636

R indices (all data)	R1 = 0.0263, wR2 = 0.0643

Absolute structure parameter	0.043(13)

Largest diff. peak and hole	0.273 and -0.380 e.Å-3

Table 2.  Atomic coordinates ( x 104) and equivalent isotropic displacement parameters (Å2x 103)

for 2008sjc0003.  U(eq) is defined as one third of the trace of the orthogonalized Uij tensor.

________________________________________________________________________________

x	y	z	U(eq)

________________________________________________________________________________

C(1)	2846(1)	5539(2)	8342(3)	24(1)

C(2)	2117(2)	6000(2)	7107(3)	27(1)

C(3)	2470(2)	6732(2)	5747(3)	30(1)

C(4)	3547(2)	6986(2)	5704(3)	31(1)

C(5)	4232(2)	6473(2)	6961(3)	25(1)

N(1)	3905(1)	5754(1)	8275(2)	21(1)

Cu(1)	5000	5000	10000	23(1)

P(1)	5000	10000	7500	20(1)

F(1)	5000	10000	5185(3)	47(1)

F(2)	5347(1)	8778(1)	7500(3)	54(1)

________________________________________________________________________________

Table 3.   Bond lengths [Å] and angles [º] for 2008sjc0003.

_____________________________________________________

C(1)-N(1) 	1.352(2)

C(1)-C(2) 	1.376(3)

C(2)-C(3) 	1.384(3)

C(3)-C(4) 	1.384(3)

C(4)-C(5) 	1.378(3)

C(5)-N(1) 	1.342(2)

N(1)-Cu(1) 	2.0454(16)

Cu(1)-N(1)#1 	2.0454(16)

Cu(1)-N(1)#2 	2.0454(16)

Cu(1)-N(1)#3 	2.0454(16)

P(1)-F(2)#4 	1.5874(14)

P(1)-F(2)#5 	1.5874(14)

P(1)-F(2) 	1.5874(14)

P(1)-F(2)#6 	1.5874(14)

P(1)-F(1)#4 	1.600(2)

P(1)-F(1) 	1.600(2)

N(1)-C(1)-C(2)	122.98(18)

C(1)-C(2)-C(3)	119.16(18)

C(4)-C(3)-C(2)	118.48(19)

C(5)-C(4)-C(3)	119.0(2)

N(1)-C(5)-C(4)	123.32(19)

C(5)-N(1)-C(1)	117.05(16)

C(5)-N(1)-Cu(1)	119.98(13)

C(1)-N(1)-Cu(1)	122.93(13)

N(1)#1-Cu(1)-N(1)#2	108.69(9)

N(1)#1-Cu(1)-N(1)	109.86(5)

N(1)#2-Cu(1)-N(1)	109.86(5)

N(1)#1-Cu(1)-N(1)#3	109.86(5)

N(1)#2-Cu(1)-N(1)#3	109.86(5)

N(1)-Cu(1)-N(1)#3	108.69(9)

F(2)#4-P(1)-F(2)#5	90.000(1)

F(2)#4-P(1)-F(2)	90.000(1)

F(2)#5-P(1)-F(2)	179.98(13)

F(2)#4-P(1)-F(2)#6	179.98(13)

F(2)#5-P(1)-F(2)#6	90.000(1)

F(2)-P(1)-F(2)#6	90.000(1)

F(2)#4-P(1)-F(1)#4	89.99(7)

F(2)#5-P(1)-F(1)#4	90.01(7)

F(2)-P(1)-F(1)#4	90.01(7)

F(2)#6-P(1)-F(1)#4	89.99(7)

F(2)#4-P(1)-F(1)	90.01(7)

F(2)#5-P(1)-F(1)	89.99(7)

F(2)-P(1)-F(1)	89.99(7)

F(2)#6-P(1)-F(1)	90.01(7)

F(1)#4-P(1)-F(1)	180.000(1)

_____________________________________________________________

Symmetry transformations used to generate equivalent atoms:

#1 y,-x+1,-z+2    #2 -y+1,x,-z+2    #3 -x+1,-y+1,z

#4 y-1/2,-x+3/2,-z+3/2    #5 -x+1,-y+2,z    #6 -y+3/2,x+1/2,-z+3/2

Table 4.   Anisotropic displacement parameters (Å2x 103)for 2008sjc0003.  The anisotropic

displacement factor exponent takes the form: -2p2[ h2a*2U11 + ... + 2 h k a* b* U12 ]

______________________________________________________________________________

U11	U22	U33	U23	U13	U12

______________________________________________________________________________

C(1)	20(1) 	20(1)	31(1) 	0(1)	-1(1) 	-3(1)

C(2)	20(1) 	26(1)	36(1) 	-6(1)	-4(1) 	0(1)

C(3)	30(1) 	33(1)	27(1) 	-1(1)	-5(1) 	9(1)

C(4)	33(1) 	33(1)	27(1) 	7(1)	5(1) 	6(1)

C(5)	20(1) 	27(1)	29(1) 	4(1)	5(1) 	1(1)

N(1)	18(1) 	20(1)	26(1) 	0(1)	0(1) 	1(1)

Cu(1)	19(1) 	19(1)	29(1) 	0	0 	0

P(1)	20(1) 	20(1)	20(1) 	0	0 	0

F(1)	70(1) 	49(1)	22(1) 	0	0 	10(1)

F(2)	75(1) 	25(1)	61(1) 	4(1)	-3(1) 	13(1)

______________________________________________________________________________