|  | Departmental Single Crystal X-Ray Diffraction Service School of Chemistry - University of Southampton Contact: Dr Mark E Light, light@soton.ac.uk, ex 29429 |
| --- | --- |

Table 1. Crystal data and structure refinement details.

Identification code 	06skc0036p21c

Empirical formula 	C10H20N2O6

Formula weight 	264.28

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P21/c

Unit cell dimensions	a = 9.6872(5) Å	( = 90°

b = 6.5461(3) Å	( = 102.698(3)°

c = 10.8209(5) Å	(  = 90°

Volume	669.41(6) Å3

Z	2

Density (calculated)	1.311 Mg / m3

Absorption coefficient	0.108 mm(1

F(000)	284

Crystal	block; colourless

Crystal size	0.24 ( 0.18 ( 0.10 mm3

( range for data collection	3.66 ( 23.31°

Index ranges	(10 ( h ( 10, (7 ( k ( 7, (12 ( l ( 12

Reflections collected	6699

Independent reflections	954 [Rint = 0.0315]

Completeness to ( = 23.31°	99.3 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.9893 and 0.9745

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	954 / 0 / 85

Goodness-of-fit on F2	1.094

Final R indices [F2 > 2((F2)]	R1 = 0.0280, wR2 = 0.0683

R indices (all data)	R1 = 0.0332, wR2 = 0.0714

Extinction coefficient	0.042(8)

Largest diff. peak and hole	0.118 and (0.146 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit ). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: Sheldrick, G. M. SADABS - Bruker Nonius area detector scaling and absorption correction - V2.10 Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: Cameron - A Molecular Graphics Package. (D. M. Watkin, L. Pearce and C. K. Prout, Chemical Crystallography Laboratory, University of Oxford, 1993).

Special details:

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C1	9519(1)	810(2)	10216(1)	22(1)	1

O1A	8476(1)	1451(2)	9433(1)	30(1)	1

O1B	9879(1)	1356(2)	11361(1)	32(1)	1

C23	12861(2)	2686(2)	13705(2)	31(1)	1

C22	11861(2)	1087(2)	14003(1)	28(1)	1

C26	13352(1)	(1508(2)	13322(1)	26(1)	1

C25	14294(1)	195(2)	13058(1)	31(1)	1

N21	11891(1)	(726(2)	13187(1)	22(1)	1

O24	14266(1)	1901(2)	13863(1)	33(1)	1

Table 3. Bond lengths [Å] and angles [°].

C1(O1A	1.2402(16)

C1(O1B	1.2630(16)

C1(C1i	1.551(3)

C23(O24	1.4289(17)

C23(C22	1.508(2)

C23(H23A	0.9900

C23(H23B	0.9900

C22(N21	1.4836(17)

C22(H22A	0.9900

C22(H22B	0.9900

C26(N21	1.4814(16)

C26(C25	1.507(2)

C26(H26A	0.9900

C26(H26B	0.9900

C25(O24	1.4205(17)

C25(H25A	0.9900

C25(H25B	0.9900

N21(H21B	0.9200

N21(H21A	0.9200

O1A(C1(O1B	125.63(12)

O1A(C1(C1i	118.60(14)

O1B(C1(C1i	115.77(14)

O24(C23(C22	111.38(11)

O24(C23(H23A	109.4

C22(C23(H23A	109.4

O24(C23(H23B	109.4

C22(C23(H23B	109.4

H23A(C23(H23B	108.0

N21(C22(C23	109.28(11)

N21(C22(H22A	109.8

C23(C22(H22A	109.8

N21(C22(H22B	109.8

C23(C22(H22B	109.8

H22A(C22(H22B	108.3

N21(C26(C25	109.29(11)

N21(C26(H26A	109.8

C25(C26(H26A	109.8

N21(C26(H26B	109.8

C25(C26(H26B	109.8

H26A(C26(H26B	108.3

O24(C25(C26	111.78(11)

O24(C25(H25A	109.3

C26(C25(H25A	109.3

O24(C25(H25B	109.3

C26(C25(H25B	109.3

H25A(C25(H25B	107.9

C26(N21(C22	111.18(10)

C26(N21(H21B	109.4

C22(N21(H21B	109.4

C26(N21(H21A	109.4

C22(N21(H21A	109.4

H21B(N21(H21A	108.0

C25(O24(C23	110.82(10)

Symmetry transformations used to generate equivalent atoms:

(i) (x+2,(y,(z+2

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C1	23(1) 	23(1)	20(1) 	2(1)	6(1) 	(2(1)

O1A	27(1) 	40(1)	23(1) 	(1(1)	3(1) 	11(1)

O1B	35(1) 	36(1)	22(1) 	(5(1)	1(1) 	13(1)

C23	29(1) 	23(1)	39(1) 	(2(1)	3(1) 	1(1)

C22	27(1) 	29(1)	28(1) 	(4(1)	6(1) 	1(1)

C26	24(1) 	25(1)	29(1) 	(1(1)	3(1) 	3(1)

C25	25(1) 	31(1)	39(1) 	(2(1)	9(1) 	(2(1)

N21	22(1) 	23(1)	20(1) 	2(1)	3(1) 	(3(1)

O24	25(1) 	28(1)	42(1) 	(2(1)	2(1) 	(4(1)

Table 5. Hydrogen bonds [Å and °].

D(H···A	d(D(H)	d(H···A)	d(D···A)	((DHA)

N21(H21A...O1B	0.92	2.06	2.8049(14)	137.0

N21(H21B...O1Bii	0.92	1.77	2.6825(14)	173.0

N21(H21B...O1Aii	0.92	2.59	3.2523(14)	129.1

N21(H21A...O1Ai	0.92	2.06	2.8188(14)	139.3

Symmetry transformations used to generate equivalent atoms:

(i) (x+2,(y,(z+2    (ii) (x+2,y(1/2,(z+5/2