|  | Departmental Single Crystal X-Ray Diffraction Service School of Chemistry - University of Southampton Contact: Dr Mark E Light, light@soton.ac.uk, ex 29429 |
| --- | --- |

Table 1. Crystal data and structure refinement details.

Identification code 	04skc0002a

Empirical formula 	C8H12N2O6

Formula weight 	232.20

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Triclinic

Space group 	P(1

Unit cell dimensions	a = 7.5625(18) Å	( = 66.47(3)°

b = 8.340(3) Å	( = 71.90(2)°

c = 9.193(6) Å	(  = 73.03(2)°

Volume	495.8(4) Å3

Z	2

Density (calculated)	1.555 Mg / m3

Absorption coefficient	0.135 mm(1

F(000)	244

Crystal	lath; colourless

Crystal size	0.15 ( 0.08 ( 0.02 mm3

( range for data collection	3.56 ( 27.49°

Index ranges	(9 ( h ( 9, (10 ( k ( 10, (11 ( l ( 11

Reflections collected	7286

Independent reflections	2236 [Rint = 0.0805]

Completeness to ( = 27.49°	98.3 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.9973 and 0.9801

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	2236 / 0 / 151

Goodness-of-fit on F2	1.033

Final R indices [F2 > 2((F2)]	R1 = 0.0632, wR2 = 0.1088

R indices (all data)	R1 = 0.1252, wR2 = 0.1311

Extinction coefficient	0.022(5)

Largest diff. peak and hole	0.316 and (0.325 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit ). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: Sheldrick, G. M. SADABS - Bruker Nonius area detector scaling and absorption correction - V2.10 Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: Cameron - A Molecular Graphics Package. (D. M. Watkin, L. Pearce and C. K. Prout, Chemical Crystallography Laboratory, University of Oxford, 1993).

Special details:

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C1	3077(4)	7283(4)	9353(3)	17(1)	1

C2	1351(3)	6841(4)	9187(3)	17(1)	1

C3	103(3)	8576(3)	8354(3)	16(1)	1

C4	(1494(4)	8198(4)	7922(3)	18(1)	1

O1A	4685(2)	6754(3)	8495(2)	20(1)	1

O1B	2843(2)	8104(2)	10274(2)	21(1)	1

O2	1844(2)	5695(2)	8256(2)	18(1)	1

O3	1246(2)	9621(3)	6963(2)	21(1)	1

O4A	(1585(3)	8729(3)	6489(2)	22(1)	1

O4B	(2669(2)	7348(2)	9147(2)	20(1)	1

C22	6536(4)	12946(4)	6005(3)	20(1)	1

C24	4345(4)	12032(4)	5546(3)	22(1)	1

C25	4050(4)	11616(4)	7163(3)	22(1)	1

C26	8196(4)	13701(4)	5762(3)	26(1)	1

N21	5418(3)	12204(3)	7425(2)	21(1)	1

N23	5886(3)	12868(3)	4856(3)	20(1)	1

Table 3. Bond lengths [Å] and angles [°].

C1(O1B	1.232(3)

C1(O1A	1.290(3)

C1(C2	1.521(4)

C2(O2	1.425(3)

C2(C3	1.529(4)

C2(H2	1.0000

C3(O3	1.416(3)

C3(C4	1.528(4)

C3(H3	1.0000

C4(O4A	1.228(3)

C4(O4B	1.292(3)

O1A(H1O	0.8400

O2(H2A	0.8400

O3(H3A	0.8400

C22(N23	1.325(3)

C22(N21	1.333(3)

C22(C26	1.483(4)

C24(C25	1.345(4)

C24(N23	1.382(3)

C24(H24	0.9500

C25(N21	1.383(3)

C25(H25	0.9500

C26(H26A	0.9800

C26(H26B	0.9800

C26(H26C	0.9800

N21(H21	0.8800

N23(H23	0.8800

O1B(C1(O1A	125.4(2)

O1B(C1(C2	118.5(2)

O1A(C1(C2	116.1(2)

O2(C2(C1	112.6(2)

O2(C2(C3	108.7(2)

C1(C2(C3	108.7(2)

O2(C2(H2	108.9

C1(C2(H2	108.9

C3(C2(H2	108.9

O3(C3(C4	111.7(2)

O3(C3(C2	109.3(2)

C4(C3(C2	110.9(2)

O3(C3(H3	108.3

C4(C3(H3	108.3

C2(C3(H3	108.3

O4A(C4(O4B	125.6(2)

O4A(C4(C3	119.2(2)

O4B(C4(C3	115.1(2)

C1(O1A(H1O	109.5

C2(O2(H2A	109.5

C3(O3(H3A	109.5

N23(C22(N21	106.9(2)

N23(C22(C26	126.7(2)

N21(C22(C26	126.5(2)

C25(C24(N23	106.4(2)

C25(C24(H24	126.8

N23(C24(H24	126.8

C24(C25(N21	106.8(2)

C24(C25(H25	126.6

N21(C25(H25	126.6

C22(C26(H26A	109.5

C22(C26(H26B	109.5

H26A(C26(H26B	109.5

C22(C26(H26C	109.5

H26A(C26(H26C	109.5

H26B(C26(H26C	109.5

C22(N21(C25	109.6(2)

C22(N21(H21	125.2

C25(N21(H21	125.2

C22(N23(C24	110.2(2)

C22(N23(H23	124.9

C24(N23(H23	124.9

Symmetry transformations used to generate equivalent atoms:

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C1	17(1) 	16(2)	14(1) 	1(1)	(5(1) 	(6(1)

C2	15(1) 	22(2)	17(1) 	(8(1)	(3(1) 	(7(1)

C3	13(1) 	18(2)	17(1) 	(4(1)	(2(1) 	(6(1)

C4	13(1) 	17(2)	22(1) 	(5(1)	(6(1) 	(1(1)

O1A	12(1) 	29(1)	21(1) 	(10(1)	(4(1) 	(5(1)

O1B	18(1) 	28(1)	20(1) 	(10(1)	(6(1) 	(5(1)

O2	17(1) 	17(1)	20(1) 	(5(1)	(6(1) 	(3(1)

O3	18(1) 	26(1)	18(1) 	(1(1)	(7(1) 	(10(1)

O4A	20(1) 	30(1)	17(1) 	(4(1)	(8(1) 	(7(1)

O4B	14(1) 	25(1)	19(1) 	(4(1)	(4(1) 	(6(1)

C22	19(2) 	17(2)	21(1) 	(8(1)	(4(1) 	0(1)

C24	20(2) 	23(2)	26(2) 	(9(1)	(7(1) 	(4(1)

C25	21(2) 	23(2)	24(2) 	(7(1)	(7(1) 	(7(1)

C26	20(2) 	26(2)	32(2) 	(9(1)	(8(1) 	(5(1)

N21	22(1) 	25(1)	19(1) 	(8(1)	(6(1) 	(5(1)

N23	22(1) 	21(1)	16(1) 	(5(1)	(4(1) 	(3(1)

Table 5. Hydrogen bonds [Å and °].

D(H···A	d(D(H)	d(H···A)	d(D···A)	((DHA)

O3(H3A...O4A	0.84	2.17	2.663(3)	117.2

O2(H2A...O4Bi	0.84	1.98	2.773(3)	156.4

O3(H3A...O4Aii	0.84	2.19	2.871(3)	137.6

O1A(H1O...O4Biii	0.84	1.64	2.485(2)	178.0

O1A(H1O...O4Aiii	0.84	2.78	3.335(3)	124.8

N21(H21...O1Biv	0.88	1.93	2.715(3)	148.2

N23(H23...O2v	0.88	1.98	2.825(3)	159.7

N23(H23...O1Av	0.88	2.50	3.122(3)	128.7

Symmetry transformations used to generate equivalent atoms:

(i) (x,(y+1,(z+2    (ii) (x,(y+2,(z+1    (iii) x+1,y,z

(iv)  (x+1,(y+2,(z+2    (v) (x+1,(y+2,(z+1