|  | University of Southampton · School of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	2006src0701   (306-134-A)

Empirical formula 	C7H14Cl4N3O2P3

Formula weight 	406.92

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Triclinic

Space group 	P(1

Unit cell dimensions	a = 8.03340(10) Å	( = 97.4510(10)°

b = 10.0791(2) Å	( = 111.0060(10)°

c = 11.1829(3) Å	(  = 103.9920(10)°

Volume	796.48(3) Å3

Z	2

Density (calculated)	1.697 Mg / m3

Absorption coefficient	1.043 mm(1

F(000)	412

Crystal	slab; colourless

Crystal size	0.38 ( 0.20 ( 0.05 mm3

( range for data collection	2.01 ( 27.49°

Index ranges	(10 ( h ( 10, (13 ( k ( 13, (14 ( l ( 14

Reflections collected	16270

Independent reflections	3645 [Rint = 0.0254]

Completeness to ( = 27.49°	99.5 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.9497 and 0.6926

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	3645 / 0 / 174

Goodness-of-fit on F2	1.090

Final R indices [F2 > 2((F2)]	R1 = 0.0262, wR2 = 0.0648

R indices (all data)	R1 = 0.0318, wR2 = 0.0678

Largest diff. peak and hole	0.287 and (0.490 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing, Acta Cryst. A51 (1995) 33(37; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421(426). Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: Cameron - A Molecular Graphics Package. (D. M. Watkin, L. Pearce and C. K. Prout, Chemical Crystallography Laboratory, University of Oxford, 1993).

Special details:

P1-P2 = 2.755, P2-P3 = 2.744, P1-P3 = 2.768, max deviation from mean plane = 0.084 (P1).

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C1	670(2)	4929(2)	6635(2)	16(1)	1

C2	898(2)	4277(2)	7823(2)	13(1)	1

C3	2472(2)	5345(2)	9047(2)	16(1)	1

C4	(920(2)	4066(2)	8057(2)	17(1)	1

C5	(2708(2)	3112(2)	6905(2)	26(1)	1

C6	1360(2)	2894(2)	7567(2)	19(1)	1

C7	1330(3)	2010(2)	8572(2)	26(1)	1

N1	6005(2)	6441(2)	7435(2)	19(1)	1

N2	6559(2)	9138(2)	7129(2)	19(1)	1

N3	3767(2)	7916(2)	7839(2)	18(1)	1

O1	2432(2)	5335(1)	6455(1)	15(1)	1

O2	4234(2)	5811(1)	8875(1)	17(1)	1

P1	4157(1)	6437(1)	7650(1)	13(1)	1

P2	7197(1)	7770(1)	7172(1)	15(1)	1

P3	4835(1)	9217(1)	7480(1)	13(1)	1

Cl1	9854(1)	8302(1)	8497(1)	22(1)	1

Cl2	7483(1)	7193(1)	5499(1)	28(1)	1

Cl3	5697(1)	10926(1)	8943(1)	22(1)	1

Cl4	3039(1)	9758(1)	6001(1)	25(1)	1

Table 3. Bond lengths [Å] and angles [°].

C1(O1	1.4686(19)

C1(C2	1.530(2)

C2(C3	1.533(2)

C2(C4	1.544(2)

C2(C6	1.545(2)

C3(O2	1.4684(19)

C4(C5	1.527(2)

C6(C7	1.525(2)

N1(P2	1.5747(15)

N1(P1	1.5856(14)

N2(P2	1.5839(14)

N2(P3	1.5860(14)

N3(P3	1.5678(14)

N3(P1	1.5985(14)

O1(P1	1.5753(11)

O2(P1	1.5688(12)

P2(Cl2	1.9951(6)

P2(Cl1	2.0027(6)

P3(Cl3	2.0007(6)

P3(Cl4	2.0043(6)

O1(C1(C2	111.38(12)

C1(C2(C3	108.25(13)

C1(C2(C4	108.13(13)

C3(C2(C4	106.54(13)

C1(C2(C6	109.31(13)

C3(C2(C6	111.24(13)

C4(C2(C6	113.19(13)

O2(C3(C2	112.38(13)

C5(C4(C2	115.34(14)

C7(C6(C2	115.13(15)

P2(N1(P1	121.30(9)

P2(N2(P3	119.88(9)

P3(N3(P1	121.87(9)

C1(O1(P1	115.90(10)

C3(O2(P1	117.20(10)

O2(P1(O1	104.33(6)

O2(P1(N1	107.74(7)

O1(P1(N1	108.26(7)

O2(P1(N3	109.52(7)

O1(P1(N3	109.60(7)

N1(P1(N3	116.66(8)

N1(P2(N2	119.81(8)

N1(P2(Cl2	108.97(6)

N2(P2(Cl2	108.16(6)

N1(P2(Cl1	108.32(6)

N2(P2(Cl1	108.83(6)

Cl2(P2(Cl1	101.13(3)

N3(P3(N2	118.88(7)

N3(P3(Cl3	109.12(6)

N2(P3(Cl3	108.29(6)

N3(P3(Cl4	110.43(6)

N2(P3(Cl4	107.85(6)

Cl3(P3(Cl4	100.72(2)

Symmetry transformations used to generate equivalent atoms:

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C1	11(1) 	20(1)	15(1) 	6(1)	4(1) 	2(1)

C2	12(1) 	12(1)	13(1) 	4(1)	4(1) 	3(1)

C3	14(1) 	16(1)	14(1) 	4(1)	6(1) 	2(1)

C4	16(1) 	18(1)	19(1) 	6(1)	9(1) 	5(1)

C5	15(1) 	33(1)	25(1) 	8(1)	7(1) 	0(1)

C6	19(1) 	13(1)	26(1) 	5(1)	11(1) 	5(1)

C7	24(1) 	16(1)	40(1) 	14(1)	11(1) 	7(1)

N1	16(1) 	13(1)	32(1) 	7(1)	12(1) 	7(1)

N2	20(1) 	16(1)	32(1) 	11(1)	17(1) 	9(1)

N3	17(1) 	13(1)	29(1) 	6(1)	14(1) 	5(1)

O1	14(1) 	16(1)	14(1) 	4(1)	6(1) 	2(1)

O2	12(1) 	18(1)	16(1) 	7(1)	2(1) 	1(1)

P1	12(1) 	11(1)	16(1) 	4(1)	5(1) 	3(1)

P2	13(1) 	15(1)	19(1) 	6(1)	9(1) 	7(1)

P3	13(1) 	12(1)	16(1) 	4(1)	6(1) 	5(1)

Cl1	14(1) 	20(1)	28(1) 	7(1)	5(1) 	4(1)

Cl2	34(1) 	42(1)	22(1) 	10(1)	16(1) 	24(1)

Cl3	26(1) 	16(1)	19(1) 	(1(1)	8(1) 	3(1)

Cl4	24(1) 	27(1)	21(1) 	7(1)	2(1) 	13(1)