|  | Departmental Single Crystal X-Ray Diffraction Service School of Chemistry - University of Southampton Contact: Dr Mark E Light, light@soton.ac.uk, ex 29429 |
| --- | --- |

Table 1. Crystal data and structure refinement details.

Identification code 	06skc0053c2c

Empirical formula 	C10H16N4O5

Formula weight 	272.27

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	C2/c

Unit cell dimensions	a = 9.1937(6) Å	( = 90°

b = 13.5734(6) Å	( = 99.252(4)°

c = 10.5047(5) Å	(  = 90°

Volume	1293.83(12) Å3

Z	4

Density (calculated)	1.398 Mg / m3

Absorption coefficient	0.113 mm(1

F(000)	576

Crystal	fragment; colourless

Crystal size	0.15 ( 0.07 ( 0.02 mm3

( range for data collection	3.00 ( 27.47°

Index ranges	(11 ( h ( 11, (17 ( k ( 17, (13 ( l ( 13

Reflections collected	14887

Independent reflections	1488 [Rint = 0.1136]

Completeness to ( = 27.47°	99.9 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.9977 and 0.9833

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	1488 / 2 / 92

Goodness-of-fit on F2	1.072

Final R indices [F2 > 2((F2)]	R1 = 0.0485, wR2 = 0.1051

R indices (all data)	R1 = 0.0664, wR2 = 0.1131

Largest diff. peak and hole	0.297 and (0.304 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit ). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: Sheldrick, G. M. SADABS - Bruker Nonius area detector scaling and absorption correction - V2.10 Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: Cameron - A Molecular Graphics Package. (D. M. Watkin, L. Pearce and C. K. Prout, Chemical Crystallography Laboratory, University of Oxford, 1993).

Special details:

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C1	2109(2)	2982(1)	5183(2)	18(1)	1

O1A	1821(1)	3024(1)	6308(1)	22(1)	1

O1B	1842(1)	3629(1)	4332(1)	24(1)	1

C22	1926(2)	4182(1)	11476(2)	22(1)	1

C24	3382(2)	3952(1)	10020(2)	20(1)	1

C25	3652(2)	3236(1)	10926(2)	23(1)	1

C26	4023(2)	4145(2)	8833(2)	28(1)	1

N21	2732(2)	3393(1)	11816(1)	22(1)	1

N23	2290(2)	4533(1)	10390(1)	20(1)	1

O1W	0	4231(1)	7500	30(1)	1

Table 3. Bond lengths [Å] and angles [°].

C1(O1B	1.248(2)

C1(O1A	1.253(2)

C1(C1i	1.570(3)

C22(N21	1.319(2)

C22(N23	1.328(2)

C22(H22	0.9500

C24(C25	1.356(3)

C24(N23	1.380(2)

C24(C26	1.485(2)

C25(N21	1.374(2)

C25(H25	0.9500

C26(H26A	0.9800

C26(H26B	0.9800

C26(H26C	0.9800

N21(H21	0.8800

N23(H23	0.8800

O1W(H1W	0.905(15)

O1B(C1(O1A	126.55(15)

O1B(C1(C1i	117.16(18)

O1A(C1(C1i	116.29(18)

N21(C22(N23	108.37(15)

N21(C22(H22	125.8

N23(C22(H22	125.8

C25(C24(N23	105.72(15)

C25(C24(C26	131.56(17)

N23(C24(C26	122.71(16)

C24(C25(N21	107.63(15)

C24(C25(H25	126.2

N21(C25(H25	126.2

C24(C26(H26A	109.5

C24(C26(H26B	109.5

H26A(C26(H26B	109.5

C24(C26(H26C	109.5

H26A(C26(H26C	109.5

H26B(C26(H26C	109.5

C22(N21(C25	108.83(15)

C22(N21(H21	125.6

C25(N21(H21	125.6

C22(N23(C24	109.45(15)

C22(N23(H23	125.3

C24(N23(H23	125.3

Symmetry transformations used to generate equivalent atoms:

(i) (x+1/2,(y+1/2,(z+1

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C1	18(1) 	17(1)	18(1) 	(2(1)	5(1) 	(3(1)

O1A	29(1) 	20(1)	19(1) 	0(1)	10(1) 	3(1)

O1B	35(1) 	17(1)	21(1) 	2(1)	8(1) 	4(1)

C22	24(1) 	20(1)	22(1) 	(1(1)	7(1) 	1(1)

C24	19(1) 	22(1)	20(1) 	(2(1)	3(1) 	(2(1)

C25	23(1) 	24(1)	23(1) 	(1(1)	6(1) 	4(1)

C26	26(1) 	36(1)	23(1) 	2(1)	7(1) 	(2(1)

N21	27(1) 	21(1)	19(1) 	3(1)	6(1) 	1(1)

N23	23(1) 	17(1)	20(1) 	2(1)	5(1) 	1(1)

O1W	31(1) 	19(1)	45(1) 	0	23(1) 	0

Table 5. Hydrogen bonds [Å and °].

D(H···A	d(D(H)	d(H···A)	d(D···A)	((DHA)

N21(H21...O1Aii	0.88	1.90	2.7376(19)	157.4

N21(H21...O1Biii	0.88	2.34	2.9083(19)	122.7

N23(H23...O1Biv	0.88	1.91	2.7358(19)	156.2

O1W(H1W...O1Av	0.905(15)	1.889(18)	2.7804(16)	168.1(16)

Symmetry transformations used to generate equivalent atoms:

(i) (x+1/2,(y+1/2,(z+1    (ii) (x+1/2,(y+1/2,(z+2

(iii) x,y,z+1    (iv)  x,(y+1,z+1/2    (v) (x,y,(z+3/2