|  | # Departmental Single Crystal X-Ray Diffraction Service School of Chemistry - University of Southampton Contact: Dr Mark E Light, light@soton.ac.uk, ex 29429 |
| --- | --- |

Table 1. Crystal data and structure refinement details.

Identification code 	06skc0058p21c

Empirical formula 	C8H22N2O6

Formula weight 	242.28

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P21/c

Unit cell dimensions	a = 7.5550(3) Å	 = 90°

b = 10.9180(4) Å	 = 111.565(2)°

c = 8.1170(2) Å	  = 90°

Volume	622.67(4) Å3

Z	2

Density (calculated)	1.292 Mg / m3

Absorption coefficient	0.109 mm1

F(000)	264

Crystal	plate; colourless

Crystal size	0.40  0.20  0.18 mm3

 range for data collection	3.28  23.32°

Index ranges	8  h  8, 12  k  12, 8  l  8

Reflections collected	5898

Independent reflections	635 [Rint = 0.0337]

Completeness to  = 23.32°	70.9 %

Max. and min. transmission	0.9806 and 0.9576

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	635 / 3 / 85

Goodness-of-fit on F2	1.081

Final R indices [F2 > 2(F2)]	R1 = 0.0323, wR2 = 0.0793

R indices (all data)	R1 = 0.0373, wR2 = 0.0821

Extinction coefficient	0.054(12)

Largest diff. peak and hole	0.104 and 0.114 e Å3

Diffractometer: Nonius KappaCCD area detector ( scans and  scans to fill asymmetric unit ). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: Sheldrick, G. M. SADABS - Bruker Nonius area detector scaling and absorption correction - V2.10 Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: Cameron - A Molecular Graphics Package. (D. M. Watkin, L. Pearce and C. K. Prout, Chemical Crystallography Laboratory, University of Oxford, 1993).

Special details:

Table 2. Atomic coordinates [ 104], equivalent isotropic displacement parameters [Å2  103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C1	5853(3)	450(2)	5381(2)	18(1)	1

O1A	6976(2)	506(1)	4556(2)	23(1)	1

O1B	5970(2)	1039(1)	6721(2)	31(1)	1

C21	8765(3)	234(2)	1831(3)	24(1)	1

C23	7321(3)	2193(2)	2123(2)	23(1)	1

C24	5355(3)	655(2)	74(2)	19(1)	1

N22	6980(2)	854(1)	1774(2)	17(1)	1

O1W	8815(2)	2664(1)	4337(2)	32(1)	1

Table 3. Bond lengths [Å] and angles [°].

C1O1B	1.239(2)

C1O1A	1.261(2)

C1C1i	1.557(4)

C21N22	1.495(2)

C21H21A	0.9800

C21H21B	0.9800

C21H21C	0.9800

C23N22	1.493(2)

C23H23A	0.9800

C23H23B	0.9800

C23H23C	0.9800

C24N22	1.488(2)

C24C24ii	1.517(3)

C24H24A	0.9900

C24H24B	0.9900

N22H22	0.9300

O1WH1W	0.847(16)

O1WH2W	0.852(17)

O1BC1O1A	126.62(16)

O1BC1C1i	117.27(17)

O1AC1C1i	116.11(17)

N22C21H21A	109.5

N22C21H21B	109.5

H21AC21H21B	109.5

N22C21H21C	109.5

H21AC21H21C	109.5

H21BC21H21C	109.5

N22C23H23A	109.5

N22C23H23B	109.5

H23AC23H23B	109.5

N22C23H23C	109.5

H23AC23H23C	109.5

H23BC23H23C	109.5

N22C24C24ii	111.00(17)

N22C24H24A	109.4

C24iiC24H24A	109.4

N22C24H24B	109.4

C24iiC24H24B	109.4

H24AC24H24B	108.0

C24N22C23	110.17(14)

C24N22C21	112.95(13)

C23N22C21	110.30(13)

C24N22H22	107.7

C23N22H22	107.7

C21N22H22	107.7

H1WO1WH2W	106(2)

Symmetry transformations used to generate equivalent atoms:

(i) x+1,y,z+1    (ii) x+1,y,z

Table 4. Anisotropic displacement parameters [Å2 103]. The anisotropic displacement

factor exponent takes the form: 2 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C1	20(1) 	20(1)	17(1) 	2(1)	9(1) 	2(1)

O1A	24(1) 	26(1)	24(1) 	4(1)	14(1) 	6(1)

O1B	30(1) 	41(1)	27(1) 	18(1)	16(1) 	14(1)

C21	17(1) 	27(1)	29(1) 	1(1)	9(1) 	0(1)

C23	26(1) 	22(1)	21(1) 	4(1)	9(1) 	4(1)

C24	20(1) 	21(1)	15(1) 	1(1)	5(1) 	2(1)

N22	17(1) 	20(1)	15(1) 	1(1)	7(1) 	3(1)

O1W	25(1) 	28(1)	33(1) 	10(1)	1(1) 	5(1)

Table 5. Hydrogen bonds [Å and °].

DH···A	d(DH)	d(H···A)	d(D···A)	(DHA)

N22H22...O1A	0.93	1.84	2.7032(17)	153.7

O1WH2W...O1A	0.852(17)	1.929(18)	2.7743(17)	172(2)

N22H22...O1Bi	0.93	2.27	2.9158(18)	125.7

O1WH1W...O1Biii	0.847(16)	1.957(18)	2.7883(19)	167(2)

Symmetry transformations used to generate equivalent atoms:

(i) x+1,y,z+1    (ii) x+1,y,z    (iii) x,y1/2,z1/2