|  | # Departmental Single Crystal X-Ray Diffraction Service School of Chemistry - University of Southampton Contact: Dr Mark E Light, light@soton.ac.uk, ex 29429 |
| --- | --- |

Table 1. Crystal data and structure refinement details.

Identification code 	06skc0068p21c

Empirical formula 	C8H14N4O6

Formula weight 	262.23

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P21/c

Unit cell dimensions	a = 8.322(4) Å	 = 90°

b = 11.203(5) Å	 = 97.79(3)°

c = 11.915(5) Å	  = 90°

Volume	1100.6(9) Å3

Z	4

Density (calculated)	1.583 Mg / m3

Absorption coefficient	0.136 mm1

F(000)	552

Crystal	plate; colourless

Crystal size	0.10  0.08  0.01 mm3

 range for data collection	3.07  25.00°

Index ranges	9  h  9, 13  k  13, 14  l  14

Reflections collected	15954

Independent reflections	1934 [Rint = 0.1842]

Completeness to  = 25.00°	99.8 %

Absorption correction	Semiempirical from equivalents

Max. and min. transmission	0.9986 and 0.9865

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	1934 / 0 / 153

Goodness-of-fit on F2	1.243

Final R indices [F2 > 2(F2)]	R1 = 0.1421, wR2 = 0.2116

R indices (all data)	R1 = 0.2012, wR2 = 0.2343

Largest diff. peak and hole	0.360 and 0.354 e Å3

Diffractometer: Nonius KappaCCD area detector ( scans and  scans to fill asymmetric unit ). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: Sheldrick, G. M. SADABS - Bruker Nonius area detector scaling and absorption correction - V2.10 Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: Cameron - A Molecular Graphics Package. (D. M. Watkin, L. Pearce and C. K. Prout, Chemical Crystallography Laboratory, University of Oxford, 1993).

Special details:

Table 2. Atomic coordinates [ 104], equivalent isotropic displacement parameters [Å2  103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C1	2026(9)	1130(7)	4687(6)	19(1)	1

C2	2938(9)	1534(7)	5644(6)	19(1)	1

O1A	1413(6)	1852(5)	4105(4)	22(1)	1

O1B	2003(6)	22(5)	4570(5)	20(1)	1

O2A	2945(7)	2683(5)	5775(4)	21(1)	1

O2B	3593(6)	840(5)	6199(4)	21(1)	1

C22	253(10)	242(8)	7596(7)	24(2)	1

C24	981(9)	1354(7)	8617(6)	20(1)	1

C25	1828(10)	220(7)	8983(7)	20(1)	1

N21	932(8)	699(6)	8465(5)	22(2)	1

N23	357(8)	918(6)	7603(6)	27(2)	1

O22	395(7)	884(5)	6900(4)	23(1)	1

C32	5205(9)	2108(7)	2907(6)	17(2)	1

C34	6098(10)	3733(8)	3830(6)	24(2)	1

C35	6704(10)	2591(7)	4315(7)	25(2)	1

N31	5828(8)	1674(6)	3796(5)	20(2)	1

N33	5444(8)	3293(6)	2851(5)	21(2)	1

O32	4552(6)	1510(5)	2210(4)	23(1)	1

Table 3. Bond lengths [Å] and angles [°].

C1O1A	1.221(9)

C1O1B	1.298(9)

C1C2	1.522(10)

C2O2B	1.199(9)

C2O2A	1.297(9)

O1BH1	0.8400

O2AH2	0.8400

C22O22	1.272(10)

C22N23	1.303(11)

C22N21	1.346(10)

C24N23	1.462(9)

C24C25	1.544(10)

C24H24A	0.9900

C24H24B	0.9900

C25N21	1.457(9)

C25H25A	0.9900

C25H25B	0.9900

N21H21	0.8800

N23H23	0.8800

C32O32	1.248(9)

C32N31	1.333(9)

C32N33	1.343(10)

C34N33	1.439(10)

C34C35	1.517(11)

C34H34A	0.9900

C34H34B	0.9900

C35N31	1.446(10)

C35H35A	0.9900

C35H35B	0.9900

N31H31	0.8800

N33H33	0.8800

O1AC1O1B	125.8(7)

O1AC1C2	121.1(7)

O1BC1C2	113.1(7)

O2BC2O2A	124.5(7)

O2BC2C1	122.1(7)

O2AC2C1	113.4(7)

C1O1BH1	109.5

C2O2AH2	109.5

O22C22N23	127.1(8)

O22C22N21	123.1(8)

N23C22N21	109.8(8)

N23C24C25	100.7(6)

N23C24H24A	111.6

C25C24H24A	111.6

N23C24H24B	111.6

C25C24H24B	111.6

H24AC24H24B	109.4

N21C25C24	100.5(6)

N21C25H25A	111.7

C24C25H25A	111.7

N21C25H25B	111.7

C24C25H25B	111.7

H25AC25H25B	109.4

C22N21C25	110.5(7)

C22N21H21	124.8

C25N21H21	124.8

C22N23C24	111.7(7)

C22N23H23	124.1

C24N23H23	124.1

O32C32N31	125.8(7)

O32C32N33	125.0(7)

N31C32N33	109.2(7)

N33C34C35	101.7(7)

N33C34H34A	111.4

C35C34H34A	111.4

N33C34H34B	111.4

C35C34H34B	111.4

H34AC34H34B	109.3

N31C35C34	102.9(6)

N31C35H35A	111.2

C34C35H35A	111.2

N31C35H35B	111.2

C34C35H35B	111.2

H35AC35H35B	109.1

C32N31C35	110.7(7)

C32N31H31	124.6

C35N31H31	124.6

C32N33C34	111.6(6)

C32N33H33	124.2

C34N33H33	124.2

Symmetry transformations used to generate equivalent atoms:

Table 4. Anisotropic displacement parameters [Å2 103]. The anisotropic displacement

factor exponent takes the form: 2 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C1	13(3) 	23(3)	19(3) 	7(3)	4(2) 	1(2)

C2	13(3) 	23(3)	19(3) 	7(3)	4(2) 	1(2)

O1A	27(3) 	19(3)	24(3) 	4(2)	13(2) 	4(3)

O1B	21(3) 	14(3)	29(3) 	1(2)	16(3) 	1(2)

O2A	22(3) 	18(3)	23(3) 	1(2)	4(2) 	10(2)

O2B	23(3) 	22(3)	21(3) 	4(2)	11(3) 	3(3)

C22	21(5) 	25(5)	25(5) 	6(4)	0(4) 	0(4)

C24	21(3) 	14(3)	25(3) 	4(3)	2(3) 	3(3)

C25	21(3) 	14(3)	25(3) 	4(3)	2(3) 	3(3)

N21	25(4) 	20(4)	22(4) 	8(3)	8(3) 	7(3)

N23	42(5) 	19(4)	21(4) 	4(3)	10(3) 	0(3)

O22	34(3) 	20(3)	17(3) 	4(3)	9(3) 	6(3)

C32	9(4) 	17(5)	24(5) 	10(4)	3(4) 	4(3)

C34	18(4) 	33(5)	21(4) 	1(4)	6(4) 	5(4)

C35	21(5) 	29(5)	26(5) 	3(4)	5(4) 	1(4)

N31	23(4) 	14(4)	22(4) 	0(3)	5(3) 	1(3)

N33	24(4) 	20(4)	19(4) 	7(3)	6(3) 	5(3)

O32	25(3) 	21(3)	21(3) 	3(2)	0(3) 	1(3)

Table 5. Hydrogen bonds [Å and °].

DH···A	d(DH)	d(H···A)	d(D···A)	(DHA)

O1BH1...O22i	0.84	1.71	2.535(8)	167.3

N23H23...O1Ai	0.88	2.06	2.867(8)	152.1

O2AH2...O32ii	0.84	1.66	2.480(8)	164.4

N21H21...O1Aii	0.88	2.04	2.890(8)	162.2

N31H31...O2Biii	0.88	2.07	2.858(8)	147.9

N33H33...O2Biv	0.88	2.06	2.831(8)	146.5

Symmetry transformations used to generate equivalent atoms:

(i) x,y,z+1    (ii) x,y1/2,z+1/2    (iii) x1,y,z+1

(iv)  x,y1/2,z1/2