|  | Departmental Single Crystal X-Ray Diffraction Service School of Chemistry - University of Southampton Contact: Dr Mark E Light, light@soton.ac.uk, ex 29429 |
| --- | --- |

Table 1. Crystal data and structure refinement details.

Identification code 	06skc0073p21n

Empirical formula 	C7H16N2O4

Formula weight 	192.22

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P21/n

Unit cell dimensions	a = 8.6426(5) Å	( = 90°

b = 6.0715(5) Å	( = 102.765(5)°

c = 18.9467(14) Å	(  = 90°

Volume	969.63(12) Å3

Z	4

Density (calculated)	1.317 Mg / m3

Absorption coefficient	0.107 mm(1

F(000)	416

Crystal	plate; colourless

Crystal size	0.27 ( 0.14 ( 0.03 mm3

( range for data collection	3.53 ( 27.48°

Index ranges	(11 ( h ( 10, (7 ( k ( 7, (24 ( l ( 24

Reflections collected	14599

Independent reflections	2218 [Rint = 0.1419]

Completeness to ( = 27.48°	99.7 %

Max. and min. transmission	0.9968 and 0.9717

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	2218 / 0 / 126

Goodness-of-fit on F2	1.032

Final R indices [F2 > 2((F2)]	R1 = 0.0603, wR2 = 0.1202

R indices (all data)	R1 = 0.1330, wR2 = 0.1463

Largest diff. peak and hole	0.283 and (0.319 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit ). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: Sheldrick, G. M. SADABS - Bruker Nonius area detector scaling and absorption correction - V2.10 Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: Cameron - A Molecular Graphics Package. (D. M. Watkin, L. Pearce and C. K. Prout, Chemical Crystallography Laboratory, University of Oxford, 1993).

Special details:

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C1	1602(3)	5791(4)	(213(1)	20(1)	1

C2	2728(3)	4730(4)	424(1)	24(1)	1

C3	3553(3)	2685(4)	237(1)	23(1)	1

C4	5061(3)	2126(4)	793(1)	25(1)	1

C5	4885(3)	1244(4)	1513(1)	21(1)	1

O1A	1050(2)	4668(3)	(765(1)	25(1)	1

O1B	1289(2)	7796(3)	(151(1)	27(1)	1

O5A	6172(2)	1064(3)	1992(1)	26(1)	1

O5B	3573(2)	703(3)	1624(1)	31(1)	1

C22	4737(3)	(3723(4)	2731(1)	24(1)	1

C23	4977(3)	(5785(4)	3178(1)	24(1)	1

N21	5961(2)	(2025(3)	3001(1)	21(1)	1

N24	4538(2)	(5515(4)	3885(1)	22(1)	1

Table 3. Bond lengths [Å] and angles [°].

C1(O1A	1.252(3)

C1(O1B	1.258(3)

C1(C2	1.516(3)

C2(C3	1.512(4)

C2(H2A	0.9900

C2(H2B	0.9900

C3(C4	1.522(3)

C3(H3A	0.9900

C3(H3B	0.9900

C4(C5	1.504(4)

C4(H4A	0.9900

C4(H4B	0.9900

C5(O5B	1.242(3)

C5(O5A	1.275(3)

C22(N21	1.485(3)

C22(C23	1.500(4)

C22(H22A	0.9900

C22(H22B	0.9900

C23(N24	1.479(3)

C23(H23A	0.9900

C23(H23B	0.9900

N21(H21A	0.9100

N21(H21B	0.9100

N21(H21C	0.9100

N24(H24A	0.9100

N24(H24B	0.9100

N24(H24C	0.9100

O1A(C1(O1B	123.7(2)

O1A(C1(C2	119.5(2)

O1B(C1(C2	116.8(2)

C3(C2(C1	114.6(2)

C3(C2(H2A	108.6

C1(C2(H2A	108.6

C3(C2(H2B	108.6

C1(C2(H2B	108.6

H2A(C2(H2B	107.6

C2(C3(C4	113.4(2)

C2(C3(H3A	108.9

C4(C3(H3A	108.9

C2(C3(H3B	108.9

C4(C3(H3B	108.9

H3A(C3(H3B	107.7

C5(C4(C3	117.7(2)

C5(C4(H4A	107.9

C3(C4(H4A	107.9

C5(C4(H4B	107.9

C3(C4(H4B	107.9

H4A(C4(H4B	107.2

O5B(C5(O5A	122.8(2)

O5B(C5(C4	121.8(2)

O5A(C5(C4	115.4(2)

N21(C22(C23	112.7(2)

N21(C22(H22A	109.1

C23(C22(H22A	109.1

N21(C22(H22B	109.1

C23(C22(H22B	109.1

H22A(C22(H22B	107.8

N24(C23(C22	112.8(2)

N24(C23(H23A	109.0

C22(C23(H23A	109.0

N24(C23(H23B	109.0

C22(C23(H23B	109.0

H23A(C23(H23B	107.8

C22(N21(H21A	109.5

C22(N21(H21B	109.5

H21A(N21(H21B	109.5

C22(N21(H21C	109.5

H21A(N21(H21C	109.5

H21B(N21(H21C	109.5

C23(N24(H24A	109.5

C23(N24(H24B	109.5

H24A(N24(H24B	109.5

C23(N24(H24C	109.5

H24A(N24(H24C	109.5

H24B(N24(H24C	109.5

Symmetry transformations used to generate equivalent atoms:

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C1	18(1) 	21(2)	22(1) 	0(1)	6(1) 	(3(1)

C2	22(1) 	25(2)	23(2) 	(2(1)	3(1) 	0(1)

C3	25(1) 	26(2)	19(1) 	3(1)	6(1) 	2(1)

C4	23(1) 	26(2)	27(2) 	2(1)	6(1) 	2(1)

C5	24(1) 	17(1)	24(1) 	0(1)	6(1) 	1(1)

O1A	29(1) 	23(1)	20(1) 	0(1)	1(1) 	(3(1)

O1B	33(1) 	20(1)	26(1) 	0(1)	4(1) 	6(1)

O5A	22(1) 	31(1)	23(1) 	6(1)	2(1) 	(2(1)

O5B	22(1) 	41(1)	30(1) 	10(1)	6(1) 	(4(1)

C22	23(1) 	28(2)	20(1) 	(1(1)	2(1) 	(3(1)

C23	26(1) 	23(2)	23(1) 	(3(1)	6(1) 	(1(1)

N21	21(1) 	22(1)	20(1) 	4(1)	3(1) 	1(1)

N24	23(1) 	23(1)	23(1) 	0(1)	7(1) 	(3(1)

Table 5. Hydrogen bonds [Å and °].

D(H···A	d(D(H)	d(H···A)	d(D···A)	((DHA)

N21(H21C...O5A	0.91	1.82	2.713(3)	166.7

N21(H21A...O5Ai	0.91	1.84	2.733(3)	168.1

N21(H21B...O1Aii	0.91	1.86	2.728(3)	159.9

N24(H24A...O1Bii	0.91	1.78	2.670(3)	163.6

N24(H24B...O1Aiii	0.91	2.07	2.850(3)	142.6

N24(H24B...O1Biv	0.91	2.29	2.843(3)	118.7

N24(H24C...O5Bv	0.91	1.87	2.750(3)	162.5

Symmetry transformations used to generate equivalent atoms:

(i) (x+3/2,y(1/2,(z+1/2    (ii) x+1/2,(y+1/2,z+1/2

(iii) x+1/2,(y(1/2,z+1/2    (iv)  (x+1/2,y(3/2,(z+1/2

(v) (x+1/2,y(1/2,(z+1/2