|  | Departmental Single Crystal X-Ray Diffraction Service School of Chemistry - University of Southampton Contact: Dr Mark E Light, light@soton.ac.uk, ex 29429 |
| --- | --- |

Table 1. Crystal data and structure refinement details.

Identification code 	06skc0079p21c

Empirical formula 	C6H7NO3S

Formula weight 	173.19

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P21/c

Unit cell dimensions	a = 5.7944(2) Å	( = 90°

b = 7.4316(5) Å	( = 96.289(4)°

c = 15.9213(10) Å	(  = 90°

Volume	681.47(7) Å3

Z	4

Density (calculated)	1.688 Mg / m3

Absorption coefficient	0.424 mm(1

F(000)	360

Crystal	block; colourless

Crystal size	0.20 ( 0.05 ( 0.03 mm3

( range for data collection	3.03 ( 27.47°

Index ranges	(6 ( h ( 7, (9 ( k ( 9, (20 ( l ( 20

Reflections collected	8270

Independent reflections	1567 [Rint = 0.0505]

Completeness to ( = 27.47°	99.7 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.9874 and 0.9200

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	1567 / 0 / 104

Goodness-of-fit on F2	1.101

Final R indices [F2 > 2((F2)]	R1 = 0.0434, wR2 = 0.0951

R indices (all data)	R1 = 0.0589, wR2 = 0.1022

Largest diff. peak and hole	0.329 and (0.526 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit ). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: Sheldrick, G. M. SADABS - Bruker Nonius area detector scaling and absorption correction - V2.10 Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: Cameron - A Molecular Graphics Package. (D. M. Watkin, L. Pearce and C. K. Prout, Chemical Crystallography Laboratory, University of Oxford, 1993).

Special details:

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C1	1278(4)	7191(3)	553(1)	12(1)	1

C2	(929(4)	7961(3)	482(1)	13(1)	1

C3	(2111(4)	8233(3)	(316(1)	13(1)	1

C4	(1078(4)	7710(3)	(1023(1)	12(1)	1

C5	1100(4)	6934(3)	(962(1)	14(1)	1

C6	2294(4)	6682(3)	(162(2)	14(1)	1

N4	(2370(3)	7932(3)	(1866(1)	14(1)	1

O1A	4115(3)	8596(2)	1747(1)	27(1)	1

O1B	1187(3)	6502(3)	2142(1)	29(1)	1

O1C	4494(3)	5426(2)	1485(1)	16(1)	1

S1	2885(1)	6901(1)	1559(1)	14(1)	1

Table 3. Bond lengths [Å] and angles [°].

C1(C6	1.390(3)

C1(C2	1.394(3)

C1(S1	1.775(2)

C2(C3	1.390(3)

C2(H2	0.9500

C3(C4	1.388(3)

C3(H3	0.9500

C4(C5	1.381(3)

C4(N4	1.472(3)

C5(C6	1.394(3)

C5(H5	0.9500

C6(H6	0.9500

N4(H4A	0.9100

N4(H4B	0.9100

N4(H4C	0.9100

O1A(S1	1.4623(18)

O1B(S1	1.4556(19)

O1C(S1	1.4522(17)

C6(C1(C2	120.8(2)

C6(C1(S1	118.57(18)

C2(C1(S1	120.60(17)

C3(C2(C1	119.3(2)

C3(C2(H2	120.3

C1(C2(H2	120.3

C4(C3(C2	119.2(2)

C4(C3(H3	120.4

C2(C3(H3	120.4

C5(C4(C3	122.1(2)

C5(C4(N4	118.7(2)

C3(C4(N4	119.1(2)

C4(C5(C6	118.6(2)

C4(C5(H5	120.7

C6(C5(H5	120.7

C1(C6(C5	120.0(2)

C1(C6(H6	120.0

C5(C6(H6	120.0

C4(N4(H4A	109.5

C4(N4(H4B	109.5

H4A(N4(H4B	109.5

C4(N4(H4C	109.5

H4A(N4(H4C	109.5

H4B(N4(H4C	109.5

O1C(S1(O1B	112.52(11)

O1C(S1(O1A	111.36(11)

O1B(S1(O1A	113.13(12)

O1C(S1(C1	107.24(10)

O1B(S1(C1	106.01(11)

O1A(S1(C1	106.03(11)

Symmetry transformations used to generate equivalent atoms:

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C1	13(1) 	9(1)	13(1) 	1(1)	0(1) 	(2(1)

C2	15(1) 	11(1)	14(1) 	0(1)	3(1) 	0(1)

C3	10(1) 	11(1)	17(1) 	1(1)	0(1) 	1(1)

C4	15(1) 	9(1)	11(1) 	1(1)	(2(1) 	(1(1)

C5	16(1) 	12(1)	12(1) 	1(1)	2(1) 	0(1)

C6	13(1) 	11(1)	17(1) 	1(1)	0(1) 	1(1)

N4	16(1) 	12(1)	12(1) 	1(1)	(3(1) 	0(1)

O1A	33(1) 	12(1)	32(1) 	(6(1)	(18(1) 	1(1)

O1B	26(1) 	47(1)	13(1) 	3(1)	4(1) 	7(1)

O1C	18(1) 	12(1)	17(1) 	0(1)	(2(1) 	4(1)

S1	17(1) 	13(1)	12(1) 	(2(1)	(3(1) 	2(1)

Table 5. Hydrogen bonds [Å and °].

D(H···A	d(D(H)	d(H···A)	d(D···A)	((DHA)

N4(H4A...O1Bi	0.91	1.89	2.762(3)	161.3

N4(H4B...O1Aii	0.91	1.89	2.785(3)	165.5

N4(H4C...O1Ciii	0.91	2.09	2.877(3)	143.7

N4(H4C...S1iii	0.91	2.99	3.642(2)	130.2

N4(H4C...O1Aiv	0.91	2.41	3.054(3)	127.4

Symmetry transformations used to generate equivalent atoms:

(i) x,(y+3/2,z(1/2    (ii) (x,(y+2,(z    (iii) (x,(y+1,(z

(iv)  x(1,(y+3/2,z(1/2