|  | Departmental Single Crystal X-Ray Diffraction Service School of Chemistry - University of Southampton Contact: Dr Mark E Light, light@soton.ac.uk, ex 29429 |
| --- | --- |

Table 1. Crystal data and structure refinement details.

Identification code 	06skc0075p(1

Empirical formula 	C22H30N4O9S3

Formula weight 	590.68

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Triclinic

Space group 	P(1

Unit cell dimensions	a = 10.0617(6) Å	( = 90.665(3)°

b = 10.7224(6) Å	( = 105.835(3)°

c = 12.7612(8) Å	(  = 99.831(3)°

Volume	1302.59(13) Å3

Z	2

Density (calculated)	1.506 Mg / m3

Absorption coefficient	0.344 mm(1

F(000)	620

Crystal	plate; colourless

Crystal size	0.14 ( 0.09 ( 0.02 mm3

( range for data collection	3.05 ( 27.48°

Index ranges	(13 ( h ( 13, (13 ( k ( 13, (16 ( l ( 16

Reflections collected	33410

Independent reflections	5944 [Rint = 0.1208]

Completeness to ( = 27.48°	99.7 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.9932 and 0.9535

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	5944 / 0 / 345

Goodness-of-fit on F2	1.101

Final R indices [F2 > 2((F2)]	R1 = 0.0848, wR2 = 0.1455

R indices (all data)	R1 = 0.1441, wR2 = 0.1711

Largest diff. peak and hole	0.642 and (0.576 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit ). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: Sheldrick, G. M. SADABS - Bruker Nonius area detector scaling and absorption correction - V2.10 Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: Cameron - A Molecular Graphics Package. (D. M. Watkin, L. Pearce and C. K. Prout, Chemical Crystallography Laboratory, University of Oxford, 1993).

Special details:

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C1	2967(5)	1112(4)	1694(4)	23(1)	1

C2	3915(5)	350(4)	2250(4)	22(1)	1

C3	4231(5)	(602(5)	1638(4)	28(1)	1

C4	3638(6)	(776(5)	531(5)	37(1)	1

C5	2724(7)	(21(5)	(13(4)	43(2)	1

C6	2401(6)	913(5)	572(4)	34(1)	1

N2	4437(4)	452(4)	3380(3)	24(1)	1

O1A	1609(4)	1621(3)	3050(3)	28(1)	1

O1B	1669(4)	3016(3)	1578(3)	34(1)	1

O1C	3738(3)	3039(3)	3098(3)	26(1)	1

S1	2457(1)	2299(1)	2394(1)	19(1)	1

C22	9860(6)	3814(5)	3538(5)	34(1)	1

C23	8783(7)	4527(5)	2850(6)	48(2)	1

C24	8041(10)	3598(8)	1908(6)	82(3)	1

C25	7903(8)	2345(6)	2394(6)	66(2)	1

N21	9172(4)	2449(4)	3341(3)	23(1)	1

C31	2116(5)	6961(4)	3068(4)	19(1)	1

C32	1529(5)	8038(4)	2776(4)	20(1)	1

C33	763(5)	8167(4)	1723(4)	23(1)	1

C34	626(5)	7212(5)	925(4)	29(1)	1

C35	1250(5)	6162(5)	1201(4)	26(1)	1

C36	1992(5)	6033(4)	2275(4)	23(1)	1

N32	1750(4)	9082(3)	3604(3)	18(1)	1

O31A	4282(3)	7811(3)	4675(3)	23(1)	1

O31B	3396(4)	5552(3)	4502(3)	28(1)	1

O31C	2091(4)	7018(4)	5069(3)	35(1)	1

S31	3040(1)	6811(1)	4445(1)	21(1)	1

C41	7179(5)	7613(4)	3023(4)	19(1)	1

C42	6478(5)	6719(4)	3556(4)	19(1)	1

C43	5566(5)	5669(4)	2989(4)	22(1)	1

C44	5315(5)	5522(5)	1874(4)	29(1)	1

C45	6015(5)	6394(5)	1327(4)	30(1)	1

C46	6951(5)	7444(5)	1912(4)	24(1)	1

N42	6663(4)	6875(3)	4726(3)	21(1)	1

O41A	8948(3)	9661(3)	2979(3)	23(1)	1

O41B	9346(3)	8465(3)	4617(3)	24(1)	1

O41C	7458(3)	9679(3)	4195(3)	25(1)	1

S41	8335(1)	8986(1)	3760(1)	18(1)	1

Table 3. Bond lengths [Å] and angles [°].

C1(C6	1.389(7)

C1(C2	1.410(7)

C1(S1	1.768(5)

C2(N2	1.389(6)

C2(C3	1.407(6)

C3(C4	1.372(7)

C3(H3	0.9500

C4(C5	1.380(8)

C4(H4	0.9500

C5(C6	1.375(7)

C5(H5	0.9500

C6(H6	0.9500

N2(H2A	0.8800

N2(H2B	0.8800

O1A(S1	1.467(3)

O1B(S1	1.442(3)

O1C(S1	1.449(3)

C22(N21	1.495(6)

C22(C23	1.520(8)

C22(H22A	0.9900

C22(H22B	0.9900

C23(C24	1.491(10)

C23(H23A	0.9900

C23(H23B	0.9900

C24(C25	1.486(10)

C24(H24A	0.9900

C24(H24B	0.9900

C25(N21	1.487(7)

C25(H25A	0.9900

C25(H25B	0.9900

N21(H21A	0.9200

N21(H21B	0.9200

C31(C36	1.376(6)

C31(C32	1.394(6)

C31(S31	1.774(5)

C32(C33	1.377(6)

C32(N32	1.477(6)

C33(C34	1.398(7)

C33(H33	0.9500

C34(C35	1.385(7)

C34(H34	0.9500

C35(C36	1.391(7)

C35(H35	0.9500

C36(H36	0.9500

N32(H32A	0.9100

N32(H32B	0.9100

N32(H32C	0.9100

O31A(S31	1.461(3)

O31B(S31	1.452(3)

O31C(S31	1.441(4)

C41(C46	1.379(6)

C41(C42	1.387(6)

C41(S41	1.786(5)

C42(C43	1.378(6)

C42(N42	1.458(6)

C43(C44	1.377(7)

C43(H43	0.9500

C44(C45	1.384(7)

C44(H44	0.9500

C45(C46	1.395(7)

C45(H45	0.9500

C46(H46	0.9500

N42(H42A	0.9100

N42(H42B	0.9100

N42(H42C	0.9100

O41A(S41	1.449(3)

O41B(S41	1.464(3)

O41C(S41	1.456(3)

C6(C1(C2	119.3(4)

C6(C1(S1	119.0(4)

C2(C1(S1	121.7(4)

N2(C2(C3	120.1(4)

N2(C2(C1	121.6(4)

C3(C2(C1	118.2(4)

C4(C3(C2	120.7(5)

C4(C3(H3	119.6

C2(C3(H3	119.6

C3(C4(C5	121.1(5)

C3(C4(H4	119.4

C5(C4(H4	119.4

C6(C5(C4	119.0(5)

C6(C5(H5	120.5

C4(C5(H5	120.5

C5(C6(C1	121.8(5)

C5(C6(H6	119.1

C1(C6(H6	119.1

C2(N2(H2A	120.0

C2(N2(H2B	120.0

H2A(N2(H2B	120.0

O1B(S1(O1C	113.9(2)

O1B(S1(O1A	112.7(2)

O1C(S1(O1A	110.2(2)

O1B(S1(C1	107.2(2)

O1C(S1(C1	106.6(2)

O1A(S1(C1	105.7(2)

N21(C22(C23	104.8(4)

N21(C22(H22A	110.8

C23(C22(H22A	110.8

N21(C22(H22B	110.8

C23(C22(H22B	110.8

H22A(C22(H22B	108.9

C24(C23(C22	102.3(5)

C24(C23(H23A	111.3

C22(C23(H23A	111.3

C24(C23(H23B	111.3

C22(C23(H23B	111.3

H23A(C23(H23B	109.2

C25(C24(C23	104.9(6)

C25(C24(H24A	110.8

C23(C24(H24A	110.8

C25(C24(H24B	110.8

C23(C24(H24B	110.8

H24A(C24(H24B	108.8

C24(C25(N21	104.8(6)

C24(C25(H25A	110.8

N21(C25(H25A	110.8

C24(C25(H25B	110.8

N21(C25(H25B	110.8

H25A(C25(H25B	108.9

C25(N21(C22	107.9(4)

C25(N21(H21A	110.1

C22(N21(H21A	110.1

C25(N21(H21B	110.1

C22(N21(H21B	110.1

H21A(N21(H21B	108.4

C36(C31(C32	119.4(4)

C36(C31(S31	120.7(4)

C32(C31(S31	120.0(3)

C33(C32(C31	121.6(4)

C33(C32(N32	118.6(4)

C31(C32(N32	119.8(4)

C32(C33(C34	118.6(4)

C32(C33(H33	120.7

C34(C33(H33	120.7

C35(C34(C33	120.0(5)

C35(C34(H34	120.0

C33(C34(H34	120.0

C34(C35(C36	120.5(4)

C34(C35(H35	119.7

C36(C35(H35	119.7

C31(C36(C35	119.8(4)

C31(C36(H36	120.1

C35(C36(H36	120.1

C32(N32(H32A	109.5

C32(N32(H32B	109.5

H32A(N32(H32B	109.5

C32(N32(H32C	109.5

H32A(N32(H32C	109.5

H32B(N32(H32C	109.5

O31C(S31(O31B	114.5(2)

O31C(S31(O31A	112.3(2)

O31B(S31(O31A	112.3(2)

O31C(S31(C31	105.1(2)

O31B(S31(C31	106.6(2)

O31A(S31(C31	105.1(2)

C46(C41(C42	119.2(4)

C46(C41(S41	120.2(4)

C42(C41(S41	120.6(3)

C43(C42(C41	120.9(4)

C43(C42(N42	118.1(4)

C41(C42(N42	121.0(4)

C44(C43(C42	119.7(5)

C44(C43(H43	120.2

C42(C43(H43	120.2

C43(C44(C45	120.5(5)

C43(C44(H44	119.8

C45(C44(H44	119.8

C44(C45(C46	119.3(5)

C44(C45(H45	120.3

C46(C45(H45	120.3

C41(C46(C45	120.4(5)

C41(C46(H46	119.8

C45(C46(H46	119.8

C42(N42(H42A	109.5

C42(N42(H42B	109.5

H42A(N42(H42B	109.5

C42(N42(H42C	109.5

H42A(N42(H42C	109.5

H42B(N42(H42C	109.5

O41A(S41(O41C	113.99(19)

O41A(S41(O41B	113.8(2)

O41C(S41(O41B	112.5(2)

O41A(S41(C41	106.0(2)

O41C(S41(C41	105.5(2)

O41B(S41(C41	103.8(2)

Symmetry transformations used to generate equivalent atoms:

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C1	31(3) 	18(2)	21(2) 	0(2)	8(2) 	5(2)

C2	21(2) 	18(2)	28(3) 	2(2)	10(2) 	1(2)

C3	26(3) 	24(2)	39(3) 	0(2)	15(2) 	9(2)

C4	57(4) 	30(3)	33(3) 	(1(2)	24(3) 	12(3)

C5	87(5) 	29(3)	16(3) 	0(2)	11(3) 	23(3)

C6	53(4) 	25(3)	23(3) 	2(2)	4(2) 	19(3)

N2	24(2) 	20(2)	27(2) 	(1(2)	3(2) 	9(2)

O1A	30(2) 	19(2)	42(2) 	4(2)	21(2) 	5(2)

O1B	54(2) 	26(2)	22(2) 	4(2)	2(2) 	23(2)

O1C	25(2) 	20(2)	29(2) 	(5(1)	5(2) 	(1(1)

S1	25(1) 	13(1)	20(1) 	0(1)	6(1) 	5(1)

C22	29(3) 	25(3)	55(4) 	3(2)	23(3) 	5(2)

C23	42(4) 	30(3)	80(5) 	17(3)	26(3) 	12(3)

C24	121(8) 	95(6)	47(5) 	26(4)	17(5) 	77(6)

C25	86(6) 	43(4)	46(4) 	(13(3)	(30(4) 	28(4)

N21	26(2) 	22(2)	24(2) 	1(2)	10(2) 	11(2)

C31	16(2) 	20(2)	23(2) 	3(2)	11(2) 	(1(2)

C32	17(2) 	18(2)	25(2) 	1(2)	8(2) 	1(2)

C33	20(2) 	22(2)	24(2) 	4(2)	3(2) 	4(2)

C34	27(3) 	36(3)	23(3) 	(6(2)	2(2) 	9(2)

C35	24(3) 	25(2)	27(3) 	(11(2)	6(2) 	2(2)

C36	23(2) 	16(2)	30(3) 	(2(2)	7(2) 	1(2)

N32	22(2) 	14(2)	19(2) 	3(2)	7(2) 	4(2)

O31A	25(2) 	18(2)	23(2) 	(2(1)	(1(1) 	5(1)

O31B	32(2) 	19(2)	33(2) 	7(1)	9(2) 	9(2)

O31C	38(2) 	47(2)	31(2) 	13(2)	20(2) 	24(2)

S31	25(1) 	17(1)	22(1) 	4(1)	7(1) 	7(1)

C41	17(2) 	20(2)	20(2) 	(1(2)	4(2) 	5(2)

C42	17(2) 	20(2)	19(2) 	2(2)	6(2) 	5(2)

C43	16(2) 	19(2)	30(3) 	0(2)	6(2) 	1(2)

C44	30(3) 	27(3)	26(3) 	(6(2)	5(2) 	2(2)

C45	32(3) 	33(3)	23(3) 	(4(2)	7(2) 	5(2)

C46	22(2) 	27(2)	25(3) 	3(2)	11(2) 	5(2)

N42	23(2) 	16(2)	24(2) 	3(2)	6(2) 	2(2)

O41A	24(2) 	17(2)	29(2) 	5(1)	11(2) 	2(1)

O41B	19(2) 	21(2)	26(2) 	5(1)	(1(1) 	2(1)

O41C	24(2) 	22(2)	28(2) 	(5(1)	7(2) 	5(1)

S41	19(1) 	15(1)	21(1) 	1(1)	5(1) 	2(1)

Table 5. Hydrogen bonds [Å and °].

D(H···A	d(D(H)	d(H···A)	d(D···A)	((DHA)

N42(H42C...O31A	0.91	1.85	2.737(5)	163.1

N42(H42C...S31	0.91	2.80	3.553(4)	140.6

N2(H2B...O1C	0.88	2.39	2.978(5)	124.6

N32(H32B...O31C	0.91	2.24	2.918(5)	130.3

N42(H42A...O41B	0.91	2.22	2.976(5)	140.3

N42(H42A...S41	0.91	2.59	3.061(4)	112.9

N2(H2A...O41Ci	0.88	2.47	3.188(5)	138.8

N21(H21A...O41Ai	0.92	2.46	2.980(5)	116.1

N2(H2B...O31Aii	0.88	2.32	2.935(5)	126.8

N21(H21B...O31Cii	0.92	2.09	2.773(5)	130.1

N42(H42A...O1Aii	0.91	2.51	3.149(5)	128.1

N42(H42B...O31Bii	0.91	1.88	2.791(5)	174.5

N21(H21A...O1Aiii	0.92	1.99	2.858(5)	156.2

N21(H21B...O41Biv	0.92	2.35	2.901(5)	118.2

N32(H32A...N2v	0.91	2.10	2.937(6)	153.3

N32(H32C...O1Av	0.91	2.15	2.837(5)	131.4

N32(H32B...O41Bvi	0.91	2.39	3.022(5)	126.8

N32(H32C...O41Avi	0.91	2.16	2.890(5)	136.6

N32(H32C...S41vi	0.91	3.02	3.480(4)	113.5

N32(H32B...O41Cvii	0.91	2.48	2.936(5)	111.2

Symmetry transformations used to generate equivalent atoms:

(i) x,y(1,z    (ii) (x+1,(y+1,(z+1    (iii) x+1,y,z    (iv)  (x+2,(y+1,(z+1

(v) x,y+1,z    (vi) x(1,y,z    (vii) (x+1,(y+2,(z+1