|  | University of Southampton · School of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	2008src0818 / MAB/JT/12

Empirical formula 	C6H19B5N2O10

Formula weight 	333.28

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Triclinic

Space group 	P(1

Unit cell dimensions	a = 8.8129(2) Å	( = 74.0430(10)°

b = 8.8960(2) Å	( = 78.8540(10)°

c = 10.3618(2) Å	(  = 88.9620(10)°

Volume	765.80(3) Å3

Z	2

Density (calculated)	1.445 Mg / m3

Absorption coefficient	0.125 mm(1

F(000)	348

Crystal	Cut Block; Colourless

Crystal size	0.28 ( 0.23 ( 0.18 mm3

( range for data collection	3.41 ( 27.48°

Index ranges	(11 ( h ( 11, (11 ( k ( 11, (13 ( l ( 12

Reflections collected	16010

Independent reflections	3493 [Rint = 0.0281]

Completeness to ( = 27.48°	99.1 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.9779 and 0.9659

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	3493 / 0 / 214

Goodness-of-fit on F2	1.051

Final R indices [F2 > 2((F2)]	R1 = 0.0322, wR2 = 0.0817

R indices (all data)	R1 = 0.0358, wR2 = 0.0842

Largest diff. peak and hole	0.234 and (0.243 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing, Acta Cryst. A51 (1995) 33(37; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421(426). Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: ORTEP3 for Windows (L. J. Farrugia, J. Appl. Crystallogr. 1997, 30, 565).

Special details:

All hydrogen atoms were fixed using a standard riding model.

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

B1	929(1)	1916(1)	1913(1)	13(1)	1

B2	(918(1)	4061(1)	2004(1)	17(1)	1

B3	(967(1)	1951(1)	4032(1)	15(1)	1

B4	3757(1)	1440(1)	1379(1)	15(1)	1

B5	2002(1)	(2(1)	660(1)	15(1)	1

O1	233(1)	3384(1)	1303(1)	16(1)	1

O2	(1500(1)	3377(1)	3380(1)	21(1)	1

O3	153(1)	1230(1)	3346(1)	15(1)	1

O4	2570(1)	2249(1)	1888(1)	16(1)	1

O5	3469(1)	211(1)	880(1)	19(1)	1

O6	793(1)	821(1)	1098(1)	15(1)	1

O7	(1524(1)	5430(1)	1417(1)	28(1)	1

O8	(1608(1)	1351(1)	5377(1)	21(1)	1

O9	5217(1)	1915(1)	1369(1)	20(1)	1

O10	1882(1)	(1056(1)	(58(1)	19(1)	1

C11	4606(1)	2516(1)	4682(1)	22(1)	1

C12	4985(1)	3927(1)	3455(1)	23(1)	1

C13	2371(1)	4825(1)	4097(1)	27(1)	1

C14	2088(1)	3405(1)	5324(1)	26(1)	1

C15	3215(2)	1611(2)	7021(1)	37(1)	1

C16	3869(2)	5876(2)	1735(1)	41(1)	1

N11	3527(1)	2917(1)	5781(1)	22(1)	1

N12	3532(1)	4495(1)	2959(1)	22(1)	1

Table 3. Bond lengths [Å] and angles [°].

B1(O1	1.4653(12)

B1(O3	1.4725(12)

B1(O6	1.4734(12)

B1(O4	1.4752(12)

B2(O7	1.3538(13)

B2(O1	1.3609(12)

B2(O2	1.3851(13)

B3(O8	1.3578(13)

B3(O3	1.3604(12)

B3(O2	1.3838(13)

B4(O9	1.3585(13)

B4(O4	1.3638(12)

B4(O5	1.3782(13)

B5(O6	1.3588(12)

B5(O10	1.3637(13)

B5(O5	1.3806(13)

O7(H7	0.8400

O8(H8	0.8400

O9(H9	0.8400

O10(H10	0.8400

C11(N11	1.4571(14)

C11(C12	1.5089(16)

C11(H11A	0.9900

C11(H11B	0.9900

C12(N12	1.4995(14)

C12(H12A	0.9900

C12(H12B	0.9900

C13(N12	1.4944(14)

C13(C14	1.5097(17)

C13(H13A	0.9900

C13(H13B	0.9900

C14(N11	1.4561(14)

C14(H14A	0.9900

C14(H14B	0.9900

C15(N11	1.4597(15)

C15(H15A	0.9800

C15(H15B	0.9800

C15(H15C	0.9800

C16(N12	1.4886(15)

C16(H16A	0.9800

C16(H16B	0.9800

C16(H16C	0.9800

N12(H12	0.9300

O1(B1(O3	111.17(7)

O1(B1(O6	108.26(8)

O3(B1(O6	109.99(8)

O1(B1(O4	108.52(8)

O3(B1(O4	108.34(8)

O6(B1(O4	110.56(7)

O7(B2(O1	122.58(9)

O7(B2(O2	116.89(9)

O1(B2(O2	120.52(9)

O8(B3(O3	123.04(9)

O8(B3(O2	116.22(9)

O3(B3(O2	120.73(9)

O9(B4(O4	117.17(9)

O9(B4(O5	122.17(9)

O4(B4(O5	120.65(9)

O6(B5(O10	123.31(9)

O6(B5(O5	121.69(9)

O10(B5(O5	114.97(9)

B2(O1(B1	123.94(8)

B3(O2(B2	119.84(8)

B3(O3(B1	123.55(8)

B4(O4(B1	123.50(8)

B4(O5(B5	118.78(8)

B5(O6(B1	122.66(8)

B2(O7(H7	109.5

B3(O8(H8	109.5

B4(O9(H9	109.5

B5(O10(H10	109.5

N11(C11(C12	110.29(9)

N11(C11(H11A	109.6

C12(C11(H11A	109.6

N11(C11(H11B	109.6

C12(C11(H11B	109.6

H11A(C11(H11B	108.1

N12(C12(C11	109.65(9)

N12(C12(H12A	109.7

C11(C12(H12A	109.7

N12(C12(H12B	109.7

C11(C12(H12B	109.7

H12A(C12(H12B	108.2

N12(C13(C14	110.51(9)

N12(C13(H13A	109.5

C14(C13(H13A	109.5

N12(C13(H13B	109.5

C14(C13(H13B	109.5

H13A(C13(H13B	108.1

N11(C14(C13	110.81(9)

N11(C14(H14A	109.5

C13(C14(H14A	109.5

N11(C14(H14B	109.5

C13(C14(H14B	109.5

H14A(C14(H14B	108.1

N11(C15(H15A	109.5

N11(C15(H15B	109.5

H15A(C15(H15B	109.5

N11(C15(H15C	109.5

H15A(C15(H15C	109.5

H15B(C15(H15C	109.5

N12(C16(H16A	109.5

N12(C16(H16B	109.5

H16A(C16(H16B	109.5

N12(C16(H16C	109.5

H16A(C16(H16C	109.5

H16B(C16(H16C	109.5

C14(N11(C11	109.32(8)

C14(N11(C15	109.96(10)

C11(N11(C15	111.93(9)

C16(N12(C13	112.35(10)

C16(N12(C12	110.99(10)

C13(N12(C12	110.07(8)

C16(N12(H12	107.7

C13(N12(H12	107.7

C12(N12(H12	107.7

Symmetry transformations used to generate equivalent atoms:

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

B1	14(1) 	14(1)	12(1) 	(4(1)	(2(1) 	4(1)

B2	18(1) 	17(1)	14(1) 	(3(1)	(1(1) 	5(1)

B3	15(1) 	17(1)	13(1) 	(3(1)	(2(1) 	3(1)

B4	16(1) 	16(1)	13(1) 	(4(1)	(2(1) 	3(1)

B5	17(1) 	15(1)	13(1) 	(4(1)	(2(1) 	4(1)

O1	18(1) 	15(1)	12(1) 	(2(1)	(1(1) 	6(1)

O2	25(1) 	21(1)	13(1) 	0(1)	2(1) 	12(1)

O3	17(1) 	15(1)	11(1) 	(2(1)	(1(1) 	5(1)

O4	14(1) 	17(1)	17(1) 	(8(1)	(2(1) 	3(1)

O5	15(1) 	21(1)	24(1) 	(12(1)	(4(1) 	6(1)

O6	15(1) 	17(1)	14(1) 	(6(1)	(3(1) 	4(1)

O7	35(1) 	24(1)	15(1) 	4(1)	6(1) 	17(1)

O8	22(1) 	22(1)	13(1) 	1(1)	1(1) 	10(1)

O9	14(1) 	23(1)	25(1) 	(13(1)	(1(1) 	4(1)

O10	17(1) 	23(1)	23(1) 	(14(1)	(6(1) 	7(1)

C11	22(1) 	22(1)	27(1) 	(11(1)	(9(1) 	6(1)

C12	20(1) 	28(1)	23(1) 	(12(1)	(2(1) 	(3(1)

C13	30(1) 	28(1)	30(1) 	(15(1)	(12(1) 	13(1)

C14	20(1) 	35(1)	25(1) 	(14(1)	(2(1) 	1(1)

C15	55(1) 	27(1)	25(1) 	0(1)	(12(1) 	(9(1)

C16	72(1) 	22(1)	28(1) 	1(1)	(17(1) 	(7(1)

N11	25(1) 	21(1)	19(1) 	(5(1)	(6(1) 	(1(1)

N12	31(1) 	18(1)	19(1) 	(6(1)	(8(1) 	1(1)

Table 5. Hydrogen coordinates [( 104] and isotropic displacement parameters [Å2 ( 103].

Atom 	x	y	z	Ueq	S.o.f.

H7	(1090	5751	589	42	1

H8	(1156	536	5704	31	1

H9	5858	1399	971	30	1

H10	1014	(991	(288	29	1

H11A	4142	1666	4419	27	1

H11B	5568	2136	5003	27	1

H12A	5476	4769	3708	27	1

H12B	5724	3646	2715	27	1

H13A	1387	5116	3783	32	1

H13B	2755	5717	4357	32	1

H14A	1344	3654	6077	31	1

H14B	1629	2538	5081	31	1

H15A	2724	735	6833	55	1

H15B	2521	1939	7747	55	1

H15C	4189	1281	7317	55	1

H16A	4284	6747	1986	61	1

H16B	2914	6183	1396	61	1

H16C	4632	5605	1019	61	1

H12	3118	3695	2700	26	1

Table 6. Hydrogen bonds [Å and °].

D(H···A	d(D(H)	d(H···A)	d(D···A)	((DHA)

O7(H7...O1i	0.84	1.90	2.7422(10)	175.0

O8(H8...O3ii	0.84	1.91	2.7466(10)	172.6

O9(H9...O10iii	0.84	2.09	2.8508(10)	150.6

O10(H10...O6iv	0.84	1.92	2.7570(10)	171.0

N12(H12...O4	0.93	1.84	2.7548(11)	169.2

Symmetry transformations used to generate equivalent atoms:

(i) (x,(y+1,(z    (ii) (x,(y,(z+1    (iii) (x+1,(y,(z

(iv)  (x,(y,(z