|  | University of Southampton · School of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	2008src0842 / CMS-A

Empirical formula 	C21H19NO5S

Formula weight 	397.43

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Triclinic

Space group 	P(1

Unit cell dimensions	a = 9.5497(4) Å	( = 104.436(2)°

b = 10.3189(4) Å	( = 107.828(2)°

c = 11.1034(4) Å	(  = 104.170(2)°

Volume	945.55(6) Å3

Z	2

Density (calculated)	1.396 Mg / m3

Absorption coefficient	0.205 mm(1

F(000)	416

Crystal	Cut Block; Colourless

Crystal size	0.28 ( 0.22 ( 0.12 mm3

( range for data collection	3.22 ( 27.48°

Index ranges	(12 ( h ( 12, (13 ( k ( 13, (14 ( l ( 13

Reflections collected	21235

Independent reflections	4327 [Rint = 0.0491]

Completeness to ( = 27.48°	99.7 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.9759 and 0.9449

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	4327 / 52 / 288

Goodness-of-fit on F2	1.054

Final R indices [F2 > 2((F2)]	R1 = 0.0427, wR2 = 0.1008

R indices (all data)	R1 = 0.0626, wR2 = 0.1126

Largest diff. peak and hole	0.243 and (0.276 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing, Acta Cryst. A51 (1995) 33(37; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421(426). Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: ORTEP3 for Windows (L. J. Farrugia, J. Appl. Crystallogr. 1997, 30, 565).

Special details:

All hydrogen atoms were fixed using a standard riding model.

The thiophene ring was disordered over 2 main positions and restraints have been applied to ring atoms.

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C1	1484(2)	6865(2)	4882(2)	17(1)	1

C2	636(2)	8451(2)	3942(2)	17(1)	1

C3	(657(2)	7010(2)	3132(2)	17(1)	1

C4	(73(2)	5957(2)	3729(2)	17(1)	1

C5	70(2)	4949(2)	2497(2)	18(1)	1

C6	(1613(2)	3977(2)	1487(2)	22(1)	1

C7	(2211(2)	5033(2)	880(2)	22(1)	1

C8	(777(2)	6422(2)	1657(2)	18(1)	1

C9	(655(2)	7510(2)	963(2)	19(1)	1

C10	(1961(2)	8962(2)	105(2)	30(1)	1

C11	(3518(3)	9152(3)	(164(3)	62(1)	1

C12	3231(2)	9426(2)	5884(2)	17(1)	1

C13	4675(2)	9268(2)	6076(2)	19(1)	1

C14	6024(2)	10394(2)	6986(2)	21(1)	1

C15	5940(2)	11673(2)	7679(2)	21(1)	1

C16	4490(2)	11809(2)	7489(2)	26(1)	1

C17	3121(2)	10679(2)	6600(2)	23(1)	1

N1	1823(1)	8278(1)	4923(1)	16(1)	1

O1	2325(1)	6482(1)	5672(1)	22(1)	1

O2	653(1)	9567(1)	3768(1)	21(1)	1

O3	532(1)	5929(1)	1838(1)	18(1)	1

O4	442(1)	8006(1)	700(1)	24(1)	1

O5	(1957(1)	7844(1)	699(1)	24(1)	1

S1	3116(3)	4923(3)	2981(3)	24(1)	0.494(3)

C18	1220(80)	4210(80)	2830(90)	19(1)	0.494(3)

C19	3560(20)	3780(20)	3460(30)	22(2)	0.494(3)

C20	2610(20)	2660(20)	3600(20)	21(2)	0.494(3)

C21	1043(10)	3041(8)	3192(10)	30(2)	0.494(3)

S2	686(2)	2690(2)	3210(2)	22(1)	0.506(3)

C118	1230(80)	4220(80)	2840(90)	19(1)	0.506(3)

C119	2354(19)	2660(20)	3610(20)	22(3)	0.506(3)

C120	3600(20)	3550(20)	3520(30)	22(2)	0.506(3)

C121	2761(11)	4598(10)	3021(12)	37(3)	0.506(3)

Table 3. Bond lengths [Å] and angles [°].

C1(O1	1.2112(18)

C1(N1	1.4003(19)

C1(C4	1.510(2)

C2(O2	1.2114(18)

C2(N1	1.3945(19)

C2(C3	1.517(2)

C3(C4	1.536(2)

C3(C8	1.556(2)

C3(H3	1.0000

C4(C5	1.564(2)

C4(H4	1.0000

C5(O3	1.4499(18)

C5(C18	1.490(9)

C5(C118	1.496(8)

C5(C6	1.547(2)

C6(C7	1.550(2)

C6(H6A	0.9900

C6(H6B	0.9900

C7(C8	1.540(2)

C7(H7A	0.9900

C7(H7B	0.9900

C8(O3	1.4390(17)

C8(C9	1.513(2)

C9(O4	1.2012(19)

C9(O5	1.3368(18)

C10(O5	1.4653(19)

C10(C11	1.496(3)

C10(H10A	0.9900

C10(H10B	0.9900

C11(H11A	0.9800

C11(H11B	0.9800

C11(H11C	0.9800

C12(C13	1.385(2)

C12(C17	1.386(2)

C12(N1	1.4352(19)

C13(C14	1.384(2)

C13(H13	0.9500

C14(C15	1.387(2)

C14(H14	0.9500

C15(C16	1.383(2)

C15(H15	0.9500

C16(C17	1.391(2)

C16(H16	0.9500

C17(H17	0.9500

S1(C19	1.506(16)

S1(C18	1.72(9)

C18(C21	1.36(8)

C19(C20	1.363(11)

C19(H19	0.9500

C20(C21	1.601(17)

C20(H20	0.9500

C21(H21	0.9500

S2(C119	1.527(15)

S2(C118	1.72(9)

C118(C121	1.35(8)

C119(C120	1.365(11)

C119(H119	0.9500

C120(C121	1.600(17)

C120(H120	0.9500

C121(H121	0.9500

O1(C1(N1	123.84(14)

O1(C1(C4	127.49(14)

N1(C1(C4	108.67(12)

O2(C2(N1	125.28(14)

O2(C2(C3	126.32(14)

N1(C2(C3	108.40(12)

C2(C3(C4	105.23(12)

C2(C3(C8	112.33(12)

C4(C3(C8	101.56(11)

C2(C3(H3	112.3

C4(C3(H3	112.3

C8(C3(H3	112.3

C1(C4(C3	104.99(12)

C1(C4(C5	113.84(12)

C3(C4(C5	101.65(11)

C1(C4(H4	111.9

C3(C4(H4	111.9

C5(C4(H4	111.9

O3(C5(C18	111(4)

O3(C5(C118	111(4)

C18(C5(C118	1(7)

O3(C5(C6	103.01(12)

C18(C5(C6	116(3)

C118(C5(C6	116(3)

O3(C5(C4	101.68(11)

C18(C5(C4	116(4)

C118(C5(C4	115(4)

C6(C5(C4	107.44(12)

C5(C6(C7	101.47(12)

C5(C6(H6A	111.5

C7(C6(H6A	111.5

C5(C6(H6B	111.5

C7(C6(H6B	111.5

H6A(C6(H6B	109.3

C8(C7(C6	101.45(12)

C8(C7(H7A	111.5

C6(C7(H7A	111.5

C8(C7(H7B	111.5

C6(C7(H7B	111.5

H7A(C7(H7B	109.3

O3(C8(C9	110.85(12)

O3(C8(C7	103.32(11)

C9(C8(C7	115.76(13)

O3(C8(C3	101.98(11)

C9(C8(C3	114.85(12)

C7(C8(C3	108.59(12)

O4(C9(O5	125.31(14)

O4(C9(C8	125.53(14)

O5(C9(C8	109.17(12)

O5(C10(C11	107.68(15)

O5(C10(H10A	110.2

C11(C10(H10A	110.2

O5(C10(H10B	110.2

C11(C10(H10B	110.2

H10A(C10(H10B	108.5

C10(C11(H11A	109.5

C10(C11(H11B	109.5

H11A(C11(H11B	109.5

C10(C11(H11C	109.5

H11A(C11(H11C	109.5

H11B(C11(H11C	109.5

C13(C12(C17	121.10(14)

C13(C12(N1	119.71(13)

C17(C12(N1	119.19(13)

C14(C13(C12	119.07(14)

C14(C13(H13	120.5

C12(C13(H13	120.5

C13(C14(C15	120.67(14)

C13(C14(H14	119.7

C15(C14(H14	119.7

C16(C15(C14	119.62(15)

C16(C15(H15	120.2

C14(C15(H15	120.2

C15(C16(C17	120.47(14)

C15(C16(H16	119.8

C17(C16(H16	119.8

C12(C17(C16	119.02(14)

C12(C17(H17	120.5

C16(C17(H17	120.5

C2(N1(C1	112.65(12)

C2(N1(C12	123.79(12)

C1(N1(C12	123.56(12)

C8(O3(C5	96.99(10)

C9(O5(C10	115.24(12)

C19(S1(C18	92(2)

C21(C18(C5	128(7)

C21(C18(S1	110.0(11)

C5(C18(S1	122(6)

C20(C19(S1	128(2)

C20(C19(H19	116.2

S1(C19(H19	116.2

C19(C20(C21	97.6(18)

C19(C20(H20	131.2

C21(C20(H20	131.2

C18(C21(C20	113(3)

C18(C21(H21	123.5

C20(C21(H21	123.5

C119(S2(C118	91.3(18)

C121(C118(C5	131(7)

C121(C118(S2	110.0(13)

C5(C118(S2	119(6)

C120(C119(S2	127.2(17)

C120(C119(H119	116.4

S2(C119(H119	116.4

C119(C120(C121	97.6(17)

C119(C120(H120	131.2

C121(C120(H120	131.2

C118(C121(C120	114(3)

C118(C121(H121	123.2

C120(C121(H121	123.2

Symmetry transformations used to generate equivalent atoms:

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C1	19(1) 	18(1)	18(1) 	7(1)	9(1) 	8(1)

C2	18(1) 	18(1)	17(1) 	7(1)	9(1) 	9(1)

C3	16(1) 	17(1)	20(1) 	7(1)	7(1) 	7(1)

C4	16(1) 	15(1)	19(1) 	7(1)	6(1) 	6(1)

C5	19(1) 	17(1)	19(1) 	8(1)	7(1) 	7(1)

C6	20(1) 	19(1)	21(1) 	5(1)	4(1) 	6(1)

C7	21(1) 	21(1)	20(1) 	4(1)	4(1) 	8(1)

C8	15(1) 	20(1)	19(1) 	7(1)	6(1) 	10(1)

C9	20(1) 	20(1)	14(1) 	5(1)	4(1) 	9(1)

C10	39(1) 	36(1)	30(1) 	23(1)	15(1) 	23(1)

C11	68(2) 	106(2)	80(2) 	77(2)	50(2) 	70(2)

C12	16(1) 	16(1)	16(1) 	6(1)	5(1) 	4(1)

C13	19(1) 	18(1)	20(1) 	6(1)	7(1) 	8(1)

C14	16(1) 	23(1)	22(1) 	9(1)	6(1) 	8(1)

C15	20(1) 	20(1)	20(1) 	6(1)	4(1) 	4(1)

C16	26(1) 	20(1)	29(1) 	3(1)	8(1) 	11(1)

C17	18(1) 	20(1)	29(1) 	6(1)	7(1) 	9(1)

N1	16(1) 	15(1)	19(1) 	6(1)	5(1) 	6(1)

O1	22(1) 	20(1)	21(1) 	10(1)	5(1) 	7(1)

O2	21(1) 	18(1)	24(1) 	9(1)	7(1) 	9(1)

O3	19(1) 	19(1)	20(1) 	10(1)	8(1) 	10(1)

O4	24(1) 	27(1)	26(1) 	13(1)	11(1) 	11(1)

O5	24(1) 	30(1)	26(1) 	17(1)	11(1) 	16(1)

S1	24(1) 	23(1)	31(1) 	15(1)	10(1) 	14(1)

C18	20(1) 	17(1)	20(2) 	6(1)	7(1) 	8(1)

C19	26(1) 	16(5)	31(2) 	13(4)	9(1) 	14(2)

C20	17(4) 	24(3)	27(4) 	6(2)	8(3) 	16(3)

C21	25(3) 	27(4)	32(3) 	5(2)	8(2) 	8(2)

S2	25(1) 	17(1)	27(1) 	10(1)	12(1) 	12(1)

C118	20(1) 	17(1)	20(2) 	6(1)	7(1) 	8(1)

C119	26(6) 	23(3)	30(3) 	15(2)	20(4) 	14(4)

C120	26(1) 	16(5)	31(2) 	13(4)	9(1) 	14(2)

C121	52(6) 	21(4)	37(3) 	16(3)	13(4) 	14(4)

Table 5. Hydrogen coordinates [( 104] and isotropic displacement parameters [Å2 ( 103].

Atom 	x	y	z	Ueq	S.o.f.

H3	(1689	7013	3172	20	1

H4	(833	5426	4040	20	1

H6A	(2258	3594	1952	26	1

H6B	(1603	3174	784	26	1

H7A	(2470	4730	(105	27	1

H7B	(3141	5137	1054	27	1

H10A	(1798	8681	(748	36	1

H10B	(1106	9867	736	36	1

H11A	(4355	8247	(781	93	1

H11B	(3559	9886	(575	93	1

H11C	(3658	9446	688	93	1

H13	4737	8400	5589	23	1

H14	7018	10289	7138	25	1

H15	6873	12450	8281	26	1

H16	4430	12681	7969	32	1

H17	2124	10765	6484	28	1

H19	4626	3854	3692	27	0.494(3)

H20	2810	1888	3859	26	0.494(3)

H21	88	2505	3205	36	0.494(3)

H119	2545	1946	3966	26	0.506(3)

H120	4638	3551	3688	27	0.506(3)

H121	3287	5410	2865	44	0.506(3)