Table 1.  Crystal data and structure refinement for 2008src0940.

Identification code 	2008src0940

Empirical formula 	C8 H12 Cl F N O2 Si

Formula weight 	236.73

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Triclinic

Space group 	P-1

Unit cell dimensions	a = 7.2306(5) Å	a= 119.096(4)º.

b = 9.4023(8) Å	b= 96.715(5)º.

c = 9.5351(8) Å	g = 98.833(5)º.

Volume	545.76(8) Å3

Z	2

Density (calculated)	1.441 Mg/m3

Absorption coefficient	0.448 mm-1

F(000)	246

Crystal size	0.36 x 0.26 x 0.08 mm3

Theta range for data collection	2.92 to 27.50º.

Index ranges	-9<=h<=9, -12<=k<=12, -12<=l<=12

Reflections collected	12277

Independent reflections	2511 [R(int) = 0.0571]

Completeness to theta = 27.50º	99.5 %

Absorption correction	Semi-empirical from equivalents

Max. and min. transmission	0.9650 and 0.8552

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	2511 / 0 / 129

Goodness-of-fit on F2	1.064

Final R indices [I>2sigma(I)]	R1 = 0.0826, wR2 = 0.2210

R indices (all data)	R1 = 0.1003, wR2 = 0.2356

Largest diff. peak and hole	2.752 and -0.706 e.Å-3

Table 2.  Atomic coordinates ( x 104) and equivalent isotropic displacement parameters (Å2x 103)

for 2008src0940.  U(eq) is defined as one third of the trace of the orthogonalized Uij tensor.

________________________________________________________________________________

x	y	z	U(eq)

________________________________________________________________________________

Si(1)	3091(2)	2053(1)	7099(1)	28(1)

Cl(1)	5918(2)	3801(2)	5950(2)	40(1)

O(1)	3977(4)	2652(3)	9408(3)	26(1)

N(1)	2322(5)	-22(4)	8380(4)	22(1)

C(1)	2142(6)	-76(5)	6801(5)	26(1)

C(5)	1845(6)	-1186(6)	10046(5)	28(1)

C(6)	1550(6)	-1362(5)	8519(5)	24(1)

C(2)	3351(5)	1495(5)	9697(5)	22(1)

C(4)	2897(6)	352(6)	11432(5)	28(1)

C(3)	3651(6)	1675(5)	11278(5)	25(1)

C(8)	5677(7)	2929(6)	7267(6)	37(1)

F(1)	2425(4)	1226(4)	5056(3)	38(1)

C(7)	458(7)	-2947(5)	6976(5)	31(1)

C(9)	1528(9)	3598(7)	7770(7)	46(1)

________________________________________________________________________________

Table 3.   Bond lengths [Å] and angles [º] for 2008src0940.

_____________________________________________________

Si(1)-F(1) 	1.680(3)

Si(1)-C(8) 	1.879(5)

Si(1)-C(1) 	1.881(4)

Si(1)-C(9) 	1.889(6)

Si(1)-O(1) 	1.981(3)

Cl(1)-C(8) 	1.813(5)

O(1)-C(2) 	1.279(5)

N(1)-C(2) 	1.371(5)

N(1)-C(6) 	1.371(5)

N(1)-C(1) 	1.471(5)

C(1)-H(1A) 	0.9900

C(1)-H(1B) 	0.9900

C(5)-C(6) 	1.369(6)

C(5)-C(4) 	1.408(6)

C(5)-H(5) 	0.9500

C(6)-C(7) 	1.498(6)

C(2)-C(3) 	1.418(5)

C(4)-C(3) 	1.362(6)

C(4)-H(4) 	0.9500

C(3)-H(3) 	0.9500

C(8)-H(8B) 	0.9900

C(8)-H(8A) 	0.9900

C(7)-H(7A) 	0.9800

C(7)-H(7C) 	0.9800

C(7)-H(7B) 	0.9800

C(9)-H(9A) 	0.9800

C(9)-H(9B) 	0.9800

C(9)-H(9C) 	0.9800

F(1)-Si(1)-C(8)	95.31(18)

F(1)-Si(1)-C(1)	89.40(16)

C(8)-Si(1)-C(1)	123.9(2)

F(1)-Si(1)-C(9)	98.37(19)

C(8)-Si(1)-C(9)	116.4(3)

C(1)-Si(1)-C(9)	118.1(2)

F(1)-Si(1)-O(1)	170.17(15)

C(8)-Si(1)-O(1)	84.56(17)

C(1)-Si(1)-O(1)	82.58(14)

C(9)-Si(1)-O(1)	90.45(19)

C(2)-O(1)-Si(1)	114.1(2)

C(2)-N(1)-C(6)	123.3(3)

C(2)-N(1)-C(1)	113.4(3)

C(6)-N(1)-C(1)	123.3(3)

N(1)-C(1)-Si(1)	111.7(3)

N(1)-C(1)-H(1A)	109.3

Si(1)-C(1)-H(1A)	109.3

N(1)-C(1)-H(1B)	109.3

Si(1)-C(1)-H(1B)	109.3

H(1A)-C(1)-H(1B)	107.9

C(6)-C(5)-C(4)	120.1(4)

C(6)-C(5)-H(5)	120.0

C(4)-C(5)-H(5)	120.0

C(5)-C(6)-N(1)	118.4(4)

C(5)-C(6)-C(7)	123.9(4)

N(1)-C(6)-C(7)	117.6(4)

O(1)-C(2)-N(1)	117.3(3)

O(1)-C(2)-C(3)	124.6(4)

N(1)-C(2)-C(3)	118.1(4)

C(3)-C(4)-C(5)	120.9(4)

C(3)-C(4)-H(4)	119.5

C(5)-C(4)-H(4)	119.5

C(4)-C(3)-C(2)	119.1(4)

C(4)-C(3)-H(3)	120.4

C(2)-C(3)-H(3)	120.4

Cl(1)-C(8)-Si(1)	111.6(3)

Cl(1)-C(8)-H(8B)	109.3

Si(1)-C(8)-H(8B)	109.3

Cl(1)-C(8)-H(8A)	109.3

Si(1)-C(8)-H(8A)	109.3

H(8B)-C(8)-H(8A)	108.0

C(6)-C(7)-H(7A)	109.5

C(6)-C(7)-H(7C)	109.5

H(7A)-C(7)-H(7C)	109.5

C(6)-C(7)-H(7B)	109.5

H(7A)-C(7)-H(7B)	109.5

H(7C)-C(7)-H(7B)	109.5

Si(1)-C(9)-H(9A)	109.5

Si(1)-C(9)-H(9B)	109.5

H(9A)-C(9)-H(9B)	109.5

Si(1)-C(9)-H(9C)	109.5

H(9A)-C(9)-H(9C)	109.5

H(9B)-C(9)-H(9C)	109.5

_____________________________________________________________

Symmetry transformations used to generate equivalent atoms:

Table 4.   Anisotropic displacement parameters (Å2x 103)for 2008src0940.  The anisotropic

displacement factor exponent takes the form: -2p2[ h2a*2U11 + ... + 2 h k a* b* U12 ]

______________________________________________________________________________

U11	U22	U33	U23	U13	U12

______________________________________________________________________________

Si(1)	41(1) 	25(1)	19(1) 	13(1)	3(1) 	7(1)

Cl(1)	50(1) 	36(1)	41(1) 	23(1)	19(1) 	9(1)

O(1)	35(2) 	22(1)	19(1) 	10(1)	1(1) 	5(1)

N(1)	25(2) 	25(2)	17(2) 	12(1)	4(1) 	9(1)

C(1)	32(2) 	27(2)	16(2) 	10(2)	2(2) 	6(2)

C(5)	27(2) 	34(2)	35(2) 	24(2)	12(2) 	14(2)

C(6)	23(2) 	27(2)	28(2) 	16(2)	9(2) 	12(2)

C(2)	22(2) 	28(2)	18(2) 	12(2)	6(1) 	11(2)

C(4)	28(2) 	42(2)	24(2) 	21(2)	10(2) 	19(2)

C(3)	26(2) 	32(2)	17(2) 	12(2)	4(1) 	11(2)

C(8)	41(2) 	39(3)	29(2) 	21(2)	3(2) 	-3(2)

F(1)	51(2) 	41(2)	20(1) 	18(1)	2(1) 	4(1)

C(7)	35(2) 	26(2)	31(2) 	13(2)	9(2) 	9(2)

C(9)	65(3) 	39(3)	40(3) 	24(2)	0(2) 	19(3)

______________________________________________________________________________