|  | Single Crystal X-Ray Diffraction Service National Crystallography Service Contact: Dr S.K.Callear, S.K.Callear@soton.ac.uk |
| --- | --- |

Table 1. Crystal data and structure refinement details.

Identification code 	2008src1000  (BF_IPr)

Empirical formula 	C27H36BClF2N2

Formula weight 	472.84

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P2/n

Unit cell dimensions	a = 12.4636(8) Å	( = 90°

b = 7.3364(8) Å	( = 91.529(6)°

c = 15.1611(16) Å	(  = 90°

Volume	1385.8(2) Å3

Z	2

Density (calculated)	1.133 Mg / m3

Absorption coefficient	0.167 mm(1

F(000)	504

Crystal	plate; colourless

Crystal size	0.08 ( 0.05 ( 0.01 mm3

( range for data collection	3.27 ( 27.48°

Index ranges	(15 ( h ( 15, (9 ( k ( 9, (19 ( l ( 19

Reflections collected	12239

Independent reflections	3138 [Rint = 0.1728]

Completeness to ( = 27.48°	98.6 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.9983 and 0.9867

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	3138 / 108 / 167

Goodness-of-fit on F2	1.124

Final R indices [F2 > 2((F2)]	R1 = 0.1746, wR2 = 0.2436

R indices (all data)	R1 = 0.3297, wR2 = 0.3107

Largest diff. peak and hole	0.351 and (0.335 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: Sheldrick, G. M. SADABS - Bruker Nonius area detector scaling and absorption correction - V2.10 Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: ORTEP-3 (L.G. Farrugia, J. Appl. Cryst. (1997) 30, 565).

Special details:

All hydrogen atoms fixed as riding in calculated positions.

The BF2Cl group is highly disordered, however the refinement became unstable when the atoms were split further, therefore the group is modelled in two parts.

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C1	3724(5)	2171(8)	3823(3)	37(2)	1

C2	3265(5)	2324(9)	4637(4)	46(2)	1

C3	3976(5)	2630(10)	5360(4)	53(2)	1

C4	5063(5)	2743(9)	5240(4)	51(2)	1

C5	5473(5)	2599(9)	4414(4)	51(2)	1

C6	4811(5)	2315(9)	3681(4)	41(2)	1

C7	5263(6)	2168(12)	2755(5)	67(2)	1

C8	5851(7)	351(14)	2643(6)	102(3)	1

C9	5973(7)	3819(14)	2549(6)	113(4)	1

C10	2061(5)	2157(12)	4785(5)	66(2)	1

C11	1632(7)	3535(17)	5411(7)	139(5)	1

C12	1797(6)	182(15)	5098(6)	97(3)	1

C14	2500	2806(12)	2500	37(2)	1

C15	2830(5)	(118(9)	2858(4)	49(2)	1

N13	3012(4)	1668(7)	3076(3)	42(1)	1

B1	2337(13)	5002(15)	2586(12)	28(3)	0.50

F1	2169(13)	5663(19)	1706(10)	101(6)	0.50

F2	3379(11)	5708(17)	2831(9)	72(4)	0.50

Cl1	1395(7)	5754(8)	3297(6)	164(3)	0.50

Table 3. Bond lengths [Å] and angles [°].

C1(C2	1.379(7)

C1(C6	1.381(8)

C1(N13	1.467(7)

C2(C3	1.409(8)

C2(C10	1.528(9)

C3(C4	1.374(9)

C3(H3	0.9500

C4(C5	1.369(8)

C4(H4	0.9500

C5(C6	1.381(8)

C5(H5	0.9500

C6(C7	1.532(9)

C7(C8	1.532(11)

C7(C9	1.536(11)

C7(H7	1.0000

C8(H8A	0.9800

C8(H8B	0.9800

C8(H8C	0.9800

C9(H9A	0.9800

C9(H9B	0.9800

C9(H9C	0.9800

C10(C11	1.496(11)

C10(C12	1.563(12)

C10(H10	1.0000

C11(H11A	0.9800

C11(H11B	0.9800

C11(H11C	0.9800

C12(H12A	0.9800

C12(H12B	0.9800

C12(H12C	0.9800

C14(N13i	1.355(7)

C14(N13	1.355(7)

C14(B1i	1.630(14)

C14(B1	1.630(14)

C15(C15i	1.346(11)

C15(N13	1.369(7)

C15(H15	0.9500

B1(F1	1.43(2)

B1(F2	1.44(2)

B1(Cl1	1.708(15)

C2(C1(C6	124.4(5)

C2(C1(N13	117.0(5)

C6(C1(N13	118.4(5)

C1(C2(C3	116.2(6)

C1(C2(C10	123.9(5)

C3(C2(C10	119.9(6)

C4(C3(C2	120.5(6)

C4(C3(H3	119.7

C2(C3(H3	119.7

C5(C4(C3	120.7(6)

C5(C4(H4	119.7

C3(C4(H4	119.7

C4(C5(C6	121.2(6)

C4(C5(H5	119.4

C6(C5(H5	119.4

C1(C6(C5	117.0(5)

C1(C6(C7	121.5(5)

C5(C6(C7	121.5(6)

C6(C7(C8	110.5(6)

C6(C7(C9	111.0(7)

C8(C7(C9	112.6(7)

C6(C7(H7	107.5

C8(C7(H7	107.5

C9(C7(H7	107.5

C7(C8(H8A	109.5

C7(C8(H8B	109.5

H8A(C8(H8B	109.5

C7(C8(H8C	109.5

H8A(C8(H8C	109.5

H8B(C8(H8C	109.5

C7(C9(H9A	109.5

C7(C9(H9B	109.5

H9A(C9(H9B	109.5

C7(C9(H9C	109.5

H9A(C9(H9C	109.5

H9B(C9(H9C	109.5

C11(C10(C2	114.1(7)

C11(C10(C12	110.6(8)

C2(C10(C12	109.6(6)

C11(C10(H10	107.4

C2(C10(H10	107.4

C12(C10(H10	107.4

C10(C11(H11A	109.5

C10(C11(H11B	109.5

H11A(C11(H11B	109.5

C10(C11(H11C	109.5

H11A(C11(H11C	109.5

H11B(C11(H11C	109.5

C10(C12(H12A	109.5

C10(C12(H12B	109.5

H12A(C12(H12B	109.5

C10(C12(H12C	109.5

H12A(C12(H12C	109.5

H12B(C12(H12C	109.5

N13i(C14(N13	104.0(7)

N13i(C14(B1i	127.9(8)

N13(C14(B1i	127.1(8)

N13i(C14(B1	127.1(8)

N13(C14(B1	127.9(8)

B1i(C14(B1	17.2(10)

C15i(C15(N13	106.8(3)

C15i(C15(H15	126.6

N13(C15(H15	126.6

C14(N13(C15	111.2(5)

C14(N13(C1	127.4(5)

C15(N13(C1	121.3(5)

F1(B1(F2	103.2(9)

F1(B1(C14	106.0(11)

F2(B1(C14	105.3(11)

F1(B1(Cl1	113.1(13)

F2(B1(Cl1	110.6(12)

C14(B1(Cl1	117.3(8)

Symmetry transformations used to generate equivalent atoms:

(i) (x+1/2,y,(z+1/2

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C1	54(4) 	36(4)	20(3) 	(3(3)	(8(3) 	11(3)

C2	48(4) 	60(5)	29(3) 	(1(3)	(4(3) 	15(3)

C3	57(4) 	72(5)	30(3) 	5(4)	(6(3) 	3(4)

C4	58(4) 	57(5)	37(4) 	4(3)	(17(3) 	2(4)

C5	43(4) 	59(5)	50(4) 	8(4)	(6(3) 	(1(3)

C6	50(4) 	40(4)	33(3) 	10(3)	0(3) 	3(3)

C7	68(5) 	90(6)	45(4) 	12(4)	10(4) 	(14(5)

C8	119(8) 	119(9)	69(6) 	(6(6)	39(5) 	36(7)

C9	111(8) 	143(10)	86(7) 	42(7)	29(6) 	(52(7)

C10	44(4) 	111(7)	44(4) 	(11(5)	(2(3) 	11(4)

C11	79(7) 	224(14)	113(8) 	(95(9)	(4(6) 	56(8)

C12	46(5) 	160(10)	86(7) 	22(7)	4(4) 	(16(6)

C14	54(5) 	33(5)	24(4) 	0	(9(4) 	0

C15	88(5) 	23(3)	37(4) 	6(3)	(9(3) 	1(3)

N13	60(3) 	35(3)	31(3) 	(1(2)	(10(2) 	8(3)

F1	172(17) 	41(6)	87(11) 	(7(8)	(83(9) 	(9(10)

F2	92(9) 	24(5)	97(11) 	(5(7)	(42(6) 	(5(6)

Cl1	199(8) 	52(3)	244(9) 	(3(5)	97(6) 	9(4)