|  | Single Crystal X-Ray Diffraction Service National Crystallography Service Contact: Dr S.K.Callear, S.K.Callear@soton.ac.uk |
| --- | --- |

Table 1. Crystal data and structure refinement details.

Identification code 	2009src0001 (bc29)

Empirical formula 	C22H35BN2O4

Formula weight 	402.33

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Triclinic

Space group 	P(1

Unit cell dimensions	a = 10.0998(2) Å	( = 100.067(2)°

b = 10.2807(2) Å	( = 100.4290(10)°

c = 11.7549(3) Å	(  = 103.216(2)°

Volume	1138.41(4) Å3

Z	2

Density (calculated)	1.174 Mg / m3

Absorption coefficient	0.079 mm(1

F(000)	436

Crystal	block; colourless

Crystal size	0.19 ( 0.10 ( 0.03 mm3

( range for data collection	3.06 ( 27.48°

Index ranges	(13 ( h ( 13, (13 ( k ( 13, (15 ( l ( 15

Reflections collected	23179

Independent reflections	5193 [Rint = 0.0435]

Completeness to ( = 27.48°	99.7 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.9976 and 0.9851

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	5193 / 0 / 269

Goodness-of-fit on F2	1.070

Final R indices [F2 > 2((F2)]	R1 = 0.0555, wR2 = 0.1051

R indices (all data)	R1 = 0.0740, wR2 = 0.1151

Largest diff. peak and hole	0.265 and (0.251 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: Sheldrick, G. M. SADABS - Bruker Nonius area detector scaling and absorption correction - V2.10 Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: ORTEP-3 (L.G. Farrugia, J. Appl. Cryst. (1997) 30, 565).

Special details:

All hydrogens fixed using a standard riding model.

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C3	2324(2)	1485(2)	7521(2)	24(1)	1

C4	2676(2)	3043(2)	7528(2)	23(1)	1

C6	1353(2)	600(2)	6365(2)	34(1)	1

C7	3576(2)	934(2)	7860(2)	37(1)	1

C8	3956(2)	3902(2)	8486(2)	32(1)	1

C9	2773(2)	3387(2)	6336(2)	31(1)	1

C10	(170(2)	2618(2)	9245(1)	19(1)	1

C11	(224(2)	1871(2)	10132(2)	24(1)	1

C12	(1136(2)	1947(2)	10875(2)	28(1)	1

C13	(2039(2)	2770(2)	10735(2)	29(1)	1

C14	(2020(2)	3502(2)	9851(2)	25(1)	1

C15	(1101(2)	3446(2)	9107(1)	20(1)	1

C16	(1117(2)	4238(2)	8140(1)	22(1)	1

C18	(1291(2)	4044(2)	6040(1)	22(1)	1

C19	(1764(2)	3065(2)	4831(2)	25(1)	1

C21	(3654(2)	1699(2)	5514(2)	26(1)	1

C22	(3140(2)	2713(2)	6709(2)	23(1)	1

C23	(4126(2)	2391(2)	3579(1)	22(1)	1

C26	(6582(2)	1650(2)	2511(2)	24(1)	1

C27	(6361(2)	959(2)	1334(2)	36(1)	1

C28	(6694(2)	3098(2)	2547(2)	38(1)	1

C29	(7864(2)	798(2)	2803(2)	31(1)	1

B1	927(2)	2491(2)	8486(2)	20(1)	1

N17	(1631(1)	3319(1)	6953(1)	19(1)	1

N20	(3250(2)	2375(2)	4591(1)	26(1)	1

O2	1506(1)	1403(1)	8424(1)	25(1)	1

O5	1475(1)	3424(1)	7876(1)	23(1)	1

O24	(3754(1)	2998(1)	2843(1)	29(1)	1

O25	(5441(1)	1645(1)	3495(1)	24(1)	1

Table 3. Bond lengths [Å] and angles [°].

C3(O2	1.461(2)

C3(C7	1.517(2)

C3(C6	1.521(3)

C3(C4	1.558(2)

C4(O5	1.4597(19)

C4(C9	1.518(2)

C4(C8	1.524(2)

C6(H6A	0.9800

C6(H6B	0.9800

C6(H6C	0.9800

C7(H7A	0.9800

C7(H7B	0.9800

C7(H7C	0.9800

C8(H8A	0.9800

C8(H8B	0.9800

C8(H8C	0.9800

C9(H9A	0.9800

C9(H9B	0.9800

C9(H9C	0.9800

C10(C11	1.400(2)

C10(C15	1.412(2)

C10(B1	1.557(2)

C11(C12	1.385(2)

C11(H11	0.9500

C12(C13	1.386(3)

C12(H12	0.9500

C13(C14	1.386(3)

C13(H13	0.9500

C14(C15	1.389(2)

C14(H14	0.9500

C15(C16	1.510(2)

C16(N17	1.470(2)

C16(H16A	0.9900

C16(H16B	0.9900

C18(N17	1.457(2)

C18(C19	1.516(2)

C18(H18A	0.9900

C18(H18B	0.9900

C19(N20	1.458(2)

C19(H19A	0.9900

C19(H19B	0.9900

C21(N20	1.455(2)

C21(C22	1.518(2)

C21(H21A	0.9900

C21(H21B	0.9900

C22(N17	1.462(2)

C22(H22A	0.9900

C22(H22B	0.9900

C23(O24	1.216(2)

C23(O25	1.350(2)

C23(N20	1.353(2)

C26(O25	1.4793(19)

C26(C28	1.513(2)

C26(C27	1.519(2)

C26(C29	1.520(2)

C27(H27A	0.9800

C27(H27B	0.9800

C27(H27C	0.9800

C28(H28A	0.9800

C28(H28B	0.9800

C28(H28C	0.9800

C29(H29A	0.9800

C29(H29B	0.9800

C29(H29C	0.9800

B1(O5	1.372(2)

B1(O2	1.373(2)

O2(C3(C7	109.15(14)

O2(C3(C6	106.00(14)

C7(C3(C6	110.84(16)

O2(C3(C4	102.03(12)

C7(C3(C4	115.33(15)

C6(C3(C4	112.66(15)

O5(C4(C9	108.67(14)

O5(C4(C8	106.23(13)

C9(C4(C8	110.46(15)

O5(C4(C3	101.99(12)

C9(C4(C3	115.19(15)

C8(C4(C3	113.47(15)

C3(C6(H6A	109.5

C3(C6(H6B	109.5

H6A(C6(H6B	109.5

C3(C6(H6C	109.5

H6A(C6(H6C	109.5

H6B(C6(H6C	109.5

C3(C7(H7A	109.5

C3(C7(H7B	109.5

H7A(C7(H7B	109.5

C3(C7(H7C	109.5

H7A(C7(H7C	109.5

H7B(C7(H7C	109.5

C4(C8(H8A	109.5

C4(C8(H8B	109.5

H8A(C8(H8B	109.5

C4(C8(H8C	109.5

H8A(C8(H8C	109.5

H8B(C8(H8C	109.5

C4(C9(H9A	109.5

C4(C9(H9B	109.5

H9A(C9(H9B	109.5

C4(C9(H9C	109.5

H9A(C9(H9C	109.5

H9B(C9(H9C	109.5

C11(C10(C15	117.96(15)

C11(C10(B1	117.61(15)

C15(C10(B1	124.43(15)

C12(C11(C10	121.94(16)

C12(C11(H11	119.0

C10(C11(H11	119.0

C11(C12(C13	119.54(16)

C11(C12(H12	120.2

C13(C12(H12	120.2

C14(C13(C12	119.56(16)

C14(C13(H13	120.2

C12(C13(H13	120.2

C13(C14(C15	121.47(16)

C13(C14(H14	119.3

C15(C14(H14	119.3

C14(C15(C10	119.52(15)

C14(C15(C16	120.35(15)

C10(C15(C16	120.12(14)

N17(C16(C15	111.60(13)

N17(C16(H16A	109.3

C15(C16(H16A	109.3

N17(C16(H16B	109.3

C15(C16(H16B	109.3

H16A(C16(H16B	108.0

N17(C18(C19	110.22(13)

N17(C18(H18A	109.6

C19(C18(H18A	109.6

N17(C18(H18B	109.6

C19(C18(H18B	109.6

H18A(C18(H18B	108.1

N20(C19(C18	110.43(14)

N20(C19(H19A	109.6

C18(C19(H19A	109.6

N20(C19(H19B	109.6

C18(C19(H19B	109.6

H19A(C19(H19B	108.1

N20(C21(C22	109.62(14)

N20(C21(H21A	109.7

C22(C21(H21A	109.7

N20(C21(H21B	109.7

C22(C21(H21B	109.7

H21A(C21(H21B	108.2

N17(C22(C21	110.79(14)

N17(C22(H22A	109.5

C21(C22(H22A	109.5

N17(C22(H22B	109.5

C21(C22(H22B	109.5

H22A(C22(H22B	108.1

O24(C23(O25	125.07(15)

O24(C23(N20	123.47(15)

O25(C23(N20	111.46(14)

O25(C26(C28	110.07(14)

O25(C26(C27	110.01(14)

C28(C26(C27	113.05(16)

O25(C26(C29	102.46(13)

C28(C26(C29	110.10(15)

C27(C26(C29	110.64(15)

C26(C27(H27A	109.5

C26(C27(H27B	109.5

H27A(C27(H27B	109.5

C26(C27(H27C	109.5

H27A(C27(H27C	109.5

H27B(C27(H27C	109.5

C26(C28(H28A	109.5

C26(C28(H28B	109.5

H28A(C28(H28B	109.5

C26(C28(H28C	109.5

H28A(C28(H28C	109.5

H28B(C28(H28C	109.5

C26(C29(H29A	109.5

C26(C29(H29B	109.5

H29A(C29(H29B	109.5

C26(C29(H29C	109.5

H29A(C29(H29C	109.5

H29B(C29(H29C	109.5

O5(B1(O2	112.76(15)

O5(B1(C10	126.37(15)

O2(B1(C10	120.78(15)

C18(N17(C22	110.00(12)

C18(N17(C16	110.97(12)

C22(N17(C16	110.90(13)

C23(N20(C21	125.44(14)

C23(N20(C19	120.38(14)

C21(N20(C19	114.19(13)

B1(O2(C3	106.89(13)

B1(O5(C4	107.16(13)

C23(O25(C26	119.61(13)

Symmetry transformations used to generate equivalent atoms:

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C3	25(1) 	24(1)	27(1) 	5(1)	12(1) 	8(1)

C4	20(1) 	24(1)	26(1) 	4(1)	9(1) 	7(1)

C6	36(1) 	28(1)	34(1) 	(4(1)	14(1) 	2(1)

C7	34(1) 	37(1)	52(1) 	17(1)	21(1) 	19(1)

C8	21(1) 	35(1)	34(1) 	0(1)	6(1) 	1(1)

C9	30(1) 	36(1)	32(1) 	12(1)	14(1) 	10(1)

C10	16(1) 	20(1)	19(1) 	1(1)	2(1) 	2(1)

C11	23(1) 	22(1)	23(1) 	4(1)	3(1) 	4(1)

C12	29(1) 	29(1)	22(1) 	7(1)	7(1) 	2(1)

C13	24(1) 	35(1)	23(1) 	(1(1)	11(1) 	2(1)

C14	20(1) 	27(1)	25(1) 	(2(1)	3(1) 	6(1)

C15	18(1) 	19(1)	19(1) 	(1(1)	1(1) 	2(1)

C16	22(1) 	19(1)	21(1) 	0(1)	1(1) 	7(1)

C18	18(1) 	22(1)	24(1) 	6(1)	4(1) 	3(1)

C19	20(1) 	30(1)	24(1) 	5(1)	4(1) 	3(1)

C21	24(1) 	27(1)	22(1) 	9(1)	0(1) 	(3(1)

C22	17(1) 	28(1)	23(1) 	9(1)	3(1) 	3(1)

C23	23(1) 	22(1)	20(1) 	2(1)	6(1) 	5(1)

C26	23(1) 	26(1)	21(1) 	7(1)	0(1) 	8(1)

C27	31(1) 	51(1)	23(1) 	2(1)	1(1) 	14(1)

C28	32(1) 	29(1)	54(1) 	13(1)	4(1) 	11(1)

C29	24(1) 	36(1)	30(1) 	11(1)	0(1) 	4(1)

B1	19(1) 	20(1)	19(1) 	2(1)	1(1) 	4(1)

N17	16(1) 	20(1)	18(1) 	2(1)	2(1) 	3(1)

N20	22(1) 	32(1)	20(1) 	9(1)	1(1) 	(3(1)

O2	26(1) 	25(1)	29(1) 	9(1)	12(1) 	10(1)

O5	20(1) 	22(1)	29(1) 	6(1)	9(1) 	7(1)

O24	28(1) 	37(1)	23(1) 	11(1)	7(1) 	5(1)

O25	22(1) 	27(1)	20(1) 	7(1)	(1(1) 	2(1)