|  | # Single Crystal X-Ray Diffraction Service National Crystallography Service Contact: Dr S.K.Callear, S.K.Callear@soton.ac.uk |
| --- | --- |

Table 1. Crystal data and structure refinement details.

Identification code 	2009src0013 (TDB – ZIF?)

Empirical formula 	C7.50H9.50N4.50O0.50Zn

Formula weight 	236.07

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Orthorhombic

Space group 	Pbca

Unit cell dimensions	a = 15.5741(6) Å	 = 90°

b = 14.8047(4) Å	 = 90°

c = 18.4602(8) Å	  = 90°

Volume	4256.4(3) Å3

Z	16

Density (calculated)	1.474 Mg / m3

Absorption coefficient	2.277 mm1

F(000)	1920

Crystal	block; colourless

Crystal size	0.38  0.22  0.10 mm3

 range for data collection	2.91  27.48°

Index ranges	20  h  19, 16  k  19, 22  l  23

Reflections collected	31399

Independent reflections	4866 [Rint = 0.0956]

Completeness to  = 27.48°	99.8 %

Absorption correction	Semiempirical from equivalents

Max. and min. transmission	0.8043 and 0.4783

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	4866 / 8 / 244

Goodness-of-fit on F2	1.014

Final R indices [F2 > 2(F2)]	R1 = 0.0473, wR2 = 0.0994

R indices (all data)	R1 = 0.0889, wR2 = 0.1143

Largest diff. peak and hole	0.570 and 0.558 e Å3

Diffractometer: Nonius KappaCCD area detector ( scans and  scans to fill asymmetric unit). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: Sheldrick, G. M. SADABS - Bruker Nonius area detector scaling and absorption correction - V2.10 Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: ORTEP-3 (L.G. Farrugia, J. Appl. Cryst. (1997) 30, 565).

Special details:

All hydrogens fixed using a riding model.

The DMF molecule was refined isotropically due to it being disordered; the disorder results in larger thermal parameters where the molecule is moving about its position.

Table 2. Atomic coordinates [ 104], equivalent isotropic displacement parameters [Å2  103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C52	2689(4)	11611(4)	6069(4)	46(2)	0.791(8)

C54	1482(4)	11365(4)	5270(4)	59(2)	0.791(8)

C55	1272(6)	12121(6)	6434(6)	106(3)	0.791(8)

N53	1851(4)	11670(5)	5927(3)	48(2)	0.791(8)

O51	3203(3)	11199(4)	5662(4)	54(2)	0.791(8)

C62	2436(13)	11599(17)	5460(13)	73(9)	0.209(8)

C64	1077(16)	12390(20)	5702(18)	106(13)	0.209(8)

C65	2040(20)	11990(30)	6678(13)	128(15)	0.209(8)

N63	1850(10)	11954(15)	5891(9)	29(5)	0.209(8)

O61	3161(11)	11411(14)	5737(12)	36(6)	0.209(8)

C2	1047(2)	8445(2)	5519(2)	24(1)	1

C4	2203(3)	9171(3)	5733(2)	46(1)	1

C5	1744(3)	9117(3)	6352(2)	46(1)	1

N1	1004(2)	8651(2)	6217(2)	26(1)	1

N3	1754(2)	8753(2)	5189(2)	27(1)	1

C22	975(2)	7362(2)	8076(2)	27(1)	1

C24	713(3)	6292(3)	3444(2)	34(1)	1

C25	1166(3)	6721(3)	3961(2)	35(1)	1

N21	1340(2)	7585(2)	3737(2)	27(1)	1

N23	589(2)	8126(2)	7873(2)	27(1)	1

C32	1432(2)	7321(3)	6412(2)	29(1)	1

C34	311(2)	6562(3)	6110(2)	34(1)	1

N31	3264(2)	8378(2)	3961(2)	28(1)	1

N33	576(2)	7325(2)	6475(2)	27(1)	1

C42	943(2)	9878(2)	6379(2)	26(1)	1

C43	3988(2)	8858(3)	4159(2)	35(1)	1

C44	1970(3)	9871(3)	2880(2)	40(1)	1

C45	1427(3)	9517(3)	7424(2)	39(1)	1

N41	771(2)	9353(2)	6948(2)	26(1)	1

N43	1661(2)	9640(2)	3551(2)	29(1)	1

Zn1	2032(1)	8592(1)	4157(1)	24(1)	1

Zn2	77(1)	8345(1)	6913(1)	26(1)	1

Table 3. Bond lengths [Å] and angles [°].

C52O51	1.256(8)

C52N53	1.334(8)

C52H52	0.9500

C54N53	1.416(8)

C54H54A	0.9800

C54H54B	0.9800

C54H54C	0.9800

C55N53	1.461(10)

C55H55A	0.9800

C55H55B	0.9800

C55H55C	0.9800

C62O61	1.270(18)

C62N63	1.320(17)

C62H62	0.9500

C64N63	1.411(17)

C64H64A	0.9800

C64H64B	0.9800

C64H64C	0.9800

C65N63	1.482(18)

C65H65A	0.9800

C65H65B	0.9800

C65H65C	0.9800

C2N1	1.326(5)

C2N3	1.339(4)

C2H2	0.9500

C4C5	1.350(6)

C4N3	1.371(5)

C4H4	0.9500

C5N1	1.366(5)

C5H5	0.9500

N1Zn2	1.986(3)

N3Zn1	1.968(3)

C22N23	1.335(5)

C22N21i	1.348(5)

C22H22	0.9500

C24C25	1.346(5)

C24N23ii	1.376(5)

C24H24	0.9500

C25N21	1.371(5)

C25H25	0.9500

N21C22ii	1.348(5)

N21Zn1	1.995(3)

N23C24i	1.376(5)

N23Zn2	1.969(3)

C32N31iii	1.331(5)

C32N33	1.339(4)

C32H32	0.9500

C34C43iii	1.352(5)

C34N33	1.379(5)

C34H34	0.9500

N31C32iv	1.331(5)

N31C43	1.382(5)

N31Zn1	1.977(3)

N33Zn2	1.991(3)

C42N43v	1.333(4)

C42N41	1.335(5)

C42H42	0.9500

C43C34iv	1.352(5)

C43H43	0.9500

C44C45v	1.361(6)

C44N43	1.372(5)

C44H44	0.9500

C45C44v	1.361(6)

C45N41	1.370(5)

C45H45	0.9500

N41Zn2	1.994(3)

N43C42v	1.333(4)

N43Zn1	1.999(3)

O51C52N53	122.5(7)

O51C52H52	118.7

N53C52H52	118.7

C52N53C54	123.0(6)

C52N53C55	120.5(7)

C54N53C55	116.4(6)

O61C62N63	117(2)

O61C62H62	121.3

N63C62H62	121.3

N63C64H64A	109.5

N63C64H64B	109.5

H64AC64H64B	109.5

N63C64H64C	109.5

H64AC64H64C	109.5

H64BC64H64C	109.5

N63C65H65A	109.5

N63C65H65B	109.5

H65AC65H65B	109.5

N63C65H65C	109.5

H65AC65H65C	109.5

H65BC65H65C	109.5

C62N63C64	128.6(19)

C62N63C65	118.0(18)

C64N63C65	113.1(19)

N1C2N3	113.9(3)

N1C2H2	123.1

N3C2H2	123.1

C5C4N3	108.9(4)

C5C4H4	125.6

N3C4H4	125.6

C4C5N1	108.8(4)

C4C5H5	125.6

N1C5H5	125.6

C2N1C5	104.5(3)

C2N1Zn2	127.8(2)

C5N1Zn2	127.6(3)

C2N3C4	103.9(3)

C2N3Zn1	125.4(2)

C4N3Zn1	130.7(3)

N23C22N21i	113.3(3)

N23C22H22	123.4

N21iC22H22	123.4

C25C24N23ii	108.7(3)

C25C24H24	125.7

N23iiC24H24	125.7

C24C25N21	109.3(4)

C24C25H25	125.3

N21C25H25	125.3

C22iiN21C25	104.1(3)

C22iiN21Zn1	122.4(2)

C25N21Zn1	133.3(3)

C22N23C24i	104.6(3)

C22N23Zn2	125.1(3)

C24iN23Zn2	130.0(3)

N31iiiC32N33	113.8(3)

N31iiiC32H32	123.1

N33C32H32	123.1

C43iiiC34N33	108.3(3)

C43iiiC34H34	125.8

N33C34H34	125.8

C32ivN31C43	104.3(3)

C32ivN31Zn1	124.3(3)

C43N31Zn1	131.4(3)

C32N33C34	104.6(3)

C32N33Zn2	123.2(3)

C34N33Zn2	131.8(2)

N43vC42N41	113.8(3)

N43vC42H42	123.1

N41C42H42	123.1

C34ivC43N31	109.0(4)

C34ivC43H43	125.5

N31C43H43	125.5

C45vC44N43	108.6(3)

C45vC44H44	125.7

N43C44H44	125.7

C44vC45N41	108.5(4)

C44vC45H45	125.7

N41C45H45	125.7

C42N41C45	104.5(3)

C42N41Zn2	122.9(3)

C45N41Zn2	130.4(3)

C42vN43C44	104.5(3)

C42vN43Zn1	127.1(3)

C44N43Zn1	126.6(3)

N3Zn1N31	114.17(13)

N3Zn1N21	110.38(12)

N31Zn1N21	109.48(13)

N3Zn1N43	112.59(13)

N31Zn1N43	107.58(12)

N21Zn1N43	101.90(13)

N23Zn2N1	109.00(12)

N23Zn2N33	116.60(13)

N1Zn2N33	106.35(12)

N23Zn2N41	111.23(13)

N1Zn2N41	109.32(12)

N33Zn2N41	104.02(12)

Symmetry transformations used to generate equivalent atoms:

(i) x,y+3/2,z+1/2    (ii) x,y+3/2,z1/2    (iii) x1/2,y+3/2,z+1

(iv)  x+1/2,y+3/2,z+1    (v) x,y+2,z+1

Table 4. Anisotropic displacement parameters [Å2 103]. The anisotropic displacement

factor exponent takes the form: 2 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C2	20(2) 	34(2)	19(2) 	3(2)	3(2) 	3(2)

C4	36(2) 	69(3)	34(3) 	14(2)	4(2) 	24(2)

C5	36(2) 	74(3)	28(3) 	21(2)	3(2) 	23(2)

N1	20(2) 	36(2)	20(2) 	2(1)	1(1) 	5(1)

N3	26(2) 	34(2)	21(2) 	2(1)	2(1) 	4(1)

C22	28(2) 	33(2)	20(2) 	2(2)	1(2) 	2(2)

C24	42(2) 	32(2)	28(2) 	2(2)	10(2) 	10(2)

C25	42(2) 	32(2)	29(2) 	11(2)	12(2) 	1(2)

N21	27(2) 	33(2)	20(2) 	1(1)	2(1) 	1(1)

N23	25(2) 	35(2)	21(2) 	2(2)	2(1) 	1(1)

C32	24(2) 	41(2)	21(2) 	1(2)	0(2) 	3(2)

C34	20(2) 	40(2)	42(3) 	1(2)	1(2) 	6(2)

N31	24(2) 	33(2)	25(2) 	0(1)	1(1) 	0(1)

N33	23(2) 	33(2)	24(2) 	3(1)	2(1) 	2(1)

C42	26(2) 	32(2)	19(2) 	0(2)	3(2) 	2(2)

C43	28(2) 	32(2)	44(3) 	0(2)	2(2) 	2(2)

C44	38(2) 	45(3)	38(3) 	13(2)	19(2) 	8(2)

C45	43(2) 	46(2)	29(2) 	12(2)	17(2) 	14(2)

N41	27(2) 	34(2)	19(2) 	3(1)	1(1) 	0(1)

N43	26(2) 	32(2)	28(2) 	5(2)	2(1) 	4(1)

Zn1	22(1) 	31(1)	20(1) 	1(1)	0(1) 	1(1)

Zn2	23(1) 	35(1)	19(1) 	2(1)	2(1) 	1(1)