|  | Single Crystal X-Ray Diffraction Service National Crystallography Service Contact: Dr S.K.Callear, S.K.Callear@soton.ac.uk |
| --- | --- |

Table 1. Crystal data and structure refinement details.

Identification code 	2008src1285 (HP122(5))

Empirical formula 	C14H15N3OS

Formula weight 	273.35

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P21

Unit cell dimensions	a = 6.2780(3) Å	( = 90°

b = 7.5736(2) Å	( = 101.879(2)°

c = 13.9057(7) Å	(  = 90°

Volume	647.02(5) Å3

Z	2

Density (calculated)	1.403 Mg / m3

Absorption coefficient	0.245 mm(1

F(000)	288

Crystal	block; colourless

Crystal size	0.25 ( 0.22 ( 0.06 mm3

( range for data collection	3.08 ( 27.47°

Index ranges	(8 ( h ( 8, (9 ( k ( 9, (16 ( l ( 18

Reflections collected	8645

Independent reflections	2932 [Rint = 0.0590]

Completeness to ( = 27.47°	99.6 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.9854 and 0.9412

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	2932 / 1 / 172

Goodness-of-fit on F2	1.030

Final R indices [F2 > 2((F2)]	R1 = 0.0474, wR2 = 0.1012

R indices (all data)	R1 = 0.0664, wR2 = 0.1111

Absolute structure parameter	(0.14(10)

Largest diff. peak and hole	0.221 and (0.319 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: Sheldrick, G. M. SADABS - Bruker Nonius area detector scaling and absorption correction - V2.10 Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: ORTEP-3 (L.G. Farrugia, J. Appl. Cryst. (1997) 30, 565).

Special details:

All hydrogens were fixed using a standard riding model.

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C2	11700(5)	7317(4)	7292(2)	28(1)	1

C3	10768(5)	6559(4)	8002(2)	32(1)	1

C4	8598(5)	6053(4)	7727(2)	34(1)	1

C5	7503(5)	6283(4)	6777(2)	29(1)	1

C6	8579(4)	7059(3)	6088(2)	24(1)	1

C8	5354(4)	6834(4)	4689(2)	27(1)	1

C9	5336(5)	5653(4)	3816(2)	24(1)	1

C11	8625(4)	7128(3)	3521(2)	21(1)	1

C12	8658(5)	8234(4)	4425(2)	29(1)	1

C13	5256(4)	6791(4)	2178(2)	22(1)	1

C14	6404(4)	7359(3)	1398(2)	21(1)	1

C15	8407(4)	6913(4)	1236(2)	24(1)	1

C16	8805(4)	7648(4)	345(2)	26(1)	1

C17	7117(4)	8635(4)	(139(2)	27(1)	1

N1	10676(4)	7564(3)	6354(2)	28(1)	1

N7	7572(4)	7339(4)	5126(2)	39(1)	1

N10	6411(3)	6534(3)	3107(2)	23(1)	1

O18	3273(3)	6515(3)	1959(1)	30(1)	1

S1	4989(1)	8650(1)	458(1)	26(1)	1

Table 3. Bond lengths [Å] and angles [°].

C2(N1	1.344(4)

C2(C3	1.374(4)

C2(H2	0.9500

C3(C4	1.391(4)

C3(H3	0.9500

C4(C5	1.369(4)

C4(H4	0.9500

C5(C6	1.409(4)

C5(H5	0.9500

C6(N1	1.348(3)

C6(N7	1.374(4)

C8(N7	1.451(4)

C8(C9	1.507(4)

C8(H8A	0.9900

C8(H8B	0.9900

C9(N10	1.465(3)

C9(H9A	0.9900

C9(H9B	0.9900

C11(N10	1.462(3)

C11(C12	1.507(4)

C11(H11A	0.9900

C11(H11B	0.9900

C12(N7	1.465(3)

C12(H12A	0.9900

C12(H12B	0.9900

C13(O18	1.237(3)

C13(N10	1.358(3)

C13(C14	1.484(4)

C14(C15	1.365(4)

C14(S1	1.725(3)

C15(C16	1.427(4)

C15(H15	0.9500

C16(C17	1.357(4)

C16(H16	0.9500

C17(S1	1.712(2)

C17(H17	0.9500

N1(C2(C3	124.6(3)

N1(C2(H2	117.7

C3(C2(H2	117.7

C2(C3(C4	117.1(3)

C2(C3(H3	121.5

C4(C3(H3	121.5

C5(C4(C3	119.9(3)

C5(C4(H4	120.0

C3(C4(H4	120.0

C4(C5(C6	119.6(3)

C4(C5(H5	120.2

C6(C5(H5	120.2

N1(C6(N7	116.7(2)

N1(C6(C5	120.7(3)

N7(C6(C5	122.5(2)

N7(C8(C9	109.9(2)

N7(C8(H8A	109.7

C9(C8(H8A	109.7

N7(C8(H8B	109.7

C9(C8(H8B	109.7

H8A(C8(H8B	108.2

N10(C9(C8	110.2(2)

N10(C9(H9A	109.6

C8(C9(H9A	109.6

N10(C9(H9B	109.6

C8(C9(H9B	109.6

H9A(C9(H9B	108.1

N10(C11(C12	110.4(2)

N10(C11(H11A	109.6

C12(C11(H11A	109.6

N10(C11(H11B	109.6

C12(C11(H11B	109.6

H11A(C11(H11B	108.1

N7(C12(C11	111.7(2)

N7(C12(H12A	109.3

C11(C12(H12A	109.3

N7(C12(H12B	109.3

C11(C12(H12B	109.3

H12A(C12(H12B	107.9

O18(C13(N10	121.5(2)

O18(C13(C14	119.0(2)

N10(C13(C14	119.5(2)

C15(C14(C13	130.7(3)

C15(C14(S1	111.28(19)

C13(C14(S1	117.80(19)

C14(C15(C16	112.3(3)

C14(C15(H15	123.9

C16(C15(H15	123.9

C17(C16(C15	112.8(2)

C17(C16(H16	123.6

C15(C16(H16	123.6

C16(C17(S1	111.8(2)

C16(C17(H17	124.1

S1(C17(H17	124.1

C2(N1(C6	118.1(2)

C6(N7(C8	125.1(2)

C6(N7(C12	122.4(2)

C8(N7(C12	112.4(2)

C13(N10(C11	127.5(2)

C13(N10(C9	118.4(2)

C11(N10(C9	114.0(2)

C17(S1(C14	91.86(13)

Symmetry transformations used to generate equivalent atoms:

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C2	28(1) 	27(2)	30(2) 	(2(1)	6(1) 	(1(1)

C3	35(2) 	33(2)	29(2) 	4(1)	6(1) 	6(1)

C4	39(2) 	35(2)	32(2) 	9(1)	15(2) 	1(1)

C5	30(2) 	26(2)	32(2) 	0(1)	12(1) 	(3(1)

C6	26(1) 	22(1)	25(2) 	(8(1)	10(1) 	(5(1)

C8	23(1) 	33(2)	26(2) 	(3(1)	11(1) 	(7(1)

C9	22(1) 	26(2)	24(2) 	1(1)	7(1) 	(6(1)

C11	17(1) 	26(2)	21(1) 	4(1)	1(1) 	(5(1)

C12	31(2) 	35(2)	20(1) 	(3(1)	6(1) 	(16(1)

C13	16(1) 	27(1)	22(2) 	(2(1)	4(1) 	1(1)

C14	17(1) 	25(1)	19(1) 	(2(1)	0(1) 	(2(1)

C15	17(1) 	30(2)	26(2) 	(1(1)	2(1) 	0(1)

C16	21(1) 	35(2)	24(1) 	(4(1)	7(1) 	(2(1)

C17	28(1) 	33(1)	22(1) 	1(2)	7(1) 	(4(2)

N1	29(1) 	32(1)	24(1) 	(3(1)	8(1) 	(5(1)

N7	34(1) 	65(2)	19(1) 	(3(1)	9(1) 	(30(1)

N10	15(1) 	34(1)	19(1) 	1(1)	2(1) 	(7(1)

O18	14(1) 	46(1)	28(1) 	(1(1)	3(1) 	(1(1)

S1	21(1) 	32(1)	24(1) 	2(1)	2(1) 	3(1)