|  | Single Crystal X-Ray Diffraction Service National Crystallography Service Contact: Dr S.K.Callear, S.K.Callear@soton.ac.uk |
| --- | --- |

Table 1. Crystal data and structure refinement details.

Identification code 	2009src0059p21c  (JN50)

Empirical formula 	C10H10La2O16S2W2

Formula weight 	1095.82

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P21/c

Unit cell dimensions	a = 17.1242(11) Å	( = 90°

b = 7.4638(5) Å	( = 91.048(4)°

c = 7.6228(5) Å	(  = 90°

Volume	974.12(11) Å3

Z	2

Density (calculated)	3.736 Mg / m3

Absorption coefficient	16.365 mm(1

F(000)	984

Crystal	lath; colourless

Crystal size	0.10 ( 0.04 ( 0.01 mm3

( range for data collection	2.98 ( 27.47°

Index ranges	(22 ( h ( 22, (9 ( k ( 9, (9 ( l ( 9

Reflections collected	10570

Independent reflections	2214 [Rint = 0.0782]

Completeness to ( = 27.47°	99.8 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.8535 and 0.2914

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	2214 / 33 / 153

Goodness-of-fit on F2	1.121

Final R indices [F2 > 2((F2)]	R1 = 0.0595, wR2 = 0.1166

R indices (all data)	R1 = 0.0770, wR2 = 0.1255

Largest diff. peak and hole	2.082 and (2.510 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: Sheldrick, G. M. SADABS - Bruker Nonius area detector scaling and absorption correction - V2.10 Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: ORTEP-3 (L.G. Farrugia, J. Appl. Cryst. (1997) 30, 565).

Special details:

All hydrogen atoms except water hydrogens were fixed using a standard riding model. The water hydrogen atoms were restrained used DFIX, DANG and the thermal parameters were refined.

The ISOR command was used for atoms C1, C2, C3, C4, C5 and C6 as these were non- positive definites. This is not surprising for these types of structures were a number of heavy atoms are present with light atoms.

The second WGHT parameter is larger than usual - this is due to the difference in the weights of the atoms present. To address this problem a number of absorption corrections were tried, of which this was found to give the best results.

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C1	963(9)	3930(20)	620(20)	18(3)	1

C2	741(9)	2270(20)	1140(20)	15(3)	1

C3	(58(9)	1810(20)	1167(18)	16(3)	1

C4	401(9)	5240(20)	(30(20)	18(3)	1

C5	618(9)	6970(20)	(627(19)	13(3)	1

O3	3919(7)	4440(16)	492(15)	26(3)	1

O4	3734(7)	4058(14)	4103(15)	23(3)	1

O21	1973(7)	6050(15)	2107(14)	23(3)	1

O22	2246(7)	5021(17)	(850(15)	25(3)	1

O23	2348(7)	2951(16)	1598(15)	24(3)	1

O1W	2403(7)	(725(16)	649(15)	23(3)	1

O1	5145(7)	5808(15)	2828(13)	19(2)	1

O2	3685(6)	7686(15)	2565(14)	20(2)	1

La1	3445(1)	917(1)	2377(1)	14(1)	1

W1	4134(1)	5552(1)	2508(1)	14(1)	1

S1	1956(2)	4537(5)	875(5)	17(1)	1

Table 3. Bond lengths [Å] and angles [°].

C1(C2	1.36(2)

C1(C4	1.45(2)

C1(S1	1.768(16)

C2(C3	1.41(2)

C2(H2	0.9500

C3(C5i	1.38(2)

C3(H3	0.9500

C4(C5	1.42(2)

C4(C4i	1.42(3)

C5(C3i	1.38(2)

C5(H5	0.9500

O3(W1	1.779(12)

O3(La1ii	2.510(12)

O4(W1	1.795(11)

O4(La1iii	2.553(12)

O4(La1	2.729(11)

O21(S1	1.469(12)

O22(S1	1.459(12)

O22(La1ii	2.575(12)

O23(S1	1.464(12)

O23(La1	2.480(11)

O1W(La1	2.518(11)

O1W(H2W	0.85(2)

O1W(H1W	0.85(2)

O1(W1	1.755(12)

O1(La1iv	2.423(12)

O2(W1	1.770(11)

O2(La1v	2.450(11)

La1(O1vi	2.423(12)

La1(O2vii	2.450(11)

La1(O3iii	2.510(12)

La1(O4ii	2.553(12)

La1(O22iii	2.575(12)

La1(W1	3.6555(10)

C2(C1(C4	121.9(14)

C2(C1(S1	118.5(12)

C4(C1(S1	119.5(12)

C1(C2(C3	120.1(14)

C1(C2(H2	119.9

C3(C2(H2	119.9

C5i(C3(C2	120.3(14)

C5i(C3(H3	119.9

C2(C3(H3	119.9

C5(C4(C4i	120.0(18)

C5(C4(C1	123.2(14)

C4i(C4(C1	116.8(18)

C3i(C5(C4	120.7(14)

C3i(C5(H5	119.6

C4(C5(H5	119.6

W1(O3(La1ii	157.7(7)

W1(O4(La1iii	137.8(6)

W1(O4(La1	106.0(5)

La1iii(O4(La1	116.2(4)

S1(O22(La1ii	133.9(7)

S1(O23(La1	157.8(7)

La1(O1W(H2W	136(10)

La1(O1W(H1W	114(10)

H2W(O1W(H1W	108(5)

W1(O1(La1iv	167.5(6)

W1(O2(La1v	163.2(6)

O1vi(La1(O2vii	78.7(4)

O1vi(La1(O23	139.2(4)

O2vii(La1(O23	137.9(4)

O1vi(La1(O3iii	75.7(4)

O2vii(La1(O3iii	77.8(4)

O23(La1(O3iii	121.5(4)

O1vi(La1(O1W	130.4(4)

O2vii(La1(O1W	70.6(4)

O23(La1(O1W	69.3(4)

O3iii(La1(O1W	131.1(4)

O1vi(La1(O4ii	74.1(4)

O2vii(La1(O4ii	91.7(4)

O23(La1(O4ii	85.5(4)

O3iii(La1(O4ii	149.4(4)

O1W(La1(O4ii	68.9(4)

O1vi(La1(O22iii	146.0(4)

O2vii(La1(O22iii	80.6(4)

O23(La1(O22iii	71.6(4)

O3iii(La1(O22iii	73.8(4)

O1W(La1(O22iii	65.0(4)

O4ii(La1(O22iii	133.3(4)

O1vi(La1(O4	83.6(4)

O2vii(La1(O4	142.0(3)

O23(La1(O4	73.7(4)

O3iii(La1(O4	65.3(4)

O1W(La1(O4	142.3(4)

O4ii(La1(O4	115.4(3)

O22iii(La1(O4	96.9(4)

O1vi(La1(W1	73.3(3)

O2vii(La1(W1	151.2(3)

O23(La1(W1	70.7(3)

O3iii(La1(W1	88.6(3)

O1W(La1(W1	134.5(3)

O4ii(La1(W1	87.2(2)

O22iii(La1(W1	120.2(3)

O4(La1(W1	28.2(2)

O1(W1(O2	109.0(5)

O1(W1(O3	111.1(5)

O2(W1(O3	111.0(5)

O1(W1(O4	111.2(5)

O2(W1(O4	111.8(5)

O3(W1(O4	102.7(5)

O1(W1(La1	115.1(4)

O2(W1(La1	135.4(4)

O3(W1(La1	58.2(4)

O4(W1(La1	45.9(4)

O22(S1(O23	112.2(7)

O22(S1(O21	112.5(7)

O23(S1(O21	112.2(7)

O22(S1(C1	107.9(7)

O23(S1(C1	105.4(7)

O21(S1(C1	106.1(7)

Symmetry transformations used to generate equivalent atoms:

(i) (x,(y+1,(z    (ii) x,(y+1/2,z(1/2    (iii) x,(y+1/2,z+1/2

(iv)  (x+1,y+1/2,(z+1/2    (v) x,y+1,z    (vi) (x+1,y(1/2,(z+1/2

(vii) x,y(1,z

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C1	18(6) 	18(6)	18(6) 	(6(5)	(1(5) 	(3(5)

C2	12(6) 	14(6)	21(6) 	(5(5)	0(5) 	7(5)

C3	25(7) 	17(6)	5(5) 	(7(5)	1(5) 	0(5)

C4	19(6) 	19(6)	16(6) 	(1(5)	(3(5) 	6(5)

C5	15(6) 	11(6)	15(6) 	0(5)	1(5) 	(3(5)

O3	30(7) 	27(7)	21(6) 	1(5)	10(5) 	4(5)

O4	28(7) 	7(5)	33(7) 	3(5)	(4(5) 	4(5)

O21	38(7) 	15(6)	15(5) 	3(4)	(1(5) 	(6(5)

O22	21(6) 	31(7)	24(6) 	4(5)	0(5) 	4(5)

O23	16(6) 	24(6)	31(6) 	8(5)	(7(5) 	6(5)

O1W	32(7) 	20(6)	17(6) 	6(4)	(6(5) 	(17(5)

O1	30(6) 	18(6)	11(5) 	4(4)	7(4) 	(3(5)

O2	18(6) 	15(6)	27(6) 	1(5)	(5(5) 	(1(4)

La1	17(1) 	11(1)	14(1) 	0(1)	0(1) 	1(1)

W1	17(1) 	10(1)	14(1) 	0(1)	0(1) 	0(1)

S1	19(2) 	14(2)	18(2) 	2(1)	1(1) 	(1(2)

Table 5. Hydrogen bonds [Å and °].

D(H···A	d(D(H)	d(H···A)	d(D···A)	((DHA)

O1W(H2W...O21ii	0.85(2)	1.95(3)	2.796(15)	176(22)

O1W(H2W...S1ii	0.85(2)	3.01(6)	3.810(12)	158(13)

O1W(H1W...S1vii	0.85(2)	2.89(9)	3.622(12)	145(13)

O1W(H1W...O21vii	0.85(2)	1.92(4)	2.756(15)	169(16)

Symmetry transformations used to generate equivalent atoms:

(i) (x,(y+1,(z    (ii) x,(y+1/2,z(1/2    (iii) x,(y+1/2,z+1/2

(iv)  (x+1,y+1/2,(z+1/2    (v) x,y+1,z    (vi) (x+1,y(1/2,(z+1/2

(vii) x,y(1,z