|  | University of Southampton · Department of Chemistry # EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	01SRC873

Empirical formula 	C19H18B2Fe2O8

Formula weight 	507.66

Temperature 	120(2) K

## Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	C2/c

Unit cell dimensions	a = 26.798(2) Å

b = 6.0907(6) Å	 = 108.968(3)°

c = 12.6373(15) Å

Volume	1950.7(3) Å3

Z	4

Density (calculated)	1.729 Mg / m3

Absorption coefficient	1.534 mm1

F(000)	1032

Crystal	Colourless Plate

Crystal size	0.15  0.15  0.02 mm3

 range for data collection	3.22  25.01°

Index ranges	31  h  30, 6  k  6, 15  l  13

Reflections collected	4641

Independent reflections	1649 [Rint = 0.0580]

Completeness to  = 25.01°	95.6 %

Max. and min. transmission	0.9700 and 0.8025

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	1649 / 0 / 141

Goodness-of-fit on F2	1.089

Final R indices [F2 > 2(F2)]	R1 = 0.0427, wR2 = 0.0886

R indices (all data)	R1 = 0.0732, wR2 = 0.1054

Largest diff. peak and hole	0.474 and 0.412 e Å3

Diffractometer: Nonius KappaCCD area detector ( scans and  scans to fill asymmetric unit sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing, Acta Cryst. A51 (1995) 3337; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421426). Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: Cameron - A Molecular Graphics Package. (D. M. Watkin, L. Pearce and C. K. Prout, Chemical Crystallography Laboratory, University of Oxford, 1993).

Special details:  All hydrogen atoms were placed in idealised positions and refined using a riding model.

Table 2. Atomic coordinates [ 104], equivalent isotropic displacement parameters [Å2  103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C1	2007(2)	5079(8)	712(4)	43(1)	1

C2	2232(2)	3074(8)	1175(4)	38(1)	1

C3	2013(2)	2457(8)	1986(3)	34(1)	1

C4	1654(2)	4085(8)	2043(4)	37(1)	1

C5	1651(2)	5714(8)	1263(4)	44(1)	1

C6	1418(2)	1594(7)	831(4)	28(1)	1

C7	955(2)	915(7)	624(3)	27(1)	1

C9	454(2)	7545(7)	1854(3)	27(1)	1

C10	0	6045(10)	2500	23(1)	1

C11	150(2)	4656(7)	1657(3)	26(1)	1

B1	795(2)	4387(9)	646(4)	26(1)	1

Fe1	1415(1)	2747(1)	421(1)	26(1)	1

O1	1431(1)	892(5)	1668(3)	37(1)	1

O2	654(1)	282(5)	782(2)	34(1)	1

O3	889(1)	6302(5)	1116(2)	27(1)	1

O4	300(1)	3532(5)	919(2)	28(1)	1

Table 3. Bond lengths [Å] and angles [°].

C1C2	1.403(7)

C1C5	1.405(7)

C1Fe1	2.070(5)

C2C3	1.389(7)

C2Fe1	2.094(5)

C3C4	1.400(7)

C3Fe1	2.110(4)

C4C5	1.397(7)

C4Fe1	2.103(4)

C5Fe1	2.088(5)

C6O1	1.151(5)

C6Fe1	1.734(5)

C7O2	1.152(5)

C7Fe1	1.743(5)

C9O3	1.447(5)

C9C10	1.528(5)

C10C11i	1.513(5)

C10C11	1.513(5)

C10C9i	1.528(5)

C11O4	1.436(5)

B1O4	1.360(6)

B1O3	1.369(6)

B1Fe1	2.030(5)

C2C1C5	107.6(4)

C2C1Fe1	71.2(3)

C5C1Fe1	70.9(3)

C3C2C1	108.4(5)

C3C2Fe1	71.3(3)

C1C2Fe1	69.4(3)

C2C3C4	108.0(4)

C2C3Fe1	70.1(3)

C4C3Fe1	70.3(3)

C5C4C3	108.2(4)

C5C4Fe1	69.9(3)

C3C4Fe1	70.9(2)

C4C5C1	107.8(5)

C4C5Fe1	71.1(3)

C1C5Fe1	69.6(3)

O1C6Fe1	177.6(4)

O2C7Fe1	178.5(4)

O3C9C10	111.4(3)

C11iC10C11	112.0(5)

C11iC10C9	111.3(2)

C11C10C9	107.7(2)

C11iC10C9i	107.7(2)

C11C10C9i	111.3(2)

C9C10C9i	106.5(5)

O4C11C10	111.4(3)

O4B1O3	121.2(4)

O4B1Fe1	120.0(3)

O3B1Fe1	118.7(3)

C6Fe1C7	95.1(2)

C6Fe1B1	80.77(19)

C7Fe1B1	87.0(2)

C6Fe1C1	102.1(2)

C7Fe1C1	161.91(19)

B1Fe1C1	101.2(2)

C6Fe1C5	136.5(2)

C7Fe1C5	126.2(2)

B1Fe1C5	87.7(2)

C1Fe1C5	39.5(2)

C6Fe1C2	98.0(2)

C7Fe1C2	132.8(2)

B1Fe1C2	139.9(2)

C1Fe1C2	39.4(2)

C5Fe1C2	65.6(2)

C6Fe1C4	163.0(2)

C7Fe1C4	96.3(2)

B1Fe1C4	112.36(19)

C1Fe1C4	65.7(2)

C5Fe1C4	38.9(2)

C2Fe1C4	65.04(19)

C6Fe1C3	126.4(2)

C7Fe1C3	99.55(19)

B1Fe1C3	150.71(19)

C1Fe1C3	65.59(19)

C5Fe1C3	65.34(19)

C2Fe1C3	38.60(18)

C4Fe1C3	38.81(18)

B1O3C9	120.1(4)

B1O4C11	121.7(4)

Symmetry transformations used to generate equivalent atoms:

(i) x,y,z1/2

Table 4. Anisotropic displacement parameters [Å2 103]. The anisotropic displacement

factor exponent takes the form: 2 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C1	55(4) 	44(3)	22(3) 	2(2)	0(3) 	27(3)

C2	24(3) 	52(3)	36(3) 	10(2)	6(2) 	2(2)

C3	32(3) 	40(3)	21(2) 	0(2)	2(2) 	5(2)

C4	32(3) 	52(3)	25(3) 	19(2)	7(2) 	3(2)

C5	44(3) 	31(3)	37(3) 	10(2)	14(3) 	8(2)

C6	27(3) 	25(3)	30(3) 	2(2)	8(2) 	5(2)

C7	32(3) 	28(3)	21(2) 	2(2)	7(2) 	5(2)

C9	34(3) 	19(2)	22(2) 	3(2)	2(2) 	1(2)

C10	28(4) 	23(4)	18(3) 	0	7(3) 	0

C11	22(3) 	33(3)	20(2) 	5(2)	4(2) 	4(2)

B1	35(3) 	29(3)	16(3) 	4(2)	12(2) 	1(2)

Fe1	27(1) 	29(1)	20(1) 	1(1)	6(1) 	1(1)

O1	41(2) 	43(2)	31(2) 	13(2)	17(2) 	11(2)

O2	40(2) 	36(2)	26(2) 	3(1)	12(2) 	1(2)

O3	26(2) 	30(2)	21(2) 	3(1)	2(1) 	2(1)

O4	26(2) 	33(2)	24(2) 	7(1)	6(1) 	1(1)

Table 5. Hydrogen coordinates [ 104] and isotropic displacement parameters [Å2  103].

Atom 	x	y	z	Ueq	S.o.f.

H1	2081	5865	131	52	1

H2	2490	2275	968	46	1

H3	2092	1158	2425	40	1

H4	1447	4082	2528	44	1

H5	1445	7018	1129	53	1

H9A	578	8387	2389	32	1

H9B	325	8606	1407	32	1

H11A	306	5607	1212	31	1

H11B	419	3567	2057	31	1