|  | Single Crystal X-Ray Diffraction Service National Crystallography Service Contact: Dr S.K.Callear, S.K.Callear@soton.ac.uk |
| --- | --- |

Table 1. Crystal data and structure refinement details.

Identification code 	2009src0060p(1 (JN51)

Empirical formula 	C20H20La4O32S4W4

Formula weight 	2191.64

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Triclinic

Space group 	P(1

Unit cell dimensions	a = 7.2550(2) Å	( = 80.4080(10)°

b = 8.1110(2) Å	( = 78.6810(10)°

c = 16.9310(4) Å	(  = 89.6740(10)°

Volume	962.90(4) Å3

Z	1

Density (calculated)	3.780 Mg / m3

Absorption coefficient	16.555 mm(1

F(000)	984

Crystal	blade; colourless

Crystal size	0.14 ( 0.03 ( 0.01 mm3

( range for data collection	3.02 ( 27.48°

Index ranges	(9 ( h ( 9, (10 ( k ( 10, (21 ( l ( 21

Reflections collected	19673

Independent reflections	4394 [Rint = 0.0598]

Completeness to ( = 27.48°	99.6 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.8519 and 0.2052

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	4394 / 18 / 289

Goodness-of-fit on F2	1.119

Final R indices [F2 > 2((F2)]	R1 = 0.0387, wR2 = 0.0779

R indices (all data)	R1 = 0.0483, wR2 = 0.0827

Largest diff. peak and hole	2.116 and (1.758 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: Sheldrick, G. M. SADABS - Bruker Nonius area detector scaling and absorption correction - V2.10 Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: ORTEP-3 (L.G. Farrugia, J. Appl. Cryst. (1997) 30, 565).

Special details:

All hydrogens were fixed using a standard riding model. Hydrogen atoms on the water molecules O1w and O2w could not be located from the difference map. This is not surprising when heavy atoms are involved in the structure. The location of one of the hydrogens on each of the water molecules can be deduced from the short contact with the sulphate oxygen (O1w-H...O3 and O2w-H...O23) however the location of the second hydrogen is not certain.

The second WGHT parameter is higher than usual due to the large difference in atom weights present in the structure.

As there are 2 independent W2O8 units present in the structure (though half of each is related by symmetry) the formula is that shown above in spite of the alerts Checkcif brings up (due to the manner it calculates Z).

O32 and O36 were modelled using the ISOR restraint due to the former being a non-positive definite, and the latter having a very small ADP in one direction. This appears to be a trend for oxygen atoms that are positioned within a lattice surrounded by 3 co-ordinating cations.

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C1	(3243(15)	(386(13)	882(6)	19(2)	1

C2	(2083(14)	(1515(12)	1261(6)	14(2)	1

C3	(207(14)	(1586(12)	959(6)	13(2)	1

C4	588(13)	(555(12)	204(6)	13(2)	1

C5	(2508(14)	599(14)	168(7)	20(2)	1

O1	(1619(9)	(3825(8)	2471(4)	12(1)	1

O2	(3965(9)	(1760(9)	2756(4)	14(1)	1

O3	(4525(9)	(3892(9)	1980(4)	14(1)	1

S1	(3125(3)	(2843(3)	2179(1)	11(1)	1

C21	2485(14)	(6484(12)	688(6)	13(2)	1

C22	728(12)	(6842(11)	1238(6)	10(2)	1

C23	(907(13)	(6246(12)	1042(6)	12(2)	1

C24	(882(13)	(5184(12)	277(6)	14(2)	1

C25	(2553(14)	(4530(14)	52(6)	19(2)	1

O21	1016(9)	(6859(9)	2739(4)	15(1)	1

O22	(1147(9)	(8844(8)	2464(4)	14(1)	1

O23	2210(9)	(9213(8)	2099(4)	11(1)	1

S21	692(3)	(8035(3)	2203(1)	9(1)	1

O1W	2032(9)	(3005(9)	2620(4)	18(2)	1

O2W	(4925(10)	(7997(10)	2646(5)	21(2)	1

O31	(3126(9)	(6755(8)	3739(4)	11(1)	1

O32	(855(9)	(6520(8)	5124(4)	12(1)	1

O33	(819(8)	(9309(8)	4498(4)	11(1)	1

O34	(5770(9)	(8448(8)	4859(4)	14(1)	1

O35	(6948(9)	(5674(8)	3848(4)	11(1)	1

O36	(6283(8)	(5702(8)	5504(4)	9(1)	1

O37	(3030(9)	(9271(9)	6121(4)	14(1)	1

O38	711(9)	(8237(8)	6259(4)	12(1)	1

La1	(332(1)	(4856(1)	3702(1)	8(1)	1

La2	(3494(1)	(9859(1)	3728(1)	8(1)	1

W1	(781(1)	(8691(1)	5563(1)	8(1)	1

W2	(5262(1)	(6282(1)	4427(1)	8(1)	1

Table 3. Bond lengths [Å] and angles [°].

C1(C5	1.346(15)

C1(C2	1.402(15)

C2(C3	1.362(14)

C2(S1	1.772(10)

C3(C4	1.423(13)

C4(C5i	1.415(14)

C4(C4i	1.426(19)

C5(C4i	1.415(14)

O1(S1	1.464(7)

O1(La1	2.468(7)

O2(S1	1.464(7)

O2(La2ii	2.506(7)

O3(S1	1.452(7)

C21(C25iii	1.372(14)

C21(C22	1.422(13)

C22(C23	1.358(13)

C22(S21	1.751(10)

C23(C24	1.428(14)

C24(C25	1.415(14)

C24(C24iii	1.431(19)

C25(C21iii	1.372(14)

O21(S21	1.471(7)

O21(La1	2.549(7)

O22(S21	1.444(7)

O22(La2	2.481(7)

O23(S21	1.458(6)

O1W(La1	2.536(7)

O2W(La2	2.554(7)

O31(W2	1.828(7)

O31(La2	2.537(6)

O31(La1	2.537(6)

O32(W1	1.798(6)

O32(La1	2.514(7)

O32(La1iv	2.713(7)

O33(W1	1.955(6)

O33(W1v	1.995(6)

O33(La2	2.619(6)

O34(W2	1.797(7)

O34(La2vi	2.511(7)

O34(La2	2.678(7)

O35(W2	1.733(6)

O35(La1vii	2.587(6)

O36(W2	1.961(6)

O36(W2viii	1.998(6)

O36(La1viii	2.634(6)

O37(W1	1.742(6)

O37(La2vi	2.575(7)

O38(W1	1.830(7)

O38(La1iv	2.532(7)

O38(La2v	2.536(7)

La1(O38iv	2.532(7)

La1(O35ix	2.587(6)

La1(O36viii	2.634(6)

La1(O32iv	2.713(7)

La1(W1iv	3.4769(6)

La1(W2	3.6725(6)

La2(O2(x) 	2.506(7)

La2(O34vi	2.511(7)

La2(O38v	2.536(7)

La2(O37vi	2.575(7)

La2(W2	3.4601(6)

La2(W1v	3.6596(6)

W1(O33v	1.995(6)

W1(W1v	3.1465(7)

W1(La1iv	3.4769(6)

W1(La2v	3.6596(6)

W2(O36viii	1.998(6)

W2(W2viii	3.1421(7)

C5(C1(C2	119.2(10)

C3(C2(C1	122.4(9)

C3(C2(S1	119.8(8)

C1(C2(S1	117.7(8)

C2(C3(C4	118.9(9)

C5i(C4(C3	122.6(9)

C5i(C4(C4i	118.1(11)

C3(C4(C4i	119.3(11)

C1(C5(C4i	122.0(10)

S1(O1(La1	143.3(4)

S1(O2(La2ii	148.0(4)

O3(S1(O1	112.0(4)

O3(S1(O2	112.2(4)

O1(S1(O2	111.4(4)

O3(S1(C2	106.9(4)

O1(S1(C2	107.1(4)

O2(S1(C2	106.9(4)

C25iii(C21(C22	119.6(9)

C23(C22(C21	121.8(9)

C23(C22(S21	119.4(7)

C21(C22(S21	118.8(7)

C22(C23(C24	120.0(9)

C25(C24(C23	121.7(9)

C25(C24(C24iii	119.9(11)

C23(C24(C24iii	118.4(11)

C21iii(C25(C24	120.3(9)

S21(O21(La1	148.7(4)

S21(O22(La2	140.5(4)

O22(S21(O23	113.1(4)

O22(S21(O21	111.9(4)

O23(S21(O21	111.6(4)

O22(S21(C22	106.5(4)

O23(S21(C22	106.5(4)

O21(S21(C22	106.6(4)

W2(O31(La2	103.7(3)

W2(O31(La1	113.6(3)

La2(O31(La1	133.5(3)

W1(O32(La1	135.9(3)

W1(O32(La1iv	98.8(3)

La1(O32(La1iv	118.0(2)

W1(O33(W1v	105.6(3)

W1(O33(La2	134.2(3)

W1v(O33(La2	104.2(3)

W2(O34(La2vi	136.1(3)

W2(O34(La2	99.4(3)

La2vi(O34(La2	115.9(2)

W2(O35(La1vii	152.1(3)

W2(O36(W2viii	105.1(3)

W2(O36(La1viii	134.8(3)

W2viii(O36(La1viii	104.1(3)

W1(O37(La2vi	153.7(4)

W1(O38(La1iv	104.6(3)

W1(O38(La2v	112.9(3)

La1iv(O38(La2v	133.0(3)

O1(La1(O32	148.1(2)

O1(La1(O38iv	76.7(2)

O32(La1(O38iv	110.9(2)

O1(La1(O1W	68.1(2)

O32(La1(O1W	143.7(2)

O38iv(La1(O1W	66.4(2)

O1(La1(O31	73.0(2)

O32(La1(O31	77.1(2)

O38iv(La1(O31	121.4(2)

O1W(La1(O31	136.9(2)

O1(La1(O21	77.3(2)

O32(La1(O21	106.4(2)

O38iv(La1(O21	141.3(2)

O1W(La1(O21	77.4(2)

O31(La1(O21	76.7(2)

O1(La1(O35ix	130.3(2)

O32(La1(O35ix	77.9(2)

O38iv(La1(O35ix	109.4(2)

O1W(La1(O35ix	70.0(2)

O31(La1(O35ix	128.5(2)

O21(La1(O35ix	68.4(2)

O1(La1(O36viii	84.3(2)

O32(La1(O36viii	70.7(2)

O38iv(La1(O36viii	69.6(2)

O1W(La1(O36viii	132.1(2)

O31(La1(O36viii	58.7(2)

O21(La1(O36viii	135.0(2)

O35ix(La1(O36viii	145.0(2)

O1(La1(O32iv	136.4(2)

O32(La1(O32iv	62.0(2)

O38iv(La1(O32iv	59.9(2)

O1W(La1(O32iv	89.6(2)

O31(La1(O32iv	132.4(2)

O21(La1(O32iv	135.7(2)

O35ix(La1(O32iv	67.4(2)

O36viii(La1(O32iv	84.25(19)

O1(La1(W1iv	105.83(16)

O32(La1(W1iv	90.30(15)

O38iv(La1(W1iv	30.62(15)

O1W(La1(W1iv	69.97(17)

O31(La1(W1iv	140.49(15)

O21(La1(W1iv	142.63(15)

O35ix(La1(W1iv	83.38(15)

O36viii(La1(W1iv	81.82(13)

O32iv(La1(W1iv	30.74(13)

O1(La1(W2	79.73(15)

O32(La1(W2	68.53(15)

O38iv(La1(W2	99.28(15)

O1W(La1(W2	146.89(16)

O31(La1(W2	27.14(15)

O21(La1(W2	103.80(15)

O35ix(La1(W2	141.92(15)

O36viii(La1(W2	31.86(13)

O32iv(La1(W2	109.36(14)

W1iv(La1(W2	113.465(16)

O22(La2(O2(x) 	75.3(2)

O22(La2(O34vi	148.9(2)

O2(x) (La2(O34vi	107.2(2)

O22(La2(O38v	73.1(2)

O2(x) (La2(O38v	77.2(2)

O34vi(La2(O38v	77.2(2)

O22(La2(O31	76.1(2)

O2(x) (La2(O31	139.0(2)

O34vi(La2(O31	112.6(2)

O38v(La2(O31	121.0(2)

O22(La2(O2W	67.4(2)

O2(x) (La2(O2W	75.9(2)

O34vi(La2(O2W	143.8(2)

O38v(La2(O2W	136.4(2)

O31(La2(O2W	66.2(2)

O22(La2(O37vi	128.8(2)

O2(x) (La2(O37vi	67.4(2)

O34vi(La2(O37vi	77.5(2)

O38v(La2(O37vi	127.3(2)

O31(La2(O37vi	111.3(2)

O2W(La2(O37vi	70.4(2)

O22(La2(O33	85.3(2)

O2(x) (La2(O33	135.6(2)

O34vi(La2(O33	71.3(2)

O38v(La2(O33	58.9(2)

O31(La2(O33	69.6(2)

O2W(La2(O33	132.1(2)

O37vi(La2(O33	145.7(2)

O22(La2(O34	136.0(2)

O2(x) (La2(O34	135.0(2)

O34vi(La2(O34	64.1(2)

O38v(La2(O34	134.6(2)

O31(La2(O34	60.4(2)

O2W(La2(O34	87.9(2)

O37vi(La2(O34	67.6(2)

O33(La2(O34	85.9(2)

O22(La2(W2	105.15(16)

O2(x) (La2(W2	141.05(16)

O34vi(La2(W2	92.04(15)

O38v(La2(W2	141.14(15)

O31(La2(W2	30.88(15)

O2W(La2(W2	69.11(17)

O37vi(La2(W2	84.93(15)

O33(La2(W2	82.28(14)

O34(La2(W2	30.83(14)

O22(La2(W1v	80.94(16)

O2(x) (La2(W1v	104.63(15)

O34vi(La2(W1v	68.31(15)

O38v(La2(W1v	27.43(15)

O31(La2(W1v	99.26(14)

O2W(La2(W1v	147.25(17)

O37vi(La2(W1v	140.89(16)

O33(La2(W1v	31.90(14)

O34(La2(W1v	110.99(15)

W2(La2(W1v	113.978(16)

O37(W1(O32	106.6(3)

O37(W1(O38	109.1(3)

O32(W1(O38	92.5(3)

O37(W1(O33	103.3(3)

O32(W1(O33	89.8(3)

O38(W1(O33	145.3(3)

O37(W1(O33v	110.5(3)

O32(W1(O33v	142.0(3)

O38(W1(O33v	82.9(3)

O33(W1(O33v	74.4(3)

O37(W1(W1v	111.4(2)

O32(W1(W1v	119.8(2)

O38(W1(W1v	115.6(2)

O33(W1(W1v	37.63(19)

O33v(W1(W1v	36.76(18)

O37(W1(La1iv	103.5(2)

O32(W1(La1iv	50.4(2)

O38(W1(La1iv	44.8(2)

O33(W1(La1iv	137.0(2)

O33v(W1(La1iv	124.86(18)

W1v(W1(La1iv	144.749(19)

O37(W1(La2v	122.9(2)

O32(W1(La2v	117.7(2)

O38(W1(La2v	39.7(2)

O33(W1(La2v	110.61(18)

O33v(W1(La2v	43.94(18)

W1v(W1(La2v	76.245(15)

La1iv(W1(La2v	81.226(14)

O35(W2(O34	106.4(3)

O35(W2(O31	108.2(3)

O34(W2(O31	92.8(3)

O35(W2(O36	105.0(3)

O34(W2(O36	88.8(3)

O31(W2(O36	144.8(3)

O35(W2(O36viii	110.2(3)

O34(W2(O36viii	142.6(3)

O31(W2(O36viii	82.8(3)

O36(W2(O36viii	74.9(3)

O35(W2(W2viii	112.4(2)

O34(W2(W2viii	119.5(2)

O31(W2(W2viii	115.5(2)

O36(W2(W2viii	37.89(17)

O36viii(W2(W2viii	37.06(18)

O35(W2(La2	103.5(2)

O34(W2(La2	49.8(2)

O31(W2(La2	45.43(19)

O36(W2(La2	135.01(19)

O36viii(W2(La2	125.15(18)

W2viii(W2(La2	143.85(2)

O35(W2(La1	121.0(2)

O34(W2(La1	118.8(2)

O31(W2(La1	39.29(19)

O36(W2(La1	111.36(17)

O36viii(W2(La1	44.08(18)

W2viii(W2(La1	76.730(15)

La2(W2(La1	81.585(14)

Symmetry transformations used to generate equivalent atoms:

(i) (x,(y,(z    (ii) x,y+1,z    (iii) (x,(y(1,(z    (iv)  (x,(y(1,(z+1

(v) (x,(y(2,(z+1    (vi) (x(1,(y(2,(z+1    (vii) x(1,y,z

(viii) (x(1,(y(1,(z+1    (xi) x+1,y,z    (x)  x,y(1,z

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C1	21(5) 	20(5)	15(5) 	(5(4)	0(4) 	0(4)

C2	22(5) 	8(4)	13(5) 	(5(4)	(3(4) 	(4(4)

C3	21(5) 	13(5)	6(4) 	(2(4)	(3(4) 	1(4)

C4	16(5) 	11(5)	12(5) 	(2(4)	(8(4) 	(3(4)

C5	18(5) 	24(6)	22(6) 	(10(5)	(4(4) 	10(4)

O1	12(3) 	16(3)	9(3) 	(4(3)	(1(2) 	0(3)

O2	16(3) 	16(4)	10(3) 	(4(3)	0(3) 	0(3)

O3	10(3) 	20(4)	11(3) 	(7(3)	3(3) 	(3(3)

S1	10(1) 	12(1)	11(1) 	(3(1)	(2(1) 	(1(1)

C21	19(5) 	11(5)	11(5) 	0(4)	(9(4) 	2(4)

C22	6(4) 	8(4)	11(5) 	0(4)	5(3) 	0(3)

C23	13(4) 	13(5)	12(5) 	(2(4)	(5(4) 	(7(4)

C24	19(5) 	12(5)	11(5) 	(1(4)	(5(4) 	0(4)

C25	13(5) 	30(6)	14(5) 	(7(4)	2(4) 	(9(4)

O21	15(3) 	15(4)	15(4) 	(2(3)	(6(3) 	(2(3)

O22	12(3) 	15(3)	14(4) 	(1(3)	(1(3) 	(3(3)

O23	14(3) 	9(3)	11(3) 	(1(2)	(6(2) 	7(2)

S21	6(1) 	12(1)	9(1) 	(2(1)	(1(1) 	(1(1)

O1W	14(3) 	18(4)	18(4) 	4(3)	(3(3) 	(4(3)

O2W	18(4) 	24(4)	22(4) 	(4(3)	(8(3) 	3(3)

O31	15(3) 	8(3)	9(3) 	2(3)	(4(3) 	(5(3)

O32	16(3) 	4(3)	16(3) 	1(2)	(6(2) 	0(2)

O33	7(3) 	17(3)	10(3) 	(3(3)	(3(2) 	1(3)

O34	17(3) 	8(3)	18(4) 	(4(3)	1(3) 	0(3)

O35	9(3) 	17(3)	8(3) 	(5(3)	0(2) 	3(3)

O36	8(3) 	9(3)	9(3) 	(1(2)	(1(2) 	(7(2)

O37	15(3) 	17(4)	10(3) 	(6(3)	1(3) 	(3(3)

O38	14(3) 	12(3)	11(3) 	(4(3)	(2(3) 	1(3)

La1	7(1) 	7(1)	9(1) 	(1(1)	(1(1) 	(2(1)

La2	7(1) 	7(1)	9(1) 	(2(1)	(1(1) 	(1(1)

W1	8(1) 	7(1)	9(1) 	(1(1)	(1(1) 	(1(1)

W2	8(1) 	7(1)	9(1) 	(2(1)	(2(1) 	(1(1)