|  | Single Crystal X-Ray Diffraction Service National Crystallography Service Contact: Dr S.K.Callear, S.K.Callear@soton.ac.uk |
| --- | --- |

Table 1. Crystal data and structure refinement details.

Identification code 	2009src0114 (RRP293)

Empirical formula 	C22H25ClN5OPPd

Formula weight 	548.29

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Triclinic

Space group 	P(1

Unit cell dimensions	a = 8.8363(4) Å	( = 86.643(3)°

b = 10.2749(3) Å	( = 86.468(2)°

c = 11.6567(5) Å	(  = 86.435(2)°

Volume	1052.69(7) Å3

Z	2

Density (calculated)	1.730 Mg / m3

Absorption coefficient	1.111 mm(1

F(000)	556

Crystal	lath; colourless

Crystal size	0.08 ( 0.04 ( 0.01 mm3

( range for data collection	2.96 ( 27.48°

Index ranges	(11 ( h ( 11, (13 ( k ( 12, (15 ( l ( 15

Reflections collected	16112

Independent reflections	4783 [Rint = 0.0534]

Completeness to ( = 27.48°	98.8 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.9890 and 0.9164

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	4783 / 0 / 281

Goodness-of-fit on F2	1.124

Final R indices [F2 > 2((F2)]	R1 = 0.0532, wR2 = 0.1018

R indices (all data)	R1 = 0.0686, wR2 = 0.1097

Largest diff. peak and hole	0.642 and (0.633 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: Sheldrick, G. M. SADABS - Bruker Nonius area detector scaling and absorption correction - V2.10 Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: ORTEP-3 (L.G. Farrugia, J. Appl. Cryst. (1997) 30, 565).

Special details:

All hydrogens fixed using a standard riding model.

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C2	2654(5)	9320(4)	4801(4)	21(1)	1

C3	1160(6)	8680(5)	4817(4)	27(1)	1

C5	1750(5)	8335(4)	2755(4)	22(1)	1

C6	1002(6)	8642(5)	1742(5)	32(1)	1

C7	1794(7)	8848(5)	702(5)	34(1)	1

C8	3372(7)	8782(5)	651(4)	32(1)	1

C9	4145(6)	8450(5)	1644(4)	23(1)	1

C10	3347(5)	8197(4)	2701(4)	16(1)	1

C11	4203(5)	7800(4)	3730(4)	15(1)	1

C12	5414(5)	6743(4)	3736(4)	17(1)	1

C13	5855(5)	6008(4)	2788(4)	21(1)	1

C14	6897(5)	4967(4)	2884(4)	20(1)	1

C15	7497(5)	4610(4)	3934(4)	21(1)	1

C16	7065(5)	5331(4)	4886(4)	20(1)	1

C17	6047(5)	6426(4)	4820(4)	16(1)	1

C18	(601(7)	7563(7)	3765(8)	61(2)	1

C20	8283(6)	5629(5)	7537(4)	24(1)	1

C22	7961(6)	5338(5)	9617(4)	29(1)	1

C24	5721(5)	6473(5)	8882(4)	21(1)	1

C25	7776(5)	8285(5)	7919(4)	21(1)	1

C27	9713(6)	6859(5)	8780(5)	27(1)	1

C28	7531(6)	7592(5)	9933(4)	25(1)	1

N1	3887(4)	8305(3)	4707(3)	17(1)	1

N4	882(5)	8133(4)	3794(4)	28(1)	1

N21	9038(5)	5607(4)	8634(4)	25(1)	1

N23	6780(5)	6364(4)	9824(3)	22(1)	1

N26	8592(5)	7952(4)	8966(3)	23(1)	1

O3	298(4)	8606(4)	5657(3)	41(1)	1

P19	6711(1)	6926(1)	7480(1)	17(1)	1

Cl1	3912(2)	9000(1)	7423(1)	29(1)	1

Pd1	5175(1)	7565(1)	6061(1)	17(1)	1

Table 3. Bond lengths [Å] and angles [°].

C2(N1	1.464(5)

C2(C3	1.510(7)

C2(H2A	0.9900

C2(H2B	0.9900

C3(O3	1.205(6)

C3(N4	1.389(7)

C5(C6	1.398(7)

C5(N4	1.405(6)

C5(C10	1.408(6)

C6(C7	1.375(8)

C6(H6	0.9500

C7(C8	1.389(8)

C7(H7	0.9500

C8(C9	1.395(7)

C8(H8	0.9500

C9(C10	1.401(6)

C9(H9	0.9500

C10(C11	1.480(6)

C11(N1	1.288(6)

C11(C12	1.477(6)

C12(C13	1.397(6)

C12(C17	1.426(6)

C13(C14	1.371(6)

C13(H13	0.9500

C14(C15	1.385(6)

C14(H14	0.9500

C15(C16	1.391(6)

C15(H15	0.9500

C16(C17	1.397(6)

C16(H16	0.9500

C17(Pd1	2.001(4)

C18(N4	1.472(7)

C18(H18A	0.9800

C18(H18B	0.9800

C18(H18C	0.9800

C20(N21	1.477(6)

C20(P19	1.866(5)

C20(H20A	0.9900

C20(H20B	0.9900

C22(N23	1.456(6)

C22(N21	1.469(7)

C22(H22A	0.9900

C22(H22B	0.9900

C24(N23	1.481(6)

C24(P19	1.855(5)

C24(H24A	0.9900

C24(H24B	0.9900

C25(N26	1.468(6)

C25(P19	1.845(5)

C25(H25A	0.9900

C25(H25B	0.9900

C27(N26	1.467(6)

C27(N21	1.475(6)

C27(H27A	0.9900

C27(H27B	0.9900

C28(N26	1.467(6)

C28(N23	1.476(6)

C28(H28A	0.9900

C28(H28B	0.9900

N1(Pd1	2.083(4)

P19(Pd1	2.2463(12)

Cl1(Pd1	2.4070(12)

N1(C2(C3	108.4(4)

N1(C2(H2A	110.0

C3(C2(H2A	110.0

N1(C2(H2B	110.0

C3(C2(H2B	110.0

H2A(C2(H2B	108.4

O3(C3(N4	122.3(5)

O3(C3(C2	123.1(5)

N4(C3(C2	114.5(4)

C6(C5(N4	119.0(5)

C6(C5(C10	119.2(5)

N4(C5(C10	121.7(4)

C7(C6(C5	121.4(5)

C7(C6(H6	119.3

C5(C6(H6	119.3

C6(C7(C8	119.7(5)

C6(C7(H7	120.2

C8(C7(H7	120.2

C7(C8(C9	120.0(5)

C7(C8(H8	120.0

C9(C8(H8	120.0

C8(C9(C10	120.7(5)

C8(C9(H9	119.7

C10(C9(H9	119.7

C9(C10(C5	118.9(4)

C9(C10(C11	119.2(4)

C5(C10(C11	121.9(4)

N1(C11(C12	114.8(4)

N1(C11(C10	122.2(4)

C12(C11(C10	122.8(4)

C13(C12(C17	120.4(4)

C13(C12(C11	123.9(4)

C17(C12(C11	115.5(4)

C14(C13(C12	120.7(4)

C14(C13(H13	119.6

C12(C13(H13	119.6

C13(C14(C15	120.2(4)

C13(C14(H14	119.9

C15(C14(H14	119.9

C14(C15(C16	119.7(4)

C14(C15(H15	120.2

C16(C15(H15	120.2

C15(C16(C17	122.2(4)

C15(C16(H16	118.9

C17(C16(H16	118.9

C16(C17(C12	116.8(4)

C16(C17(Pd1	129.9(3)

C12(C17(Pd1	113.1(3)

N4(C18(H18A	109.5

N4(C18(H18B	109.5

H18A(C18(H18B	109.5

N4(C18(H18C	109.5

H18A(C18(H18C	109.5

H18B(C18(H18C	109.5

N21(C20(P19	111.2(3)

N21(C20(H20A	109.4

P19(C20(H20A	109.4

N21(C20(H20B	109.4

P19(C20(H20B	109.4

H20A(C20(H20B	108.0

N23(C22(N21	115.2(4)

N23(C22(H22A	108.5

N21(C22(H22A	108.5

N23(C22(H22B	108.5

N21(C22(H22B	108.5

H22A(C22(H22B	107.5

N23(C24(P19	111.4(3)

N23(C24(H24A	109.4

P19(C24(H24A	109.4

N23(C24(H24B	109.4

P19(C24(H24B	109.4

H24A(C24(H24B	108.0

N26(C25(P19	112.8(3)

N26(C25(H25A	109.0

P19(C25(H25A	109.0

N26(C25(H25B	109.0

P19(C25(H25B	109.0

H25A(C25(H25B	107.8

N26(C27(N21	113.9(4)

N26(C27(H27A	108.8

N21(C27(H27A	108.8

N26(C27(H27B	108.8

N21(C27(H27B	108.8

H27A(C27(H27B	107.7

N26(C28(N23	115.0(4)

N26(C28(H28A	108.5

N23(C28(H28A	108.5

N26(C28(H28B	108.5

N23(C28(H28B	108.5

H28A(C28(H28B	107.5

C11(N1(C2	118.9(4)

C11(N1(Pd1	116.2(3)

C2(N1(Pd1	124.9(3)

C3(N4(C5	124.2(4)

C3(N4(C18	115.6(5)

C5(N4(C18	118.7(5)

C22(N21(C27	108.8(4)

C22(N21(C20	111.0(4)

C27(N21(C20	111.3(4)

C22(N23(C28	107.8(4)

C22(N23(C24	110.4(4)

C28(N23(C24	112.0(4)

C28(N26(C27	109.0(4)

C28(N26(C25	110.7(4)

C27(N26(C25	110.4(4)

C25(P19(C24	99.3(2)

C25(P19(C20	97.8(2)

C24(P19(C20	97.4(2)

C25(P19(Pd1	111.84(15)

C24(P19(Pd1	114.94(15)

C20(P19(Pd1	130.39(16)

C17(Pd1(N1	80.27(16)

C17(Pd1(P19	100.36(13)

N1(Pd1(P19	174.46(11)

C17(Pd1(Cl1	173.96(13)

N1(Pd1(Cl1	93.87(10)

P19(Pd1(Cl1	85.61(4)

Symmetry transformations used to generate equivalent atoms:

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C2	27(3) 	18(2)	17(2) 	(2(2)	2(2) 	9(2)

C3	23(3) 	22(2)	31(3) 	11(2)	6(2) 	9(2)

C5	19(2) 	16(2)	31(3) 	(6(2)	(1(2) 	(4(2)

C6	29(3) 	24(3)	44(3) 	(9(2)	(18(2) 	2(2)

C7	44(3) 	27(3)	33(3) 	(8(2)	(24(3) 	10(2)

C8	56(4) 	20(3)	18(2) 	(5(2)	(3(2) 	9(2)

C9	29(3) 	23(2)	17(2) 	(5(2)	(6(2) 	8(2)

C10	22(2) 	15(2)	12(2) 	(1(2)	(6(2) 	2(2)

C11	15(2) 	14(2)	16(2) 	(3(2)	0(2) 	(3(2)

C12	18(2) 	15(2)	18(2) 	1(2)	2(2) 	(4(2)

C13	25(3) 	21(2)	16(2) 	0(2)	(2(2) 	(2(2)

C14	19(2) 	21(2)	19(2) 	(7(2)	3(2) 	0(2)

C15	18(2) 	17(2)	26(2) 	0(2)	0(2) 	0(2)

C16	22(2) 	19(2)	19(2) 	(1(2)	(1(2) 	2(2)

C17	16(2) 	21(2)	14(2) 	(4(2)	1(2) 	(7(2)

C18	26(3) 	51(4)	108(7) 	(14(4)	8(4) 	(20(3)

C20	25(3) 	22(2)	25(3) 	(6(2)	(5(2) 	6(2)

C22	38(3) 	27(3)	23(3) 	3(2)	(11(2) 	(2(2)

C24	23(2) 	23(2)	15(2) 	0(2)	(2(2) 	0(2)

C25	24(3) 	23(2)	17(2) 	(4(2)	0(2) 	1(2)

C27	23(3) 	27(3)	33(3) 	(8(2)	(8(2) 	(1(2)

C28	30(3) 	35(3)	12(2) 	(6(2)	(6(2) 	0(2)

N1	21(2) 	15(2)	13(2) 	1(1)	2(2) 	2(2)

N4	15(2) 	24(2)	45(3) 	0(2)	3(2) 	(4(2)

N21	24(2) 	26(2)	25(2) 	(2(2)	(7(2) 	3(2)

N23	28(2) 	25(2)	15(2) 	(1(2)	(5(2) 	(1(2)

N26	22(2) 	26(2)	22(2) 	(6(2)	(5(2) 	(1(2)

O3	32(2) 	46(2)	39(2) 	16(2)	17(2) 	12(2)

P19	19(1) 	19(1)	13(1) 	(2(1)	(2(1) 	2(1)

Cl1	35(1) 	33(1)	16(1) 	(7(1)	(4(1) 	14(1)

Pd1	20(1) 	18(1)	12(1) 	(1(1)	(1(1) 	3(1)