|  | Single Crystal X-Ray Diffraction Service National Crystallography Service Contact: Dr S.K.Callear, S.K.Callear@soton.ac.uk |
| --- | --- |

Table 1. Crystal data and structure refinement details.

Identification code 	2008src1291p21c  (HP122(7))

Empirical formula 	C10H15N3O2S

Formula weight 	241.31

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P21/c

Unit cell dimensions	a = 20.4469(13) Å	( = 90°

b = 5.6971(3) Å	( = 93.743(4)°

c = 9.6808(5) Å	(  = 90°

Volume	1125.29(11) Å3

Z	4

Density (calculated)	1.424 Mg / m3

Absorption coefficient	0.277 mm(1

F(000)	512

Crystal	lath; colourless

Crystal size	0.23 ( 0.03 ( 0.01 mm3

( range for data collection	3.00 ( 25.02°

Index ranges	(24 ( h ( 24, (6 ( k ( 6, (11 ( l ( 11

Reflections collected	8885

Independent reflections	1981 [Rint = 0.1029]

Completeness to ( = 25.00°	99.7 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.9972 and 0.9390

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	1981 / 0 / 146

Goodness-of-fit on F2	1.143

Final R indices [F2 > 2((F2)]	R1 = 0.0876, wR2 = 0.1490

R indices (all data)	R1 = 0.1461, wR2 = 0.1760

Largest diff. peak and hole	0.394 and (0.402 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: Sheldrick, G. M. SADABS - Bruker Nonius area detector scaling and absorption correction - V2.10 Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: ORTEP-3 (L.G. Farrugia, J. Appl. Cryst. (1997) 30, 565).

Special details:

All hydrogens fixed using a standard riding model

Due to the weakly diffracting nature of the crystals, data were only included out to 25deg (ACTA 50).

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C2	1045(3)	3398(12)	(1517(6)	34(2)	1

C3	557(3)	5076(13)	(1562(6)	32(1)	1

C4	630(3)	6884(12)	(615(6)	35(2)	1

C5	1173(3)	6995(11)	306(6)	26(1)	1

C6	1642(2)	5214(10)	284(5)	19(1)	1

C8	2227(3)	6505(10)	2462(5)	20(1)	1

C9	2917(3)	7155(10)	2970(6)	23(1)	1

C11	3324(3)	3807(10)	1702(5)	21(1)	1

C12	2635(3)	3174(10)	1202(6)	24(1)	1

C15	4529(3)	7063(10)	3214(6)	25(1)	1

N1	1579(2)	3413(9)	(621(5)	29(1)	1

N7	2217(2)	5251(8)	1139(4)	20(1)	1

N10	3316(2)	4969(9)	3065(4)	18(1)	1

O13	4286(2)	2792(7)	3991(4)	24(1)	1

O14	3862(2)	6092(7)	5315(3)	23(1)	1

S1	4006(1)	5098(3)	4008(1)	20(1)	1

Table 3. Bond lengths [Å] and angles [°].

C2(N1	1.349(7)

C2(C3	1.380(9)

C2(H2	0.9500

C3(C4	1.381(9)

C3(H3	0.9500

C4(C5	1.379(8)

C4(H4	0.9500

C5(C6	1.398(8)

C5(H5	0.9500

C6(N1	1.350(7)

C6(N7	1.394(6)

C8(N7	1.465(7)

C8(C9	1.510(7)

C8(H8A	0.9900

C8(H8B	0.9900

C9(N10	1.489(7)

C9(H9A	0.9900

C9(H9B	0.9900

C11(N10	1.478(6)

C11(C12	1.503(8)

C11(H11A	0.9900

C11(H11B	0.9900

C12(N7	1.459(7)

C12(H12A	0.9900

C12(H12B	0.9900

C15(S1	1.759(6)

C15(H15A	0.9800

C15(H15B	0.9800

C15(H15C	0.9800

N10(S1	1.631(4)

O13(S1	1.434(4)

O14(S1	1.435(4)

N1(C2(C3	124.7(6)

N1(C2(H2	117.7

C3(C2(H2	117.7

C2(C3(C4	116.7(5)

C2(C3(H3	121.7

C4(C3(H3	121.6

C5(C4(C3	120.7(6)

C5(C4(H4	119.6

C3(C4(H4	119.6

C4(C5(C6	118.7(6)

C4(C5(H5	120.6

C6(C5(H5	120.6

N1(C6(N7	116.1(5)

N1(C6(C5	121.7(5)

N7(C6(C5	122.2(5)

N7(C8(C9	111.3(4)

N7(C8(H8A	109.4

C9(C8(H8A	109.4

N7(C8(H8B	109.4

C9(C8(H8B	109.4

H8A(C8(H8B	108.0

N10(C9(C8	108.2(4)

N10(C9(H9A	110.1

C8(C9(H9A	110.1

N10(C9(H9B	110.1

C8(C9(H9B	110.1

H9A(C9(H9B	108.4

N10(C11(C12	109.3(4)

N10(C11(H11A	109.8

C12(C11(H11A	109.8

N10(C11(H11B	109.8

C12(C11(H11B	109.8

H11A(C11(H11B	108.3

N7(C12(C11	110.7(5)

N7(C12(H12A	109.5

C11(C12(H12A	109.5

N7(C12(H12B	109.5

C11(C12(H12B	109.5

H12A(C12(H12B	108.1

S1(C15(H15A	109.5

S1(C15(H15B	109.5

H15A(C15(H15B	109.5

S1(C15(H15C	109.5

H15A(C15(H15C	109.5

H15B(C15(H15C	109.5

C6(N1(C2	117.5(5)

C6(N7(C12	118.8(5)

C6(N7(C8	119.3(4)

C12(N7(C8	112.6(4)

C11(N10(C9	110.9(4)

C11(N10(S1	117.4(3)

C9(N10(S1	116.6(4)

O13(S1(O14	118.5(2)

O13(S1(N10	106.5(2)

O14(S1(N10	106.9(2)

O13(S1(C15	108.9(3)

O14(S1(C15	107.4(3)

N10(S1(C15	108.2(2)

Symmetry transformations used to generate equivalent atoms:

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C2	29(4) 	38(4)	33(3) 	(9(3)	(2(3) 	(6(3)

C3	25(3) 	42(4)	27(3) 	(1(3)	(5(2) 	(7(4)

C4	31(4) 	42(4)	32(3) 	6(3)	(3(3) 	9(3)

C5	28(3) 	31(4)	20(3) 	(5(3)	(1(3) 	7(3)

C6	18(3) 	20(3)	20(3) 	5(3)	6(2) 	(5(3)

C8	20(3) 	17(3)	23(3) 	(1(2)	1(2) 	3(2)

C9	29(3) 	19(3)	21(3) 	(3(2)	(2(2) 	3(3)

C11	25(3) 	22(3)	16(3) 	(3(2)	(1(2) 	7(3)

C12	28(3) 	17(3)	25(3) 	(7(3)	(5(2) 	2(3)

C15	17(3) 	28(3)	28(3) 	7(3)	(1(2) 	(1(3)

N1	30(3) 	29(3)	28(3) 	(3(2)	(2(2) 	(3(2)

N7	18(2) 	18(3)	24(2) 	(1(2)	(2(2) 	6(2)

N10	17(2) 	20(2)	16(2) 	0(2)	3(2) 	1(2)

O13	27(2) 	17(2)	26(2) 	1(2)	(1(2) 	3(2)

O14	30(2) 	22(2)	17(2) 	0(2)	(1(2) 	1(2)

S1	23(1) 	19(1)	18(1) 	0(1)	1(1) 	0(1)