|  | Single Crystal X-Ray Diffraction Service National Crystallography Service Contact: Dr S.K.Callear, S.K.Callear@soton.ac.uk |
| --- | --- |

Table 1. Crystal data and structure refinement details.

Identification code 	2009src0239

Empirical formula 	C18H28I2N4O2

Formula weight 	586.24

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Orthorhombic

Space group 	P212121

Unit cell dimensions	a = 8.9301(2) Å	( = 90°

b = 10.8793(2) Å	( = 90°

c = 23.2605(4) Å	(  = 90°

Volume	2259.83(8) Å3

Z	4

Density (calculated)	1.723 Mg / m3

Absorption coefficient	2.802 mm(1

F(000)	1144

Crystal	block; colourless

Crystal size	0.43 ( 0.35 ( 0.15 mm3

( range for data collection	2.95 ( 27.48°

Index ranges	(11 ( h ( 10, (14 ( k ( 12, (25 ( l ( 30

Reflections collected	19225

Independent reflections	5180 [Rint = 0.0479]

Completeness to ( = 27.48°	99.8 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.6786 and 0.3788

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	5180 / 0 / 239

Goodness-of-fit on F2	1.045

Final R indices [F2 > 2((F2)]	R1 = 0.0313, wR2 = 0.0689

R indices (all data)	R1 = 0.0374, wR2 = 0.0723

Absolute structure parameter	(0.01(2)

Largest diff. peak and hole	1.061 and (0.846 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: Sheldrick, G. M. SADABS - Bruker Nonius area detector scaling and absorption correction - V2.10 Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: ORTEP-3 (L.G. Farrugia, J. Appl. Cryst. (1997) 30, 565).

Special details:

All hydrogens fixed using a standard riding model.

The large Ueq(max)/Ueq(min) ratio for the carbon and hydrogen atoms is due to the dimethyl groups on the imidazolium groups being able to rotate, thus creating larger ellipsoids than usual. It was not possible, however, to model these atoms as disordered.

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C6	5241(5)	10459(4)	2045(2)	28(1)	1

C7	6500(5)	9817(5)	2359(2)	39(1)	1

C8	5163(6)	11830(4)	2189(2)	34(1)	1

C9	701(4)	7824(3)	1901(2)	15(1)	1

C10	1435(4)	6810(3)	1539(2)	14(1)	1

C12	(365(4)	8417(4)	1473(2)	18(1)	1

C13	241(4)	10578(4)	3988(2)	18(1)	1

C15	(1376(4)	12290(3)	4080(2)	13(1)	1

C16	(769(4)	11203(3)	4426(2)	14(1)	1

C22	(4695(5)	7977(4)	4342(2)	27(1)	1

C23	(4674(8)	6901(5)	4740(3)	60(2)	1

C24	(6283(6)	8448(6)	4227(3)	54(2)	1

O11	362(3)	8307(2)	917(1)	20(1)	1

O14	(524(3)	10723(2)	3447(1)	17(1)	1

C2	3074(5)	9088(4)	1847(2)	19(1)	1

C4	1765(5)	9271(4)	2644(2)	21(1)	1

C5	2968(5)	10000(4)	2684(2)	21(1)	1

C18	(2618(4)	9492(4)	4283(2)	15(1)	1

C20	(3910(5)	9621(4)	5085(2)	25(1)	1

C21	(2827(5)	10490(4)	5101(2)	19(1)	1

N1	3799(4)	9869(3)	2189(2)	18(1)	1

N3	1832(4)	8694(3)	2114(1)	15(1)	1

N17	(2035(3)	10397(3)	4596(1)	14(1)	1

N19	(3760(4)	8992(3)	4565(2)	18(1)	1

I1	5647(1)	7104(1)	1005(1)	20(1)	1

I2	(723(1)	6946(1)	3512(1)	24(1)	1

Table 3. Bond lengths [Å] and angles [°].

C6(N1	1.478(5)

C6(C7	1.512(7)

C6(C8	1.530(7)

C6(H6	1.0000

C7(H7A	0.9800

C7(H7B	0.9800

C7(H7C	0.9800

C8(H8A	0.9800

C8(H8B	0.9800

C8(H8C	0.9800

C9(N3	1.470(5)

C9(C12	1.521(5)

C9(C10	1.535(5)

C9(H9	1.0000

C10(O14i	1.436(4)

C10(C15i	1.532(5)

C10(H10	1.0000

C12(O11	1.454(5)

C12(H12A	0.9900

C12(H12B	0.9900

C13(O14	1.439(5)

C13(C16	1.523(5)

C13(H13A	0.9900

C13(H13B	0.9900

C15(O11ii	1.430(4)

C15(C16	1.529(5)

C15(C10ii	1.532(5)

C15(H15	1.0000

C16(N17	1.484(5)

C16(H16	1.0000

C22(N19	1.478(5)

C22(C23	1.492(7)

C22(C24	1.531(7)

C22(H22	1.0000

C23(H23A	0.9800

C23(H23B	0.9800

C23(H23C	0.9800

C24(H24A	0.9800

C24(H24B	0.9800

C24(H24C	0.9800

O11(C15i	1.430(4)

O14(C10ii	1.436(4)

C2(N1	1.333(5)

C2(N3	1.341(5)

C2(H2	0.9500

C4(C5	1.338(6)

C4(N3	1.384(5)

C4(H4	0.9500

C5(N1	1.376(5)

C5(H5	0.9500

C18(N19	1.329(5)

C18(N17	1.331(5)

C18(H18	0.9500

C20(C21	1.353(6)

C20(N19	1.397(6)

C20(H20	0.9500

C21(N17	1.376(5)

C21(H21	0.9500

N1(C6(C7	109.7(4)

N1(C6(C8	109.5(4)

C7(C6(C8	112.3(4)

N1(C6(H6	108.4

C7(C6(H6	108.4

C8(C6(H6	108.4

C6(C7(H7A	109.5

C6(C7(H7B	109.5

H7A(C7(H7B	109.5

C6(C7(H7C	109.5

H7A(C7(H7C	109.5

H7B(C7(H7C	109.5

C6(C8(H8A	109.5

C6(C8(H8B	109.5

H8A(C8(H8B	109.5

C6(C8(H8C	109.5

H8A(C8(H8C	109.5

H8B(C8(H8C	109.5

N3(C9(C12	112.1(3)

N3(C9(C10	110.7(3)

C12(C9(C10	102.3(3)

N3(C9(H9	110.5

C12(C9(H9	110.5

C10(C9(H9	110.5

O14i(C10(C15i	106.4(3)

O14i(C10(C9	109.7(3)

C15i(C10(C9	104.9(3)

O14i(C10(H10	111.8

C15i(C10(H10	111.8

C9(C10(H10	111.8

O11(C12(C9	105.6(3)

O11(C12(H12A	110.6

C9(C12(H12A	110.6

O11(C12(H12B	110.6

C9(C12(H12B	110.6

H12A(C12(H12B	108.8

O14(C13(C16	104.8(3)

O14(C13(H13A	110.8

C16(C13(H13A	110.8

O14(C13(H13B	110.8

C16(C13(H13B	110.8

H13A(C13(H13B	108.9

O11ii(C15(C16	111.8(3)

O11ii(C15(C10ii	106.9(3)

C16(C15(C10ii	104.1(3)

O11ii(C15(H15	111.3

C16(C15(H15	111.3

C10ii(C15(H15	111.3

N17(C16(C13	111.4(3)

N17(C16(C15	109.1(3)

C13(C16(C15	101.7(3)

N17(C16(H16	111.4

C13(C16(H16	111.4

C15(C16(H16	111.4

N19(C22(C23	111.2(4)

N19(C22(C24	109.6(4)

C23(C22(C24	112.4(5)

N19(C22(H22	107.8

C23(C22(H22	107.8

C24(C22(H22	107.8

C22(C23(H23A	109.5

C22(C23(H23B	109.5

H23A(C23(H23B	109.5

C22(C23(H23C	109.5

H23A(C23(H23C	109.5

H23B(C23(H23C	109.5

C22(C24(H24A	109.5

C22(C24(H24B	109.5

H24A(C24(H24B	109.5

C22(C24(H24C	109.5

H24A(C24(H24C	109.5

H24B(C24(H24C	109.5

C15i(O11(C12	110.0(3)

C10ii(O14(C13	109.9(3)

N1(C2(N3	109.3(4)

N1(C2(H2	125.4

N3(C2(H2	125.4

C5(C4(N3	107.2(4)

C5(C4(H4	126.4

N3(C4(H4	126.4

C4(C5(N1	108.3(4)

C4(C5(H5	125.9

N1(C5(H5	125.9

N19(C18(N17	109.5(3)

N19(C18(H18	125.3

N17(C18(H18	125.3

C21(C20(N19	107.3(4)

C21(C20(H20	126.3

N19(C20(H20	126.3

C20(C21(N17	107.1(4)

C20(C21(H21	126.5

N17(C21(H21	126.5

C2(N1(C5	107.6(3)

C2(N1(C6	124.4(4)

C5(N1(C6	128.0(4)

C2(N3(C4	107.6(3)

C2(N3(C9	128.2(3)

C4(N3(C9	124.2(3)

C18(N17(C21	108.7(3)

C18(N17(C16	126.2(3)

C21(N17(C16	125.2(3)

C18(N19(C20	107.5(3)

C18(N19(C22	124.5(4)

C20(N19(C22	128.0(4)

Symmetry transformations used to generate equivalent atoms:

(i) (x,y(1/2,(z+1/2    (ii) (x,y+1/2,(z+1/2

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C6	27(2) 	40(3)	18(2) 	(8(2)	6(2) 	(22(2)

C7	17(2) 	40(3)	61(4) 	(22(3)	4(2) 	(7(2)

C8	43(3) 	28(3)	30(3) 	7(2)	(8(2) 	(19(2)

C9	12(2) 	16(2)	16(2) 	(1(2)	(2(2) 	0(2)

C10	14(2) 	13(2)	14(2) 	0(2)	2(2) 	(3(2)

C12	17(2) 	17(2)	20(2) 	(5(2)	0(2) 	2(2)

C13	12(2) 	17(2)	24(2) 	2(2)	1(2) 	0(2)

C15	10(2) 	11(2)	18(2) 	0(2)	2(2) 	1(2)

C16	11(2) 	14(2)	16(2) 	2(2)	(4(2) 	(4(2)

C22	28(2) 	30(3)	22(2) 	0(2)	0(2) 	(13(2)

C23	92(5) 	25(3)	64(4) 	12(3)	(29(4) 	(29(3)

C24	29(3) 	45(4)	88(5) 	(13(3)	(14(3) 	(10(3)

O11	25(2) 	14(1)	21(2) 	1(1)	(5(1) 	7(1)

O14	25(2) 	13(1)	13(1) 	2(1)	2(1) 	7(1)

C2	24(2) 	22(2)	12(2) 	(5(2)	2(2) 	(2(2)

C4	27(2) 	25(2)	10(2) 	(7(2)	5(2) 	1(2)

C5	28(2) 	18(2)	17(2) 	(3(2)	4(2) 	(2(2)

C18	12(2) 	17(2)	16(2) 	(1(2)	2(2) 	0(2)

C20	26(2) 	33(3)	15(2) 	5(2)	6(2) 	(5(2)

C21	20(2) 	25(2)	12(2) 	0(2)	(1(2) 	0(2)

N1	19(2) 	18(2)	16(2) 	(5(2)	3(1) 	(4(2)

N3	15(2) 	14(2)	15(2) 	(5(1)	(2(2) 	(1(1)

N17	12(2) 	18(2)	11(2) 	3(1)	1(1) 	0(1)

N19	18(2) 	17(2)	19(2) 	2(2)	1(2) 	(6(2)

I1	12(1) 	27(1)	20(1) 	3(1)	0(1) 	(1(1)

I2	34(1) 	17(1)	22(1) 	(1(1)	0(1) 	0(1)