|  | University of Southampton · Department of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	01SRC618

Empirical formula 	C19H5BF10FeO2

Formula weight 	521.89

Temperature 	120(2) K

## Wavelength 	0.71073 Å

Crystal system 	Triclinic

Space group 	P(1

Unit cell dimensions	a = 10.6895(2) Å	( = 93.628(3)°

b = 13.4060(2) Å	( = 93.588(3)°

c = 13.6885(2) Å	(  = 113.060(3)°

Volume	1793.08(5) Å3

Z	4

Density (calculated)	1.933 Mg / m3

Absorption coefficient	0.959 mm(1

F(000)	1024

Crystal	Colourless Block

Crystal size	0.20 ( 0.20 ( 0.10 mm3

( range for data collection	3.00 ( 25.03°

Index ranges	(12 ( h ( 12, (15 ( k ( 15, (16 ( l ( 16

Reflections collected	12458

Independent reflections	6094 [Rint = 0.0589]

Completeness to ( = 25.03°	96.3 %

Max. and min. transmission	0.9102 and 0.8314

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	6094 / 0 / 595

Goodness-of-fit on F2	0.942

Final R indices [F2 > 2((F2)]	R1 = 0.0431, wR2 = 0.0741

R indices (all data)	R1 = 0.0829, wR2 = 0.0858

Largest diff. peak and hole	0.356 and (0.431 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill Ewald sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing, Acta Cryst. A51 (1995) 33(37; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421(426). Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: Cameron - A Molecular Graphics Package. (D. M. Watkin, L. Pearce and C. K. Prout, Chemical Crystallography Laboratory, University of Oxford, 1993).

Special details:  All hydrogen atoms were placed in idealised positions and refined using a riding model.

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

Fe1	5677(1)	2459(1)	4592(1)	17(1)	1

Fe2	3214(1)	(2538(1)	10318(1)	18(1)	1

F16	1237(2)	(1061(2)	12143(1)	24(1)	1

F17	139(2)	(1520(2)	13874(1)	29(1)	1

F6	3685(2)	4075(2)	6404(1)	26(1)	1

F20	292(2)	(4783(2)	11383(1)	24(1)	1

F14	(3002(2)	(3569(2)	8721(1)	30(1)	1

F15	(1250(2)	(4036(2)	9914(1)	24(1)	1

F5	1507(2)	620(2)	4698(1)	25(1)	1

F19	(799(2)	(5228(2)	13109(1)	27(1)	1

F9	2963(2)	334(2)	8056(1)	26(1)	1

F18	(849(2)	(3600(2)	14367(1)	26(1)	1

F10	3637(2)	530(2)	6201(1)	22(1)	1

F11	1992(2)	(413(2)	9977(1)	25(1)	1

F2	1553(2)	4186(2)	3009(1)	30(1)	1

F1	3755(2)	4317(2)	4168(1)	26(1)	1

F12	245(2)	41(2)	8778(1)	28(1)	1

F3	(687(2)	2280(2)	2698(1)	29(1)	1

F7	3068(3)	3884(2)	8289(1)	34(1)	1

F4	(704(2)	502(2)	3543(1)	33(1)	1

F8	2691(2)	2015(2)	9118(1)	32(1)	1

F13	(2282(2)	(1517(2)	8161(1)	31(1)	1

O1	5200(3)	3415(2)	2829(2)	31(1)	1

O4	3364(3)	(3944(2)	11813(2)	29(1)	1

O3	4165(3)	(561(2)	11652(2)	33(1)	1

C31	(1766(4)	(2793(3)	9017(2)	22(1)	1

C12	409(4)	1434(3)	3700(2)	20(1)	1

C20	2443(4)	(2994(3)	8825(2)	20(1)	1

C13	1550(4)	1522(3)	4273(2)	17(1)	1

C33	835(4)	(2892(3)	11709(2)	14(1)	1

C5	6849(4)	3384(3)	5873(2)	19(1)	1

C9	2668(4)	3351(3)	4006(2)	17(1)	1

C29	(124(4)	(973(3)	9060(2)	19(1)	1

C28	775(4)	(1230(3)	9661(2)	20(1)	1

C32	(837(4)	(3011(3)	9637(2)	18(1)	1

C30	(1381(4)	(1745(3)	8743(2)	23(1)	1

C8	2719(4)	2452(3)	4447(2)	16(1)	1

C11	425(4)	2344(3)	3272(2)	21(1)	1

C38	293(4)	(3948(3)	11994(2)	17(1)	1

C34	746(4)	(2106(3)	12376(2)	18(1)	1

O2	3876(3)	249(2)	3833(2)	31(1)	1

C15	3521(4)	3133(3)	6805(2)	19(1)	1

C26	3271(4)	(3381(3)	11231(3)	21(1)	1

C25	3788(4)	(1339(3)	11124(3)	23(1)	1

C35	189(4)	(2316(3)	13255(2)	18(1)	1

C24	3104(4)	(3665(3)	9147(2)	21(1)	1

C19	3513(4)	1389(3)	6697(2)	17(1)	1

B2	1439(5)	(2592(3)	10678(3)	17(1)	1

C27	455(4)	(2255(3)	9971(2)	17(1)	1

C18	3172(4)	1278(3)	7652(2)	20(1)	1

C22	4704(5)	(1918(3)	9304(2)	27(1)	1

C1	7516(4)	3787(3)	5037(2)	22(1)	1

C17	3014(4)	2110(3)	8177(2)	21(1)	1

C7	4594(5)	1130(3)	4133(2)	23(1)	1

C37	(268(4)	(4190(3)	12868(2)	18(1)	1

C10	1553(4)	3300(3)	3427(2)	20(1)	1

C36	(317(4)	(3377(3)	13501(2)	20(1)	1

C4	6705(4)	2292(3)	5889(2)	20(1)	1

C14	3697(4)	2319(3)	6229(2)	17(1)	1

C2	7807(4)	2949(3)	4546(3)	23(1)	1

C6	5373(4)	3034(3)	3529(3)	23(1)	1

C23	4494(4)	(2995(3)	9426(2)	23(1)	1

C16	3208(4)	3057(3)	7758(2)	23(1)	1

C3	7313(4)	2031(3)	5069(2)	23(1)	1

C21	3425(4)	(1916(3)	8935(2)	24(1)	1

B1	3997(5)	2449(3)	5104(3)	16(1)	1

Table 3. Bond lengths [Å] and angles [°].

Fe1(C7	1.749(4)

Fe1(C6	1.760(4)

Fe1(B1	1.964(4)

Fe1(C1	2.092(4)

Fe1(C5	2.101(4)

Fe1(C4	2.099(3)

Fe1(C2	2.114(4)

Fe1(C3	2.122(4)

Fe2(C26	1.751(4)

Fe2(C25	1.760(4)

Fe2(B2	1.965(5)

Fe2(C24	2.096(3)

Fe2(C21	2.107(3)

Fe2(C20	2.113(3)

Fe2(C23	2.123(3)

Fe2(C22	2.131(4)

F16(C34	1.357(4)

F17(C35	1.340(4)

F6(C15	1.361(4)

F20(C38	1.354(3)

F14(C31	1.339(4)

F15(C32	1.355(4)

F5(C13	1.361(4)

F19(C37	1.353(4)

F9(C18	1.357(4)

F18(C36	1.347(4)

F10(C19	1.354(3)

F11(C28	1.353(4)

F2(C10	1.352(4)

F1(C9	1.353(4)

F12(C29	1.349(4)

F3(C11	1.353(4)

F7(C16	1.350(4)

F4(C12	1.339(4)

F8(C17	1.355(4)

F13(C30	1.351(4)

O1(C6	1.152(4)

O4(C26	1.157(4)

O3(C25	1.145(4)

C31(C30	1.384(5)

C31(C32	1.395(5)

C12(C13	1.369(5)

C12(C11	1.380(5)

C20(C21	1.407(5)

C20(C24	1.418(5)

C13(C8	1.370(5)

C33(C34	1.386(4)

C33(C38	1.395(5)

C33(B2	1.598(5)

C5(C1	1.410(5)

C5(C4	1.414(5)

C9(C10	1.366(5)

C9(C8	1.398(4)

C29(C30	1.358(5)

C29(C28	1.384(5)

C28(C27	1.382(5)

C32(C27	1.381(5)

C8(B1	1.589(5)

C11(C10	1.365(5)

C38(C37	1.373(5)

C34(C35	1.373(5)

O2(C7	1.158(4)

C15(C16	1.366(5)

C15(C14	1.385(4)

C35(C36	1.381(5)

C24(C23	1.414(5)

C19(C18	1.381(4)

C19(C14	1.389(5)

B2(C27	1.595(5)

C18(C17	1.360(5)

C22(C23	1.394(5)

C22(C21	1.428(5)

C1(C2	1.420(4)

C17(C16	1.373(5)

C37(C36	1.367(4)

C4(C3	1.422(5)

C14(B1	1.600(5)

C2(C3	1.398(5)

C7(Fe1(C6	93.98(17)

C7(Fe1(B1	82.27(17)

C6(Fe1(B1	91.48(17)

C7(Fe1(C1	157.88(16)

C6(Fe1(C1	92.98(17)

B1(Fe1(C1	118.51(15)

C7(Fe1(C5	142.13(14)

C6(Fe1(C5	123.54(15)

B1(Fe1(C5	91.00(16)

C1(Fe1(C5	39.29(13)

C7(Fe1(C4	105.12(15)

C6(Fe1(C4	158.78(17)

B1(Fe1(C4	100.04(15)

C1(Fe1(C4	65.87(14)

C5(Fe1(C4	39.33(12)

C7(Fe1(C2	118.68(16)

C6(Fe1(C2	97.36(17)

B1(Fe1(C2	156.37(16)

C1(Fe1(C2	39.46(13)

C5(Fe1(C2	65.86(14)

C4(Fe1(C2	65.53(14)

C7(Fe1(C3	94.39(16)

C6(Fe1(C3	131.47(16)

B1(Fe1(C3	137.01(15)

C1(Fe1(C3	65.57(14)

C5(Fe1(C3	65.85(13)

C4(Fe1(C3	39.37(13)

C2(Fe1(C3	38.53(13)

C26(Fe2(C25	95.00(16)

C26(Fe2(B2	91.20(16)

C25(Fe2(B2	80.99(17)

C26(Fe2(C24	94.65(14)

C25(Fe2(C24	161.25(17)

B2(Fe2(C24	114.84(17)

C26(Fe2(C21	158.26(14)

C25(Fe2(C21	101.84(15)

B2(Fe2(C21	104.85(15)

C24(Fe2(C21	65.48(14)

C26(Fe2(C20	128.21(16)

C25(Fe2(C20	136.38(14)

B2(Fe2(C20	91.16(16)

C24(Fe2(C20	39.36(12)

C21(Fe2(C20	38.94(14)

C26(Fe2(C23	94.17(14)

C25(Fe2(C23	123.93(18)

B2(Fe2(C23	153.79(17)

C24(Fe2(C23	39.16(15)

C21(Fe2(C23	65.02(13)

C20(Fe2(C23	65.54(14)

C26(Fe2(C22	125.66(16)

C25(Fe2(C22	96.02(17)

B2(Fe2(C22	143.09(15)

C24(Fe2(C22	65.33(15)

C21(Fe2(C22	39.38(14)

C20(Fe2(C22	65.71(15)

C23(Fe2(C22	38.25(13)

F14(C31(C30	121.4(3)

F14(C31(C32	120.7(3)

C30(C31(C32	117.8(4)

F4(C12(C13	122.2(3)

F4(C12(C11	119.7(3)

C13(C12(C11	118.1(4)

C21(C20(C24	107.2(4)

C21(C20(Fe2	70.3(2)

C24(C20(Fe2	69.68(19)

F5(C13(C12	117.2(3)

F5(C13(C8	118.4(3)

C12(C13(C8	124.4(3)

C34(C33(C38	114.5(3)

C34(C33(B2	121.3(3)

C38(C33(B2	124.1(3)

C1(C5(C4	107.6(3)

C1(C5(Fe1	70.0(2)

C4(C5(Fe1	70.3(2)

F1(C9(C10	118.2(3)

F1(C9(C8	119.1(3)

C10(C9(C8	122.7(4)

F12(C29(C30	119.6(3)

F12(C29(C28	120.3(4)

C30(C29(C28	120.2(3)

F11(C28(C29	117.0(3)

F11(C28(C27	120.1(3)

C29(C28(C27	122.8(4)

F15(C32(C27	119.3(3)

F15(C32(C31	116.7(4)

C27(C32(C31	124.0(3)

F13(C30(C29	121.4(3)

F13(C30(C31	118.4(4)

C29(C30(C31	120.1(3)

C13(C8(C9	114.9(3)

C13(C8(B1	120.0(3)

C9(C8(B1	125.2(3)

F3(C11(C10	120.3(3)

F3(C11(C12	119.4(4)

C10(C11(C12	120.3(3)

F20(C38(C37	117.7(3)

F20(C38(C33	119.4(3)

C37(C38(C33	122.9(3)

F16(C34(C35	117.8(3)

F16(C34(C33	117.9(3)

C35(C34(C33	124.3(3)

F6(C15(C16	117.7(3)

F6(C15(C14	118.1(3)

C16(C15(C14	124.2(3)

O4(C26(Fe2	176.6(3)

O3(C25(Fe2	179.6(3)

F17(C35(C34	121.6(3)

F17(C35(C36	120.0(3)

C34(C35(C36	118.4(3)

C23(C24(C20	108.1(4)

C23(C24(Fe2	71.4(2)

C20(C24(Fe2	70.95(19)

F10(C19(C18	117.3(3)

F10(C19(C14	119.7(3)

C18(C19(C14	123.0(3)

C27(B2(C33	111.4(3)

C27(B2(Fe2	122.7(3)

C33(B2(Fe2	125.8(2)

C28(C27(C32	115.0(3)

C28(C27(B2	125.0(4)

C32(C27(B2	120.0(3)

F9(C18(C17	120.2(3)

F9(C18(C19	120.1(3)

C17(C18(C19	119.7(3)

C23(C22(C21	107.3(4)

C23(C22(Fe2	70.6(2)

C21(C22(Fe2	69.4(2)

C5(C1(C2	108.2(3)

C5(C1(Fe1	70.7(2)

C2(C1(Fe1	71.1(2)

F8(C17(C18	120.2(3)

F8(C17(C16	119.9(3)

C18(C17(C16	119.8(3)

O2(C7(Fe1	179.8(4)

F19(C37(C36	119.3(3)

F19(C37(C38	120.9(3)

C36(C37(C38	119.9(3)

F2(C10(C11	119.7(3)

F2(C10(C9	120.7(4)

C11(C10(C9	119.6(3)

F18(C36(C37	120.5(3)

F18(C36(C35	119.5(3)

C37(C36(C35	120.0(3)

C5(C4(C3	108.1(3)

C5(C4(Fe1	70.40(19)

C3(C4(Fe1	71.18(19)

C15(C14(C19	114.3(3)

C15(C14(B1	121.2(3)

C19(C14(B1	124.4(3)

C3(C2(C1	108.2(3)

C3(C2(Fe1	71.0(2)

C1(C2(Fe1	69.4(2)

O1(C6(Fe1	178.7(3)

C22(C23(C24	108.7(3)

C22(C23(Fe2	71.2(2)

C24(C23(Fe2	69.4(2)

F7(C16(C15	121.6(3)

F7(C16(C17	119.4(3)

C15(C16(C17	119.0(3)

C2(C3(C4	107.9(3)

C2(C3(Fe1	70.4(2)

C4(C3(Fe1	69.4(2)

C20(C21(C22	108.6(3)

C20(C21(Fe2	70.77(19)

C22(C21(Fe2	71.22(19)

C8(B1(C14	111.6(3)

C8(B1(Fe1	124.7(2)

C14(B1(Fe1	123.4(3)

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

Fe1	18(1) 	18(1)	16(1) 	1(1)	2(1) 	8(1)

Fe2	18(1) 	21(1)	15(1) 	3(1)	4(1) 	9(1)

F16	32(2) 	18(1)	25(1) 	5(1)	6(1) 	11(1)

F17	41(2) 	28(1)	22(1) 	(4(1)	9(1) 	18(1)

F6	33(2) 	19(1)	28(1) 	2(1)	4(1) 	13(1)

F20	32(2) 	20(1)	22(1) 	0(1)	9(1) 	12(1)

F14	20(2) 	38(1)	29(1) 	(2(1)	(2(1) 	11(1)

F15	23(2) 	22(1)	24(1) 	4(1)	3(1) 	6(1)

F5	28(2) 	20(1)	26(1) 	8(1)	0(1) 	6(1)

F19	31(2) 	20(1)	29(1) 	8(1)	11(1) 	7(1)

F9	29(2) 	32(1)	21(1) 	14(1)	7(1) 	13(1)

F18	27(2) 	35(1)	18(1) 	6(1)	10(1) 	11(1)

F10	25(2) 	21(1)	21(1) 	3(1)	5(1) 	12(1)

F11	27(2) 	22(1)	25(1) 	5(1)	1(1) 	9(1)

F2	39(2) 	29(1)	30(1) 	7(1)	0(1) 	22(1)

F1	29(2) 	19(1)	29(1) 	4(1)	2(1) 	8(1)

F12	37(2) 	30(1)	26(1) 	10(1)	5(1) 	20(1)

F3	23(2) 	50(2)	20(1) 	1(1)	(3(1) 	22(1)

F7	42(2) 	36(1)	28(1) 	(10(1)	7(1) 	20(1)

F4	21(2) 	36(1)	31(1) 	4(1)	(6(1) 	1(1)

F8	29(2) 	48(2)	16(1) 	2(1)	8(1) 	12(1)

F13	30(2) 	49(2)	24(1) 	5(1)	(2(1) 	28(1)

O1	41(2) 	40(2)	18(1) 	10(1)	8(1) 	20(2)

O4	35(2) 	37(2)	23(1) 	12(1)	5(1) 	20(2)

O3	29(2) 	32(2)	33(2) 	(10(1)	0(1) 	9(2)

C31	16(3) 	29(2)	16(2) 	(9(2)	4(2) 	6(2)

C12	17(3) 	23(2)	14(2) 	1(2)	1(2) 	2(2)

C20	20(3) 	27(2)	13(2) 	(1(2)	3(2) 	10(2)

C13	21(3) 	21(2)	12(2) 	2(2)	4(2) 	11(2)

C33	11(2) 	17(2)	14(2) 	2(2)	2(2) 	6(2)

C5	12(2) 	21(2)	22(2) 	(1(2)	1(2) 	6(2)

C9	17(3) 	16(2)	18(2) 	(2(2)	3(2) 	5(2)

C29	20(3) 	20(2)	17(2) 	2(2)	7(2) 	9(2)

C28	22(3) 	26(2)	15(2) 	(3(2)	1(2) 	12(2)

C32	23(3) 	22(2)	15(2) 	2(2)	5(2) 	13(2)

C30	26(3) 	38(3)	15(2) 	2(2)	3(2) 	23(2)

C8	17(2) 	16(2)	14(2) 	0(2)	4(2) 	6(2)

C11	22(3) 	35(3)	11(2) 	2(2)	2(2) 	18(2)

C38	16(2) 	21(2)	15(2) 	(2(2)	1(2) 	9(2)

C34	14(2) 	18(2)	20(2) 	4(2)	0(2) 	5(2)

O2	30(2) 	24(2)	38(2) 	(6(1)	(1(1) 	10(2)

C15	17(3) 	16(2)	21(2) 	1(2)	0(2) 	5(2)

C26	15(3) 	30(2)	21(2) 	0(2)	5(2) 	11(2)

C25	20(3) 	32(3)	20(2) 	9(2)	5(2) 	12(2)

C35	16(2) 	22(2)	17(2) 	(5(2)	1(2) 	11(2)

C24	28(3) 	22(2)	16(2) 	2(2)	5(2) 	10(2)

C19	11(2) 	22(2)	17(2) 	(1(2)	2(2) 	6(2)

B2	22(3) 	8(2)	18(2) 	(3(2)	0(2) 	4(2)

C27	23(3) 	20(2)	13(2) 	2(2)	6(2) 	13(2)

C18	18(3) 	23(2)	17(2) 	7(2)	0(2) 	7(2)

C22	25(3) 	31(3)	21(2) 	2(2)	10(2) 	6(2)

C1	18(3) 	17(2)	29(2) 	2(2)	3(2) 	4(2)

C17	20(3) 	34(2)	9(2) 	1(2)	5(2) 	9(2)

C7	31(3) 	28(3)	18(2) 	4(2)	3(2) 	19(2)

C37	16(2) 	16(2)	21(2) 	2(2)	3(2) 	4(2)

C10	27(3) 	27(2)	15(2) 	6(2)	4(2) 	19(2)

C36	17(3) 	28(2)	12(2) 	2(2)	5(2) 	6(2)

C4	15(3) 	23(2)	19(2) 	5(2)	1(2) 	5(2)

C14	16(2) 	21(2)	14(2) 	0(2)	0(2) 	8(2)

C2	14(3) 	31(2)	23(2) 	2(2)	4(2) 	7(2)

C6	21(3) 	27(2)	22(2) 	(3(2)	5(2) 	12(2)

C23	28(3) 	32(2)	17(2) 	4(2)	9(2) 	19(2)

C16	20(3) 	27(2)	20(2) 	(9(2)	2(2) 	11(2)

C3	19(3) 	27(2)	23(2) 	(1(2)	(3(2) 	12(2)

C21	35(3) 	27(2)	16(2) 	7(2)	10(2) 	18(2)

B1	22(3) 	5(2)	18(2) 	1(2)	4(2) 	3(2)

Table 5. Hydrogen coordinates [( 104] and isotropic displacement parameters [Å2 ( 103].

Atom 	x	y	z	Ueq	S.o.f.

H20	1511	(3229	8581	24	1

H5	6551	3776	6341	23	1

H24	2686	(4431	9171	26	1

H22	5542	(1300	9441	32	1

H1	7733	4497	4836	27	1

H4	6277	1814	6364	24	1

H2	8259	3002	3964	28	1

H23	5172	(3238	9659	27	1

H3	7373	1352	4905	27	1

H21	3265	(1291	8788	28	1