|  | Single Crystal X-Ray Diffraction Service National Crystallography Service Contact: Dr S.K.Callear, S.K.Callear@soton.ac.uk |
| --- | --- |

Table 1. Crystal data and structure refinement details.

Identification code 	2009src0288cc

Empirical formula 	C9H12Cl2N2O3Si

Formula weight 	295.20

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	Cc

Unit cell dimensions	a = 10.6695(9) Å	( = 90°

b = 17.3082(17) Å	( = 116.560(3)°

c = 7.7714(6) Å	(  = 90°

Volume	1283.69(19) Å3

Z	4

Density (calculated)	1.527 Mg / m3

Absorption coefficient	0.596 mm(1

F(000)	608

Crystal	fragment; brown

Crystal size	0.12 ( 0.05 ( 0.02 mm3

( range for data collection	2.99 ( 27.48°

Index ranges	(13 ( h ( 13, (22 ( k ( 22, (10 ( l ( 10

Reflections collected	10860

Independent reflections	2873 [Rint = 0.0713]

Completeness to ( = 27.48°	99.9 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.9882 and 0.9319

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	2873 / 8 / 167

Goodness-of-fit on F2	1.104

Final R indices [F2 > 2((F2)]	R1 = 0.0664, wR2 = 0.1369

R indices (all data)	R1 = 0.0982, wR2 = 0.1554

Absolute structure parameter	0.14(14)

Largest diff. peak and hole	0.716 and (0.364 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: Sheldrick, G. M. SADABS - Bruker Nonius area detector scaling and absorption correction - V2.10 Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: ORTEP-3 (L.G. Farrugia, J. Appl. Cryst. (1997) 30, 565).

Special details:

All hydrogens fixed using a standard riding model.

Methyl and methylene chloride groups disordered with 64.593% in position 1.

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C10	3110(20)	7792(7)	1290(30)	48(2)	0.646(5)

Cl1	2669(3)	7942(1)	(1038(3)	56(1)	0.646(5)

C11	3720(20)	9511(9)	2930(20)	48(2)	0.646(5)

C20	3680(40)	9491(15)	2590(50)	48(2)	0.354(5)

Cl2	2712(5)	10171(2)	2804(7)	55(2)	0.354(5)

C21	3010(40)	7700(12)	1470(60)	48(2)	0.354(5)

C2	(1182(6)	8673(3)	2179(8)	39(1)	1

C3	(2473(6)	8825(4)	695(8)	44(1)	1

C4	(2488(6)	9026(3)	(1087(8)	42(1)	1

C5	(1276(5)	9075(3)	(1253(7)	37(1)	1

C6	47(5)	8917(3)	315(7)	39(1)	1

C7	(3793(6)	8784(5)	889(9)	63(2)	1

C9	1393(5)	8521(4)	3569(8)	44(1)	1

N1	2(5)	8719(3)	2003(6)	38(1)	1

N8	(1362(5)	9266(3)	(3121(6)	43(1)	1

O6	1219(4)	8937(3)	321(5)	53(1)	1

O8A	(2519(4)	9281(3)	(4509(6)	58(1)	1

O8B	(293(5)	9410(3)	(3266(6)	63(1)	1

Si1	2758(2)	8589(1)	2649(2)	47(1)	1

Cl3	4361(1)	8112(1)	5545(2)	49(1)	1

Table 3. Bond lengths [Å] and angles [°].

C10(Cl1	1.672(18)

C10(Si1	1.873(10)

C10(H10A	0.9900

C10(H10B	0.9900

C11(Si1	1.855(9)

C11(H11A	0.9800

C11(H11B	0.9800

C11(H11C	0.9800

C20(Cl2	1.63(4)

C20(Si1	1.860(14)

C20(H20A	0.9900

C20(H20B	0.9900

C21(Si1	1.871(14)

C21(H21A	0.9800

C21(H21B	0.9800

C21(H21C	0.9800

C2(N1	1.333(7)

C2(C3	1.369(8)

C2(H2	0.9500

C3(C4	1.421(8)

C3(C7	1.484(8)

C4(C5	1.359(8)

C4(H4	0.9500

C5(C6	1.419(7)

C5(N8	1.451(7)

C6(O6	1.249(7)

C6(N1	1.377(7)

C7(H7A	0.9800

C7(H7B	0.9800

C7(H7C	0.9800

C9(N1	1.479(6)

C9(Si1	1.892(6)

C9(H9A	0.9900

C9(H9B	0.9900

N8(O8B	1.222(6)

N8(O8A	1.223(6)

O6(Si1	1.918(4)

Si1(Cl3	2.2864(19)

Cl1(C10(Si1	117.8(10)

Cl1(C10(H10A	107.9

Si1(C10(H10A	107.9

Cl1(C10(H10B	107.9

Si1(C10(H10B	107.9

H10A(C10(H10B	107.2

Si1(C11(H11A	109.5

Si1(C11(H11B	109.5

Si1(C11(H11C	109.5

Cl2(C20(Si1	103.6(18)

Cl2(C20(H20A	111.0

Si1(C20(H20A	111.0

Cl2(C20(H20B	111.0

Si1(C20(H20B	111.0

H20A(C20(H20B	109.0

Si1(C21(H21A	109.5

Si1(C21(H21B	109.5

H21A(C21(H21B	109.5

Si1(C21(H21C	109.5

H21A(C21(H21C	109.5

H21B(C21(H21C	109.5

N1(C2(C3	123.0(5)

N1(C2(H2	118.5

C3(C2(H2	118.5

C2(C3(C4	115.9(5)

C2(C3(C7	123.3(6)

C4(C3(C7	120.8(5)

C5(C4(C3	120.8(5)

C5(C4(H4	119.6

C3(C4(H4	119.6

C4(C5(C6	122.0(5)

C4(C5(N8	118.2(5)

C6(C5(N8	119.8(5)

O6(C6(N1	117.7(5)

O6(C6(C5	127.4(5)

N1(C6(C5	114.9(5)

C3(C7(H7A	109.5

C3(C7(H7B	109.5

H7A(C7(H7B	109.5

C3(C7(H7C	109.5

H7A(C7(H7C	109.5

H7B(C7(H7C	109.5

N1(C9(Si1	109.5(4)

N1(C9(H9A	109.8

Si1(C9(H9A	109.8

N1(C9(H9B	109.8

Si1(C9(H9B	109.8

H9A(C9(H9B	108.2

C2(N1(C6	123.4(5)

C2(N1(C9	123.4(4)

C6(N1(C9	113.1(4)

O8B(N8(O8A	122.0(5)

O8B(N8(C5	119.7(4)

O8A(N8(C5	118.3(5)

C6(O6(Si1	115.4(4)

C11(Si1(C20	8.0(15)

C11(Si1(C21	125.0(12)

C20(Si1(C21	118.9(12)

C11(Si1(C10	117.6(7)

C20(Si1(C10	111.2(14)

C21(Si1(C10	8.0(12)

C11(Si1(C9	119.0(7)

C20(Si1(C9	124.7(13)

C21(Si1(C9	116.0(9)

C10(Si1(C9	123.2(5)

C11(Si1(O6	92.0(6)

C20(Si1(O6	87.2(12)

C21(Si1(O6	92.6(14)

C10(Si1(O6	90.0(7)

C9(Si1(O6	84.1(2)

C11(Si1(Cl3	93.6(6)

C20(Si1(Cl3	99.0(11)

C21(Si1(Cl3	88.8(14)

C10(Si1(Cl3	92.3(7)

C9(Si1(Cl3	88.23(16)

O6(Si1(Cl3	171.99(14)

Symmetry transformations used to generate equivalent atoms:

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C10	42(3) 	55(3)	40(5) 	13(3)	11(3) 	(11(2)

Cl1	72(2) 	59(2)	43(1) 	(8(1)	31(1) 	7(1)

C11	42(3) 	55(3)	40(5) 	13(3)	11(3) 	(11(2)

C20	42(3) 	55(3)	40(5) 	13(3)	11(3) 	(11(2)

Cl2	75(3) 	38(2)	50(3) 	(3(2)	27(2) 	(3(2)

C21	42(3) 	55(3)	40(5) 	13(3)	11(3) 	(11(2)

C2	41(3) 	41(3)	35(3) 	(4(2)	18(2) 	(3(2)

C3	34(3) 	57(4)	43(3) 	(5(3)	18(3) 	1(3)

C4	35(3) 	38(3)	40(3) 	(2(2)	6(2) 	3(2)

C5	36(3) 	34(3)	30(3) 	(1(2)	6(2) 	(2(2)

C6	34(3) 	41(3)	36(3) 	2(2)	9(2) 	(6(2)

C7	35(3) 	95(6)	54(4) 	(6(4)	17(3) 	9(3)

C9	30(3) 	59(4)	32(3) 	13(3)	6(2) 	(6(2)

N1	39(2) 	42(3)	25(2) 	0(2)	8(2) 	(8(2)

N8	48(3) 	41(3)	32(3) 	6(2)	10(2) 	(3(2)

O6	27(2) 	82(3)	38(2) 	21(2)	6(2) 	(10(2)

O8A	46(2) 	64(3)	39(2) 	12(2)	(3(2) 	(7(2)

O8B	51(3) 	94(4)	40(2) 	19(2)	16(2) 	5(2)

Si1	29(1) 	67(1)	33(1) 	13(1)	4(1) 	(10(1)

Cl3	37(1) 	57(1)	36(1) 	8(1)	2(1) 	(4(1)