|  | Single Crystal X-Ray Diffraction Service National Crystallography Service Contact: Dr S.K.Callear, S.K.Callear@soton.ac.uk |
| --- | --- |

Smaller disordered component not labelled- numbering is the sameas large component except for an additional 1 prefixing the number.

Table 1. Crystal data and structure refinement details.

Identification code 	2008src1083 (SBP162)

Empirical formula 	C24H16N2O4

Formula weight 	396.39

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P2/n

Unit cell dimensions	a = 22.6513(8) Å	( = 90°

b = 7.5907(5) Å	( = 101.110(3)°

c = 22.7311(14) Å	(  = 90°

Volume	3835.1(4) Å3

Z	8

Density (calculated)	1.373 Mg / m3

Absorption coefficient	0.095 mm(1

F(000)	1648

Crystal	block; colourless

Crystal size	0.36 ( 0.22 ( 0.10 mm3

( range for data collection	2.92 ( 25.00°

Index ranges	(22 ( h ( 25, (9 ( k ( 9, (27 ( l ( 27

Reflections collected	26118

Independent reflections	6422 [Rint = 0.0815]

Completeness to ( = 25.00°	95.2 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.9906 and 0.9666

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	6422 / 746 / 643

Goodness-of-fit on F2	1.055

Final R indices [F2 > 2((F2)]	R1 = 0.0763, wR2 = 0.1921

R indices (all data)	R1 = 0.1392, wR2 = 0.2287

Largest diff. peak and hole	0.425 and (0.416 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: Sheldrick, G. M. SADABS - Bruker Nonius area detector scaling and absorption correction - V2.10 Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: ORTEP-3 (L.G. Farrugia, J. Appl. Cryst. (1997) 30, 565).

Special details:

All hydrogens fixed using a standard riding model.

Due to the weakly diffracting nature of the crystals, data were only included out to 25deg.

One of the two independent molecules in the unit cell is seen as disordered due to a stacking fault in the crystal. The occupancy of the major component was found to be 90.438%. The secondary component of the disorder was refined isotropically due to it only being present less than 10% of the time; the other molecule and the major component of the disordered assembly were refined anisotropically. Restraints were used to ensure appropriate bond lengths and angles (DFIX,  FLAT) and that the minor component was modelled on the major component. This was necessary as the minor component atoms were located from approximately 0.6-0.8 of an electron.

Interestingly the stacking fault results in the minor component and the independent non-disordered molecule overlaying in the unit cell.

The data was tested for merohedral twinning using ROTAX before the minor component was modelled, but the matricies suggested did not yield any reduction in R values after 25+ refinement cycles. To ensure that it was a stacking fault that was being observed, the data was also processed and solved in the triclinic space group P-1 which showed 4 independent molecules, 2 of which were disordered with an ~9:1 ratio between their major and minor components.

Three datasets were collected from the sample to investigate whether this was a fault particular to one crystal or seen throughout the sample. All datasets gave the same result.

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C131	1320(18)	4980(70)	2935(18)	33(8)	0.096(3)

C132	1653(18)	5470(70)	2470(18)	34(9)	0.096(3)

C133	1490(20)	4770(70)	1880(20)	38(10)	0.096(3)

C134	951(17)	3870(60)	1728(17)	16(8)	0.096(3)

C135	659(19)	3440(70)	2193(19)	29(8)	0.096(3)

C136	870(20)	4000(70)	2810(20)	34(9)	0.096(3)

C137	1550(20)	5560(80)	3570(20)	45(9)	0.096(3)

C138	2232(19)	7090(70)	4255(18)	36(10)	0.096(3)

C139	729(16)	3060(70)	1089(14)	24(9)	0.096(3)

C140	1067(10)	2500(50)	675(15)	31(9)	0.096(3)

C141	787(17)	2140(50)	88(14)	17(9)	0.096(3)

C142	168(18)	2350(90)	(86(17)	24(9)	0.096(3)

C143	(171(12)	2910(120)	330(20)	35(10)	0.096(3)

C144	110(16)	3260(110)	920(20)	30(11)	0.096(3)

C145	(90(30)	1850(70)	(688(15)	32(12)	0.096(3)

C147	(782(10)	3150(70)	30(20)	27(12)	0.096(3)

C149	1696(9)	1890(50)	965(14)	42(9)	0.096(3)

C150	1834(11)	770(50)	1455(14)	40(9)	0.096(3)

C151	2422(13)	200(40)	1650(12)	41(9)	0.096(3)

C152	2872(10)	750(40)	1355(12)	30(8)	0.096(3)

C153	2735(11)	1870(40)	865(12)	29(8)	0.096(3)

C154	2146(12)	2440(40)	670(12)	46(11)	0.096(3)

C155	3480(20)	420(70)	1500(20)	41(9)	0.096(3)

C156	4228(19)	(970(70)	2240(20)	42(11)	0.096(3)

N146	(300(20)	1470(80)	(1166(15)	19(9)	0.096(3)

N148	(1264(12)	3330(60)	(220(20)	19(9)	0.096(3)

O137	1201(12)	5380(50)	3942(13)	38(8)	0.096(3)

O138	2011(13)	6280(50)	3660(13)	37(7)	0.096(3)

O156	3580(13)	(340(50)	2059(14)	41(7)	0.096(3)

O155	3859(16)	510(60)	1242(16)	59(10)	0.096(3)

C31	1355(2)	3631(7)	2958(2)	32(1)	0.904(3)

C32	1692(2)	4086(7)	2531(2)	40(1)	0.904(3)

C33	1489(2)	3692(8)	1933(2)	40(1)	0.904(3)

C34	943(2)	2842(7)	1747(2)	28(1)	0.904(3)

C35	609(2)	2364(7)	2172(2)	30(1)	0.904(3)

C36	814(2)	2752(8)	2778(2)	36(1)	0.904(3)

C37	1530(2)	4153(8)	3599(2)	38(1)	0.904(3)

C38	2234(2)	5625(8)	4332(2)	44(1)	0.904(3)

C39	699(2)	2497(7)	1097(2)	30(1)	0.904(3)

C40	1038(2)	1654(7)	720(2)	28(1)	0.904(3)

C41	800(2)	1476(7)	112(2)	29(1)	0.904(3)

C42	233(2)	2089(10)	(126(2)	31(2)	0.904(3)

C43	(121(2)	2901(12)	246(2)	31(1)	0.904(3)

C44	126(3)	3113(13)	856(3)	34(2)	0.904(3)

C45	(5(3)	1907(10)	(753(2)	36(2)	0.904(3)

C47	(717(2)	3500(9)	4(3)	32(2)	0.904(3)

C49	1648(2)	918(6)	952(2)	29(1)	0.904(3)

C50	1746(2)	(236(7)	1438(2)	39(1)	0.904(3)

C51	2315(2)	(890(7)	1654(2)	37(1)	0.904(3)

C52	2794(2)	(439(7)	1391(2)	37(1)	0.904(3)

C53	2691(2)	642(8)	891(2)	42(1)	0.904(3)

C54	2123(2)	1311(7)	674(2)	39(1)	0.904(3)

C55	3424(2)	(1031(8)	1620(2)	45(1)	0.904(3)

C56	4094(2)	(2326(8)	2419(3)	56(2)	0.904(3)

N46	(202(3)	1771(11)	(1252(2)	51(2)	0.904(3)

N48	(1190(2)	3963(7)	(205(2)	41(1)	0.904(3)

O37A	2054(1)	5024(5)	3718(1)	39(1)	0.904(3)

O37B	1230(2)	3867(6)	3972(1)	58(1)	0.904(3)

O55A	3835(2)	(870(6)	1356(2)	60(1)	0.904(3)

O55B	3489(1)	(1781(5)	2161(1)	47(1)	0.904(3)

C1	6308(2)	126(5)	2922(2)	30(1)	1

C2	6636(2)	527(6)	2485(2)	37(1)	1

C3	6445(2)	(50(6)	1897(2)	35(1)	1

C4	5922(2)	(1054(6)	1742(2)	30(1)	1

C5	5593(2)	(1421(6)	2183(2)	33(1)	1

C6	5777(2)	(856(6)	2763(2)	34(1)	1

C7	6480(2)	739(6)	3553(2)	33(1)	1

C8	7211(2)	2076(6)	4292(2)	44(1)	1

C9	5692(2)	(1685(5)	1116(2)	28(1)	1

C10	6060(2)	(2518(5)	770(2)	30(1)	1

C11	5811(2)	(3023(6)	178(2)	33(1)	1

C12	5207(2)	(2764(6)	(63(2)	32(1)	1

C13	4838(2)	(1979(6)	294(2)	33(1)	1

C14	5081(2)	(1440(6)	873(2)	31(1)	1

C15	4953(2)	(3283(6)	(675(2)	40(1)	1

C17	4208(2)	(1711(6)	50(2)	37(1)	1

C19	6704(2)	(2963(6)	999(2)	31(1)	1

C20	6871(2)	(4028(7)	1501(2)	46(1)	1

C21	7467(2)	(4504(7)	1688(2)	46(1)	1

C22	7910(2)	(3914(6)	1386(2)	34(1)	1

C23	7739(2)	(2869(6)	889(2)	37(1)	1

C24	7145(2)	(2391(6)	696(2)	37(1)	1

C25	8546(2)	(4456(6)	1565(2)	36(1)	1

C26	9295(2)	(5712(7)	2314(2)	49(1)	1

N16	4735(2)	(3664(6)	(1152(2)	55(1)	1

N18	3711(2)	(1508(6)	(154(2)	52(1)	1

O7A	7018(1)	1493(4)	3675(1)	39(1)	1

O7B	6166(1)	543(4)	3924(1)	47(1)	1

O25A	8680(1)	(5105(4)	2124(1)	43(1)	1

O25B	8911(1)	(4363(5)	1241(1)	48(1)	1

Table 3. Bond lengths [Å] and angles [°].

C131(C136	1.24(6)

C131(C132	1.46(6)

C131(C137	1.50(6)

C132(C133	1.43(6)

C132(H132	0.9500

C133(C134	1.37(6)

C133(H133	0.9500

C134(C135	1.39(6)

C134(C139	1.57(5)

C135(C136	1.46(6)

C135(H135	0.9500

C136(H136	0.9500

C137(O138	1.16(6)

C137(O137	1.27(5)

C138(O138	1.48(5)

C138(H13A	0.9800

C138(H13B	0.9800

C138(H13C	0.9800

C139(C140	1.3900

C139(C144	1.3900

C140(C141	1.3900

C140(C149	1.52(3)

C141(C142	1.3900

C141(H141	0.9500

C142(C143	1.3900

C142(C145	1.4301

C143(C144	1.3900

C143(C147	1.4301

C144(H144	0.9500

C145(N146	1.1401(10)

C147(N148	1.1401(10)

C149(C150	1.3900

C149(C154	1.3900

C150(C151	1.3900

C150(H150	0.9500

C151(C152	1.3900

C151(H151	0.9500

C152(C155	1.37(5)

C152(C153	1.3900

C153(C154	1.3900

C153(H153	0.9500

C154(H154	0.9500

C155(O155	1.14(5)

C155(O156	1.37(6)

C156(O156	1.52(5)

C156(H15A	0.9800

C156(H15B	0.9800

C156(H15C	0.9800

C31(C36	1.386(7)

C31(C32	1.388(6)

C31(C37	1.489(6)

C32(C33	1.382(6)

C32(H32	0.9500

C33(C34	1.386(7)

C33(H33	0.9500

C34(C35	1.385(6)

C34(C39	1.498(6)

C35(C36	1.399(6)

C35(H35	0.9500

C36(H36	0.9500

C37(O37B	1.204(5)

C37(O37A	1.340(6)

C38(O37A	1.451(5)

C38(H38A	0.9800

C38(H38B	0.9800

C38(H38C	0.9800

C39(C44	1.390(6)

C39(C40	1.410(6)

C40(C41	1.389(5)

C40(C49	1.488(6)

C41(C42	1.376(6)

C41(H41	0.9500

C42(C43	1.415(6)

C42(C45	1.4302(8)

C43(C44	1.401(6)

C43(C47	1.4303(8)

C44(H44	0.9500

C45(N46	1.1400(8)

C47(N48	1.1402(8)

C49(C54	1.382(6)

C49(C50	1.395(6)

C50(C51	1.379(6)

C50(H50	0.9500

C51(C52	1.379(6)

C51(H51	0.9500

C52(C53	1.385(7)

C52(C55	1.492(6)

C53(C54	1.383(6)

C53(H53	0.9500

C54(H54	0.9500

C55(O55A	1.206(6)

C55(O55B	1.336(6)

C56(O55B	1.444(5)

C56(H56A	0.9800

C56(H56B	0.9800

C56(H56C	0.9800

C1(C2	1.385(5)

C1(C6	1.402(5)

C1(C7	1.486(5)

C2(C3	1.394(5)

C2(H2	0.9500

C3(C4	1.395(5)

C3(H3	0.9500

C4(C5	1.389(5)

C4(C9	1.496(5)

C5(C6	1.372(5)

C5(H5	0.9500

C6(H6	0.9500

C7(O7B	1.212(4)

C7(O7A	1.328(5)

C8(O7A	1.454(4)

C8(H8A	0.9800

C8(H8B	0.9800

C8(H8C	0.9800

C9(C14	1.400(5)

C9(C10	1.403(5)

C10(C11	1.409(5)

C10(C19	1.489(5)

C11(C12	1.385(5)

C11(H11	0.9500

C12(C13	1.405(6)

C12(C15	1.453(5)

C13(C14	1.387(5)

C13(C17	1.442(6)

C14(H14	0.9500

C15(N16	1.138(5)

C17(N18	1.141(5)

C19(C24	1.387(5)

C19(C20	1.391(5)

C20(C21	1.385(6)

C20(H20	0.9500

C21(C22	1.394(5)

C21(H21	0.9500

C22(C23	1.373(5)

C22(C25	1.478(5)

C23(C24	1.382(5)

C23(H23	0.9500

C24(H24	0.9500

C25(O25B	1.210(5)

C25(O25A	1.341(5)

C26(O25A	1.452(5)

C26(H26A	0.9800

C26(H26B	0.9800

C26(H26C	0.9800

C136(C131(C132	120(4)

C136(C131(C137	121(4)

C132(C131(C137	119(4)

C133(C132(C131	121(4)

C133(C132(H132	119.7

C131(C132(H132	119.7

C134(C133(C132	118(4)

C134(C133(H133	120.8

C132(C133(H133	120.8

C133(C134(C135	117(4)

C133(C134(C139	122(4)

C135(C134(C139	120(4)

C134(C135(C136	123(4)

C134(C135(H135	118.6

C136(C135(H135	118.6

C131(C136(C135	120(4)

C131(C136(H136	120.1

C135(C136(H136	120.1

O138(C137(O137	126(5)

O138(C137(C131	116(4)

O137(C137(C131	118(4)

O138(C138(H13A	109.5

O138(C138(H13B	109.5

H13A(C138(H13B	109.5

O138(C138(H13C	109.5

H13A(C138(H13C	109.5

H13B(C138(H13C	109.5

C140(C139(C144	120.0

C140(C139(C134	129(3)

C144(C139(C134	110(3)

C139(C140(C141	120.0

C139(C140(C149	113(3)

C141(C140(C149	125(3)

C140(C141(C142	120.0

C140(C141(H141	120.0

C142(C141(H141	120.0

C143(C142(C141	120.0

C143(C142(C145	124(4)

C141(C142(C145	116(4)

C144(C143(C142	120.0

C144(C143(C147	130(3)

C142(C143(C147	109(3)

C143(C144(C139	120.0

C143(C144(H144	120.0

C139(C144(H144	120.0

N146(C145(C142	179(5)

N148(C147(C143	178(4)

C150(C149(C154	120.0

C150(C149(C140	125(2)

C154(C149(C140	114(2)

C151(C150(C149	120.0

C151(C150(H150	120.0

C149(C150(H150	120.0

C150(C151(C152	120.0

C150(C151(H151	120.0

C152(C151(H151	120.0

C155(C152(C151	128(3)

C155(C152(C153	112(3)

C151(C152(C153	120.0

C154(C153(C152	120.0

C154(C153(H153	120.0

C152(C153(H153	120.0

C153(C154(C149	120.0

C153(C154(H154	120.0

C149(C154(H154	120.0

O155(C155(C152	133(5)

O155(C155(O156	120(4)

C152(C155(O156	107(4)

O156(C156(H15A	109.5

O156(C156(H15B	109.5

H15A(C156(H15B	109.5

O156(C156(H15C	109.5

H15A(C156(H15C	109.5

H15B(C156(H15C	109.5

C137(O138(C138	119(4)

C155(O156(C156	112(3)

C36(C31(C32	119.2(4)

C36(C31(C37	118.1(4)

C32(C31(C37	122.6(4)

C33(C32(C31	120.7(4)

C33(C32(H32	119.7

C31(C32(H32	119.7

C32(C33(C34	120.6(4)

C32(C33(H33	119.7

C34(C33(H33	119.7

C35(C34(C33	119.0(4)

C35(C34(C39	119.7(4)

C33(C34(C39	121.3(4)

C34(C35(C36	120.7(4)

C34(C35(H35	119.7

C36(C35(H35	119.7

C31(C36(C35	119.9(4)

C31(C36(H36	120.1

C35(C36(H36	120.1

O37B(C37(O37A	123.1(4)

O37B(C37(C31	124.1(4)

O37A(C37(C31	112.8(4)

C44(C39(C40	119.4(4)

C44(C39(C34	117.9(4)

C40(C39(C34	122.6(4)

C41(C40(C39	119.7(4)

C41(C40(C49	118.1(4)

C39(C40(C49	122.1(4)

C42(C41(C40	120.9(4)

C42(C41(H41	119.6

C40(C41(H41	119.6

C41(C42(C43	120.4(3)

C41(C42(C45	120.3(5)

C43(C42(C45	119.3(5)

C44(C43(C42	118.5(3)

C44(C43(C47	120.7(5)

C42(C43(C47	120.8(4)

C39(C44(C43	121.1(4)

C39(C44(H44	119.5

C43(C44(H44	119.5

N46(C45(C42	179.0(7)

N48(C47(C43	178.0(6)

C54(C49(C50	118.5(4)

C54(C49(C40	120.6(4)

C50(C49(C40	120.9(4)

C51(C50(C49	120.3(4)

C51(C50(H50	119.9

C49(C50(H50	119.9

C52(C51(C50	121.0(4)

C52(C51(H51	119.5

C50(C51(H51	119.5

C51(C52(C53	118.8(4)

C51(C52(C55	123.6(5)

C53(C52(C55	117.6(4)

C54(C53(C52	120.5(4)

C54(C53(H53	119.7

C52(C53(H53	119.7

C49(C54(C53	120.8(4)

C49(C54(H54	119.6

C53(C54(H54	119.6

O55A(C55(O55B	122.9(4)

O55A(C55(C52	125.0(5)

O55B(C55(C52	112.2(4)

C37(O37A(C38	115.0(3)

C55(O55B(C56	115.0(4)

C2(C1(C6	118.9(3)

C2(C1(C7	123.2(4)

C6(C1(C7	117.9(3)

C1(C2(C3	120.6(4)

C1(C2(H2	119.7

C3(C2(H2	119.7

C2(C3(C4	120.4(3)

C2(C3(H3	119.8

C4(C3(H3	119.8

C5(C4(C3	118.3(3)

C5(C4(C9	119.0(3)

C3(C4(C9	122.6(3)

C6(C5(C4	121.7(4)

C6(C5(H5	119.2

C4(C5(H5	119.2

C5(C6(C1	120.1(4)

C5(C6(H6	120.0

C1(C6(H6	120.0

O7B(C7(O7A	123.1(3)

O7B(C7(C1	123.6(4)

O7A(C7(C1	113.3(3)

O7A(C8(H8A	109.5

O7A(C8(H8B	109.5

H8A(C8(H8B	109.5

O7A(C8(H8C	109.5

H8A(C8(H8C	109.5

H8B(C8(H8C	109.5

C14(C9(C10	119.2(3)

C14(C9(C4	118.1(3)

C10(C9(C4	122.7(3)

C9(C10(C11	119.0(3)

C9(C10(C19	123.7(3)

C11(C10(C19	117.2(3)

C12(C11(C10	121.5(4)

C12(C11(H11	119.2

C10(C11(H11	119.2

C11(C12(C13	118.9(3)

C11(C12(C15	121.3(4)

C13(C12(C15	119.8(3)

C14(C13(C12	120.1(3)

C14(C13(C17	120.3(4)

C12(C13(C17	119.6(3)

C13(C14(C9	121.1(4)

C13(C14(H14	119.4

C9(C14(H14	119.4

N16(C15(C12	177.7(5)

N18(C17(C13	178.6(4)

C24(C19(C20	118.8(3)

C24(C19(C10	120.4(3)

C20(C19(C10	120.8(3)

C21(C20(C19	119.9(4)

C21(C20(H20	120.0

C19(C20(H20	120.0

C20(C21(C22	121.1(4)

C20(C21(H21	119.4

C22(C21(H21	119.4

C23(C22(C21	118.4(4)

C23(C22(C25	119.5(4)

C21(C22(C25	122.0(4)

C22(C23(C24	121.0(4)

C22(C23(H23	119.5

C24(C23(H23	119.5

C23(C24(C19	120.8(4)

C23(C24(H24	119.6

C19(C24(H24	119.6

O25B(C25(O25A	122.9(4)

O25B(C25(C22	124.0(4)

O25A(C25(C22	113.1(3)

O25A(C26(H26A	109.5

O25A(C26(H26B	109.5

H26A(C26(H26B	109.5

O25A(C26(H26C	109.5

H26A(C26(H26C	109.5

H26B(C26(H26C	109.5

C7(O7A(C8	115.2(3)

C25(O25A(C26	115.2(3)

Symmetry transformations used to generate equivalent atoms:

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C31	25(2) 	44(3)	26(2) 	(2(2)	5(2) 	4(2)

C32	28(3) 	58(4)	34(2) 	(8(2)	9(2) 	(2(2)

C33	37(3) 	58(4)	28(2) 	(2(3)	16(2) 	(6(3)

C34	29(2) 	30(3)	26(2) 	1(2)	7(2) 	8(2)

C35	27(2) 	35(3)	27(2) 	4(2)	3(2) 	3(2)

C36	30(3) 	55(4)	23(2) 	4(2)	9(2) 	3(2)

C37	29(3) 	60(4)	26(2) 	3(2)	4(2) 	3(2)

C38	44(3) 	61(4)	25(2) 	3(2)	(1(2) 	(2(3)

C39	31(3) 	33(4)	28(2) 	(1(2)	9(2) 	0(2)

C40	33(2) 	30(3)	23(2) 	4(2)	11(2) 	0(2)

C41	38(3) 	24(3)	25(2) 	5(2)	11(2) 	5(2)

C42	40(3) 	35(4)	20(2) 	3(2)	10(2) 	4(2)

C43	36(3) 	32(3)	27(3) 	5(2)	9(2) 	6(2)

C44	37(3) 	42(4)	25(2) 	(1(2)	10(2) 	6(2)

C45	31(3) 	50(4)	28(2) 	0(2)	11(2) 	1(2)

C47	37(3) 	36(4)	25(3) 	3(2)	7(2) 	(1(2)

C49	33(2) 	31(3)	23(2) 	(8(2)	6(2) 	2(2)

C50	30(3) 	50(4)	40(3) 	7(2)	14(2) 	1(2)

C51	31(3) 	45(3)	35(2) 	5(2)	8(2) 	4(2)

C52	32(2) 	52(3)	26(2) 	(13(2)	5(2) 	4(2)

C53	34(3) 	66(4)	29(2) 	(5(2)	12(2) 	(7(2)

C54	40(3) 	56(4)	22(2) 	(1(2)	9(2) 	(2(2)

C55	31(3) 	64(4)	38(3) 	(26(3)	3(2) 	8(2)

C56	33(3) 	53(4)	75(4) 	(14(3)	(6(3) 	9(3)

N46	47(4) 	73(5)	34(3) 	(6(3)	12(2) 	(7(3)

N48	40(3) 	45(4)	40(2) 	5(3)	8(2) 	(1(2)

O37A	37(2) 	53(3)	26(2) 	(3(2)	5(1) 	1(2)

O37B	52(2) 	100(4)	22(2) 	(2(2)	10(2) 	(21(2)

O55A	33(2) 	93(4)	54(2) 	(23(2)	12(2) 	7(2)

O55B	36(2) 	58(3)	43(2) 	(12(2)	(1(1) 	10(2)

C1	25(2) 	39(3)	26(2) 	0(2)	4(2) 	7(2)

C2	27(2) 	50(3)	33(2) 	(5(2)	7(2) 	(4(2)

C3	26(2) 	53(3)	28(2) 	(7(2)	12(2) 	(2(2)

C4	22(2) 	44(3)	23(2) 	(1(2)	6(2) 	5(2)

C5	30(2) 	39(3)	32(2) 	(2(2)	9(2) 	(3(2)

C6	35(2) 	44(3)	25(2) 	0(2)	12(2) 	0(2)

C7	34(2) 	40(3)	25(2) 	2(2)	5(2) 	5(2)

C8	51(3) 	53(3)	25(2) 	(8(2)	0(2) 	(4(2)

C9	29(2) 	37(3)	21(2) 	4(2)	7(2) 	(3(2)

C10	30(2) 	38(3)	22(2) 	6(2)	5(2) 	0(2)

C11	34(2) 	40(3)	27(2) 	4(2)	10(2) 	(3(2)

C12	28(2) 	42(3)	26(2) 	8(2)	3(2) 	(6(2)

C13	23(2) 	45(3)	30(2) 	11(2)	3(2) 	(5(2)

C14	26(2) 	42(3)	24(2) 	5(2)	7(2) 	0(2)

C15	28(2) 	59(3)	32(2) 	5(2)	3(2) 	(9(2)

C17	34(3) 	52(3)	26(2) 	7(2)	7(2) 	(6(2)

C19	25(2) 	44(3)	22(2) 	(6(2)	3(2) 	5(2)

C20	37(3) 	70(4)	37(2) 	19(2)	21(2) 	15(2)

C21	43(3) 	62(3)	36(2) 	18(2)	14(2) 	18(2)

C22	28(2) 	46(3)	29(2) 	(3(2)	9(2) 	6(2)

C23	27(2) 	59(3)	25(2) 	3(2)	6(2) 	(7(2)

C24	32(2) 	54(3)	22(2) 	4(2)	1(2) 	(7(2)

C25	38(3) 	41(3)	28(2) 	(6(2)	4(2) 	4(2)

C26	31(3) 	58(3)	54(3) 	3(3)	(2(2) 	15(2)

N16	49(2) 	78(3)	37(2) 	(11(2)	4(2) 	(16(2)

N18	37(2) 	73(3)	43(2) 	7(2)	(1(2) 	(1(2)

O7A	32(2) 	53(2)	30(1) 	(6(1)	2(1) 	(4(1)

O7B	50(2) 	63(2)	31(2) 	(8(2)	15(1) 	(10(2)

O25A	37(2) 	58(2)	35(2) 	5(2)	7(1) 	12(1)

O25B	31(2) 	76(3)	38(2) 	(9(2)	10(1) 	3(2)