|  | University of Southampton · Department of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	01SRC401

Empirical formula 	C21H16O9

Formula weight 	412.34

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Orthorhombic

Space group 	Pbca

Unit cell dimensions	a = 7.41810(10) Å

b = 16.6837(3) Å

c = 27.9934(5) Å

Volume	3464.50(10) Å3

Z	8

Density (calculated)	1.581 Mg / m3

Absorption coefficient	0.126 mm(1

F(000)	1712

Crystal	Colourless plate

Crystal size	0.10 ( 0.10 ( 0.02 mm3

( range for data collection	2.91 ( 25.03°

Index ranges	(8 ( h ( 8, (19 ( k ( 19, (25 ( l ( 33

Reflections collected	15941

Independent reflections	3054 [Rint = 0.1471]

Completeness to ( = 25.03°	99.8 %

Max. and min. transmission	0.9975 and 0.9875

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	3054 / 0 / 273

Goodness-of-fit on F2	0.921

Final R indices [F2 > 2((F2)]	R1 = 0.0501, wR2 = 0.0858

R indices (all data)	R1 = 0.1285, wR2 = 0.1049

Extinction coefficient	0.0008(3)

Largest diff. peak and hole	0.282 and (0.336 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill Ewald sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing, Acta Cryst. A51 (1995) 33(37; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421(426). Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: Cameron - A Molecular Graphics Package. (D. M. Watkin, L. Pearce and C. K. Prout, Chemical Crystallography Laboratory, University of Oxford, 1993).

Special details:  All hydrogen atoms were placed in idealised positions and refined using a riding model.

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C1	(2313(4)	608(2)	3030(1)	27(1)	1

C2	(1256(4)	1777(2)	3299(1)	19(1)	1

C3	166(4)	1367(2)	3084(1)	18(1)	1

C4	1896(4)	1639(2)	3090(1)	20(1)	1

C5	2161(4)	2381(2)	3322(1)	15(1)	1

C6	745(4)	2783(2)	3533(1)	15(1)	1

C7	(1020(4)	2489(2)	3532(1)	19(1)	1

C8	3923(4)	2838(2)	3371(1)	19(1)	1

C9	3263(4)	3673(2)	3539(1)	17(1)	1

C10	1317(4)	3572(2)	3755(1)	16(1)	1

C11	1303(4)	3526(2)	4300(1)	15(1)	1

C12	(64(4)	3923(2)	4553(1)	18(1)	1

C13	(51(4)	3850(2)	5042(1)	18(1)	1

C14	1234(4)	3410(2)	5280(1)	18(1)	1

C15	2561(4)	3007(2)	5044(1)	24(1)	1

C16	2578(4)	3075(2)	4546(1)	22(1)	1

C17	(546(5)	3998(2)	5822(1)	30(1)	1

C18	4861(4)	3018(2)	2901(1)	19(1)	1

C19	3937(4)	3757(2)	2729(1)	19(1)	1

C20	4622(5)	4130(2)	3847(1)	21(1)	1

C21	5205(4)	5317(2)	4271(1)	31(1)	1

O1	(2856(3)	1378(1)	3214(1)	25(1)	1

O2	(495(3)	690(1)	2858(1)	25(1)	1

O3	172(3)	4211(1)	3621(1)	19(1)	1

O4	(1274(3)	4163(1)	5360(1)	28(1)	1

O5	888(3)	3424(1)	5767(1)	26(1)	1

O6	3076(3)	4128(1)	3095(1)	20(1)	1

O7	6049(3)	3861(1)	3967(1)	35(1)	1

O8	4016(3)	4857(1)	3964(1)	26(1)	1

O9	3886(3)	4040(1)	2334(1)	25(1)	1

Table 3. Bond lengths [Å] and angles [°].

C1(O2	1.439(3)

C1(O1	1.441(3)

C2(C7	1.366(4)

C2(O1	1.382(3)

C2(C3	1.394(4)

C3(C4	1.362(4)

C3(O2	1.385(3)

C4(C5	1.410(4)

C5(C6	1.379(4)

C5(C8	1.520(4)

C6(C7	1.398(4)

C6(C10	1.516(4)

C8(C18	1.520(4)

C8(C9	1.549(4)

C9(O6	1.462(3)

C9(C20	1.529(4)

C9(C10	1.574(4)

C10(O3	1.414(3)

C10(C11	1.526(4)

C11(C16	1.391(4)

C11(C12	1.403(4)

C12(C13	1.374(4)

C13(O4	1.375(3)

C13(C14	1.376(4)

C14(C15	1.362(4)

C14(O5	1.386(3)

C15(C16	1.401(3)

C17(O4	1.429(3)

C17(O5	1.439(3)

C18(C19	1.490(4)

C19(O9	1.203(3)

C19(O6	1.357(3)

C20(O7	1.198(3)

C20(O8	1.335(3)

C21(O8	1.452(3)

O2(C1(O1	107.3(2)

C7(C2(O1	127.7(3)

C7(C2(C3	122.4(3)

O1(C2(C3	109.8(3)

C4(C3(O2	127.7(3)

C4(C3(C2	123.0(3)

O2(C3(C2	109.3(3)

C3(C4(C5	115.4(3)

C6(C5(C4	121.2(3)

C6(C5(C8	111.8(2)

C4(C5(C8	127.0(3)

C5(C6(C7	122.8(3)

C5(C6(C10	112.7(3)

C7(C6(C10	124.6(3)

C2(C7(C6	115.2(3)

C18(C8(C5	114.4(2)

C18(C8(C9	103.3(2)

C5(C8(C9	102.0(2)

O6(C9(C20	106.4(2)

O6(C9(C8	103.78(19)

C20(C9(C8	114.2(3)

O6(C9(C10	107.2(2)

C20(C9(C10	116.3(2)

C8(C9(C10	108.0(2)

O3(C10(C6	112.1(2)

O3(C10(C11	107.4(2)

C6(C10(C11	111.4(2)

O3(C10(C9	111.6(2)

C6(C10(C9	101.1(2)

C11(C10(C9	113.3(2)

C16(C11(C12	119.8(2)

C16(C11(C10	121.1(3)

C12(C11(C10	119.1(3)

C13(C12(C11	117.1(3)

C12(C13(O4	127.3(3)

C12(C13(C14	122.4(3)

O4(C13(C14	110.3(2)

C15(C14(C13	121.9(3)

C15(C14(O5	128.2(3)

C13(C14(O5	109.8(3)

C14(C15(C16	116.7(3)

C11(C16(C15	122.1(3)

O4(C17(O5	108.1(2)

C19(C18(C8	103.4(2)

O9(C19(O6	120.1(3)

O9(C19(C18	129.4(3)

O6(C19(C18	110.5(2)

O7(C20(O8	124.6(3)

O7(C20(C9	123.7(3)

O8(C20(C9	111.7(3)

C2(O1(C1	104.6(2)

C3(O2(C1	104.8(2)

C13(O4(C17	105.3(2)

C14(O5(C17	104.7(2)

C19(O6(C9	111.2(2)

C20(O8(C21	114.9(2)

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C1	30(2) 	23(2)	28(2) 	0(2)	(3(2) 	(4(2)

C2	16(2) 	20(2)	21(2) 	5(2)	(5(2) 	(7(2)

C3	21(2) 	14(2)	19(2) 	(2(1)	0(2) 	(2(2)

C4	22(2) 	18(2)	19(2) 	(3(1)	2(1) 	4(2)

C5	15(2) 	15(2)	16(2) 	2(1)	(3(1) 	2(2)

C6	17(2) 	15(2)	13(2) 	2(1)	(2(1) 	1(2)

C7	17(2) 	21(2)	17(2) 	(2(1)	2(2) 	1(2)

C8	19(2) 	20(2)	17(2) 	(1(1)	1(1) 	5(2)

C9	21(2) 	20(2)	12(2) 	2(1)	(2(1) 	0(2)

C10	14(2) 	16(2)	19(2) 	2(1)	(1(1) 	2(2)

C11	12(2) 	16(2)	16(2) 	(1(1)	2(1) 	(2(2)

C12	21(2) 	14(2)	20(2) 	1(1)	(3(2) 	0(2)

C13	13(2) 	18(2)	22(2) 	(5(1)	6(2) 	(1(2)

C14	19(2) 	21(2)	15(2) 	(2(1)	2(1) 	(3(2)

C15	29(2) 	27(2)	18(2) 	4(2)	(4(2) 	6(2)

C16	20(2) 	24(2)	21(2) 	(6(2)	2(2) 	3(2)

C17	41(2) 	25(2)	23(2) 	2(2)	7(2) 	9(2)

C18	14(2) 	21(2)	22(2) 	(1(1)	3(1) 	3(2)

C19	16(2) 	20(2)	20(2) 	(2(2)	2(2) 	(9(2)

C20	19(2) 	28(2)	15(2) 	(1(2)	5(1) 	(1(2)

C21	24(2) 	31(2)	36(2) 	(14(2)	(3(2) 	(6(2)

O1	26(2) 	19(1)	32(1) 	(6(1)	1(1) 	(2(1)

O2	26(2) 	20(1)	31(1) 	(9(1)	0(1) 	(3(1)

O3	22(1) 	21(1)	15(1) 	0(1)	(1(1) 	5(1)

O4	30(2) 	36(1)	19(1) 	(1(1)	4(1) 	10(1)

O5	32(2) 	29(1)	17(1) 	1(1)	2(1) 	3(1)

O6	22(1) 	20(1)	19(1) 	2(1)	2(1) 	1(1)

O7	22(2) 	35(2)	48(2) 	(16(1)	(13(1) 	5(1)

O8	24(1) 	21(1)	33(1) 	(11(1)	(1(1) 	(2(1)

O9	35(2) 	23(1)	18(1) 	4(1)	5(1) 	2(1)

Table 5. Hydrogen coordinates [( 104] and isotropic displacement parameters [Å2 ( 103].

Atom 	x	y	z	Ueq	S.o.f.

H1A	(2368	198	3286	32	1

H1B	(3123	441	2767	32	1

H4	2860	1350	2948	24	1

H7	(1986	2764	3683	22	1

H8	4753	2583	3608	22	1

H12	(961	4229	4393	22	1

H15	3433	2696	5210	29	1

H16	3488	2803	4370	26	1

H17A	(1495	3778	6033	36	1

H17B	(77	4497	5968	36	1

H18A	6165	3114	2949	23	1

H18B	4703	2571	2671	23	1

H21A	4657	5839	4339	46	1

H21B	6365	5397	4110	46	1

H21C	5397	5026	4571	46	1

H3	(45	4182	3327	29	1

Table 6. Hydrogen bonds [Å and °].

D(H···A	d(D(H)	d(H···A)	d(D···A)	((DHA)

O3(H3...O9i	0.84	2.03	2.852(3)	167.4

Symmetry transformations used to generate equivalent atoms:

(i) x(1/2,y,(z+1/2