|  | Single Crystal X-Ray Diffraction Service National Crystallography Service Contact: Dr S.K.Callear, S.K.Callear@soton.ac.uk |
| --- | --- |

Table 1. Crystal data and structure refinement details.

Identification code 	2009src0344  (SM 119Cl)

Empirical formula 	C9H9Cl3F3NOSi

Formula weight 	338.61

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P21/c

Unit cell dimensions	a = 9.0871(3) Å	( = 90°

b = 7.3467(2) Å	( = 101.7870(10)°

c = 21.0204(6) Å	(  = 90°

Volume	1373.73(7) Å3

Z	4

Density (calculated)	1.637 Mg / m3

Absorption coefficient	0.774 mm(1

F(000)	680

Crystal	plate; colourless

Crystal size	0.37 ( 0.27 ( 0.08 mm3

( range for data collection	2.94 ( 27.48°

Index ranges	(11 ( h ( 11, (9 ( k ( 9, (27 ( l ( 27

Reflections collected	19825

Independent reflections	3152 [Rint = 0.0476]

Completeness to ( = 27.48°	99.8 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.9406 and 0.7626

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	3152 / 1 / 202

Goodness-of-fit on F2	1.070

Final R indices [F2 > 2((F2)]	R1 = 0.0947, wR2 = 0.2496

R indices (all data)	R1 = 0.1116, wR2 = 0.2635

Largest diff. peak and hole	1.677 and (0.906 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: Sheldrick, G. M. SADABS - Bruker Nonius area detector scaling and absorption correction - V2.10 Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: ORTEP-3 (L.G. Farrugia, J. Appl. Cryst. (1997) 30, 565).

Special details:

All hydrogens fixed using a standard riding model.

Two parts of the molecule are disordered: The fluorines on the CF3 group are rotating therefore the fluorine atoms have been left isotropic with only two positions modelled for each fluorine atom. The silicon group is also disordered with an 180deg rotation where the methylene chloride and methyl groups swop over. The position of the silicon group is also slightly offset. The occupancies of each disorder assembly were refined.

To ensure the disorder was not a product of a too high symmetry space group being selected, the structure was solved in P1 which also showed the same disorder. Due to the higher R1 and wR values relative to the Rint, merohedral twinning was tested for using ROTAX, however none of the suggested matricies lowered the R values. Instead it is assumed that the higher R values are a result of the disorder.

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C21	3507(7)	3065(11)	431(3)	43(2)	0.806(6)

C22	5093(11)	5988(10)	1451(5)	49(2)	0.806(6)

Si1	4751(2)	3548(3)	1251(1)	26(1)	0.806(6)

Cl1	2882(5)	3208(5)	1792(2)	42(1)	0.806(6)

Cl2	3409(3)	629(4)	324(1)	84(1)	0.806(6)

F8A	10159(13)	(2659(16)	2348(6)	95(4)	0.527(12)

F8B	10053(11)	(3610(12)	1342(4)	71(3)	0.527(12)

F8C	11738(12)	(1867(14)	1794(6)	91(4)	0.527(12)

C21B	4450(30)	5480(40)	1069(14)	42(6)	0.194(6)

C22B	3330(30)	2010(50)	302(13)	49(2)	0.194(6)

Si1B	4415(10)	2980(14)	1023(5)	30(2)	0.194(6)

Cl1B	2668(18)	2700(20)	1636(8)	45(3)	0.194(6)

Cl2B	5849(14)	6164(13)	1762(5)	66(3)	0.194(6)

F8D	9536(13)	(3531(16)	2075(5)	81(3)	0.473(12)

F8E	10949(18)	(3025(19)	1358(7)	104(4)	0.473(12)

F8F	11362(15)	(1787(17)	2243(7)	99(4)	0.473(12)

C2	8050(6)	(276(7)	1745(2)	36(1)	1

C3	9310(6)	(635(8)	1516(2)	43(1)	1

C4	9679(6)	462(8)	1019(2)	39(1)	1

C5	8750(5)	1838(6)	773(2)	33(1)	1

C6	7420(5)	2208(6)	1007(2)	29(1)	1

C7	5753(5)	1566(7)	1727(2)	34(1)	1

C8	10275(9)	(2243(13)	1773(3)	71(2)	1

N1	7134(4)	1115(5)	1497(2)	29(1)	1

O6	6480(4)	3455(5)	809(2)	40(1)	1

Cl5	9083(2)	3160(2)	145(1)	49(1)	1

Table 3. Bond lengths [Å] and angles [°].

C21(Cl2	1.803(9)

C21(Si1	1.892(7)

C21(H21A	0.9900

C21(H21B	0.9900

C22(Si1	1.853(9)

C22(H22A	0.9800

C22(H22B	0.9800

C22(H22C	0.9800

Si1(C7	1.891(5)

Si1(O6	1.983(4)

Si1(Cl1	2.243(4)

F8A(C8	1.271(12)

F8B(C8	1.339(12)

F8C(C8	1.349(14)

C21B(Cl2B	1.80(3)

C21B(Si1B	1.84(3)

C21B(H21C	0.9900

C21B(H21D	0.9900

C22B(Si1B	1.780(18)

C22B(H22D	0.9800

C22B(H22E	0.9800

C22B(H22F	0.9800

Si1B(C7	2.003(10)

Si1B(O6	2.047(8)

Si1B(Cl1B	2.250(17)

F8D(C8	1.387(14)

F8E(C8	1.299(15)

F8F(C8	1.290(14)

C2(N1	1.354(6)

C2(C3	1.355(7)

C2(H2	0.9500

C3(C4	1.412(8)

C3(C8	1.504(9)

C4(C5	1.350(7)

C4(H4	0.9500

C5(C6	1.421(7)

C5(Cl5	1.714(5)

C6(O6	1.264(6)

C6(N1	1.372(6)

C7(N1	1.472(6)

C7(H7A	0.9900

C7(H7B	0.9900

Cl2(C21(Si1	107.8(3)

Cl2(C21(H21A	110.2

Si1(C21(H21A	110.2

Cl2(C21(H21B	110.2

Si1(C21(H21B	110.2

H21A(C21(H21B	108.5

C22(Si1(C7	125.8(5)

C22(Si1(C21	115.4(5)

C7(Si1(C21	118.1(3)

C22(Si1(O6	91.6(3)

C7(Si1(O6	83.06(19)

C21(Si1(O6	87.1(3)

C22(Si1(Cl1	95.8(3)

C7(Si1(Cl1	88.81(19)

C21(Si1(Cl1	93.9(2)

O6(Si1(Cl1	171.24(18)

Cl2B(C21B(Si1B	108.9(16)

Cl2B(C21B(H21C	109.9

Si1B(C21B(H21C	109.9

Cl2B(C21B(H21D	109.9

Si1B(C21B(H21D	109.9

H21C(C21B(H21D	108.3

Si1B(C22B(H22D	109.5

Si1B(C22B(H22E	109.5

H22D(C22B(H22E	109.5

Si1B(C22B(H22F	109.5

H22D(C22B(H22F	109.5

H22E(C22B(H22F	109.5

C22B(Si1B(C21B	116.6(16)

C22B(Si1B(C7	124.6(13)

C21B(Si1B(C7	118.5(11)

C22B(Si1B(O6	104.8(12)

C21B(Si1B(O6	80.5(10)

C7(Si1B(O6	78.7(3)

C22B(Si1B(Cl1B	96.8(12)

C21B(Si1B(Cl1B	93.9(11)

C7(Si1B(Cl1B	85.5(6)

O6(Si1B(Cl1B	158.0(7)

N1(C2(C3	120.5(5)

N1(C2(H2	119.7

C3(C2(H2	119.7

C2(C3(C4	119.8(5)

C2(C3(C8	119.8(5)

C4(C3(C8	120.4(5)

C5(C4(C3	119.2(5)

C5(C4(H4	120.4

C3(C4(H4	120.4

C4(C5(C6	121.3(5)

C4(C5(Cl5	121.7(4)

C6(C5(Cl5	117.0(4)

O6(C6(N1	116.8(4)

O6(C6(C5	126.2(4)

N1(C6(C5	116.9(4)

N1(C7(Si1	110.5(3)

N1(C7(Si1B	107.7(4)

Si1(C7(Si1B	19.3(3)

N1(C7(H7A	109.5

Si1(C7(H7A	109.5

Si1B(C7(H7A	126.6

N1(C7(H7B	109.5

Si1(C7(H7B	109.5

Si1B(C7(H7B	93.6

H7A(C7(H7B	108.1

F8A(C8(F8F	62.3(8)

F8A(C8(F8E	132.4(10)

F8F(C8(F8E	103.7(10)

F8A(C8(F8B	115.6(10)

F8F(C8(F8B	134.3(9)

F8E(C8(F8B	40.6(7)

F8A(C8(F8C	106.9(9)

F8F(C8(F8C	47.7(7)

F8E(C8(F8C	61.0(8)

F8B(C8(F8C	100.8(8)

F8A(C8(F8D	42.2(6)

F8F(C8(F8D	101.2(9)

F8E(C8(F8D	110.1(11)

F8B(C8(F8D	77.1(8)

F8C(C8(F8D	133.7(8)

F8A(C8(C3	112.0(8)

F8F(C8(C3	111.7(9)

F8E(C8(C3	115.2(8)

F8B(C8(C3	110.4(6)

F8C(C8(C3	110.4(8)

F8D(C8(C3	113.5(7)

C2(N1(C6	122.3(4)

C2(N1(C7	122.8(4)

C6(N1(C7	114.8(4)

C6(O6(Si1	114.7(3)

C6(O6(Si1B	113.1(4)

Si1(O6(Si1B	18.8(3)

Symmetry transformations used to generate equivalent atoms:

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C21	26(3) 	67(5)	33(3) 	14(3)	2(2) 	(5(3)

C22	46(4) 	35(4)	72(6) 	(8(4)	26(4) 	0(3)

Si1	20(1) 	30(1)	29(1) 	(1(1)	6(1) 	(1(1)

Cl1	34(1) 	51(2)	48(2) 	(6(1)	21(1) 	0(1)

Cl2	64(1) 	103(2)	75(2) 	(61(2)	(6(1) 	0(1)

C21B	39(14) 	44(16)	40(14) 	(5(13)	4(12) 	0(12)

C22B	46(4) 	35(4)	72(6) 	(8(4)	26(4) 	0(3)

Si1B	18(4) 	38(5)	35(5) 	0(4)	6(3) 	(2(3)

Cl1B	28(5) 	61(9)	51(8) 	(6(5)	24(5) 	(8(5)

Cl2B	71(7) 	47(5)	75(7) 	(13(4)	3(5) 	(13(4)

C2	39(3) 	36(3)	30(2) 	2(2)	2(2) 	9(2)

C3	43(3) 	48(3)	35(2) 	1(2)	3(2) 	17(2)

C4	32(2) 	45(3)	41(3) 	(8(2)	8(2) 	6(2)

C5	31(2) 	33(2)	38(2) 	(1(2)	11(2) 	(2(2)

C6	26(2) 	27(2)	37(2) 	1(2)	9(2) 	0(2)

C7	24(2) 	44(3)	36(2) 	8(2)	9(2) 	4(2)

C8	60(4) 	111(6)	44(3) 	16(4)	13(3) 	38(4)

N1	24(2) 	32(2)	29(2) 	1(2)	6(1) 	2(2)

O6	29(2) 	41(2)	55(2) 	19(2)	19(2) 	9(1)

Cl5	42(1) 	45(1)	67(1) 	12(1)	33(1) 	2(1)