|  | University of Southampton · School of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	2009src0116 / MAB/JT/21

Empirical formula 	C7H14B5NO10

Formula weight 	326.24

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P21/c

Unit cell dimensions	a = 9.3511(2) Å	( = 90°

b = 14.5157(4) Å	( = 90.778(2)°

c = 10.4670(2) Å	(  = 90°

Volume	1420.64(6) Å3

Z	4

Density (calculated)	1.525 Mg / m3

Absorption coefficient	0.131 mm(1

F(000)	672

Crystal	block; colourless

Crystal size	0.16 ( 0.16 ( 0.14 mm3

( range for data collection	3.22 ( 27.48°

Index ranges	(12 ( h ( 11, (18 ( k ( 15, (13 ( l ( 13

Reflections collected	15637

Independent reflections	3244 [Rint = 0.0375]

Completeness to ( = 27.48°	99.8 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.9818 and 0.9793

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	3244 / 0 / 213

Goodness-of-fit on F2	1.074

Final R indices [F2 > 2((F2)]	R1 = 0.0391, wR2 = 0.0874

R indices (all data)	R1 = 0.0457, wR2 = 0.0922

Largest diff. peak and hole	0.254 and (0.240 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing, Acta Cryst. A51 (1995) 33(37; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421(426). Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: ORTEP3 for Windows (L. J. Farrugia, J. Appl. Crystallogr. 1997, 30, 565).

Special details:

All hydrogen atoms were fixed using a standard riding model.

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

B1	2081(2)	1367(1)	8997(1)	13(1)	1

B2	(532(2)	1162(1)	9058(1)	14(1)	1

B3	415(2)	2324(1)	7724(1)	14(1)	1

B4	3829(2)	1969(1)	10588(1)	16(1)	1

B5	4614(2)	894(1)	9008(1)	14(1)	1

O1	804(1)	806(1)	9241(1)	15(1)	1

O2	(735(1)	1973(1)	8395(1)	15(1)	1

O3	1770(1)	2036(1)	7968(1)	15(1)	1

O4	2448(1)	1855(1)	10191(1)	15(1)	1

O5	4945(1)	1562(1)	9922(1)	16(1)	1

O6	3232(1)	755(1)	8617(1)	14(1)	1

O7	(1694(1)	713(1)	9517(1)	16(1)	1

O8	92(1)	2959(1)	6799(1)	17(1)	1

O9	4202(1)	2461(1)	11637(1)	22(1)	1

O10	5634(1)	349(1)	8506(1)	20(1)	1

C1	6403(2)	1312(1)	3320(1)	26(1)	1

C2	7124(2)	729(1)	4326(1)	21(1)	1

C3	6689(2)	(177(1)	4515(2)	26(1)	1

C4	7346(2)	(711(1)	5453(2)	31(1)	1

C5	8447(2)	(348(1)	6189(2)	34(1)	1

C6	8913(2)	540(1)	5983(2)	31(1)	1

C7	8240(2)	1086(1)	5068(1)	26(1)	1

N1	7080(1)	1168(1)	2038(1)	18(1)	1

Table 3. Bond lengths [Å] and angles [°].

B1(O6	1.4550(17)

B1(O1	1.4706(17)

B1(O4	1.4727(17)

B1(O3	1.4761(17)

B2(O7	1.3606(17)

B2(O1	1.3632(17)

B2(O2	1.3781(18)

B3(O3	1.3556(17)

B3(O8	1.3680(18)

B3(O2	1.3897(17)

B4(O9	1.3508(18)

B4(O4	1.3615(17)

B4(O5	1.3944(18)

B5(O10	1.3506(18)

B5(O6	1.3649(17)

B5(O5	1.3938(18)

O7(H7	0.8400

O8(H8	0.8400

O9(H9	0.8400

O10(H10	0.8400

C1(C2	1.504(2)

C1(N1	1.5053(18)

C1(H1D	0.9900

C1(H1E	0.9900

C2(C3	1.391(2)

C2(C7	1.392(2)

C3(C4	1.388(2)

C3(H3	0.9500

C4(C5	1.382(3)

C4(H4	0.9500

C5(C6	1.378(3)

C5(H5	0.9500

C6(C7	1.387(2)

C6(H6	0.9500

C7(H7A	0.9500

N1(H1A	0.9100

N1(H1B	0.9100

N1(H1C	0.9100

O6(B1(O1	108.36(11)

O6(B1(O4	111.15(10)

O1(B1(O4	107.45(10)

O6(B1(O3	109.91(10)

O1(B1(O3	109.78(10)

O4(B1(O3	110.13(11)

O7(B2(O1	120.22(13)

O7(B2(O2	118.81(12)

O1(B2(O2	120.96(12)

O3(B3(O8	122.59(12)

O3(B3(O2	121.29(12)

O8(B3(O2	116.11(12)

O9(B4(O4	123.06(13)

O9(B4(O5	116.32(12)

O4(B4(O5	120.61(12)

O10(B5(O6	117.88(13)

O10(B5(O5	121.51(12)

O6(B5(O5	120.59(12)

B2(O1(B1	120.68(11)

B2(O2(B3	117.75(11)

B3(O3(B1	121.00(11)

B4(O4(B1	121.77(11)

B5(O5(B4	118.50(11)

B5(O6(B1	121.94(11)

B2(O7(H7	109.5

B3(O8(H8	109.5

B4(O9(H9	109.5

B5(O10(H10	109.5

C2(C1(N1	110.87(12)

C2(C1(H1D	109.5

N1(C1(H1D	109.5

C2(C1(H1E	109.5

N1(C1(H1E	109.5

H1D(C1(H1E	108.1

C3(C2(C7	119.39(14)

C3(C2(C1	120.14(14)

C7(C2(C1	120.47(14)

C4(C3(C2	120.04(15)

C4(C3(H3	120.0

C2(C3(H3	120.0

C5(C4(C3	120.05(16)

C5(C4(H4	120.0

C3(C4(H4	120.0

C6(C5(C4	120.29(16)

C6(C5(H5	119.9

C4(C5(H5	119.9

C5(C6(C7	120.02(16)

C5(C6(H6	120.0

C7(C6(H6	120.0

C6(C7(C2	120.16(16)

C6(C7(H7A	119.9

C2(C7(H7A	119.9

C1(N1(H1A	109.5

C1(N1(H1B	109.5

H1A(N1(H1B	109.5

C1(N1(H1C	109.5

H1A(N1(H1C	109.5

H1B(N1(H1C	109.5

Symmetry transformations used to generate equivalent atoms:

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

B1	10(1) 	15(1)	15(1) 	1(1)	(1(1) 	0(1)

B2	13(1) 	16(1)	13(1) 	(2(1)	0(1) 	1(1)

B3	14(1) 	15(1)	13(1) 	(2(1)	0(1) 	0(1)

B4	14(1) 	16(1)	16(1) 	2(1)	0(1) 	0(1)

B5	13(1) 	15(1)	15(1) 	2(1)	0(1) 	(1(1)

O1	10(1) 	16(1)	18(1) 	4(1)	0(1) 	0(1)

O2	12(1) 	16(1)	18(1) 	3(1)	1(1) 	2(1)

O3	12(1) 	17(1)	15(1) 	4(1)	0(1) 	(1(1)

O4	12(1) 	19(1)	15(1) 	(2(1)	0(1) 	2(1)

O5	10(1) 	19(1)	19(1) 	(2(1)	0(1) 	0(1)

O6	11(1) 	16(1)	16(1) 	(1(1)	0(1) 	0(1)

O7	11(1) 	18(1)	20(1) 	5(1)	0(1) 	1(1)

O8	14(1) 	20(1)	18(1) 	5(1)	1(1) 	1(1)

O9	14(1) 	28(1)	22(1) 	(9(1)	(2(1) 	2(1)

O10	11(1) 	24(1)	26(1) 	(7(1)	(1(1) 	1(1)

C1	27(1) 	32(1)	19(1) 	0(1)	4(1) 	10(1)

C2	25(1) 	21(1)	18(1) 	(1(1)	4(1) 	5(1)

C3	28(1) 	26(1)	26(1) 	(5(1)	5(1) 	(2(1)

C4	46(1) 	19(1)	30(1) 	1(1)	10(1) 	1(1)

C5	53(1) 	28(1)	21(1) 	4(1)	2(1) 	13(1)

C6	41(1) 	30(1)	21(1) 	(5(1)	(7(1) 	5(1)

C7	35(1) 	20(1)	21(1) 	(2(1)	0(1) 	0(1)

N1	17(1) 	20(1)	17(1) 	0(1)	(2(1) 	0(1)

Table 5. Hydrogen coordinates [( 104] and isotropic displacement parameters [Å2 ( 103].

Atom 	x	y	z	Ueq	S.o.f.

H7	(1433	217	9863	25	1

H8	828	3076	6377	26	1

H9	3461	2647	12001	32	1

H10	6443	528	8761	30	1

H1D	6477	1970	3563	31	1

H1E	5375	1150	3263	31	1

H3	5941	(430	4002	32	1

H4	7040	(1327	5589	38	1

H5	8884	(711	6840	41	1

H6	9696	778	6467	37	1

H7A	8541	1704	4948	31	1

H1A	7985	1399	2056	27	1

H1B	6555	1464	1425	27	1

H1C	7109	555	1859	27	1

Table 6. Hydrogen bonds [Å and °].

D(H···A	d(D(H)	d(H···A)	d(D···A)	((DHA)

O7(H7...O1i	0.84	1.85	2.6855(14)	174.5

O8(H8...O4ii	0.84	1.97	2.8030(13)	169.1

O9(H9...O3iii	0.84	1.94	2.7812(13)	173.8

O10(H10...O7iv	0.84	1.92	2.7513(13)	168.9

N1(H1A...O8v	0.91	2.20	3.1019(15)	171.0

N1(H1B...O5vi	0.91	2.17	3.0162(15)	154.9

N1(H1B...O9vi	0.91	2.64	3.3024(16)	129.8

N1(H1C...O6vii	0.91	1.99	2.8892(16)	168.8

Symmetry transformations used to generate equivalent atoms:

(i) (x,(y,(z+2    (ii) x,(y+1/2,z(1/2    (iii) x,(y+1/2,z+1/2

(iv)  x+1,y,z    (v) x+1,(y+1/2,z(1/2    (vi) x,y,z(1

(vii) (x+1,(y,(z+1