|  | University of Southampton · School of Chemistry # EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	2009src0116 / MAB/JT/21

Empirical formula 	C7H14B5NO10

Formula weight 	326.24

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P21/c

Unit cell dimensions	a = 9.3511(2) Å	 = 90°

b = 14.5157(4) Å	 = 90.778(2)°

c = 10.4670(2) Å	  = 90°

Volume	1420.64(6) Å3

Z	4

Density (calculated)	1.525 Mg / m3

Absorption coefficient	0.131 mm1

F(000)	672

Crystal	block; colourless

Crystal size	0.16  0.16  0.14 mm3

 range for data collection	3.22  27.48°

Index ranges	12  h  11, 18  k  15, 13  l  13

Reflections collected	15637

Independent reflections	3244 [Rint = 0.0375]

Completeness to  = 27.48°	99.8 %

Absorption correction	Semiempirical from equivalents

Max. and min. transmission	0.9818 and 0.9793

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	3244 / 0 / 213

Goodness-of-fit on F2	1.074

Final R indices [F2 > 2(F2)]	R1 = 0.0391, wR2 = 0.0874

R indices (all data)	R1 = 0.0457, wR2 = 0.0922

Largest diff. peak and hole	0.254 and 0.240 e Å3

Diffractometer: Nonius KappaCCD area detector ( scans and  scans to fill asymmetric unit sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing, Acta Cryst. A51 (1995) 3337; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421426). Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: ORTEP3 for Windows (L. J. Farrugia, J. Appl. Crystallogr. 1997, 30, 565).

Special details:

All hydrogen atoms were fixed using a standard riding model.

Table 2. Atomic coordinates [ 104], equivalent isotropic displacement parameters [Å2  103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

B1	2081(2)	1367(1)	8997(1)	13(1)	1

B2	532(2)	1162(1)	9058(1)	14(1)	1

B3	415(2)	2324(1)	7724(1)	14(1)	1

B4	3829(2)	1969(1)	10588(1)	16(1)	1

B5	4614(2)	894(1)	9008(1)	14(1)	1

O1	804(1)	806(1)	9241(1)	15(1)	1

O2	735(1)	1973(1)	8395(1)	15(1)	1

O3	1770(1)	2036(1)	7968(1)	15(1)	1

O4	2448(1)	1855(1)	10191(1)	15(1)	1

O5	4945(1)	1562(1)	9922(1)	16(1)	1

O6	3232(1)	755(1)	8617(1)	14(1)	1

O7	1694(1)	713(1)	9517(1)	16(1)	1

O8	92(1)	2959(1)	6799(1)	17(1)	1

O9	4202(1)	2461(1)	11637(1)	22(1)	1

O10	5634(1)	349(1)	8506(1)	20(1)	1

C1	6403(2)	1312(1)	3320(1)	26(1)	1

C2	7124(2)	729(1)	4326(1)	21(1)	1

C3	6689(2)	177(1)	4515(2)	26(1)	1

C4	7346(2)	711(1)	5453(2)	31(1)	1

C5	8447(2)	348(1)	6189(2)	34(1)	1

C6	8913(2)	540(1)	5983(2)	31(1)	1

C7	8240(2)	1086(1)	5068(1)	26(1)	1

N1	7080(1)	1168(1)	2038(1)	18(1)	1

Table 3. Bond lengths [Å] and angles [°].

B1O6	1.4550(17)

B1O1	1.4706(17)

B1O4	1.4727(17)

B1O3	1.4761(17)

B2O7	1.3606(17)

B2O1	1.3632(17)

B2O2	1.3781(18)

B3O3	1.3556(17)

B3O8	1.3680(18)

B3O2	1.3897(17)

B4O9	1.3508(18)

B4O4	1.3615(17)

B4O5	1.3944(18)

B5O10	1.3506(18)

B5O6	1.3649(17)

B5O5	1.3938(18)

O7H7	0.8400

O8H8	0.8400

O9H9	0.8400

O10H10	0.8400

C1C2	1.504(2)

C1N1	1.5053(18)

C1H1D	0.9900

C1H1E	0.9900

C2C3	1.391(2)

C2C7	1.392(2)

C3C4	1.388(2)

C3H3	0.9500

C4C5	1.382(3)

C4H4	0.9500

C5C6	1.378(3)

C5H5	0.9500

C6C7	1.387(2)

C6H6	0.9500

C7H7A	0.9500

N1H1A	0.9100

N1H1B	0.9100

N1H1C	0.9100

O6B1O1	108.36(11)

O6B1O4	111.15(10)

O1B1O4	107.45(10)

O6B1O3	109.91(10)

O1B1O3	109.78(10)

O4B1O3	110.13(11)

O7B2O1	120.22(13)

O7B2O2	118.81(12)

O1B2O2	120.96(12)

O3B3O8	122.59(12)

O3B3O2	121.29(12)

O8B3O2	116.11(12)

O9B4O4	123.06(13)

O9B4O5	116.32(12)

O4B4O5	120.61(12)

O10B5O6	117.88(13)

O10B5O5	121.51(12)

O6B5O5	120.59(12)

B2O1B1	120.68(11)

B2O2B3	117.75(11)

B3O3B1	121.00(11)

B4O4B1	121.77(11)

B5O5B4	118.50(11)

B5O6B1	121.94(11)

B2O7H7	109.5

B3O8H8	109.5

B4O9H9	109.5

B5O10H10	109.5

C2C1N1	110.87(12)

C2C1H1D	109.5

N1C1H1D	109.5

C2C1H1E	109.5

N1C1H1E	109.5

H1DC1H1E	108.1

C3C2C7	119.39(14)

C3C2C1	120.14(14)

C7C2C1	120.47(14)

C4C3C2	120.04(15)

C4C3H3	120.0

C2C3H3	120.0

C5C4C3	120.05(16)

C5C4H4	120.0

C3C4H4	120.0

C6C5C4	120.29(16)

C6C5H5	119.9

C4C5H5	119.9

C5C6C7	120.02(16)

C5C6H6	120.0

C7C6H6	120.0

C6C7C2	120.16(16)

C6C7H7A	119.9

C2C7H7A	119.9

C1N1H1A	109.5

C1N1H1B	109.5

H1AN1H1B	109.5

C1N1H1C	109.5

H1AN1H1C	109.5

H1BN1H1C	109.5

Symmetry transformations used to generate equivalent atoms:

Table 4. Anisotropic displacement parameters [Å2 103]. The anisotropic displacement

factor exponent takes the form: 2 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

B1	10(1) 	15(1)	15(1) 	1(1)	1(1) 	0(1)

B2	13(1) 	16(1)	13(1) 	2(1)	0(1) 	1(1)

B3	14(1) 	15(1)	13(1) 	2(1)	0(1) 	0(1)

B4	14(1) 	16(1)	16(1) 	2(1)	0(1) 	0(1)

B5	13(1) 	15(1)	15(1) 	2(1)	0(1) 	1(1)

O1	10(1) 	16(1)	18(1) 	4(1)	0(1) 	0(1)

O2	12(1) 	16(1)	18(1) 	3(1)	1(1) 	2(1)

O3	12(1) 	17(1)	15(1) 	4(1)	0(1) 	1(1)

O4	12(1) 	19(1)	15(1) 	2(1)	0(1) 	2(1)

O5	10(1) 	19(1)	19(1) 	2(1)	0(1) 	0(1)

O6	11(1) 	16(1)	16(1) 	1(1)	0(1) 	0(1)

O7	11(1) 	18(1)	20(1) 	5(1)	0(1) 	1(1)

O8	14(1) 	20(1)	18(1) 	5(1)	1(1) 	1(1)

O9	14(1) 	28(1)	22(1) 	9(1)	2(1) 	2(1)

O10	11(1) 	24(1)	26(1) 	7(1)	1(1) 	1(1)

C1	27(1) 	32(1)	19(1) 	0(1)	4(1) 	10(1)

C2	25(1) 	21(1)	18(1) 	1(1)	4(1) 	5(1)

C3	28(1) 	26(1)	26(1) 	5(1)	5(1) 	2(1)

C4	46(1) 	19(1)	30(1) 	1(1)	10(1) 	1(1)

C5	53(1) 	28(1)	21(1) 	4(1)	2(1) 	13(1)

C6	41(1) 	30(1)	21(1) 	5(1)	7(1) 	5(1)

C7	35(1) 	20(1)	21(1) 	2(1)	0(1) 	0(1)

N1	17(1) 	20(1)	17(1) 	0(1)	2(1) 	0(1)

Table 5. Hydrogen coordinates [ 104] and isotropic displacement parameters [Å2  103].

Atom 	x	y	z	Ueq	S.o.f.

H7	1433	217	9863	25	1

H8	828	3076	6377	26	1

H9	3461	2647	12001	32	1

H10	6443	528	8761	30	1

H1D	6477	1970	3563	31	1

H1E	5375	1150	3263	31	1

H3	5941	430	4002	32	1

H4	7040	1327	5589	38	1

H5	8884	711	6840	41	1

H6	9696	778	6467	37	1

H7A	8541	1704	4948	31	1

H1A	7985	1399	2056	27	1

H1B	6555	1464	1425	27	1

H1C	7109	555	1859	27	1

Table 6. Hydrogen bonds [Å and °].

DH···A	d(DH)	d(H···A)	d(D···A)	(DHA)

O7H7...O1i	0.84	1.85	2.6855(14)	174.5

O8H8...O4ii	0.84	1.97	2.8030(13)	169.1

O9H9...O3iii	0.84	1.94	2.7812(13)	173.8

O10H10...O7iv	0.84	1.92	2.7513(13)	168.9

N1H1A...O8v	0.91	2.20	3.1019(15)	171.0

N1H1B...O5vi	0.91	2.17	3.0162(15)	154.9

N1H1B...O9vi	0.91	2.64	3.3024(16)	129.8

N1H1C...O6vii	0.91	1.99	2.8892(16)	168.8

Symmetry transformations used to generate equivalent atoms:

(i) x,y,z+2    (ii) x,y+1/2,z1/2    (iii) x,y+1/2,z+1/2

(iv)  x+1,y,z    (v) x+1,y+1/2,z1/2    (vi) x,y,z1

(vii) x+1,y,z+1