|  | Single Crystal X-Ray Diffraction Service National Crystallography Service Contact: Dr S.K.Callear, S.K.Callear@soton.ac.uk |
| --- | --- |

Table 1. Crystal data and structure refinement details.

Identification code 	2009src0464 (HP161)

Empirical formula 	C10H6FN3O

Formula weight 	203.18

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P21/n

Unit cell dimensions	a = 8.1049(2) Å	( = 90°

b = 6.1023(2) Å	( = 92.219(2)°

c = 17.6777(5) Å	(  = 90°

Volume	873.66(4) Å3

Z	4

Density (calculated)	1.545 Mg / m3

Absorption coefficient	0.120 mm(1

F(000)	416

Crystal	block; colourless

Crystal size	0.24 ( 0.13 ( 0.06 mm3

( range for data collection	3.53 ( 27.48°

Index ranges	(10 ( h ( 10, (7 ( k ( 7, (22 ( l ( 22

Reflections collected	18331

Independent reflections	1992 [Rint = 0.0443]

Completeness to ( = 27.48°	99.7 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.9929 and 0.9718

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	1992 / 2 / 144

Goodness-of-fit on F2	1.023

Final R indices [F2 > 2((F2)]	R1 = 0.0396, wR2 = 0.0969

R indices (all data)	R1 = 0.0466, wR2 = 0.1023

Largest diff. peak and hole	0.228 and (0.258 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: Sheldrick, G. M. SADABS - Bruker Nonius area detector scaling and absorption correction - V2.10 Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: ORTEP-3 (L.G. Farrugia, J. Appl. Cryst. (1997) 30, 565).

Special details:

Hydrogens fixed using a standard riding model except H12a and H12b which were located on the difference map and allowed to refine with only their N-H bond distances restrained (DFIX).

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C1	4668(2)	2430(2)	2938(1)	22(1)	1

C2	5287(2)	4506(2)	2822(1)	23(1)	1

C3	6845(2)	5001(2)	3131(1)	20(1)	1

C4	7748(2)	3424(2)	3544(1)	17(1)	1

C5	7077(2)	1342(2)	3650(1)	20(1)	1

C6	5518(2)	833(2)	3346(1)	22(1)	1

C7	9390(2)	3934(2)	3863(1)	16(1)	1

C9	11388(2)	6167(2)	4225(1)	17(1)	1

C10	11797(2)	4036(2)	4402(1)	17(1)	1

C13	13222(2)	3235(2)	4798(1)	18(1)	1

N11	10498(1)	2639(2)	4157(1)	18(1)	1

N12	12115(1)	8103(2)	4304(1)	23(1)	1

N14	14362(1)	2544(2)	5128(1)	24(1)	1

O8	9848(1)	6125(1)	3878(1)	18(1)	1

F1	3152(1)	1932(2)	2632(1)	34(1)	1

Table 3. Bond lengths [Å] and angles [°].

C1(F1	1.3579(15)

C1(C6	1.380(2)

C1(C2	1.381(2)

C2(C3	1.3901(18)

C2(H2	0.9500

C3(C4	1.3966(18)

C3(H3	0.9500

C4(C5	1.3975(18)

C4(C7	1.4592(17)

C5(C6	1.3891(18)

C5(H5	0.9500

C6(H6	0.9500

C7(N11	1.2909(16)

C7(O8	1.3875(15)

C9(N12	1.3253(17)

C9(O8	1.3695(15)

C9(C10	1.3746(18)

C10(N11	1.4100(16)

C10(C13	1.4141(17)

C13(N14	1.1534(17)

N12(H12A	0.882(14)

N12(H12B	0.879(15)

F1(C1(C6	118.41(12)

F1(C1(C2	118.29(12)

C6(C1(C2	123.30(12)

C1(C2(C3	118.03(13)

C1(C2(H2	121.0

C3(C2(H2	121.0

C2(C3(C4	120.37(12)

C2(C3(H3	119.8

C4(C3(H3	119.8

C3(C4(C5	119.86(11)

C3(C4(C7	120.44(12)

C5(C4(C7	119.69(11)

C6(C5(C4	120.26(12)

C6(C5(H5	119.9

C4(C5(H5	119.9

C1(C6(C5	118.18(12)

C1(C6(H6	120.9

C5(C6(H6	120.9

N11(C7(O8	113.62(10)

N11(C7(C4	129.46(12)

O8(C7(C4	116.89(10)

N12(C9(O8	117.24(11)

N12(C9(C10	135.79(12)

O8(C9(C10	106.97(10)

C9(C10(N11	109.37(11)

C9(C10(C13	128.66(12)

N11(C10(C13	121.90(11)

N14(C13(C10	178.42(14)

C7(N11(C10	104.64(11)

C9(N12(H12A	118.3(11)

C9(N12(H12B	117.6(13)

H12A(N12(H12B	122.8(18)

C9(O8(C7	105.38(9)

Symmetry transformations used to generate equivalent atoms:

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C1	13(1) 	27(1)	26(1) 	(4(1)	(2(1) 	(3(1)

C2	17(1) 	24(1)	29(1) 	2(1)	(4(1) 	2(1)

C3	18(1) 	17(1)	24(1) 	0(1)	0(1) 	(1(1)

C4	16(1) 	17(1)	19(1) 	(2(1)	(1(1) 	1(1)

C5	21(1) 	18(1)	21(1) 	1(1)	(1(1) 	(1(1)

C6	20(1) 	20(1)	26(1) 	(1(1)	2(1) 	(5(1)

C7	16(1) 	12(1)	20(1) 	0(1)	(1(1) 	(1(1)

C9	15(1) 	18(1)	19(1) 	0(1)	(2(1) 	0(1)

C10	15(1) 	14(1)	22(1) 	0(1)	(2(1) 	0(1)

C13	20(1) 	12(1)	24(1) 	0(1)	(1(1) 	(2(1)

N11	16(1) 	14(1)	22(1) 	0(1)	(3(1) 	0(1)

N12	18(1) 	15(1)	35(1) 	2(1)	(8(1) 	(1(1)

N14	22(1) 	17(1)	33(1) 	2(1)	(6(1) 	0(1)

O8	15(1) 	14(1)	24(1) 	1(1)	(4(1) 	(1(1)

F1	16(1) 	39(1)	46(1) 	0(1)	(9(1) 	(8(1)

Table 5. Hydrogen bonds [Å and °].

D(H···A	d(D(H)	d(H···A)	d(D···A)	((DHA)

N12(H12A...N11i	0.882(14)	2.204(15)	3.0692(16)	166.8(15)

N12(H12B...N14ii	0.879(15)	2.157(16)	3.0151(16)	164.9(18)

Symmetry transformations used to generate equivalent atoms:

(i) x,y+1,z    (ii) (x+3,(y+1,(z+1