|  | Single Crystal X-Ray Diffraction Service National Crystallography Service Contact: Dr S.K.Callear, S.K.Callear@soton.ac.uk |
| --- | --- |

Table 1. Crystal data and structure refinement details.

Identification code 	2009src0461 (HP155)

Empirical formula 	C8H5N3OS

Formula weight 	191.21

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Triclinic

Space group 	P(1

Unit cell dimensions	a = 6.1693(5) Å	( = 87.871(5)°

b = 7.0845(6) Å	( = 74.394(5)°

c = 10.3537(8) Å	(  = 69.471(5)°

Volume	407.34(6) Å3

Z	2

Density (calculated)	1.559 Mg / m3

Absorption coefficient	0.353 mm(1

F(000)	196

Crystal	plate; colourless

Crystal size	0.11 ( 0.06 ( 0.01 mm3

( range for data collection	3.08 ( 27.48°

Index ranges	(7 ( h ( 7, (9 ( k ( 9, (13 ( l ( 13

Reflections collected	6867

Independent reflections	1849 [Rint = 0.0607]

Completeness to ( = 27.48°	99.2 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.9965 and 0.9622

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	1849 / 10 / 142

Goodness-of-fit on F2	1.129

Final R indices [F2 > 2((F2)]	R1 = 0.0642, wR2 = 0.1118

R indices (all data)	R1 = 0.0970, wR2 = 0.1271

Largest diff. peak and hole	0.306 and (0.358 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: Sheldrick, G. M. SADABS - Bruker Nonius area detector scaling and absorption correction - V2.10 Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: ORTEP-3 (L.G. Farrugia, J. Appl. Cryst. (1997) 30, 565).

Special details:

All hydrogens fixed using a standard riding model, except H12a and H12b which were located on the difference map and refined with a restraint on the N-H bond distance (DFIX).

Thiophene ring is disordered: 38.27% of the time in position b. EADP restraints used on thiophene ring, together with SAME command.

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C1	11530(30)	2050(30)	(1002(11)	25(1)	0.617(4)

C2	10650(20)	1960(20)	(2130(11)	25(1)	0.617(4)

C3	14760(30)	1253(15)	(3070(9)	25(1)	0.617(4)

C4	12642(13)	1494(14)	(3349(11)	25(1)	0.617(4)

S1	14400(4)	1625(5)	(1388(3)	25(1)	0.617(4)

C1B	11310(30)	2080(40)	(1064(14)	12(3)	0.383(4)

C2B	13870(30)	1650(30)	(1390(19)	27(2)	0.383(4)

C3B	13100(20)	1500(20)	(3475(18)	27(2)	0.383(4)

C4B	14860(40)	1350(30)	(2852(14)	27(2)	0.383(4)

S1B	10352(8)	2057(7)	(2359(4)	24(1)	0.383(4)

C8	6560(5)	3316(4)	1918(3)	22(1)	1

C5	9955(5)	2558(4)	337(3)	21(1)	1

C10	8275(5)	3527(4)	3810(3)	24(1)	1

C7	8397(5)	3271(4)	2446(3)	21(1)	1

N11	8171(5)	3715(4)	4932(3)	32(1)	1

N12	4220(5)	3734(4)	2423(3)	28(1)	1

N6	10541(4)	2797(4)	1406(2)	21(1)	1

O9	7525(3)	2861(3)	569(2)	23(1)	1

Table 3. Bond lengths [Å] and angles [°].

C1(C2	1.425(17)

C1(C5	1.435(9)

C1(S1	1.627(16)

C2(C4	1.458(12)

C2(H2	0.9500

C3(C4	1.364(8)

C3(S1	1.713(7)

C3(H3	0.9500

C4(H4	0.9500

C1B(C2B	1.45(2)

C1B(C5	1.449(13)

C1B(S1B	1.607(18)

C2B(C4B	1.464(17)

C2B(H2B	0.9500

C3B(C4B	1.379(12)

C3B(S1B	1.694(11)

C3B(H3B	0.9500

C4B(H4B	0.9500

C8(N12	1.323(4)

C8(O9	1.365(3)

C8(C7	1.375(4)

C5(N6	1.287(4)

C5(O9	1.391(3)

C10(N11	1.156(4)

C10(C7	1.409(4)

C7(N6	1.403(4)

N12(H12B	0.87(4)

N12(H12A	0.90(5)

C2(C1(C5	121.9(12)

C2(C1(S1	113.9(8)

C5(C1(S1	124.1(11)

C1(C2(C4	109.1(11)

C1(C2(H2	125.4

C4(C2(H2	125.4

C4(C3(S1	112.3(12)

C4(C3(H3	123.8

S1(C3(H3	123.8

C3(C4(C2	111.5(13)

C3(C4(H4	124.2

C2(C4(H4	124.2

C1(S1(C3	93.1(7)

C2B(C1B(C5	117.4(15)

C2B(C1B(S1B	113.4(10)

C5(C1B(S1B	129.2(11)

C1B(C2B(C4B	108.6(16)

C1B(C2B(H2B	125.7

C4B(C2B(H2B	125.7

C4B(C3B(S1B	112.0(18)

C4B(C3B(H3B	124.0

S1B(C3B(H3B	124.0

C3B(C4B(C2B	111(2)

C3B(C4B(H4B	124.4

C2B(C4B(H4B	124.4

C1B(S1B(C3B	94.7(8)

N12(C8(O9	118.3(3)

N12(C8(C7	134.5(3)

O9(C8(C7	107.2(2)

N6(C5(O9	113.5(2)

N6(C5(C1	126.7(8)

O9(C5(C1	119.8(8)

N6(C5(C1B	132.9(8)

O9(C5(C1B	113.6(8)

C1(C5(C1B	6.3(15)

N11(C10(C7	179.2(3)

C8(C7(N6	109.2(2)

C8(C7(C10	127.3(3)

N6(C7(C10	123.4(2)

C8(N12(H12B	121(2)

C8(N12(H12A	120(3)

H12B(N12(H12A	119(3)

C5(N6(C7	105.0(2)

C8(O9(C5	105.1(2)

Symmetry transformations used to generate equivalent atoms:

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C1	31(3) 	26(2)	18(2) 	(2(2)	(7(2) 	(9(2)

C2	31(3) 	26(2)	18(2) 	(2(2)	(7(2) 	(9(2)

C3	31(3) 	26(2)	18(2) 	(2(2)	(7(2) 	(9(2)

C4	31(3) 	26(2)	18(2) 	(2(2)	(7(2) 	(9(2)

S1	17(1) 	33(1)	22(1) 	(1(1)	(2(1) 	(9(1)

C1B	6(4) 	10(4)	22(5) 	4(4)	(7(3) 	(1(4)

C2B	21(4) 	34(4)	23(4) 	1(3)	4(3) 	(13(3)

C3B	21(4) 	34(4)	23(4) 	1(3)	4(3) 	(13(3)

C4B	21(4) 	34(4)	23(4) 	1(3)	4(3) 	(13(3)

S1B	27(2) 	30(1)	18(2) 	(1(1)	(7(1) 	(11(1)

C8	22(1) 	22(2)	19(1) 	(1(1)	(3(1) 	(8(1)

C5	21(1) 	19(1)	23(1) 	0(1)	(7(1) 	(6(1)

C10	19(1) 	28(2)	24(2) 	2(1)	(6(1) 	(9(1)

C7	19(1) 	24(2)	21(1) 	0(1)	(4(1) 	(8(1)

N11	26(1) 	47(2)	22(1) 	1(1)	(4(1) 	(15(1)

N12	20(1) 	39(2)	25(1) 	(8(1)	(4(1) 	(11(1)

N6	22(1) 	23(1)	18(1) 	(1(1)	(4(1) 	(8(1)

O9	22(1) 	28(1)	19(1) 	(2(1)	(7(1) 	(9(1)

Table 5. Hydrogen bonds [Å and °].

D(H···A	d(D(H)	d(H···A)	d(D···A)	((DHA)

N12(H12B...N6i	0.87(4)	2.18(4)	3.016(4)	162(3)

N12(H12A...N11ii	0.90(5)	2.16(5)	3.044(4)	168(4)

Symmetry transformations used to generate equivalent atoms:

(i) x(1,y,z    (ii) (x+1,(y+1,(z+1