|  | University of Southampton · Department of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	01SRC138s

Empirical formula 	C47H54Cl2IrN2O3P

C45H46N2OP . 2CH3OH . 2Cl

Formula weight 	988.99

## Temperature 	150(2) K

Wavelength 	0.71073 Å

Crystal system 	Triclinic

Space group 	P(1

Unit cell dimensions	a = 10.4777(4) Å	( = 97.1510(16)°

b = 10.9221(3) Å	( = 92.3640(15)°

c = 19.7314(8) Å	(  = 97.7630(15)°

Volume	2216.06(14) Å3

Z	2

Density (calculated)	1.482 Mg / m3

Absorption coefficient	3.211 mm(1

F(000)	1000

Crystal	Yellow Needle

Crystal size	0.10 ( 0.02 ( 0.02 mm3

( range for data collection	2.92 ( 23.26°

Index ranges	(9 ( h ( 11, (12 ( k ( 11, (21 ( l ( 21

Reflections collected	13807

Independent reflections	6340 [Rint = 0.1130]

Completeness to ( = 23.26°	99.4 %

Max. and min. transmission	0.9386 and 0.7396

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	6340 / 18 / 518

Goodness-of-fit on F2	1.035

Final R indices [F2 > 2((F2)]	R1 = 0.0577, wR2 = 0.1222

R indices (all data)	R1 = 0.0814, wR2 = 0.1289

Extinction coefficient	0.0006(4)

Largest diff. peak and hole	2.078 and (1.211 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill Ewald sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing, Acta Cryst. A51 (1995) 33(37; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421(426). Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: Cameron - A Molecular Graphics Package. (D. M. Watkin, L. Pearce and C. K. Prout, Chemical Crystallography Laboratory, University of Oxford, 1993).

Special details:  All hydrogen atoms were placed in idealised positions and refined using a riding model.

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C1	(907(9)	3996(9)	2875(5)	18(2)	1

C2	(175(9)	4480(9)	2394(5)	22(3)	1

C3	1176(9)	4844(9)	2688(5)	17(2)	1

C4	1147(9)	4591(9)	3372(5)	18(2)	1

C5	(127(10)	4079(9)	3500(5)	23(3)	1

C6	(2374(9)	3682(10)	2856(6)	30(3)	1

C7	(640(11)	4812(10)	1697(5)	33(3)	1

C8	2257(10)	5527(9)	2373(6)	33(3)	1

C9	2262(10)	4979(10)	3891(6)	33(3)	1

C10	(593(11)	3894(10)	4193(5)	32(3)	1

C11	858(10)	2633(9)	877(5)	21(2)	1

C12	18(10)	2647(10)	303(5)	25(3)	1

C13	362(10)	3396(10)	(204(6)	29(3)	1

C14	1545(11)	4127(10)	(143(6)	29(3)	1

C15	2378(9)	4154(10)	409(6)	32(3)	1

C16	2082(9)	3412(9)	922(5)	19(2)	1

C17	(1095(9)	828(10)	1294(5)	20(3)	1

C18	(1227(10)	(417(10)	1056(6)	29(3)	1

C19	(2404(10)	(1109(10)	911(6)	34(3)	1

C20	(3514(10)	(558(10)	1007(5)	30(3)	1

C21	(3437(10)	660(10)	1241(5)	29(3)	1

C22	(2209(10)	1372(10)	1384(5)	30(3)	1

C23	1565(9)	591(9)	1491(5)	20(2)	1

C24	2028(9)	149(9)	871(5)	22(3)	1

C25	2752(10)	(804(10)	829(5)	28(3)	1

C26	3008(10)	(1397(9)	1398(5)	26(3)	1

C27	2589(10)	(936(9)	2014(5)	24(3)	1

C28	1850(9)	39(8)	2084(5)	18(2)	1

C30	1520(9)	583(8)	2772(5)	15(2)	1

C31	97(9)	841(8)	2844(5)	17(2)	1

C32	(283(9)	956(8)	3546(5)	17(2)	1

C33	1870(9)	1834(9)	4177(5)	18(2)	1

C34	2333(9)	2111(9)	4858(5)	21(3)	1

C35	3579(10)	2678(9)	5040(5)	20(2)	1

C36	4413(10)	2964(10)	4528(5)	25(3)	1

C37	3922(9)	2668(9)	3845(5)	20(2)	1

C38	2660(9)	2151(9)	3664(5)	16(2)	1

C39	4064(10)	2992(10)	5782(5)	30(3)	1

C40	5799(9)	3532(10)	4673(5)	29(3)	1

C41	(1662(9)	641(9)	3667(5)	22(3)	1

C42	(2593(10)	456(10)	3099(5)	27(3)	1

C43	(3877(10)	222(9)	3181(6)	28(3)	1

C44	(4347(10)	177(9)	3817(6)	28(3)	1

C45	(3482(10)	352(9)	4372(6)	25(3)	1

C46	(2160(10)	632(9)	4320(5)	23(3)	1

C47	5642(13)	3265(11)	362(6)	51(4)	1

C48	4229(15)	3260(15)	7989(8)	86(5)	1

N1	2240(7)	1890(6)	2957(4)	12(2)	1

N2	540(8)	1271(7)	4091(4)	21(2)	1

O1	(1340(6)	800(7)	4879(4)	28(2)	1

O2	5918(9)	4069(7)	984(4)	51(2)	1

O3	4775(9)	3553(9)	8655(5)	64(3)	1

P1	492(2)	1754(2)	1572(1)	17(1)	1

Cl1	4547(2)	2827(3)	2093(1)	34(1)	1

Cl2	7520(3)	1664(2)	6149(1)	30(1)	1

Ir1	608(1)	2793(1)	2656(1)	15(1)	1

Table 3. Bond lengths [Å] and angles [°].

C1(C2	1.359(14)

C1(C5	1.438(13)

C1(C6	1.527(13)

C1(Ir1	2.216(9)

C2(C3	1.490(13)

C2(C7	1.540(13)

C2(Ir1	2.224(9)

C3(C4	1.412(12)

C3(C8	1.474(13)

C3(Ir1	2.232(9)

C4(C5	1.421(13)

C4(C9	1.501(13)

C4(Ir1	2.262(10)

C5(C10	1.498(13)

C5(Ir1	2.271(10)

C11(C12	1.408(13)

C11(C16	1.433(13)

C11(P1	1.795(10)

C12(C13	1.397(14)

C13(C14	1.373(14)

C14(C15	1.362(14)

C15(C16	1.394(13)

C17(C18	1.369(14)

C17(C22	1.387(13)

C17(P1	1.850(10)

C18(C19	1.356(14)

C19(C20	1.389(14)

C20(C21	1.343(14)

C21(C22	1.409(14)

C23(C24	1.391(13)

C23(C28	1.420(13)

C23(P1	1.804(10)

C24(C25	1.364(13)

C25(C26	1.399(13)

C26(C27	1.371(14)

C27(C28	1.396(13)

C28(C30	1.486(13)

C30(N1	1.515(11)

C30(C31	1.563(13)

C31(C32	1.451(13)

C31(Ir1	2.208(9)

C32(N2	1.331(12)

C32(C41	1.476(13)

C33(C38	1.382(13)

C33(C34	1.391(13)

C33(N2	1.439(12)

C34(C35	1.380(13)

C35(C36	1.401(14)

C35(C39	1.511(13)

C36(C37	1.405(13)

C36(C40	1.502(13)

C37(C38	1.379(13)

C38(N1	1.428(11)

C41(C46	1.410(13)

C41(C42	1.431(13)

C42(C43	1.355(13)

C43(C44	1.372(14)

C44(C45	1.370(14)

C45(C46	1.388(14)

C46(O1	1.349(11)

C47(O2	1.412(13)

C48(O3	1.392(15)

N1(Ir1	2.184(7)

P1(Ir1	2.283(3)

C2(C1(C5	109.2(9)

C2(C1(C6	128.0(9)

C5(C1(C6	121.5(9)

C2(C1(Ir1	72.5(5)

C5(C1(Ir1	73.4(5)

C6(C1(Ir1	131.1(7)

C1(C2(C3	108.7(8)

C1(C2(C7	127.6(9)

C3(C2(C7	123.1(9)

C1(C2(Ir1	71.9(5)

C3(C2(Ir1	70.7(5)

C7(C2(Ir1	130.4(7)

C4(C3(C8	126.8(9)

C4(C3(C2	105.4(8)

C8(C3(C2	127.0(9)

C4(C3(Ir1	72.8(5)

C8(C3(Ir1	129.3(7)

C2(C3(Ir1	70.2(5)

C3(C4(C5	109.3(9)

C3(C4(C9	123.7(9)

C5(C4(C9	126.5(9)

C3(C4(Ir1	70.5(5)

C5(C4(Ir1	72.1(6)

C9(C4(Ir1	130.0(7)

C4(C5(C1	107.3(9)

C4(C5(C10	125.0(10)

C1(C5(C10	126.8(9)

C4(C5(Ir1	71.4(6)

C1(C5(Ir1	69.3(6)

C10(C5(Ir1	133.0(7)

C12(C11(C16	117.6(9)

C12(C11(P1	125.0(8)

C16(C11(P1	117.3(7)

C13(C12(C11	121.2(10)

C14(C13(C12	119.4(10)

C15(C14(C13	121.2(10)

C14(C15(C16	121.4(10)

C15(C16(C11	119.1(9)

C18(C17(C22	118.0(10)

C18(C17(P1	122.2(8)

C22(C17(P1	119.5(8)

C19(C18(C17	121.6(10)

C18(C19(C20	120.0(10)

C21(C20(C19	120.7(10)

C20(C21(C22	118.8(10)

C17(C22(C21	120.9(10)

C24(C23(C28	119.3(9)

C24(C23(P1	123.0(8)

C28(C23(P1	117.4(8)

C25(C24(C23	120.6(10)

C24(C25(C26	121.4(10)

C27(C26(C25	118.0(10)

C26(C27(C28	122.6(9)

C27(C28(C23	117.9(9)

C27(C28(C30	120.5(9)

C23(C28(C30	121.1(9)

C28(C30(N1	110.3(7)

C28(C30(C31	116.5(8)

N1(C30(C31	100.5(7)

C32(C31(C30	113.5(8)

C32(C31(Ir1	103.6(6)

C30(C31(Ir1	91.8(5)

N2(C32(C31	124.2(9)

N2(C32(C41	117.6(9)

C31(C32(C41	118.2(9)

C38(C33(C34	119.8(9)

C38(C33(N2	126.5(9)

C34(C33(N2	113.6(9)

C35(C34(C33	121.8(9)

C34(C35(C36	119.3(9)

C34(C35(C39	121.3(9)

C36(C35(C39	119.3(9)

C35(C36(C37	117.6(9)

C35(C36(C40	123.3(9)

C37(C36(C40	119.1(10)

C38(C37(C36	123.0(9)

C37(C38(C33	118.3(9)

C37(C38(N1	119.2(8)

C33(C38(N1	122.4(8)

C46(C41(C42	116.1(9)

C46(C41(C32	124.5(9)

C42(C41(C32	119.1(9)

C43(C42(C41	121.9(10)

C42(C43(C44	121.3(11)

C45(C44(C43	118.3(10)

C44(C45(C46	122.8(10)

O1(C46(C45	120.9(10)

O1(C46(C41	119.4(9)

C45(C46(C41	119.4(10)

C38(N1(C30	112.3(7)

C38(N1(Ir1	115.3(5)

C30(N1(Ir1	94.1(5)

C32(N2(C33	132.9(9)

C11(P1(C23	104.0(5)

C11(P1(C17	103.6(5)

C23(P1(C17	102.5(5)

C11(P1(Ir1	118.6(3)

C23(P1(Ir1	111.8(3)

C17(P1(Ir1	114.5(3)

N1(Ir1(C31	65.2(3)

N1(Ir1(C1	152.8(3)

C31(Ir1(C1	115.0(4)

N1(Ir1(C2	150.0(3)

C31(Ir1(C2	144.7(4)

C1(Ir1(C2	35.6(3)

N1(Ir1(C3	111.3(3)

C31(Ir1(C3	168.8(3)

C1(Ir1(C3	62.8(3)

C2(Ir1(C3	39.1(3)

N1(Ir1(C4	96.9(3)

C31(Ir1(C4	132.2(3)

C1(Ir1(C4	61.9(3)

C2(Ir1(C4	62.0(3)

C3(Ir1(C4	36.6(3)

N1(Ir1(C5	115.5(3)

C31(Ir1(C5	109.3(3)

C1(Ir1(C5	37.3(3)

C2(Ir1(C5	60.9(4)

C3(Ir1(C5	61.7(3)

C4(Ir1(C5	36.5(3)

N1(Ir1(P1	91.6(2)

C31(Ir1(P1	78.5(3)

C1(Ir1(P1	115.4(3)

C2(Ir1(P1	97.2(3)

C3(Ir1(P1	112.7(3)

C4(Ir1(P1	148.9(2)

C5(Ir1(P1	152.7(3)

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C1	18(6) 	15(6)	20(6) 	(5(5)	(13(5) 	13(5)

C2	23(6) 	12(6)	27(6) 	(11(5)	(19(5) 	14(5)

C3	11(5) 	15(6)	26(6) 	4(5)	(5(5) 	9(4)

C4	21(6) 	20(6)	13(6) 	4(5)	(10(5) 	5(5)

C5	24(6) 	15(6)	31(7) 	2(5)	4(6) 	4(5)

C6	13(6) 	33(7)	44(8) 	2(6)	7(6) 	11(5)

C7	54(8) 	21(6)	23(6) 	7(5)	(6(6) 	4(6)

C8	31(7) 	13(6)	55(8) 	0(5)	13(6) 	5(5)

C9	30(7) 	27(7)	40(8) 	(6(6)	(16(6) 	6(5)

C10	42(7) 	36(7)	21(7) 	1(5)	5(6) 	13(6)

C11	34(7) 	12(6)	18(6) 	(1(4)	(6(5) 	13(5)

C12	15(6) 	32(7)	25(7) 	(5(5)	(5(5) 	8(5)

C13	28(7) 	36(7)	27(7) 	12(6)	(10(6) 	10(6)

C14	39(7) 	23(6)	29(7) 	15(5)	3(6) 	7(6)

C15	4(6) 	43(8)	50(8) 	11(6)	(2(6) 	1(5)

C16	23(6) 	20(6)	16(6) 	6(5)	(3(5) 	5(5)

C17	17(6) 	29(7)	14(6) 	3(5)	(2(5) 	1(5)

C18	11(6) 	37(7)	38(7) 	(1(6)	(1(5) 	0(5)

C19	27(7) 	13(6)	60(9) 	2(6)	(2(6) 	0(5)

C20	22(7) 	28(7)	38(7) 	5(6)	(4(6) 	(7(5)

C21	11(6) 	46(8)	31(7) 	3(6)	(16(5) 	8(5)

C22	26(7) 	27(7)	37(7) 	6(5)	(1(6) 	5(5)

C23	13(6) 	26(6)	20(6) 	(3(5)	1(5) 	0(5)

C24	11(6) 	27(6)	28(7) 	3(5)	(4(5) 	4(5)

C25	25(6) 	37(7)	18(6) 	(7(5)	(4(5) 	7(6)

C26	36(7) 	22(6)	21(7) 	(5(5)	1(6) 	9(5)

C27	32(7) 	14(6)	30(7) 	10(5)	(7(6) 	9(5)

C28	17(6) 	11(5)	22(6) 	(3(5)	(12(5) 	(7(4)

C30	18(5) 	3(5)	24(5) 	6(4)	(9(4) 	(1(4)

C31	18(6) 	9(5)	22(6) 	(2(4)	2(5) 	(7(4)

C32	21(6) 	5(5)	25(6) 	4(4)	(7(5) 	5(4)

C33	10(5) 	19(5)	26(5) 	6(4)	(7(5) 	1(4)

C34	11(6) 	22(6)	31(7) 	11(5)	(10(5) 	(2(5)

C35	26(5) 	22(5)	15(5) 	9(4)	(9(5) 	9(4)

C36	17(6) 	29(7)	29(7) 	0(5)	(12(5) 	9(5)

C37	18(6) 	27(6)	16(6) 	14(5)	(4(5) 	1(5)

C38	8(5) 	23(6)	19(6) 	15(5)	(5(5) 	0(4)

C39	14(6) 	45(8)	27(7) 	(4(6)	(8(5) 	1(5)

C40	14(6) 	46(8)	28(7) 	1(6)	(5(5) 	8(5)

C41	11(6) 	30(7)	25(7) 	13(5)	(2(5) 	(6(5)

C42	18(6) 	38(7)	22(6) 	2(5)	(5(5) 	(3(5)

C43	12(6) 	26(7)	43(8) 	3(6)	(4(6) 	(4(5)

C44	18(6) 	23(6)	39(8) 	4(5)	9(6) 	(8(5)

C45	21(6) 	26(7)	27(7) 	10(5)	6(6) 	(8(5)

C46	23(7) 	22(6)	23(7) 	4(5)	(8(6) 	4(5)

C47	67(10) 	41(8)	46(9) 	6(7)	0(8) 	8(7)

C48	68(11) 	79(13)	102(14) 	(3(10)	(30(11) 	5(9)

N1	4(4) 	13(4)	18(5) 	4(4)	1(4) 	1(3)

N2	23(5) 	27(5)	18(5) 	15(4)	(1(4) 	5(4)

O1	18(4) 	32(5)	30(5) 	9(4)	(4(4) 	(5(4)

O2	67(7) 	34(5)	54(6) 	9(5)	19(5) 	3(5)

O3	64(7) 	53(7)	70(7) 	6(5)	(30(6) 	3(5)

P1	14(2) 	20(2)	18(2) 	3(1)	(4(1) 	2(1)

Cl1	15(2) 	55(2)	32(2) 	13(2)	(2(1) 	1(1)

Cl2	32(2) 	30(2)	29(2) 	9(1)	0(1) 	6(1)

Ir1	12(1) 	16(1)	18(1) 	4(1)	(4(1) 	1(1)

Table 5. Hydrogen coordinates [( 104] and isotropic displacement parameters [Å2 ( 103].

Atom 	x	y	z	Ueq	S.o.f.

H6A	(2723	3554	2380	44	1

H6B	(2735	4371	3111	44	1

H6C	(2606	2920	3064	44	1

H7A	(1350	4179	1494	49	1

H7B	75	4841	1392	49	1

H7C	(940	5628	1763	49	1

H8A	2367	6410	2564	49	1

H8B	2072	5447	1877	49	1

H8C	3050	5179	2468	49	1

H9A	3073	4942	3664	50	1

H9B	2206	4416	4241	50	1

H9C	2235	5833	4106	50	1

H10A	128	3752	4492	48	1

H10B	(1269	3171	4150	48	1

H10C	(943	4639	4390	48	1

H12	(799	2137	259	30	1

H13	(217	3399	(587	35	1

H14	1787	4623	(492	35	1

H15	3179	4689	444	39	1

H16	2683	3422	1297	23	1

H18	(475	(806	991	35	1

H19	(2469	(1971	744	41	1

H20	(4336	(1047	905	37	1

H21	(4197	1034	1310	35	1

H22	(2143	2237	1544	35	1

H24	1840	514	472	26	1

H25	3088	(1070	404	33	1

H26	3460	(2099	1358	32	1

H27	2810	(1294	2410	29	1

H30	1751	47	3121	18	1

H31	(550	319	2503	21	1

H34	1775	1903	5207	26	1

H37	4484	2832	3491	24	1

H39A	3353	2796	6076	45	1

H39B	4399	3882	5877	45	1

H39C	4754	2501	5874	45	1

H40A	5842	4351	4948	44	1

H40B	6205	3629	4241	44	1

H40C	6254	2989	4927	44	1

H42	(2302	499	2652	33	1

H43	(4463	86	2790	34	1

H44	(5249	28	3872	33	1

H45	(3799	280	4811	30	1

H47A	4766	3315	184	77	1

H47B	5707	2407	441	77	1

H47C	6262	3516	29	77	1

H48A	4287	4018	7766	129	1

H48B	3322	2904	8000	129	1

H48C	4696	2653	7732	129	1

H1	2924	2037	2678	14	1

H2	204	1102	4476	26	1

H1	(1000	1549	4954	41	1

H4	5547	4702	969	77	1

H5	4246	3867	8908	96	1

Table 6. Hydrogen bonds [Å and °].

D(H···A	d(D(H)	d(H···A)	d(D···A)	((DHA)

O2(H4...O3i	0.84	2.03	2.805(13)	152.4

N1(H1...Cl1	0.93	2.23	3.147(8)	167.5

Symmetry transformations used to generate equivalent atoms:

(i) (x+1,(y+1,(z+1