|  | University of Southampton · Department of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	s92

Empirical formula 	C20H30Cl2FeN6O8

Formula weight 	609.25

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	?

Space group 	?

Unit cell dimensions	a = 19.0961(8) Å	( = 90°

b = 8.5356(5) Å	( = 115.869(4)°

c = 16.7145(7) Å	(  = 90°

Volume	2451.4(2) Å3

Z	4

Density (calculated)	1.651 Mg / m3

Absorption coefficient	0.893 mm(1

F(000)	1264

Crystal	?; ?

Crystal size	0.15 ( 0.10 ( 0.02 mm3

( range for data collection	3.22 ( 25.02°

Index ranges	(22 ( h ( 22, (10 ( k ( 10, (19 ( l ( 19

Reflections collected	12542

Independent reflections	2106 [Rint = 0.0620]

Completeness to ( = 25.02°	97.0 %

Max. and min. transmission	0.9824 and 0.8777

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	2106 / 0 / 169

Goodness-of-fit on F2	1.047

Final R indices [F2 > 2((F2)]	R1 = 0.0468, wR2 = 0.1104

R indices (all data)	R1 = 0.0600, wR2 = 0.1170

Extinction coefficient	0.0004(3)

Largest diff. peak and hole	0.705 and (0.599 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing, Acta Cryst. A51 (1995) 33(37; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421(426). Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: Cameron - A Molecular Graphics Package. (D. M. Watkin, L. Pearce and C. K. Prout, Chemical Crystallography Laboratory, University of Oxford, 1993).

Special details:

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

O1	5509(2)	2946(4)	881(2)	54(1)	1

O2	6685(2)	2657(3)	2122(2)	41(1)	1

O3	6479(2)	4831(5)	1219(4)	113(2)	1

O4	5790(2)	4547(4)	2103(2)	71(1)	1

Cl1	6129(1)	3790(1)	1577(1)	35(1)	1

C1	3772(2)	(252(4)	651(2)	20(1)	1

C2	3291(2)	(882(4)	(176(2)	24(1)	1

C3	2878(2)	97(4)	(884(2)	26(1)	1

C4	2948(2)	1715(5)	(773(2)	30(1)	1

C5	3426(2)	2343(4)	44(3)	29(1)	1

C6	3836(2)	1359(4)	758(2)	23(1)	1

C7	3700(2)	(2075(4)	1727(2)	23(1)	1

C8	4743(2)	(2333(4)	1234(2)	23(1)	1

C9	5397(2)	(1404(4)	1182(2)	25(1)	1

C10	6500(2)	(997(4)	2691(2)	25(1)	1

N1	4347(2)	1949(4)	1618(2)	34(1)	1

N2	4226(2)	(1247(3)	1422(2)	19(1)	1

N3	5781(2)	(351(3)	1964(2)	21(1)	1

Fe1	5000	251(1)	2500	18(1)	1

Table 3. Bond lengths [Å] and angles [°].

O1(Cl1	1.439(3)

O2(Cl1	1.432(3)

O3(Cl1	1.394(4)

O4(Cl1	1.451(4)

C1(C6	1.385(5)

C1(C2	1.391(5)

C1(N2	1.469(4)

C2(C3	1.380(5)

C3(C4	1.393(5)

C4(C5	1.378(5)

C5(C6	1.388(5)

C6(N1	1.432(4)

C7(N2	1.488(4)

C7(C10i	1.504(5)

C8(N2	1.484(4)

C8(C9	1.513(5)

C9(N3	1.489(4)

C10(N3	1.486(4)

C10(C7i	1.504(5)

N1(Fe1	2.055(3)

N2(Fe1	2.178(3)

N3(Fe1	2.112(3)

Fe1(N1i	2.055(3)

Fe1(N3i	2.112(3)

Fe1(N2i	2.178(3)

O3(Cl1(O2	109.9(2)

O3(Cl1(O1	110.6(3)

O2(Cl1(O1	107.28(19)

O3(Cl1(O4	113.6(3)

O2(Cl1(O4	108.6(2)

O1(Cl1(O4	106.6(2)

C6(C1(C2	119.6(3)

C6(C1(N2	118.4(3)

C2(C1(N2	121.9(3)

C3(C2(C1	120.1(3)

C2(C3(C4	120.0(3)

C5(C4(C3	120.1(3)

C4(C5(C6	119.8(3)

C1(C6(C5	120.4(3)

C1(C6(N1	117.5(3)

C5(C6(N1	122.1(3)

N2(C7(C10i	109.3(3)

N2(C8(C9	109.0(3)

N3(C9(C8	111.7(3)

N3(C10(C7i	110.6(3)

C6(N1(Fe1	114.0(2)

C1(N2(C8	111.6(2)

C1(N2(C7	110.3(2)

C8(N2(C7	112.7(2)

C1(N2(Fe1	108.30(19)

C8(N2(Fe1	105.52(18)

C7(N2(Fe1	108.11(19)

C10(N3(C9	114.8(3)

C10(N3(Fe1	108.3(2)

C9(N3(Fe1	110.50(19)

N1i(Fe1(N1	90.32(17)

N1i(Fe1(N3i	100.81(11)

N1(Fe1(N3i	98.95(11)

N1i(Fe1(N3	98.95(11)

N1(Fe1(N3	100.81(11)

N3i(Fe1(N3	151.84(16)

N1i(Fe1(N2	171.04(11)

N1(Fe1(N2	80.80(11)

N3i(Fe1(N2	81.86(10)

N3(Fe1(N2	81.72(10)

N1i(Fe1(N2i	80.80(11)

N1(Fe1(N2i	171.04(11)

N3i(Fe1(N2i	81.72(10)

N3(Fe1(N2i	81.86(10)

N2(Fe1(N2i	108.10(14)

Symmetry transformations used to generate equivalent atoms:

(i) (x+1,y,(z+1/2

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

O1	32(2) 	92(3)	28(2) 	(8(2)	5(1) 	(5(2)

O2	34(2) 	32(2)	45(2) 	7(1)	5(1) 	(1(1)

O3	63(3) 	98(3)	167(5) 	90(3)	41(3) 	(10(2)

O4	99(3) 	41(2)	65(2) 	(16(2)	27(2) 	22(2)

Cl1	32(1) 	31(1)	34(1) 	9(1)	8(1) 	(2(1)

C1	17(2) 	24(2)	21(2) 	3(1)	11(1) 	(1(1)

C2	20(2) 	27(2)	25(2) 	(1(1)	9(1) 	(4(1)

C3	17(2) 	35(2)	26(2) 	2(2)	8(1) 	(2(2)

C4	23(2) 	40(2)	32(2) 	13(2)	17(2) 	9(2)

C5	34(2) 	23(2)	41(2) 	7(2)	27(2) 	6(2)

C6	22(2) 	25(2)	28(2) 	(2(1)	17(2) 	(3(1)

C7	21(2) 	24(2)	21(2) 	2(1)	7(1) 	(7(1)

C8	25(2) 	18(2)	23(2) 	(4(1)	7(1) 	3(1)

C9	24(2) 	29(2)	22(2) 	(1(1)	11(2) 	5(2)

C10	16(2) 	29(2)	29(2) 	(4(2)	9(2) 	3(2)

N1	38(2) 	41(2)	30(2) 	(13(1)	22(2) 	(17(2)

N2	20(1) 	17(1)	22(2) 	1(1)	11(1) 	(1(1)

N3	19(1) 	22(2)	23(2) 	3(1)	9(1) 	1(1)

Fe1	13(1) 	22(1)	18(1) 	0	7(1) 	0

Table 5. Hydrogen coordinates [( 104] and isotropic displacement parameters [Å2 ( 103].

Atom 	x	y	z	Ueq	S.o.f.

H5	3246	(1986	(253	29	1

H4	2545	(335	(1447	32	1

H3	2666	2387	(1262	36	1

H2	3475	3447	119	35	1

H7A	3961	(3026	2064	27	1

H7B	3219	(2401	1207	27	1

H8A	4443	(2884	664	28	1

H8B	4960	(3128	1712	28	1

H9A	5787	(2135	1153	30	1

H9B	5186	(769	631	30	1

H77A	6828	(127	3054	30	1

H77B	6801	(1579	2434	30	1

H2A	4055	2462	1853	41	1

H2B	4677	2670	1556	41	1

H3A	5916	567	1766	26	1

Table 6. Hydrogen bonds [Å and °].

D(H···A	d(D(H)	d(H···A)	d(D···A)	((DHA)

N1(H2A...O4i	0.92	2.42	3.169(5)	138.7

N1(H2B...O1	0.92	2.33	3.092(4)	140.4

N1(H2B...O4	0.92	2.49	3.350(5)	154.9

N1(H2B...Cl1	0.92	2.92	3.776(3)	156.0

N3(H3A...O2	0.93	2.22	3.041(4)	146.6

N3(H3A...O1	0.93	2.43	3.263(5)	148.8

N3(H3A...Cl1	0.93	2.82	3.705(3)	159.7

Symmetry transformations used to generate equivalent atoms:

(i) (x+1,y,(z+1/2