Table 1.  Crystal data and structure refinement for M2.

Identification code 	99src142

Empirical formula 	C44H50NO10Re

Formula weight 	939.05

Temperature 	293(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P21/c

# Unit cell dimensions	a = 7.7320(4) Å

b = 9.8233(4) Å	 = 92.4021(12)°.

c = 56.321(2) Å

Volume	4274.0(3) Å3

# Z	4

Density (calculated)	1.459 Mg/m3

Absorption coefficient	2.900 mm-1

F(000)	1904

Crystal size	0.05 x 0.02 x 0.02 mm3

Theta range for data collection	2.95 to 25.03°.

Index ranges	-9<=h<=9, -11<=k<=11, -61<=l<=66

Reflections collected	29502

Independent reflections	7099 [R(int) = 0.0908]

Completeness to theta = 25.03°	88.4 %

Absorption correction	Empirical, SORTAV

Max. and min. transmission	0.9443 and 0.8686

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	7099 / 0 / 508

Goodness-of-fit on F2	0.902

Final R indices [I>2sigma(I)]	R1 = 0.0386, wR2 = 0.0627

R indices (all data)	R1 = 0.0979, wR2 = 0.0765

Largest diff. peak and hole	0.452 and -0.724 e.Å-3

Table 2.  Atomic coordinates ( x 104) and equivalent isotropic displacement parameters (Å2x 103) for M2.  U(eq) is defined as one third of the trace of the orthogonalized Uij tensor.

______________________________________________________________________________

x	y	z	U(eq)

______________________________________________________________________________

Re(1)	224(1)	5243(1)	597(1)	64(1)

O(4)	4019(5)	8538(4)	-389(1)	86(1)

O(2)	8019(5)	9771(4)	-1351(1)	84(1)

C(17)	4034(8)	9779(7)	-493(1)	73(2)

C(42)	1353(8)	4466(6)	311(1)	87(2)

O(5)	-3276(4)	6609(3)	1465(1)	64(1)

C(15)	5825(8)	8603(6)	-811(1)	89(2)

N(1)	742(5)	7342(4)	486(1)	60(1)

C(43)	2424(9)	5211(6)	769(1)	77(2)

O(3)	3260(5)	10733(4)	-411(1)	86(1)

C(14)	5113(7)	9780(6)	-716(1)	67(2)

C(18)	3150(9)	8339(5)	-169(1)	71(2)

C(5)	10348(7)	10181(5)	-2630(1)	74(2)

C(25)	-652(6)	7883(5)	852(1)	56(1)

C(11)	6997(7)	9843(7)	-1140(1)	70(2)

C(41)	-2104(9)	5298(6)	462(1)	81(2)

C(10)	7462(8)	10312(6)	-1557(1)	68(2)

C(30)	-885(6)	6475(5)	888(1)	54(1)

C(7)	9535(7)	10159(5)	-2190(1)	67(2)

C(29)	-1766(6)	6111(5)	1099(1)	57(1)

O(1)	6121(6)	10872(4)	-1566(1)	96(1)

C(13)	5359(7)	10981(6)	-837(1)	77(2)

O(7)	-3465(6)	5310(5)	394(1)	119(2)

C(9)	8712(6)	9984(5)	-1757(1)	67(2)

O(8)	-728(6)	2415(4)	792(1)	111(2)

C(28)	-2332(6)	7067(5)	1263(1)	57(1)

C(26)	-1255(6)	8841(5)	1016(1)	67(2)

C(44)	-363(7)	3489(6)	721(1)	79(2)

C(35)	-4561(6)	7220(5)	2552(1)	67(2)

C(16)	6774(7)	8625(6)	-1023(1)	89(2)

C(24)	211(6)	8266(5)	631(1)	62(1)

O(9)	3645(6)	5173(5)	872(1)	114(2)

O(6)	-1602(5)	7768(4)	1710(1)	103(2)

C(38)	-6474(7)	6927(5)	3201(1)	77(2)

C(34)	-4943(6)	6659(5)	2310(1)	66(2)

C(21)	1553(7)	7722(5)	261(1)	61(1)

O(10)	2008(6)	4007(5)	142(1)	127(2)

C(33)	-3752(6)	7176(5)	2112(1)	70(2)

C(12)	6324(7)	11032(6)	-1049(1)	77(2)

C(23)	4102(8)	7862(6)	8(1)	100(2)

C(27)	-2093(6)	8438(5)	1223(1)	66(2)

C(36)	-5740(7)	6729(5)	2755(1)	70(2)

C(6)	9199(7)	10728(5)	-2430(1)	73(2)

C(8)	8310(6)	10611(5)	-1989(1)	71(2)

C(22)	3284(8)	7542(6)	226(1)	97(2)

C(31)	-2850(8)	7091(5)	1680(1)	65(2)

C(32)	-4124(6)	6627(5)	1871(1)	61(1)

C(3)	11132(7)	10060(5)	-3073(1)	79(2)

C(37)	-5317(6)	7351(5)	2992(1)	72(2)

C(4)	10064(7)	10692(5)	-2874(1)	76(2)

C(20)	616(7)	8202(6)	82(1)	81(2)

C(1)	11872(8)	9835(6)	-3514(1)	116(2)

C(19)	1421(9)	8501(6)	-135(1)	91(2)

C(2)	10825(8)	10524(6)	-3314(1)	96(2)

C(39)	-6067(8)	7621(6)	3432(1)	94(2)

C(40)	-7231(8)	7236(6)	3645(1)	114(2)

______________________________________________________________________________

Table 3.   Bond lengths [Å] and angles [°] for M2.

_____________________________________________________

Re(1)-C(43) 	1.921(7)

Re(1)-C(44) 	1.919(6)

Re(1)-C(41) 	1.927(7)

Re(1)-C(42) 	2.017(7)

Re(1)-N(1) 	2.197(4)

Re(1)-C(30) 	2.235(5)

O(4)-C(17) 	1.353(6)

O(4)-C(18) 	1.449(6)

O(2)-C(10) 	1.330(6)

O(2)-C(11) 	1.457(6)

C(17)-O(3) 	1.214(6)

C(17)-C(14) 	1.537(8)

C(42)-O(10) 	1.184(6)

O(5)-C(31) 	1.329(5)

O(5)-C(28) 	1.450(5)

C(15)-C(14) 	1.396(7)

C(15)-C(16) 	1.429(7)

N(1)-C(24) 	1.299(5)

N(1)-C(21) 	1.483(6)

C(43)-O(9) 	1.089(6)

C(14)-C(13) 	1.380(7)

C(18)-C(23) 	1.299(6)

C(18)-C(19) 	1.367(7)

C(5)-C(4) 	1.474(6)

C(5)-C(6) 	1.559(6)

C(25)-C(30) 	1.411(6)

C(25)-C(26) 	1.413(6)

C(25)-C(24) 	1.484(6)

C(11)-C(12) 	1.386(7)

C(11)-C(16) 	1.380(7)

C(41)-O(7) 	1.104(6)

C(10)-O(1) 	1.174(5)

C(10)-C(9) 	1.547(7)

C(30)-C(29) 	1.442(6)

C(7)-C(6) 	1.474(6)

C(7)-C(8) 	1.573(6)

C(29)-C(28) 	1.399(6)

C(13)-C(12) 	1.432(6)

C(9)-C(8) 	1.467(6)

O(8)-C(44) 	1.167(6)

C(28)-C(27) 	1.380(6)

C(26)-C(27) 	1.412(6)

C(35)-C(34) 	1.488(5)

C(35)-C(36) 	1.567(6)

O(6)-C(31) 	1.178(6)

C(38)-C(39) 	1.492(6)

C(38)-C(37) 	1.564(6)

C(34)-C(33) 	1.565(6)

C(21)-C(20) 	1.305(6)

C(21)-C(22) 	1.373(6)

C(33)-C(32) 	1.474(6)

C(23)-C(22) 	1.442(6)

C(36)-C(37) 	1.491(6)

C(31)-C(32) 	1.556(6)

C(3)-C(2) 	1.446(7)

C(3)-C(4) 	1.546(7)

C(20)-C(19) 	1.428(6)

C(1)-C(2) 	1.565(7)

C(39)-C(40) 	1.574(7)

C(43)-Re(1)-C(44)	91.2(2)

C(43)-Re(1)-C(41)	173.1(2)

C(44)-Re(1)-C(41)	86.4(2)

C(43)-Re(1)-C(42)	89.6(3)

C(44)-Re(1)-C(42)	93.8(2)

C(41)-Re(1)-C(42)	97.0(2)

C(43)-Re(1)-N(1)	89.45(19)

C(44)-Re(1)-N(1)	174.0(2)

C(41)-Re(1)-N(1)	92.24(19)

C(42)-Re(1)-N(1)	92.10(19)

C(43)-Re(1)-C(30)	90.0(2)

C(44)-Re(1)-C(30)	96.7(2)

C(41)-Re(1)-C(30)	83.9(2)

C(42)-Re(1)-C(30)	169.4(2)

N(1)-Re(1)-C(30)	77.32(17)

C(17)-O(4)-C(18)	120.3(4)

C(10)-O(2)-C(11)	121.7(4)

O(3)-C(17)-O(4)	121.1(6)

O(3)-C(17)-C(14)	127.3(6)

O(4)-C(17)-C(14)	111.6(5)

O(10)-C(42)-Re(1)	179.7(6)

C(31)-O(5)-C(28)	119.5(4)

C(14)-C(15)-C(16)	122.1(5)

C(24)-N(1)-C(21)	121.1(4)

C(24)-N(1)-Re(1)	114.2(4)

C(21)-N(1)-Re(1)	124.6(3)

O(9)-C(43)-Re(1)	177.6(6)

C(13)-C(14)-C(15)	117.0(6)

C(13)-C(14)-C(17)	119.6(6)

C(15)-C(14)-C(17)	123.3(6)

C(23)-C(18)-C(19)	117.5(6)

C(23)-C(18)-O(4)	115.8(6)

C(19)-C(18)-O(4)	126.5(6)

C(4)-C(5)-C(6)	119.4(4)

C(30)-C(25)-C(26)	120.7(5)

C(30)-C(25)-C(24)	115.7(4)

C(26)-C(25)-C(24)	123.6(5)

C(12)-C(11)-C(16)	119.9(6)

C(12)-C(11)-O(2)	124.6(5)

C(16)-C(11)-O(2)	115.5(6)

O(7)-C(41)-Re(1)	176.6(6)

O(1)-C(10)-O(2)	118.7(5)

O(1)-C(10)-C(9)	130.0(5)

O(2)-C(10)-C(9)	111.2(5)

C(25)-C(30)-C(29)	115.4(4)

C(25)-C(30)-Re(1)	111.7(4)

C(29)-C(30)-Re(1)	132.8(4)

C(6)-C(7)-C(8)	117.8(4)

C(28)-C(29)-C(30)	123.4(5)

C(14)-C(13)-C(12)	121.9(5)

C(8)-C(9)-C(10)	116.4(4)

C(27)-C(28)-C(29)	119.9(5)

C(27)-C(28)-O(5)	120.5(5)

C(29)-C(28)-O(5)	119.4(5)

C(25)-C(26)-C(27)	122.0(5)

O(8)-C(44)-Re(1)	178.8(5)

C(34)-C(35)-C(36)	117.0(4)

C(11)-C(16)-C(15)	119.4(5)

N(1)-C(24)-C(25)	121.0(5)

C(39)-C(38)-C(37)	115.4(5)

C(35)-C(34)-C(33)	115.8(4)

C(20)-C(21)-C(22)	116.6(5)

C(20)-C(21)-N(1)	120.6(5)

C(22)-C(21)-N(1)	122.8(5)

C(32)-C(33)-C(34)	116.2(4)

C(11)-C(12)-C(13)	119.7(5)

C(18)-C(23)-C(22)	118.5(6)

C(28)-C(27)-C(26)	118.5(5)

C(37)-C(36)-C(35)	114.4(4)

C(7)-C(6)-C(5)	116.6(4)

C(9)-C(8)-C(7)	114.4(4)

C(21)-C(22)-C(23)	124.1(5)

O(6)-C(31)-O(5)	120.1(5)

O(6)-C(31)-C(32)	127.2(5)

O(5)-C(31)-C(32)	112.7(5)

C(33)-C(32)-C(31)	115.0(4)

C(2)-C(3)-C(4)	118.8(5)

C(36)-C(37)-C(38)	116.9(4)

C(5)-C(4)-C(3)	118.4(4)

C(21)-C(20)-C(19)	119.3(5)

C(18)-C(19)-C(20)	124.0(5)

C(3)-C(2)-C(1)	118.0(5)

C(38)-C(39)-C(40)	116.6(5)

_____________________________________________________________

Symmetry transformations used to generate equivalent atoms:

Table 4.   Anisotropic displacement parameters (Å2x 103)for M2.  The anisotropic

displacement factor exponent takes the form: -2p2[ h2a*2U11 + ... + 2 h k a* b* U12 ]

______________________________________________________________________________

U11	U22	U33	U23	U13	U12

______________________________________________________________________________

Re(1)	76(1) 	63(1)	54(1) 	2(1)	15(1) 	6(1)

O(4)	111(3) 	89(3)	62(3) 	19(2)	35(2) 	15(2)

O(2)	70(2) 	126(3)	57(3) 	20(2)	16(2) 	13(2)

C(17)	74(4) 	85(5)	59(5) 	10(4)	6(3) 	2(4)

C(42)	97(5) 	72(4)	93(6) 	-10(4)	17(4) 	1(3)

O(5)	79(2) 	68(2)	45(3) 	1(2)	19(2) 	-9(2)

C(15)	113(5) 	91(5)	64(5) 	28(4)	23(4) 	18(4)

N(1)	64(3) 	66(3)	50(3) 	7(2)	14(2) 	10(2)

C(43)	85(5) 	67(4)	79(5) 	5(3)	11(4) 	11(4)

O(3)	95(3) 	88(3)	77(3) 	10(2)	24(2) 	13(2)

C(14)	73(4) 	84(5)	46(4) 	12(4)	10(3) 	6(3)

C(18)	87(5) 	74(4)	54(5) 	10(3)	20(4) 	7(3)

C(5)	88(4) 	81(4)	53(4) 	3(3)	3(3) 	4(3)

C(25)	60(3) 	63(4)	44(4) 	4(3)	15(3) 	11(3)

C(11)	59(4) 	101(5)	50(4) 	12(4)	8(3) 	5(3)

C(41)	95(5) 	78(4)	69(5) 	1(3)	10(4) 	11(4)

C(10)	75(4) 	72(4)	57(5) 	12(3)	7(4) 	1(3)

C(30)	59(3) 	54(3)	49(4) 	3(3)	6(3) 	7(2)

C(7)	75(4) 	79(4)	48(4) 	8(3)	10(3) 	3(3)

C(29)	68(4) 	53(3)	49(4) 	8(3)	7(3) 	-4(3)

O(1)	98(3) 	129(4)	61(3) 	10(2)	7(2) 	38(3)

C(13)	91(4) 	84(5)	56(5) 	9(3)	16(4) 	6(3)

O(7)	94(3) 	153(4)	110(4) 	-2(3)	-20(3) 	12(3)

C(9)	63(3) 	78(4)	60(4) 	3(3)	8(3) 	-6(3)

O(8)	146(4) 	71(3)	118(4) 	20(3)	14(3) 	-7(3)

C(28)	61(3) 	63(4)	46(4) 	-1(3)	5(3) 	4(3)

C(26)	89(4) 	49(4)	65(4) 	9(3)	13(3) 	8(3)

C(44)	90(4) 	72(4)	75(5) 	-3(4)	6(3) 	13(3)

C(35)	89(4) 	67(4)	46(4) 	-6(3)	3(3) 	4(3)

C(16)	110(5) 	100(5)	60(5) 	18(4)	23(4) 	30(4)

C(24)	61(3) 	62(4)	64(4) 	12(3)	7(3) 	8(3)

O(9)	97(4) 	133(4)	111(4) 	15(3)	-21(3) 	11(3)

O(6)	101(3) 	140(4)	68(3) 	3(2)	0(2) 	-51(3)

C(38)	107(5) 	72(4)	52(4) 	0(3)	12(4) 	7(3)

C(34)	91(4) 	69(4)	39(4) 	4(3)	13(3) 	3(3)

C(21)	67(4) 	67(4)	51(4) 	3(3)	11(3) 	12(3)

O(10)	145(4) 	126(4)	112(4) 	-43(3)	54(3) 	-1(3)

C(33)	92(4) 	74(4)	43(4) 	-6(3)	6(3) 	-3(3)

C(12)	83(4) 	85(5)	63(5) 	11(4)	15(3) 	-7(3)

C(23)	67(4) 	148(6)	85(6) 	38(4)	12(4) 	17(4)

C(27)	86(4) 	59(4)	52(4) 	-5(3)	15(3) 	9(3)

C(36)	96(4) 	72(4)	41(4) 	3(3)	9(3) 	4(3)

C(6)	89(4) 	78(4)	53(4) 	3(3)	8(3) 	10(3)

C(8)	85(4) 	76(4)	53(4) 	7(3)	11(3) 	1(3)

C(22)	83(5) 	156(6)	53(5) 	38(4)	9(4) 	28(4)

C(31)	86(5) 	64(4)	46(4) 	0(3)	7(4) 	4(3)

C(32)	82(4) 	62(3)	41(4) 	4(3)	13(3) 	-3(3)

C(3)	91(4) 	85(4)	60(5) 	-5(3)	0(3) 	2(3)

C(37)	94(4) 	76(4)	46(4) 	-5(3)	7(3) 	4(3)

C(4)	96(4) 	75(4)	56(4) 	-1(3)	5(3) 	8(3)

C(20)	65(4) 	117(5)	60(4) 	27(4)	11(4) 	13(3)

C(1)	112(5) 	177(7)	58(5) 	-11(4)	3(4) 	0(5)

C(19)	84(5) 	132(5)	55(5) 	31(4)	-1(4) 	6(4)

C(2)	117(5) 	107(5)	63(5) 	-7(4)	-3(4) 	5(4)

C(39)	147(6) 	95(5)	41(4) 	-5(3)	-1(4) 	7(4)

C(40)	201(7) 	87(5)	54(5) 	-1(3)	11(5) 	15(4)

______________________________________________________________________________

Table 5.   Hydrogen coordinates ( x 104) and isotropic displacement parameters (Å2x 103)

for M2.

______________________________________________________________________________

x 	y 	z 	U(eq)

______________________________________________________________________________

H(15)	5677	7778	-733	107

H(5A)	11544	10366	-2582	89

H(5B)	10215	9200	-2635	89

H(7A)	10712	10394	-2140	80

H(7B)	9481	9175	-2203	80

H(29)	-1969	5194	1128	68

H(13)	4886	11780	-780	92

H(9A)	9867	10265	-1704	80

H(9B)	8736	9004	-1778	80

H(26)	-1096	9763	987	81

H(35A)	-4639	8204	2543	81

H(35B)	-3371	6996	2598	81

H(16)	7237	7825	-1082	107

H(24)	375	9181	596	75

H(38A)	-7673	7112	3154	92

H(38B)	-6363	5953	3225	92

H(34A)	-6133	6878	2264	79

H(34B)	-4854	5675	2319	79

H(33A)	-3839	8160	2104	84

H(33B)	-2563	6954	2158	84

H(12)	6497	11859	-1124	92

H(23)	5284	7731	-7	120

H(27)	-2475	9084	1329	79

H(36A)	-6935	6937	2710	84

H(36B)	-5641	5747	2769	84

H(6A)	9345	11707	-2421	88

H(6B)	7998	10553	-2477	88

H(8A)	8379	11592	-1972	85

H(8B)	7127	10386	-2038	85

H(22)	3972	7190	351	117

H(32A)	-5286	6899	1820	74

H(32B)	-4104	5641	1880	74

H(3A)	12347	10210	-3030	95

H(3B)	10942	9084	-3071	95

H(37A)	-5381	8332	2975	86

H(37B)	-4126	7125	3037	86

H(4A)	10285	11664	-2872	91

H(4B)	8848	10569	-2919	91

H(20)	-564	8348	96	97

H(1A)	13089	9954	-3479	174

H(1B)	11564	10247	-3664	174

H(1C)	11606	8880	-3520	174

H(19)	728	8826	-262	109

H(2A)	11062	11494	-3318	115

H(2B)	9604	10406	-3355	115

H(39A)	-6153	8596	3407	113

H(39B)	-4872	7423	3479	113

H(40A)	-8424	7403	3600	171

H(40B)	-6902	7780	3781	171

H(40C)	-7076	6290	3683	171

______________________________________________________________________________