|  | University of Southampton · Department of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	00sot036

Empirical formula 	C16H17F3O2

Formula weight 	298.30

Temperature 	293(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P21/c

Unit cell dimensions	a = 9.2288(18) Å	( = 90°

b = 20.362(4) Å	( = 91.00(3)°

c = 7.6375(15) Å	(  = 90°

Volume	1435.0(5) Å3

Z	4

Density (calculated)	1.381 Mg / m3

Absorption coefficient	0.115 mm(1

F(000)	624

Crystal	plate; colourless

Crystal size	0.25 ( 0.20 ( 0.05 mm3

( range for data collection	2.98 ( 27.50°

Index ranges	(11 ( h ( 11, (26 ( k ( 26, (9 ( l ( 9

Reflections collected	13593

Independent reflections	3244 [Rint = 0.0734]

Completeness to ( = 27.50°	98.7 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.9943 and 0.9717

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	3244 / 0 / 190

Goodness-of-fit on F2	1.136

Final R indices [F2 > 2((F2)]	R1 = 0.0571, wR2 = 0.1599

R indices (all data)	R1 = 0.0860, wR2 = 0.1774

Largest diff. peak and hole	0.511 and (0.253 e Å(3

Diffractometer: Enraf Nonius KappaCCD area detector (( scans and ( scans to fill Ewald sphere). Data collection and cell

refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography,

part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing,

Acta Cryst. A51 (1995) 33(37; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421(426). Program used to solve structure:

SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Program used to refine structure: SHELXL97 (G. M. Sheldrick

(1997), University of Göttingen, Germany).

Further information:  http://www.soton.ac.uk/~xservice/strat.htm

Special details:

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

F1	6597(2)	2792(1)	5120(2)	49(1)	1

F2	5580(1)	3519(1)	3472(2)	47(1)	1

F3	7784(1)	3256(1)	3077(2)	48(1)	1

O1	4350(2)	4916(1)	7746(2)	36(1)	1

O2	7713(2)	4456(1)	4591(2)	37(1)	1

C1	5974(2)	4074(1)	6750(2)	30(1)	1

C2	5264(2)	3553(1)	7841(3)	37(1)	1

C3	4439(2)	3876(1)	9308(3)	39(1)	1

C4	3503(2)	4417(1)	8597(3)	41(1)	1

C5	5521(2)	4693(1)	6842(2)	31(1)	1

C6	7261(2)	3914(1)	5601(2)	30(1)	1

C7	6815(2)	3370(1)	4309(3)	36(1)	1

C8	8591(2)	3698(1)	6746(3)	32(1)	1

C9	8991(2)	4230(1)	8044(3)	38(1)	1

C10	9085(3)	4135(1)	9732(3)	53(1)	1

C11	9892(2)	3480(1)	5705(2)	32(1)	1

C12	10269(2)	2821(1)	5707(3)	39(1)	1

C13	11454(3)	2600(1)	4781(4)	53(1)	1

C14	12294(2)	3039(1)	3886(3)	51(1)	1

C15	11946(3)	3691(1)	3883(3)	50(1)	1

C16	10752(2)	3914(1)	4797(3)	42(1)	1

Table 3. Bond lengths [Å] and angles [°].

F1(C7	1.347(2)

F2(C7	1.332(2)

F3(C7	1.330(2)

O1(C5	1.371(2)

O1(C4	1.444(3)

O2(C6	1.414(2)

C1(C5	1.330(3)

C1(C2	1.507(3)

C1(C6	1.524(3)

C2(C3	1.516(3)

C3(C4	1.496(3)

C6(C7	1.534(3)

C6(C8	1.558(3)

C8(C9	1.510(3)

C8(C11	1.518(3)

C9(C10	1.305(3)

C11(C16	1.383(3)

C11(C12	1.387(3)

C12(C13	1.388(3)

C13(C14	1.372(4)

C14(C15	1.367(4)

C15(C16	1.391(3)

C5(O1(C4	115.54(15)

C5(C1(C2	119.88(18)

C5(C1(C6	118.84(17)

C2(C1(C6	121.21(16)

C1(C2(C3	109.41(16)

C4(C3(C2	110.20(17)

O1(C4(C3	111.61(17)

C1(C5(O1	126.32(18)

O2(C6(C1	112.78(15)

O2(C6(C7	106.88(15)

C1(C6(C7	108.78(16)

O2(C6(C8	106.85(15)

C1(C6(C8	110.59(15)

C7(C6(C8	110.91(15)

F3(C7(F2	106.28(16)

F3(C7(F1	106.26(16)

F2(C7(F1	106.59(17)

F3(C7(C6	113.91(17)

F2(C7(C6	111.25(16)

F1(C7(C6	112.07(16)

C9(C8(C11	111.52(16)

C9(C8(C6	110.31(15)

C11(C8(C6	114.28(16)

C10(C9(C8	123.6(2)

C16(C11(C12	118.2(2)

C16(C11(C8	122.87(18)

C12(C11(C8	118.87(18)

C11(C12(C13	120.8(2)

C14(C13(C12	120.1(2)

C15(C14(C13	119.9(2)

C14(C15(C16	120.3(2)

C11(C16(C15	120.7(2)

Symmetry transformations used to generate equivalent atoms:

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

F1	68(1) 	31(1)	47(1) 	(7(1)	(1(1) 	(7(1)

F2	37(1) 	61(1)	42(1) 	(11(1)	(10(1) 	(1(1)

F3	41(1) 	67(1)	36(1) 	(15(1)	1(1) 	2(1)

O1	40(1) 	35(1)	34(1) 	1(1)	3(1) 	10(1)

O2	35(1) 	37(1)	39(1) 	13(1)	0(1) 	1(1)

C1	31(1) 	32(1)	27(1) 	2(1)	(3(1) 	0(1)

C2	37(1) 	34(1)	42(1) 	5(1)	4(1) 	(2(1)

C3	41(1) 	40(1)	35(1) 	3(1)	6(1) 	(2(1)

C4	37(1) 	47(1)	39(1) 	1(1)	7(1) 	4(1)

C5	33(1) 	30(1)	30(1) 	2(1)	1(1) 	2(1)

C6	32(1) 	28(1)	30(1) 	4(1)	0(1) 	(1(1)

C7	33(1) 	43(1)	31(1) 	(4(1)	0(1) 	4(1)

C8	32(1) 	28(1)	35(1) 	2(1)	(1(1) 	1(1)

C9	38(1) 	39(1)	38(1) 	(5(1)	(7(1) 	1(1)

C10	60(2) 	56(1)	41(1) 	(4(1)	(7(1) 	0(1)

C11	29(1) 	33(1)	33(1) 	(4(1)	(3(1) 	0(1)

C12	36(1) 	38(1)	43(1) 	3(1)	(1(1) 	7(1)

C13	42(1) 	55(1)	64(2) 	(5(1)	(2(1) 	15(1)

C14	27(1) 	71(2)	53(1) 	(13(1)	2(1) 	3(1)

C15	34(1) 	66(2)	50(1) 	(9(1)	7(1) 	(15(1)

C16	38(1) 	40(1)	48(1) 	(3(1)	2(1) 	(5(1)

Table 5. Hydrogen coordinates [( 104] and isotropic displacement parameters [Å2 ( 103].

Atom 	x	y	z	Ueq	S.o.f.

H2	7044	4575	3946	55	1

H2A	5996	3260	8328	45	1

H2B	4605	3296	7114	45	1

H3A	3841	3551	9881	47	1

H3B	5118	4052	10170	47	1

H4A	2806	4236	7763	49	1

H4B	2969	4614	9546	49	1

H5	6051	5005	6235	37	1

H8	8282	3317	7429	38	1

H9	9181	4648	7617	46	1

H10A	8901	3721	10195	63	1

H10B	9336	4481	10473	63	1

H12	9720	2523	6336	47	1

H13	11680	2155	4767	64	1

H14	13099	2892	3282	61	1

H15	12510	3987	3266	60	1

H16	10531	4360	4797	50	1