|  | University of Southampton · School of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement details.

Identification code 	2009src0893c

Empirical formula 	C31H32BNO2

Formula weight 	461.39

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Orthorhombic

Space group 	Pnma

Unit cell dimensions	a = 19.3041(7) Å	( = 90°

b = 13.1353(5) Å	( = 90°

c = 10.1462(3) Å	(  = 90°

Volume	2572.72(16) Å3

Z	4

Density (calculated)	1.191 Mg / m3

Absorption coefficient	0.073 mm(1

F(000)	984

Crystal	Cut Block; colourless

Crystal size	0.48 ( 0.34 ( 0.16 mm3

( range for data collection	3.30 ( 25.00°

Index ranges	(22 ( h ( 22, (15 ( k ( 14, (12 ( l ( 10

Reflections collected	18899

Independent reflections	2360 [Rint = 0.0416]

Completeness to ( = 25.00°	99.4 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.9885 and 0.9659

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	2360 / 0 / 212

Goodness-of-fit on F2	1.058

Final R indices [F2 > 2((F2)]	R1 = 0.0699, wR2 = 0.1670

R indices (all data)	R1 = 0.0769, wR2 = 0.1720

Largest diff. peak and hole	0.499 and (0.610 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SADABS (Sheldrick, G. M. (2007). SADABS. Version 2007/2. Bruker AXS Inc., Madison, Wisconsin, USA.). Structure solution: SHELXS97 (Sheldrick, G.M. (2008). Acta Cryst. A64, 112-122.). Structure refinement: SHELXL97 (G Sheldrick, G.M. (2008). Acta Cryst. A64, 112-122.). Graphics: CAMERON (Watkin, D. M., Pearce, L. & Prout, C. K. (1993). Chemical Crystallography Lab, University of Oxford)

Special details:

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C1	(2256(2)	(7838(4)	(827(5)	34(1)	0.50

C2	(2016(2)	(7347(15)	(2113(5)	38(4)	0.50

C3	(1082(2)	(7968(4)	(739(4)	28(1)	0.50

C4	(481(2)	(8608(4)	(1119(4)	29(1)	0.50

C5	(565(3)	(8771(4)	(2597(5)	31(1)	0.50

C6	(856(2)	(7784(3)	(3082(4)	26(1)	0.50

C7	(983(3)	(6218(4)	(1721(5)	32(1)	0.50

N1	(1234(2)	(7281(3)	(1972(3)	24(1)	0.50

O1	(1687(2)	(8538(3)	(602(3)	33(1)	0.50

O2	(835(3)	(7483(10)	(4274(5)	124(3)	1

C8	79(2)	(7500	2393(3)	20(1)	1

C9	(314(1)	(8401(2)	2381(2)	25(1)	1

C10	(1035(1)	(8406(2)	2404(2)	30(1)	1

C11	(1402(2)	(7500	2428(3)	31(1)	1

C12	1102(2)	(7500	727(3)	22(1)	1

C13	1145(2)	(6618(2)	(13(3)	51(1)	1

C14	1195(2)	(6615(2)	(1384(3)	61(1)	1

C15	1213(2)	(7500	(2081(3)	37(1)	1

C16	1266(1)	(6521(2)	3107(2)	23(1)	1

C17	1899(1)	(6074(2)	2754(2)	31(1)	1

C18	2214(1)	(5321(2)	3513(3)	43(1)	1

C19	1904(2)	(4977(2)	4660(3)	44(1)	1

C20	1278(2)	(5397(2)	5040(2)	41(1)	1

C21	972(1)	(6154(2)	4286(2)	32(1)	1

B1	931(2)	(7500	2319(3)	22(1)	1

Table 3. Bond lengths [Å] and angles [°].

C1(O1	1.451(5)

C1(C2	1.527(10)

C1(H1A	0.9900

C1(H1B	0.9900

C2(N1	1.520(5)

C2(H2A	0.9900

C2(H2B	0.9900

C3(O1	1.394(5)

C3(C4	1.483(6)

C3(N1	1.570(5)

C3(H3	1.0000

C4(C5	1.523(6)

C4(H4A	0.9900

C4(H4B	0.9900

C5(C6	1.496(6)

C5(H5A	0.9900

C5(H5B	0.9900

C6(O2	1.273(8)

C6(N1	1.496(5)

C7(N1	1.499(5)

C7(H7A	0.9800

C7(H7B	0.9800

C7(H7C	0.9800

C8(C9	1.405(3)

C8(C9i	1.405(3)

C8(B1	1.647(4)

C9(C10	1.392(3)

C9(H9	0.9500

C10(C11	1.386(3)

C10(H10	0.9500

C11(C10i	1.386(3)

C11(H11	0.9500

C12(C13i	1.383(3)

C12(C13	1.383(3)

C12(B1	1.648(4)

C13(C14	1.395(4)

C13(H13	0.9500

C14(C15	1.361(4)

C14(H14	0.9500

C15(C14i	1.361(4)

C15(H15	0.9500

C16(C17	1.402(3)

C16(C21	1.409(3)

C16(B1	1.647(3)

C17(C18	1.393(3)

C17(H17	0.9500

C18(C19	1.385(4)

C18(H18	0.9500

C19(C20	1.384(4)

C19(H19	0.9500

C20(C21	1.386(3)

C20(H20	0.9500

C21(H21	0.9500

B1(C16i	1.647(3)

O1(C1(C2	100.0(5)

O1(C1(H1A	111.8

C2(C1(H1A	111.8

O1(C1(H1B	111.8

C2(C1(H1B	111.8

H1A(C1(H1B	109.5

N1(C2(C1	104.1(5)

N1(C2(H2A	110.9

C1(C2(H2A	110.9

N1(C2(H2B	110.9

C1(C2(H2B	110.9

H2A(C2(H2B	108.9

O1(C3(C4	112.2(4)

O1(C3(N1	103.5(3)

C4(C3(N1	105.3(3)

O1(C3(H3	111.8

C4(C3(H3	111.8

N1(C3(H3	111.8

C3(C4(C5	104.6(4)

C3(C4(H4A	110.8

C5(C4(H4A	110.8

C3(C4(H4B	110.8

C5(C4(H4B	110.8

H4A(C4(H4B	108.9

C6(C5(C4	104.0(4)

C6(C5(H5A	111.0

C4(C5(H5A	111.0

C6(C5(H5B	111.0

C4(C5(H5B	111.0

H5A(C5(H5B	109.0

O2(C6(C5	124.7(7)

O2(C6(N1	126.4(6)

C5(C6(N1	108.6(3)

C6(N1(C7	112.5(3)

C6(N1(C2	112.9(5)

C7(N1(C2	113.0(8)

C6(N1(C3	104.7(3)

C7(N1(C3	109.9(3)

C2(N1(C3	103.1(5)

C3(O1(C1	106.1(3)

C9(C8(C9i	114.7(3)

C9(C8(B1	122.56(14)

C9i(C8(B1	122.56(14)

C10(C9(C8	122.9(2)

C10(C9(H9	118.5

C8(C9(H9	118.5

C11(C10(C9	120.5(2)

C11(C10(H10	119.8

C9(C10(H10	119.8

C10i(C11(C10	118.5(3)

C10i(C11(H11	120.8

C10(C11(H11	120.8

C13i(C12(C13	113.8(3)

C13i(C12(B1	122.95(15)

C13(C12(B1	122.95(15)

C12(C13(C14	123.3(3)

C12(C13(H13	118.4

C14(C13(H13	118.4

C15(C14(C13	121.1(3)

C15(C14(H14	119.4

C13(C14(H14	119.4

C14i(C15(C14	117.4(3)

C14i(C15(H15	121.3

C14(C15(H15	121.3

C17(C16(C21	115.1(2)

C17(C16(B1	123.1(2)

C21(C16(B1	121.4(2)

C18(C17(C16	122.4(2)

C18(C17(H17	118.8

C16(C17(H17	118.8

C19(C18(C17	120.5(2)

C19(C18(H18	119.7

C17(C18(H18	119.7

C20(C19(C18	118.8(2)

C20(C19(H19	120.6

C18(C19(H19	120.6

C19(C20(C21	120.2(2)

C19(C20(H20	119.9

C21(C20(H20	119.9

C20(C21(C16	122.9(2)

C20(C21(H21	118.6

C16(C21(H21	118.6

C8(B1(C16	111.76(17)

C8(B1(C16i	111.76(17)

C16(B1(C16i	102.6(2)

C8(B1(C12	104.2(2)

C16(B1(C12	113.40(17)

C16i(B1(C12	113.40(17)

Symmetry transformations used to generate equivalent atoms:

(i) x,(y(3/2,z

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C1	24(2) 	43(3)	33(2) 	6(2)	(6(2) 	5(2)

C2	25(2) 	51(11)	36(2) 	8(3)	(1(2) 	3(3)

C3	35(2) 	29(2)	19(2) 	5(2)	(2(2) 	(2(2)

C4	25(2) 	33(2)	30(2) 	5(2)	(5(2) 	4(2)

C5	35(2) 	28(2)	30(3) 	(5(2)	(1(2) 	6(2)

C6	34(2) 	30(3)	13(2) 	(3(2)	(2(2) 	1(2)

C7	41(3) 	24(2)	31(3) 	(2(2)	(3(2) 	(2(2)

N1	28(2) 	21(4)	24(2) 	1(1)	(2(1) 	(1(1)

O1	27(2) 	36(2)	36(2) 	9(2)	0(1) 	(5(1)

O2	115(4) 	187(6)	69(3) 	(61(6)	13(3) 	(100(6)

C8	29(2) 	20(1)	11(1) 	0	2(1) 	0

C9	32(1) 	20(1)	21(1) 	3(1)	(1(1) 	(1(1)

C10	34(1) 	32(1)	24(1) 	7(1)	(2(1) 	(9(1)

C11	27(2) 	45(2)	22(2) 	0	1(1) 	0

C12	19(1) 	27(2)	20(2) 	0	0(1) 	0

C13	101(2) 	27(1)	24(1) 	1(1)	(5(1) 	(8(2)

C14	105(3) 	51(2)	26(1) 	15(1)	(6(2) 	(29(2)

C15	26(2) 	66(3)	19(2) 	0	4(1) 	0

C16	30(1) 	17(1)	21(1) 	3(1)	(5(1) 	1(1)

C17	29(1) 	25(1)	39(1) 	(1(1)	(4(1) 	0(1)

C18	33(1) 	34(1)	63(2) 	2(1)	(14(1) 	(8(1)

C19	60(2) 	30(1)	42(2) 	(4(1)	(27(1) 	(8(1)

C20	66(2) 	31(1)	25(1) 	(4(1)	(10(1) 	(8(1)

C21	46(1) 	28(1)	22(1) 	(2(1)	(2(1) 	(9(1)

B1	28(2) 	19(2)	18(2) 	0	1(1) 	0