|  | University of Southampton · Department of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	00src325

Empirical formula 	H5ClO6

Formula weight 	136.49

Temperature 	150(2) K

Wavelength 	0.71073 Å

Crystal system 	Orthorhombic

Space group 	Pna21

Unit cell dimensions	a = 7.9054(3) Å	( = 90°

b = 10.5443(4) Å	( = 90°

c = 5.9511(2) Å	(  = 90°

Volume	496.07(3) Å3

Z	4

Density (calculated)	1.828 Mg / m3

Absorption coefficient	0.706 mm(1

F(000)	280

Crystal	Block; colourless

Crystal size	0.25 ( 0.25 ( 0.15 mm3

( range for data collection	3.22 ( 25.09°

Index ranges	(9 ( h ( 9, (12 ( k ( 12, (5 ( l ( 7

Reflections collected	2344

Independent reflections	716 [Rint = 0.0335]

Completeness to ( = 25.09°	98.6 %

Max. and min. transmission	0.9014 and 0.8432

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	716 / 7 / 78

Goodness-of-fit on F2	1.663

Final R indices [F2 > 2((F2)]	R1 = 0.0374, wR2 = 0.0970

R indices (all data)	R1 = 0.0376, wR2 = 0.0971

Absolute structure parameter	0.5(2)

Extinction coefficient	0.105(16)

Largest diff. peak and hole	0.472 and (0.398 e Å(3

Diffractometer: Enraf Nonius KappaCCD area detector (( scans and ( scans to fill Ewald sphere). Data collection and cell

refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography,

part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing,

Acta Cryst. A51 (1995) 33(37; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421(426). Program used to solve structure:

SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Program used to refine structure: SHELXL97 (G. M. Sheldrick

(1997), University of Göttingen, Germany).

Further information:  http://www.soton.ac.uk/~xservice/strat.htm

Special details:

Hydrogen bonds (Table 6).

The structure was refined as a racemic twin (final BASF factor:  0.5(2))

An alternative refinement was tried in the centrosymmetric space group Pnma (disorder of two O positions in the ClO4 molecule)

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

Cl1	2573(1)	4231(1)	2448(3)	8(1)	1

O1	2119(4)	5588(3)	2175(7)	11(1)	1

O2	4391(4)	4052(3)	2067(6)	14(1)	1

O3	1599(4)	3459(3)	828(6)	11(1)	1

O4	2125(4)	3835(3)	4753(5)	11(1)	1

O5	180(4)	8006(3)	2565(9)	25(1)	1

O6	1821(4)	6045(3)	7438(9)	26(1)	1

Table 3. Bond lengths [Å] and angles [°].

Cl1(O2	1.467(3)

Cl1(O4	1.477(4)

Cl1(O3	1.478(4)

Cl1(O1	1.484(3)

O2(Cl1(O4	110.0(2)

O2(Cl1(O3	109.8(2)

O4(Cl1(O3	109.0(2)

O2(Cl1(O1	110.14(18)

O4(Cl1(O1	108.4(2)

O3(Cl1(O1	109.5(2)

Symmetry transformations used to generate equivalent atoms:

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

Cl1	9(1) 	9(1)	7(1) 	(1(1)	(1(1) 	1(1)

O1	16(1) 	6(1)	12(2) 	3(2)	(2(2) 	1(1)

O2	6(1) 	21(2)	15(2) 	(4(2)	2(1) 	4(1)

O3	15(2) 	11(2)	8(2) 	(4(2)	(4(2) 	(1(1)

O4	18(2) 	12(2)	3(2) 	2(1)	3(2) 	(3(1)

O5	27(2) 	20(2)	28(2) 	6(2)	5(2) 	1(1)

O6	25(2) 	23(2)	30(2) 	0(2)	5(2) 	4(1)

Table 5. Hydrogen coordinates [( 104] and isotropic displacement parameters [Å2 ( 103].

Atom 	x	y	z	Ueq	S.o.f.

H1	(910(30)	8440(30)	2750(100)	30	1

H2	920(50)	8340(40)	1380(70)	30	1

H3	160(50)	7078(10)	2720(110)	30	1

H4	806	6293	7161	31	1

H5	2068	5521	6430	31	1

Table 6. Hydrogen bonds [Å and °].

D(H···A	d(D(H)	d(H···A)	d(D···A)	((DHA)

O5(H1...O1i	0.979(8)	1.899(18)	2.847(4)	162(5)

O5(H2...O4ii	0.982(8)	1.896(18)	2.847(5)	162(4)

O5(H3...O1	0.983(8)	2.23(3)	2.984(4)	132(3)

O6(H4...O3iii	0.86	2.08	2.916(5)	165.0

O6(H5...O4	0.84	2.04	2.835(5)	158.3

Symmetry transformations used to generate equivalent atoms:

(i) x(1/2,(y+3/2,z    (ii) (x+1/2,y+1/2,z(1/2    (iii) (x,(y+1,z+1/2