|  | University of Southampton · Department of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1.  Crystal data and structure refinement.

Identification code 	00src612

Compound 	Na6(Si3O6C18H33)2  · 18 H2O

Empirical formula 	C36H102Na6O30Si6

Formula weight 	1321.66

Temperature 	150(2) K

Wavelength 	0.71073 Å

Crystal system 	Triclinic

Space group 	P1

Unit cell dimensions	a = 9.16150(10) Å	( = 88.5860(10)°

b = 10.1143(2) Å	( = 80.2380(10)°

c = 18.1371(5) Å	(  = 70.995(2)°

Volume	1565.16(6) Å3

Z	1

Density (calculated)	1.402 Mg / m3

Absorption coefficient	0.256 mm(1

F(000)	708

Crystal	block; colourless

Crystal size	0.15 ( 0.10 ( 0.10 mm3

( range for data collection	3.00 ( 26.00°

Index ranges	(10 ( h ( 11, (12 ( k ( 12, (16 ( l ( 22

Reflections collected	10149

Independent reflections	7727 [Rint = 0.0314]

Completeness to ( = 26.00°	95.8 %

Max. and min. transmission	0.9748 and 0.9626

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	7727 / 3 / 759

Goodness-of-fit on F2	0.935

Final R indices [F2 > 2((F2)]	R1 = 0.0338, wR2 = 0.0866

R indices (all data)	R1 = 0.0389, wR2 = 0.0895

Absolute structure parameter	0.28(10)

Extinction coefficient	0.0026(9)

Largest diff. peak and hole	0.324 and (0.337 e Å(3

Diffractometer: Enraf Nonius KappaCCD area detector (( scans and ( scans to fill Ewald sphere). Data collection and cell

refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography,

part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing,

Acta Cryst. A51 (1995) 33(37; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421(426). Program used to solve structure:

SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Program used to refine structure: SHELXL97 (G. M. Sheldrick

(1997), University of Göttingen, Germany).

Further information:  http://www.soton.ac.uk/~xservice/strat.htm

Special details:

The asymmetric unit contains two Si3O6C18H33 molecules, 6 Na and 18 H2O. The arrangement of the two independent Si3O6C18H33 molecules shows approximate inversion symmetry. These molecules are arranged in chains that extend along the crystallographic a and b axes, with their oxo-O's face-to-face. They are connected to the polymeric nNa · 3n H2O core via O4 and O3 (molecule 1) and O7, O8, O9, O11, O12 (molecule 2). Thus, the molecules are infinite 2D-networks that extend parallel to the crystallographic (001) plane. The two "surfaces" of each plane are dominated by the cyclohexane groups. The coordination numbers of the Na atoms are Na1[6], Na2[5+1], Na3[6+1], Na4[6+1], Na5[6] and Na6[6]. The networks are supported by a number of hydrogen bonds (Table 5).

Due to the chemical content of the compound, the absolute structure cannot be determined reliably, the refined Flack-parameter might also suggest a racemic twin.

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

Si1	10367(1)	9712(1)	4721(1)	11(1)	1

Si2	13889(1)	8692(1)	4519(1)	11(1)	1

Si3	12168(1)	6578(1)	4626(1)	11(1)	1

O1	9208(3)	10366(3)	5474(1)	13(1)	1

O2	12125(3)	9863(3)	4680(1)	15(1)	1

O3	14979(3)	8920(3)	5065(1)	16(1)	1

O4	13640(3)	7152(3)	4698(1)	13(1)	1

O5	11975(3)	5568(3)	5295(1)	14(1)	1

O6	10639(3)	8021(3)	4659(1)	13(1)	1

C10	9553(4)	10550(4)	3882(2)	16(1)	1

C11	10277(5)	9800(5)	3132(2)	26(1)	1

C12	9462(5)	10566(5)	2502(2)	27(1)	1

C13	9460(5)	12064(5)	2465(2)	29(1)	1

C14	8749(6)	12830(5)	3220(2)	38(1)	1

C15	9574(6)	12076(5)	3836(2)	33(1)	1

C20	14706(4)	8616(4)	3499(2)	14(1)	1

C21	15084(5)	9901(4)	3187(2)	21(1)	1

C22	15540(6)	9780(5)	2340(2)	30(1)	1

C23	16898(6)	8456(5)	2090(2)	32(1)	1

C24	16584(5)	7141(5)	2409(2)	28(1)	1

C25	16116(5)	7298(4)	3262(2)	22(1)	1

C30	12560(4)	5767(4)	3672(2)	13(1)	1

C31	11146(4)	5525(4)	3421(2)	20(1)	1

C32	11552(5)	5007(5)	2602(2)	29(1)	1

C33	12960(5)	3677(5)	2475(2)	28(1)	1

C34	14377(5)	3859(5)	2749(2)	30(1)	1

C35	13948(5)	4399(4)	3566(2)	20(1)	1

Si4	7746(1)	9691(1)	8571(1)	11(1)	1

Si5	5990(1)	7613(1)	8622(1)	11(1)	1

Si6	9498(1)	6537(1)	8487(1)	11(1)	1

O7	8063(3)	10706(3)	7927(1)	15(1)	1

O8	6303(3)	9121(3)	8437(1)	12(1)	1

O9	4998(3)	7363(3)	8034(1)	15(1)	1

O10	7745(3)	6410(3)	8511(1)	13(1)	1

O11	10654(3)	5924(3)	7720(1)	14(1)	1

O12	9255(3)	8240(3)	8557(1)	13(1)	1

C40	7270(4)	10492(4)	9530(2)	15(1)	1

C41	5892(4)	11873(4)	9620(2)	19(1)	1

C42	5429(5)	12434(5)	10424(2)	26(1)	1

C43	6819(5)	12629(5)	10705(2)	28(1)	1

C44	8222(5)	11278(5)	10613(2)	24(1)	1

C45	8670(4)	10716(4)	9806(2)	18(1)	1

C50	5093(4)	7727(4)	9626(2)	14(1)	1

C51	3666(4)	9025(4)	9863(2)	20(1)	1

C52	3166(5)	9156(5)	10719(2)	27(1)	1

C53	2840(5)	7860(5)	11031(2)	32(1)	1

C54	4235(5)	6548(5)	10786(2)	30(1)	1

C55	4730(5)	6413(5)	9925(2)	22(1)	1

C60	10315(4)	5646(4)	9307(2)	15(1)	1

C61	9551(5)	6400(5)	10078(2)	23(1)	1

C62	10354(5)	5606(5)	10705(2)	26(1)	1

C63	10368(5)	4104(5)	10725(2)	25(1)	1

C64	11097(5)	3345(5)	9978(2)	29(1)	1

C65	10284(5)	4158(4)	9345(2)	24(1)	1

Na1	20021(2)	3106(2)	6594(1)	16(1)	1

Na2	5583(2)	9329(2)	7203(1)	27(1)	1

Na3	10488(2)	8331(2)	7203(1)	20(1)	1

Na4	15196(2)	6567(2)	5654(1)	22(1)	1

Na5	13959(2)	2169(2)	6264(1)	17(1)	1

Na6	16025(2)	3951(2)	6880(1)	18(1)	1

O13	19616(3)	5551(3)	6458(1)	16(1)	1

O14	21966(3)	3203(3)	7263(1)	17(1)	1

O15	17964(3)	3455(3)	7702(1)	19(1)	1

O16	21999(3)	2760(3)	5474(2)	23(1)	1

O17	17901(3)	7414(3)	5106(2)	26(1)	1

O18	17501(3)	5072(3)	4811(2)	29(1)	1

O19	14670(3)	4159(3)	5762(2)	21(1)	1

O20	16396(3)	6192(3)	6683(1)	16(1)	1

O21	12690(3)	6958(3)	6419(1)	21(1)	1

O22	12050(3)	8818(3)	8054(2)	23(1)	1

O23	20349(3)	648(3)	6735(1)	16(1)	1

O24	18111(3)	3063(3)	5898(1)	17(1)	1

O25	3729(3)	9933(3)	6452(1)	18(1)	1

O26	8253(3)	8668(3)	6529(1)	22(1)	1

O27	16021(3)	1196(3)	5271(2)	23(1)	1

O28	15618(3)	1777(3)	7263(2)	29(1)	1

O29	13828(3)	5262(3)	7692(2)	27(1)	1

O30	2882(4)	11090(3)	8230(2)	36(1)	1

Table 3. Bond lengths [Å] and angles [°].

Si1(O1	1.590(3)

Si1(O6	1.649(3)

Si1(O2	1.656(2)

Si1(C10	1.870(4)

Si2(O3	1.590(3)

Si2(O2	1.646(3)

Si2(O4	1.664(3)

Si2(C20	1.868(4)

Si3(O5	1.590(3)

Si3(O6	1.655(3)

Si3(O4	1.657(2)

Si3(C30	1.861(4)

O3(Na4	2.546(3)

O4(Na4	2.372(3)

C10(C11	1.511(5)

C10(C15	1.550(6)

C11(C12	1.528(6)

C12(C13	1.514(6)

C13(C14	1.524(6)

C14(C15	1.505(6)

C20(C21	1.523(5)

C20(C25	1.533(5)

C21(C22	1.518(5)

C22(C23	1.517(6)

C23(C24	1.530(6)

C24(C25	1.531(6)

C30(C31	1.534(5)

C30(C35	1.534(5)

C31(C32	1.532(5)

C32(C33	1.520(6)

C33(C34	1.532(6)

C34(C35	1.533(5)

Si4(O7	1.588(3)

Si4(O12	1.653(3)

Si4(O8	1.658(2)

Si4(C40	1.859(4)

Si5(O9	1.586(3)

Si5(O10	1.654(3)

Si5(O8	1.658(3)

Si5(C50	1.856(4)

Si6(O11	1.599(3)

Si6(O10	1.645(2)

Si6(O12	1.668(3)

Si6(C60	1.859(4)

O7(Na3	2.850(3)

O8(Na2	2.424(3)

O9(Na2	2.605(3)

O11(Na3	2.554(3)

O12(Na3	2.536(3)

C40(C45	1.537(5)

C40(C41	1.537(5)

C41(C42	1.518(5)

C42(C43	1.519(6)

C43(C44	1.530(6)

C44(C45	1.523(5)

C50(C51	1.529(5)

C50(C55	1.537(5)

C51(C52	1.539(5)

C52(C53	1.512(6)

C53(C54	1.524(6)

C54(C55	1.546(5)

C60(C65	1.514(6)

C60(C61	1.548(5)

C61(C62	1.528(5)

C62(C63	1.514(6)

C63(C64	1.511(6)

C64(C65	1.547(5)

Na1(O24	2.336(3)

Na1(O14	2.347(3)

Na1(O13	2.391(3)

Na1(O23	2.417(3)

Na1(O16	2.431(3)

Na1(O15	2.455(3)

Na2(O25	2.276(3)

Na2(O26	2.426(3)

Na2(O28ii	2.491(3)

Na2(O30	2.915(4)

Na3(O21	2.306(3)

Na3(O22	2.431(3)

Na3(O23ii	2.444(3)

Na3(O26	2.486(3)

Na4(O20	2.285(3)

Na4(O21	2.389(3)

Na4(O18	2.454(3)

Na4(O19	2.629(3)

Na4(O17	2.893(3)

Na5(O14iii	2.332(3)

Na5(O27	2.345(3)

Na5(O25iv	2.350(3)

Na5(O16iii	2.401(3)

Na5(O19	2.422(3)

Na5(O28	2.502(3)

Na6(O29	2.309(3)

Na6(O24	2.332(3)

Na6(O20	2.409(3)

Na6(O28	2.414(3)

Na6(O15	2.431(3)

Na6(O19	2.522(3)

O14(Na5i	2.332(3)

O16(Na5i	2.401(3)

O23(Na3iv	2.444(3)

O25(Na5ii	2.350(3)

O28(Na2iv	2.491(3)

O1(Si1(O6	109.70(13)

O1(Si1(O2	112.93(13)

O6(Si1(O2	106.28(14)

O1(Si1(C10	111.20(15)

O6(Si1(C10	108.36(15)

O2(Si1(C10	108.17(15)

O3(Si2(O2	111.99(15)

O3(Si2(O4	107.77(14)

O2(Si2(O4	105.91(13)

O3(Si2(C20	115.37(15)

O2(Si2(C20	109.43(16)

O4(Si2(C20	105.74(15)

O5(Si3(O6	113.21(13)

O5(Si3(O4	109.21(13)

O6(Si3(O4	104.12(13)

O5(Si3(C30	115.00(15)

O6(Si3(C30	107.15(15)

O4(Si3(C30	107.46(15)

Si2(O2(Si1	131.47(17)

Si2(O3(Na4	91.61(12)

Si3(O4(Si2	131.54(17)

Si3(O4(Na4	125.21(13)

Si2(O4(Na4	96.13(12)

Si1(O6(Si3	135.03(15)

C11(C10(C15	109.4(3)

C11(C10(Si1	117.4(3)

C15(C10(Si1	110.2(3)

C10(C11(C12	111.9(4)

C13(C12(C11	111.5(3)

C12(C13(C14	110.7(3)

C15(C14(C13	111.7(4)

C14(C15(C10	111.2(4)

C21(C20(C25	109.8(3)

C21(C20(Si2	116.7(3)

C25(C20(Si2	112.8(3)

C22(C21(C20	111.4(3)

C21(C22(C23	111.5(4)

C22(C23(C24	112.5(3)

C23(C24(C25	110.3(4)

C24(C25(C20	111.5(3)

C31(C30(C35	109.3(3)

C31(C30(Si3	115.1(3)

C35(C30(Si3	112.7(3)

C32(C31(C30	110.6(3)

C33(C32(C31	111.5(4)

C32(C33(C34	111.7(4)

C33(C34(C35	111.0(3)

C34(C35(C30	111.4(3)

O7(Si4(O12	112.07(13)

O7(Si4(O8	110.65(13)

O12(Si4(O8	103.62(13)

O7(Si4(C40	114.03(16)

O12(Si4(C40	107.31(16)

O8(Si4(C40	108.57(14)

O9(Si5(O10	110.99(14)

O9(Si5(O8	107.76(14)

O10(Si5(O8	105.63(13)

O9(Si5(C50	117.00(15)

O10(Si5(C50	108.45(16)

O8(Si5(C50	106.32(15)

O11(Si6(O10	112.60(13)

O11(Si6(O12	108.08(13)

O10(Si6(O12	106.60(13)

O11(Si6(C60	111.31(16)

O10(Si6(C60	108.81(15)

O12(Si6(C60	109.30(16)

O11(Si6(Na3	54.94(10)

O10(Si6(Na3	114.56(10)

O12(Si6(Na3	54.46(9)

C60(Si6(Na3	136.44(12)

Si4(O7(Na3	86.95(12)

Si5(O8(Si4	131.71(16)

Si5(O8(Na2	95.95(12)

Si4(O8(Na2	117.96(13)

Si5(O9(Na2	91.08(12)

Si6(O10(Si5	131.45(17)

Si6(O11(Na3	94.24(13)

Si4(O12(Si6	134.44(15)

Si4(O12(Na3	96.81(12)

Si6(O12(Na3	93.18(11)

C45(C40(C41	109.4(3)

C45(C40(Si4	114.1(2)

C41(C40(Si4	113.0(3)

C42(C41(C40	111.9(3)

C41(C42(C43	110.7(3)

C42(C43(C44	111.6(4)

C45(C44(C43	111.4(3)

C44(C45(C40	111.1(3)

C51(C50(C55	109.8(3)

C51(C50(Si5	115.1(3)

C55(C50(Si5	115.2(3)

C50(C51(C52	111.5(3)

C53(C52(C51	111.5(4)

C52(C53(C54	111.1(3)

C53(C54(C55	112.0(4)

C50(C55(C54	110.2(3)

C65(C60(C61	109.0(3)

C65(C60(Si6	111.3(3)

C61(C60(Si6	115.9(3)

C62(C61(C60	111.3(3)

C63(C62(C61	112.0(3)

C64(C63(C62	111.6(3)

C63(C64(C65	110.8(4)

C60(C65(C64	112.5(3)

O24(Na1(O14	177.96(15)

O24(Na1(O13	94.87(11)

O14(Na1(O13	83.58(10)

O24(Na1(O23	83.82(10)

O14(Na1(O23	97.76(11)

O13(Na1(O23	178.34(12)

O24(Na1(O16	91.91(11)

O14(Na1(O16	86.67(10)

O13(Na1(O16	86.07(11)

O23(Na1(O16	94.98(12)

O24(Na1(O15	86.36(10)

O14(Na1(O15	95.06(11)

O13(Na1(O15	94.02(11)

O23(Na1(O15	84.89(10)

O16(Na1(O15	178.27(13)

O25(Na2(O8	150.58(11)

O25(Na2(O26	114.05(10)

O8(Na2(O26	95.19(9)

O25(Na2(O28ii	91.77(11)

O8(Na2(O28ii	85.88(10)

O26(Na2(O28ii	87.95(10)

O25(Na2(O9	105.50(10)

O8(Na2(O9	62.69(9)

O26(Na2(O9	113.50(10)

O28ii(Na2(O9	142.40(11)

O25(Na2(O30	78.87(10)

O8(Na2(O30	72.96(9)

O26(Na2(O30	154.14(10)

O28ii(Na2(O30	68.70(10)

O9(Na2(O30	81.98(9)

O21(Na3(O22	92.08(10)

O21(Na3(O23ii	100.41(10)

O22(Na3(O23ii	84.46(10)

O21(Na3(O26	106.30(10)

O22(Na3(O26	159.21(11)

O23ii(Na3(O26	82.75(9)

O21(Na3(O12	135.39(10)

O22(Na3(O12	68.82(9)

O23ii(Na3(O12	116.44(10)

O26(Na3(O12	102.64(9)

O21(Na3(O11	80.03(9)

O22(Na3(O11	94.25(10)

O23ii(Na3(O11	178.64(11)

O26(Na3(O11	98.37(9)

O12(Na3(O11	62.61(9)

O21(Na3(O7	161.84(9)

O22(Na3(O7	84.74(9)

O23ii(Na3(O7	61.52(8)

O26(Na3(O7	74.76(8)

O12(Na3(O7	59.56(8)

O11(Na3(O7	117.99(9)

O20(Na4(O4	172.08(11)

O20(Na4(O21	91.30(10)

O4(Na4(O21	81.67(9)

O20(Na4(O18	94.44(11)

O4(Na4(O18	93.48(11)

O21(Na4(O18	151.26(11)

O20(Na4(O3	114.15(10)

O4(Na4(O3	64.50(9)

O21(Na4(O3	103.75(10)

O18(Na4(O3	99.49(10)

O20(Na4(O19	92.71(10)

O4(Na4(O19	88.64(10)

O21(Na4(O19	72.38(9)

O18(Na4(O19	79.23(10)

O3(Na4(O19	153.07(10)

O20(Na4(O17	79.60(9)

O4(Na4(O17	104.89(9)

O21(Na4(O17	151.27(11)

O18(Na4(O17	57.33(10)

O3(Na4(O17	57.33(8)

O19(Na4(O17	134.70(10)

O14iii(Na5(O27	177.47(12)

O14iii(Na5(O25iv	93.69(11)

O27(Na5(O25iv	88.38(11)

O14iii(Na5(O16iii	87.72(10)

O27(Na5(O16iii	93.69(11)

O25iv(Na5(O16iii	91.52(11)

O14iii(Na5(O19	101.84(11)

O27(Na5(O19	76.15(10)

O25iv(Na5(O19	164.29(12)

O16iii(Na5(O19	86.81(10)

O14iii(Na5(O28	82.29(10)

O27(Na5(O28	96.28(11)

O25iv(Na5(O28	89.79(10)

O16iii(Na5(O28	169.98(12)

O19(Na5(O28	94.56(11)

O29(Na6(O24	167.29(13)

O29(Na6(O20	82.43(11)

O24(Na6(O20	87.41(10)

O29(Na6(O28	92.57(11)

O24(Na6(O28	98.34(11)

O20(Na6(O28	171.94(12)

O29(Na6(O15	100.10(11)

O24(Na6(O15	87.00(10)

O20(Na6(O15	87.48(10)

O28(Na6(O15	87.18(10)

O29(Na6(O19	95.53(11)

O24(Na6(O19	77.25(10)

O20(Na6(O19	92.54(10)

O28(Na6(O19	94.24(11)

O15(Na6(O19	164.24(11)

Na5i(O14(Na1	92.09(11)

Na6(O15(Na1	89.06(10)

Na5i(O16(Na1	88.38(11)

Na5(O19(Na6	84.79(10)

Na5(O19(Na4	162.31(13)

Na6(O19(Na4	82.30(9)

Na4(O20(Na6	92.44(10)

Na3(O21(Na4	152.55(12)

Na1(O23(Na3iv	165.93(13)

Na6(O24(Na1	94.46(11)

Na2(O25(Na5ii	92.64(10)

Na2(O26(Na3	120.91(10)

Na6(O28(Na2iv	160.50(15)

Na6(O28(Na5	85.40(10)

Na2iv(O28(Na5	84.17(10)

Symmetry transformations used to generate equivalent atoms:

(i) x+1,y,z    (ii) x(1,y+1,z    (iii) x(1,y,z    (iv)  x+1,y(1,z

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

Si1	9(1) 	11(1)	12(1) 	0(1)	(2(1) 	(2(1)

Si2	10(1) 	12(1)	13(1) 	0(1)	(2(1) 	(4(1)

Si3	11(1) 	9(1)	13(1) 	1(1)	(2(1) 	(3(1)

O1	12(1) 	12(1)	15(1) 	2(1)	(3(1) 	(4(1)

O2	14(1) 	14(2)	19(1) 	3(1)	(6(1) 	(6(1)

O3	13(1) 	20(2)	19(1) 	(4(1)	(5(1) 	(8(1)

O4	12(1) 	14(2)	14(1) 	1(1)	(4(1) 	(5(1)

O5	16(1) 	12(1)	14(1) 	2(1)	(3(1) 	(4(1)

O6	12(1) 	11(1)	16(1) 	(1(1)	(5(1) 	(2(1)

C10	13(2) 	17(2)	17(2) 	(2(2)	(1(2) 	(4(2)

C11	36(2) 	22(2)	15(2) 	0(2)	(10(2) 	(3(2)

C12	44(3) 	24(3)	16(2) 	3(2)	(11(2) 	(14(2)

C13	32(2) 	39(3)	23(2) 	15(2)	(13(2) 	(16(2)

C14	66(3) 	17(3)	22(3) 	5(2)	(11(2) 	0(2)

C15	62(3) 	18(3)	17(2) 	4(2)	(15(2) 	(7(2)

C20	14(2) 	19(2)	11(2) 	1(2)	(3(1) 	(7(2)

C21	25(2) 	16(2)	21(2) 	1(2)	2(2) 	(10(2)

C22	48(3) 	22(3)	20(2) 	7(2)	1(2) 	(14(2)

C23	47(3) 	30(3)	18(2) 	1(2)	10(2) 	(18(2)

C24	34(2) 	26(3)	23(2) 	(2(2)	9(2) 	(13(2)

C25	23(2) 	18(2)	21(2) 	0(2)	0(2) 	(7(2)

C30	14(2) 	12(2)	14(2) 	4(2)	(4(2) 	(4(2)

C31	20(2) 	19(2)	19(2) 	(2(2)	(8(2) 	(3(2)

C32	33(2) 	32(3)	22(2) 	(2(2)	(11(2) 	(8(2)

C33	39(3) 	27(3)	23(2) 	(11(2)	(6(2) 	(14(2)

C34	28(2) 	28(3)	28(3) 	(15(2)	1(2) 	(5(2)

C35	19(2) 	15(2)	23(2) 	(5(2)	(4(2) 	(2(2)

Si4	10(1) 	11(1)	11(1) 	1(1)	(2(1) 	(3(1)

Si5	9(1) 	13(1)	12(1) 	1(1)	(2(1) 	(3(1)

Si6	10(1) 	10(1)	11(1) 	0(1)	(2(1) 	(2(1)

O7	14(1) 	18(2)	13(1) 	4(1)	(4(1) 	(8(1)

O8	10(1) 	12(2)	15(1) 	2(1)	(4(1) 	(3(1)

O9	11(1) 	18(2)	15(1) 	(1(1)	(3(1) 	(3(1)

O10	10(1) 	9(1)	18(1) 	0(1)	(3(1) 	(1(1)

O11	13(1) 	16(2)	12(1) 	(2(1)	(1(1) 	(3(1)

O12	11(1) 	10(1)	17(1) 	0(1)	(4(1) 	(3(1)

C40	16(2) 	15(2)	13(2) 	(2(2)	(2(2) 	(5(2)

C41	18(2) 	19(2)	22(2) 	(3(2)	(4(2) 	(7(2)

C42	20(2) 	24(3)	28(2) 	(11(2)	5(2) 	(4(2)

C43	31(2) 	29(3)	19(2) 	(10(2)	(1(2) 	(5(2)

C44	34(2) 	25(3)	16(2) 	(2(2)	(8(2) 	(14(2)

C45	16(2) 	20(2)	18(2) 	1(2)	(4(2) 	(7(2)

C50	13(2) 	15(2)	16(2) 	3(2)	(3(2) 	(7(2)

C51	19(2) 	23(2)	15(2) 	0(2)	1(2) 	(7(2)

C52	33(2) 	24(3)	19(2) 	(8(2)	6(2) 	(7(2)

C53	37(3) 	32(3)	22(2) 	(5(2)	13(2) 	(11(2)

C54	40(3) 	29(3)	20(2) 	3(2)	2(2) 	(14(2)

C55	32(2) 	21(2)	13(2) 	2(2)	1(2) 	(10(2)

C60	12(2) 	20(2)	11(2) 	3(2)	(4(2) 	(3(2)

C61	29(2) 	20(2)	17(2) 	(1(2)	(7(2) 	(2(2)

C62	31(2) 	32(3)	15(2) 	2(2)	(11(2) 	(6(2)

C63	36(2) 	26(3)	18(2) 	9(2)	(10(2) 	(14(2)

C64	42(3) 	20(2)	28(3) 	12(2)	(15(2) 	(9(2)

C65	32(2) 	16(2)	21(2) 	3(2)	(9(2) 	(4(2)

Na1	15(1) 	15(1)	18(1) 	0(1)	(4(1) 	(6(1)

Na2	32(1) 	32(1)	28(1) 	14(1)	(19(1) 	(17(1)

Na3	20(1) 	18(1)	21(1) 	2(1)	(1(1) 	(6(1)

Na4	20(1) 	25(1)	21(1) 	6(1)	(9(1) 	(6(1)

Na5	16(1) 	15(1)	21(1) 	2(1)	(5(1) 	(5(1)

Na6	15(1) 	15(1)	22(1) 	(2(1)	(4(1) 	(2(1)

O13	12(1) 	20(2)	16(1) 	2(1)	(5(1) 	(5(1)

O14	19(1) 	12(2)	18(1) 	(1(1)	(6(1) 	(1(1)

O15	21(1) 	19(2)	18(2) 	0(1)	(4(1) 	(6(1)

O16	23(2) 	25(2)	21(2) 	2(1)	(5(1) 	(10(1)

O17	15(1) 	20(2)	42(2) 	4(2)	(4(1) 	(4(1)

O18	35(2) 	18(2)	33(2) 	3(1)	(2(1) 	(8(1)

O19	17(1) 	19(2)	28(2) 	5(1)	(11(1) 	(4(1)

O20	15(1) 	18(2)	15(1) 	(1(1)	(5(1) 	(5(1)

O21	22(1) 	26(2)	15(1) 	2(1)	(4(1) 	(7(1)

O22	15(1) 	26(2)	27(2) 	8(1)	(7(1) 	(6(1)

O23	15(1) 	18(2)	15(1) 	1(1)	(3(1) 	(7(1)

O24	17(1) 	13(2)	21(2) 	0(1)	(6(1) 	(3(1)

O25	16(1) 	23(2)	17(1) 	1(1)	(4(1) 	(9(1)

O26	31(1) 	17(1)	23(1) 	0(1)	(4(1) 	(13(1)

O27	14(1) 	23(2)	31(2) 	(6(1)	1(1) 	(8(1)

O28	33(2) 	31(2)	29(2) 	9(1)	(17(1) 	(13(1)

O29	16(1) 	23(2)	41(2) 	(12(1)	2(1) 	(7(1)

O30	52(2) 	28(2)	32(2) 	12(1)	(16(2) 	(15(2)

Table 5. Hydrogen bonds [Å and °].

D(H···A	d(D(H)	d(H···A)	d(D···A)	((DHA)

O13(H13'...O11i	0.94	1.76	2.703(3)	171.5

O13(H13"...O5i	0.95	1.84	2.757(3)	163.1

O14(H14'...O11i	0.94	1.80	2.707(4)	160.3

O14(H14"...O30v	0.95	1.81	2.738(4)	166.8

O15(H15'...O10i	0.94	2.45	3.295(4)	148.5

O15(H15"...O7iv	0.95	1.87	2.775(4)	160.2

O16(H16'...O2iv	0.94	2.33	3.257(4)	165.4

O16(H16"...O5i	0.95	2.08	2.844(4)	136.6

O17(H17'...O3	0.94	1.75	2.627(4)	153.0

O17(H17"...O6i	0.95	1.82	2.760(3)	174.0

O18(H18'...O17	0.94	1.70	2.594(4)	156.2

O18(H18"...O19	0.95	2.46	3.244(4)	140.5

O19(H19'...O5	0.94	1.76	2.684(4)	164.3

O19(H19"...O27	0.95	2.19	2.941(4)	135.6

O20(H20'...O9i	0.94	1.73	2.672(3)	171.1

O20(H20"...O13	0.95	1.82	2.766(3)	177.2

O21(H21'...O29	0.94	2.03	2.970(4)	171.9

O21(H21"...O5	0.95	1.88	2.785(3)	160.4

O22(H22'...O12	0.94	2.08	2.809(3)	133.2

O23(H23'...O1iv	0.94	1.79	2.728(3)	175.4

O23(H23"...O7iv	0.95	1.85	2.730(3)	154.2

O24(H24'...O1iv	0.94	1.75	2.665(4)	162.3

O24(H24"...O18	0.95	1.88	2.787(4)	161.3

O25(H25'...O23vi	0.94	2.00	2.898(3)	157.0

O25(H25"...O3iii	0.95	1.75	2.659(4)	161.4

O26(H26'...O1	0.94	1.84	2.761(3)	164.3

O26(H26"...O13iii	0.95	2.26	2.986(4)	133.3

O26(H26"...O17iii	0.95	2.33	3.013(4)	128.4

O27(H27'...O3vii	0.94	1.87	2.819(4)	177.5

O27(H27"...O1iv	0.95	1.92	2.849(3)	166.9

O28(H28"...O7iv	0.95	1.75	2.628(4)	153.6

O29(H29'...O9i	0.94	1.95	2.797(4)	148.3

O29(H29"...O11	0.95	1.81	2.755(3)	174.1

O30(H30'...O22iii	0.95	1.75	2.687(4)	169.5

Symmetry transformations used to generate equivalent atoms:

(i) x+1,y,z    (ii) x(1,y+1,z    (iii) x(1,y,z    (iv)  x+1,y(1,z

(v) x+2,y(1,z    (vi) x(2,y+1,z    (vii) x,y(1,z