|  | University of Southampton · Department of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	01src265

Empirical formula 	C20H14F4I2N4O2

Formula weight 	672.15

Temperature 	150(2) K

Wavelength 	0.71073 Å

Crystal system 	Triclinic

Space group

Unit cell dimensions	a = 5.02970(10) Å	( = 78.0630(13)°

b = 10.2309(4) Å	( = 79.0470(15)°

c = 11.1000(4) Å	(  = 83.871(2)°

Volume	547.30(3) Å3

Z	1

Density (calculated)	2.039 Mg / m3

Absorption coefficient	2.932 mm(1

F(000)	320

Crystal	Block; colourless

Crystal size	0.15 ( 0.15 ( 0.10 mm3

( range for data collection	3.05 ( 25.99°

Index ranges	(6 ( h ( 6, (12 ( k ( 12, (12 ( l ( 13

Reflections collected	4361

Independent reflections	2132 [Rint = 0.0686]

Completeness to ( = 25.99°	99.1 %

Max. and min. transmission	0.7581 and 0.6675

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	2132 / 0 / 153

Goodness-of-fit on F2	1.003

Final R indices [F2 > 2((F2)]	R1 = 0.0341, wR2 = 0.0895

R indices (all data)	R1 = 0.0355, wR2 = 0.0909

Extinction coefficient	0.013(3)

Largest diff. peak and hole	1.188 and (1.466 e Å(3

Diffractometer: Enraf Nonius KappaCCD area detector (( scans and ( scans to fill Ewald sphere). Data collection and cell

refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography,

part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing,

Acta Cryst. A51 (1995) 33(37; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421(426). Program used to solve structure:

SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Program used to refine structure: SHELXL97 (G. M. Sheldrick

(1997), University of Göttingen, Germany).

Further information:  http://www.soton.ac.uk/~xservice/strat.htm

Special details:

The refinement shows that the structure contains bis-(3-pyridyl)oxalamide rather than bis-(4-pyridyl)oxalamide (as 01src157 – but the two structures are fundamentally different)

I1…N1 = 2.876(3) = infinite 1D chains

Hydrogen bonds (Table 6) => 2D sheets

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

I1	6(1)	1459(1)	2589(1)	23(1)	1

F1	(3425(5)	(1089(2)	2923(2)	32(1)	1

F2	(2655(4)	2157(2)	5298(2)	32(1)	1

C1	(2918(7)	565(3)	4059(3)	21(1)	1

C2	(3806(7)	1090(3)	5134(3)	22(1)	1

C3	(4153(7)	(542(3)	3950(3)	21(1)	1

N1	3791(7)	2460(4)	385(3)	27(1)	1

O1	2005(5)	4867(3)	(3871(2)	23(1)	1

N2	6274(5)	5207(3)	(3671(2)	18(1)	1

C4	3756(7)	3604(4)	(449(3)	24(1)	1

C5	5724(6)	3900(3)	(1497(3)	18(1)	1

C6	7817(7)	2940(4)	(1705(3)	24(1)	1

C7	7864(8)	1740(4)	(859(4)	29(1)	1

C8	5822(8)	1542(4)	169(3)	26(1)	1

C9	5614(7)	5260(3)	(2342(3)	21(1)	1

C10	4424(7)	5009(3)	(4306(3)	16(1)	1

Table 3. Bond lengths [Å] and angles [°].

I1(C1	2.102(3)

I1(N1	2.876(3)

F1(C3	1.345(4)

F2(C2	1.348(4)

C1(C3	1.385(5)

C1(C2	1.387(5)

C2(C3i	1.375(5)

C3(C2i	1.375(5)

N1(C8	1.333(5)

N1(C4	1.335(5)

O1(C10	1.233(4)

N2(C10	1.325(4)

N2(C9	1.460(4)

N2(H2	0.8800

C4(C5	1.381(4)

C4(H4	0.9500

C5(C6	1.381(5)

C5(C9	1.510(5)

C6(C7	1.383(5)

C6(H6	0.9500

C7(C8	1.380(5)

C7(H7	0.9500

C8(H8	0.9500

C9(H9A	0.9900

C9(H9B	0.9900

C10(C10ii	1.542(7)

C1(I1(N1	172.44(11)

C3(C1(C2	117.3(3)

C3(C1(I1	120.4(2)

C2(C1(I1	122.2(2)

F2(C2(C3i	118.7(3)

F2(C2(C1	119.9(3)

C3i(C2(C1	121.4(3)

F1(C3(C2i	118.2(3)

F1(C3(C1	120.5(3)

C2i(C3(C1	121.3(3)

C8(N1(C4	117.6(3)

C8(N1(I1	110.7(2)

C4(N1(I1	131.6(2)

C10(N2(C9	122.1(3)

C10(N2(H2	119.0

C9(N2(H2	119.0

N1(C4(C5	123.9(3)

N1(C4(H4	118.1

C5(C4(H4	118.1

C4(C5(C6	117.8(3)

C4(C5(C9	120.1(3)

C6(C5(C9	122.1(3)

C5(C6(C7	119.1(3)

C5(C6(H6	120.5

C7(C6(H6	120.5

C8(C7(C6	118.9(4)

C8(C7(H7	120.5

C6(C7(H7	120.5

N1(C8(C7	122.7(3)

N1(C8(H8	118.6

C7(C8(H8	118.6

N2(C9(C5	113.6(3)

N2(C9(H9A	108.8

C5(C9(H9A	108.8

N2(C9(H9B	108.8

C5(C9(H9B	108.8

H9A(C9(H9B	107.7

O1(C10(N2	125.1(3)

O1(C10(C10ii	121.7(4)

N2(C10(C10ii	113.1(3)

Symmetry transformations used to generate equivalent atoms:

(i) (x(1,(y,(z+1    (ii) (x+1,(y+1,(z(1

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

I1	20(1) 	24(1)	20(1) 	2(1)	3(1) 	(6(1)

F1	39(1) 	31(1)	24(1) 	(12(1)	10(1) 	(10(1)

F2	36(1) 	29(1)	31(1) 	(8(1)	4(1) 	(17(1)

C1	18(2) 	21(2)	20(2) 	2(1)	1(1) 	(2(1)

C2	21(2) 	20(2)	26(2) 	(6(1)	(1(1) 	(4(1)

C3	21(2) 	24(2)	16(2) 	(2(1)	1(1) 	(1(1)

N1	26(2) 	34(2)	19(2) 	(1(1)	3(1) 	(11(1)

O1	13(1) 	37(2)	16(1) 	2(1)	0(1) 	(8(1)

N2	10(1) 	28(2)	14(1) 	0(1)	(1(1) 	(4(1)

C4	20(2) 	32(2)	19(2) 	(4(1)	2(1) 	(6(1)

C5	16(1) 	26(2)	13(1) 	(5(1)	(2(1) 	(7(1)

C6	25(2) 	30(2)	13(2) 	(2(1)	6(1) 	(3(2)

C7	33(2) 	25(2)	24(2) 	(2(2)	3(2) 	(1(2)

C8	34(2) 	26(2)	17(2) 	1(1)	(5(2) 	(10(2)

C9	23(2) 	25(2)	17(2) 	(4(1)	(3(1) 	(4(1)

C10	14(2) 	19(2)	15(2) 	2(1)	(2(1) 	(5(1)

Table 5. Hydrogen coordinates [( 104] and isotropic displacement parameters [Å2 ( 103].

Atom 	x	y	z	Ueq	S.o.f.

H2	7955	5311	(4061	46(13)	1

H4	2289	4254	(313	33(11)	1

H6	9206	3101	(2418	24(10)	1

H7	9280	1064	(985	30(10)	1

H8	5864	717	748	24(10)	1

H9A	3767	5698	(2165	36(11)	1

H9B	6900	5820	(2145	9(9)	1

Table 6. Hydrogen bonds [Å and °].

D(H···A	d(D(H)	d(H···A)	d(D···A)	((DHA)

N2(H2...O1iii	0.88	2.08	2.838(3)	143.7

Symmetry transformations used to generate equivalent atoms:

(i) (x(1,(y,(z+1    (ii) (x+1,(y+1,(z(1    (iii) x+1,y,z