|  | University of Southampton · Department of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	01src265_2 (Phase 2)

Compound	C13H14N4O · 2 C6F4I2

Empirical formula 	C25H14F8I4N4O

Formula weight 	1046.00

Temperature 	150(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	C2/c

Unit cell dimensions	a = 25.1399(9) Å	( = 90°

b = 4.57150(10) Å	( = 92.3760(15)°

c = 25.8949(12) Å	(  = 90°

Volume	2973.47(19) Å3

Z	4

Density (calculated)	2.337 Mg / m3

Absorption coefficient	4.270 mm(1

F(000)	1936

Crystal	Needle; colourless

Crystal size	0.35 ( 0.04 ( 0.02 mm3

( range for data collection	3.15 ( 26.00°

Index ranges	(30 ( h ( 30, (4 ( k ( 5, (31 ( l ( 31

Reflections collected	8357

Independent reflections	2888 [Rint = 0.0632]

Completeness to ( = 26.00°	98.8 %

Max. and min. transmission	0.9195 and 0.3165

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	2888 / 0 / 198

Goodness-of-fit on F2	0.923

Final R indices [F2 > 2((F2)]	R1 = 0.0392, wR2 = 0.0556

R indices (all data)	R1 = 0.0745, wR2 = 0.0606

Largest diff. peak and hole	0.924 and (0.786 e Å(3

Diffractometer: Enraf Nonius KappaCCD area detector (( scans and ( scans to fill Ewald sphere). Data collection and cell

refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography,

part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing,

Acta Cryst. A51 (1995) 33(37; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421(426). Program used to solve structure:

SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Program used to refine structure: SHELXL97 (G. M. Sheldrick

(1997), University of Göttingen, Germany).

Further information:  http://www.soton.ac.uk/~xservice/strat.htm

Special details:

This is the 1:2 analogue of 01src264

The corrugated sheets are topologically identical with those in 01src264 (I2(N1 = 2.886(4), N2(H…O1 H-bonds, Figs.)

There are additional weak (electrostatic) interactions between I1…. O1 =3.433(1) that connect these sheets (Figs.)

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

I1	5073(1)	6890(1)	1228(1)	39(1)	1

F1	5845(1)	11215(6)	647(1)	40(1)	1

F2	4232(1)	6217(6)	275(1)	43(1)	1

C1	5038(3)	8702(10)	487(2)	28(2)	1

C2	4619(3)	8097(10)	148(2)	32(2)	1

C3	5423(3)	10580(10)	333(2)	26(1)	1

I2	3089(1)	6396(1)	1237(1)	26(1)	1

F3	2064(1)	3618(5)	653(1)	35(1)	1

F4	3386(1)	10579(6)	282(1)	34(1)	1

C11	2741(2)	7071(10)	495(2)	22(1)	1

C12	2287(3)	5591(10)	335(2)	27(2)	1

C13	2946(2)	9026(10)	151(2)	22(1)	1

O1	5000	4857(9)	2500	33(2)	1

N1	3409(2)	5458(8)	2307(2)	25(1)	1

N2	4560(2)	569(8)	2359(2)	20(1)	1

C4	3755(2)	3532(9)	2519(2)	19(1)	1

C5	3780(2)	2907(10)	3043(2)	29(2)	1

C6	3426(3)	4360(11)	3360(2)	34(2)	1

C7	3073(2)	6332(11)	3147(2)	31(2)	1

C8	3077(2)	6850(11)	2626(2)	29(2)	1

C9	4091(2)	1979(10)	2138(2)	24(1)	1

C10	5000	2072(15)	2500	23(2)	1

Table 3. Bond lengths [Å] and angles [°].

I1(C1	2.089(5)

I1(O1	3.4334(12)

F1(C3	1.342(6)

F2(C2	1.350(6)

C1(C3	1.365(7)

C1(C2	1.371(8)

C2(C3i	1.385(7)

C3(C2i	1.385(7)

I2(C11	2.101(5)

I2(N1	2.886(4)

F3(C12	1.358(5)

F4(C13	1.346(6)

C11(C12	1.375(7)

C11(C13	1.378(6)

C12(C13ii	1.377(7)

C13(C12ii	1.377(7)

O1(C10	1.273(7)

N1(C4	1.339(6)

N1(C8	1.357(6)

N2(C10	1.340(5)

N2(C9	1.440(6)

N2(H2	0.8800

C4(C5	1.387(6)

C4(C9	1.503(7)

C5(C6	1.401(7)

C5(H5	0.9500

C6(C7	1.366(7)

C6(H6	0.9500

C7(C8	1.369(7)

C7(H7	0.9500

C8(H8	0.9500

C9(H9A	0.9900

C9(H9B	0.9900

C10(N2iii	1.340(5)

C1(I1(O1	170.59(15)

C3(C1(C2	118.3(5)

C3(C1(I1	120.9(5)

C2(C1(I1	120.7(4)

F2(C2(C1	121.0(5)

F2(C2(C3i	117.9(6)

C1(C2(C3i	121.1(6)

F1(C3(C1	120.8(5)

F1(C3(C2i	118.6(5)

C1(C3(C2i	120.6(6)

C11(I2(N1	171.53(18)

C12(C11(C13	116.9(5)

C12(C11(I2	120.9(4)

C13(C11(I2	122.2(4)

F3(C12(C11	120.1(5)

F3(C12(C13ii	117.8(5)

C11(C12(C13ii	122.0(5)

F4(C13(C12ii	118.6(5)

F4(C13(C11	120.4(5)

C12ii(C13(C11	121.0(5)

C10(O1(I1	105.70(7)

C4(N1(C8	117.7(4)

C4(N1(I2	129.9(3)

C8(N1(I2	111.2(3)

C10(N2(C9	122.1(4)

C10(N2(H2	119.0

C9(N2(H2	119.0

N1(C4(C5	122.5(5)

N1(C4(C9	114.6(4)

C5(C4(C9	122.8(5)

C4(C5(C6	118.1(5)

C4(C5(H5	120.9

C6(C5(H5	120.9

C7(C6(C5	119.6(5)

C7(C6(H6	120.2

C5(C6(H6	120.2

C6(C7(C8	118.8(6)

C6(C7(H7	120.6

C8(C7(H7	120.6

N1(C8(C7	123.2(5)

N1(C8(H8	118.4

C7(C8(H8	118.4

N2(C9(C4	115.1(4)

N2(C9(H9A	108.5

C4(C9(H9A	108.5

N2(C9(H9B	108.5

C4(C9(H9B	108.5

H9A(C9(H9B	107.5

O1(C10(N2	120.9(3)

O1(C10(N2iii	120.9(3)

N2(C10(N2iii	118.3(6)

Symmetry transformations used to generate equivalent atoms:

(i) (x+1,(y+2,(z    (ii) (x+1/2,(y+3/2,(z    (iii) (x+1,y,(z+1/2

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

I1	57(1) 	36(1)	24(1) 	1(1)	3(1) 	5(1)

F1	41(3) 	52(2)	27(2) 	(4(1)	(6(2) 	(4(2)

F2	44(3) 	41(2)	44(2) 	1(2)	6(2) 	(10(2)

C1	44(5) 	27(3)	14(3) 	(4(2)	8(3) 	1(3)

C2	48(5) 	22(3)	27(4) 	(6(3)	11(4) 	(1(3)

C3	27(4) 	26(3)	23(3) 	(8(2)	(6(3) 	0(3)

I2	31(1) 	27(1)	19(1) 	1(1)	(2(1) 	2(1)

F3	38(2) 	37(2)	29(2) 	11(1)	4(2) 	(9(2)

F4	34(3) 	38(2)	30(2) 	7(1)	(4(2) 	(3(2)

C11	18(4) 	30(3)	19(3) 	1(2)	(2(3) 	5(3)

C12	39(5) 	22(3)	20(3) 	5(2)	11(3) 	0(3)

C13	17(4) 	27(3)	21(3) 	(5(2)	(2(3) 	(2(3)

O1	40(4) 	8(3)	51(4) 	0	0(3) 	0

N1	29(4) 	26(2)	20(3) 	4(2)	2(3) 	(2(2)

N2	17(3) 	12(2)	32(3) 	3(2)	(6(2) 	(2(2)

C4	23(4) 	18(3)	17(3) 	0(2)	1(3) 	(5(3)

C5	31(4) 	27(3)	28(4) 	7(2)	0(3) 	4(3)

C6	40(5) 	44(4)	16(4) 	3(3)	(2(3) 	(6(3)

C7	23(4) 	38(3)	32(4) 	(4(3)	6(3) 	(3(3)

C8	28(4) 	28(3)	31(4) 	4(3)	(1(3) 	6(3)

C9	29(4) 	21(3)	24(3) 	(2(2)	(1(3) 	(4(3)

C10	27(6) 	20(4)	21(5) 	0	4(4) 	0

Table 5. Hydrogen coordinates [( 104] and isotropic displacement parameters [Å2 ( 103].

Atom 	x	y	z	Ueq	S.o.f.

H2	4557	(1340	2402	54(19)	1

H5	4029	1532	3184	6(12)	1

H6	3432	3976	3721	26(14)	1

H7	2829	7326	3356	49(18)	1

H8	2835	8252	2481	42(17)	1

H9A	3869	486	1956	32(15)	1

H9B	4203	3413	1878	50(17)	1

Table 6. Hydrogen bonds [Å and °].

D(H···A	d(D(H)	d(H···A)	d(D···A)	((DHA)

N2(H2...O1iv	0.88	2.07	2.853(5)	147.2

Symmetry transformations used to generate equivalent atoms:

(i) (x+1,(y+2,(z    (ii) (x+1/2,(y+3/2,(z    (iii) (x+1,y,(z+1/2

(iv)  x,y(1,z