|  | University of Southampton · Department of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	01src304

Empirical formula 	C10H10FeI3

Formula weight 	566.73

Temperature 	150(2) K

Wavelength 	0.71069 Å

Crystal system 	Trigonal

Space group 	R(3m

Unit cell dimensions	a = 8.4610(6) Å	( = 90°

b = 8.4610(6) Å	( = 90°

c = 16.9880(6) Å	(  = 120°

Volume	1053.21(11) Å3

Z	3

Density (calculated)	2.681 Mg / m3

Absorption coefficient	7.634 mm(1

F(000)	765

Crystal	Plate; brown

Crystal size	0.20 ( 0.10 ( 0.05 mm3

( range for data collection	3.03 ( 26.00°

Index ranges	(10 ( h ( 10, (10 ( k ( 10, (16 ( l ( 20

Reflections collected	1416

Independent reflections	446 [Rint = 0.1701]

Completeness to ( = 26.00°	95.5 %

Max. and min. transmission	0.7014 and 0.3105

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	446 / 2 / 28

Goodness-of-fit on F2	1.022

Final R indices [F2 > 2((F2)]	R1 = 0.0600, wR2 = 0.1485

R indices (all data)	R1 = 0.0613, wR2 = 0.1516

Extinction coefficient	0.0049(13)

Largest diff. peak and hole	2.267 and (1.423 e Å(3

Diffractometer: Enraf Nonius KappaCCD area detector (( scans and ( scans to fill Ewald sphere). Data collection and cell

refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography,

part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing,

Acta Cryst. A51 (1995) 33(37; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421(426). Program used to solve structure:

SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Program used to refine structure: SHELXL97 (G. M. Sheldrick

(1997), University of Göttingen, Germany).

Further information:  http://www.soton.ac.uk/~xservice/strat.htm

Special details:

There is an entry in the Cambridge Data Base for this structure (

FECNTI, T.Bernstein, F.H.Herbstein. Acta Crystallogr.,Sect.B, 24 (1968) 1640.

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

I1	0	0	5000	26(1)	1

I2	0	0	6726(1)	36(1)	1

Fe1	3333	(3333	6667	32(1)	1

C1	3327(16)	(1780(15)	5677(7)	72(3)	1

C2	4925(13)	(1737(14)	5692(7)	74(3)	1

Table 3. Bond lengths [Å] and angles [°].

I1(I2	2.9321(8)

I1(I2i	2.9321(8)

Fe1(C1ii	2.135(9)

Fe1(C1	2.135(9)

Fe1(C1iii	2.135(9)

Fe1(C1iv	2.135(9)

Fe1(C1v	2.135(9)

Fe1(C1vi	2.135(9)

Fe1(C2ii	2.136(10)

Fe1(C2	2.136(10)

Fe1(C2iii	2.136(10)

Fe1(C2v	2.136(10)

Fe1(C2iv	2.136(10)

Fe1(C2vi	2.136(10)

C1(C2ii	1.332(7)

C1(C2	1.334(7)

C1(H1	0.9500

C2(C1iii	1.332(7)

C2(H2	0.9500

I2(I1(I2i	180.0

C1ii(Fe1(C1	64.6(5)

C1ii(Fe1(C1iii	64.6(5)

C1(Fe1(C1iii	64.6(5)

C1ii(Fe1(C1iv	115.4(5)

C1(Fe1(C1iv	179.999(3)

C1iii(Fe1(C1iv	115.4(5)

C1ii(Fe1(C1v	180.0(4)

C1(Fe1(C1v	115.4(5)

C1iii(Fe1(C1v	115.4(5)

C1iv(Fe1(C1v	64.6(5)

C1ii(Fe1(C1vi	115.4(5)

C1(Fe1(C1vi	115.4(5)

C1iii(Fe1(C1vi	179.999(3)

C1iv(Fe1(C1vi	64.6(5)

C1v(Fe1(C1vi	64.6(5)

C1ii(Fe1(C2ii	36.4(2)

C1(Fe1(C2ii	36.36(19)

C1iii(Fe1(C2ii	77.2(3)

C1iv(Fe1(C2ii	143.6(2)

C1v(Fe1(C2ii	143.6(2)

C1vi(Fe1(C2ii	102.8(3)

C1ii(Fe1(C2	77.2(3)

C1(Fe1(C2	36.4(2)

C1iii(Fe1(C2	36.36(19)

C1iv(Fe1(C2	143.6(2)

C1v(Fe1(C2	102.8(3)

C1vi(Fe1(C2	143.64(19)

C2ii(Fe1(C2	66.3(5)

C1ii(Fe1(C2iii	36.36(19)

C1(Fe1(C2iii	77.2(3)

C1iii(Fe1(C2iii	36.4(2)

C1iv(Fe1(C2iii	102.8(3)

C1v(Fe1(C2iii	143.65(19)

C1vi(Fe1(C2iii	143.6(2)

C2ii(Fe1(C2iii	66.3(5)

C2(Fe1(C2iii	66.3(5)

C1ii(Fe1(C2v	143.6(2)

C1(Fe1(C2v	143.6(2)

C1iii(Fe1(C2v	102.8(3)

C1iv(Fe1(C2v	36.36(19)

C1v(Fe1(C2v	36.4(2)

C1vi(Fe1(C2v	77.2(3)

C2ii(Fe1(C2v	179.999(4)

C2(Fe1(C2v	113.7(5)

C2iii(Fe1(C2v	113.7(5)

C1ii(Fe1(C2iv	102.8(3)

C1(Fe1(C2iv	143.6(2)

C1iii(Fe1(C2iv	143.65(19)

C1iv(Fe1(C2iv	36.4(2)

C1v(Fe1(C2iv	77.2(3)

C1vi(Fe1(C2iv	36.36(19)

C2ii(Fe1(C2iv	113.7(5)

C2(Fe1(C2iv	179.999(2)

C2iii(Fe1(C2iv	113.7(5)

C2v(Fe1(C2iv	66.3(5)

C1ii(Fe1(C2vi	143.64(19)

C1(Fe1(C2vi	102.8(3)

C1iii(Fe1(C2vi	143.6(2)

C1iv(Fe1(C2vi	77.2(3)

C1v(Fe1(C2vi	36.36(19)

C1vi(Fe1(C2vi	36.4(2)

C2ii(Fe1(C2vi	113.7(5)

C2(Fe1(C2vi	113.7(5)

C2iii(Fe1(C2vi	180.0(7)

C2v(Fe1(C2vi	66.3(5)

C2iv(Fe1(C2vi	66.3(5)

C2ii(C1(C2	122.3(11)

C2ii(C1(Fe1	71.9(7)

C2(C1(Fe1	71.8(7)

C2ii(C1(H1	118.8

C2(C1(H1	118.8

Fe1(C1(H1	130.3

C1iii(C2(C1	117.6(12)

C1iii(C2(Fe1	71.8(7)

C1(C2(Fe1	71.8(7)

C1iii(C2(H2	121.2

C1(C2(H2	121.2

Fe1(C2(H2	127.1

Symmetry transformations used to generate equivalent atoms:

(i) (x,(y,(z+1    (ii) (y,x(y(1,z    (iii) (x+y+1,(x,z

(iv)  (x+2/3,(y(2/3,(z+4/3    (v) y+2/3,(x+y+1/3,(z+4/3

(vi) x(y(1/3,x(2/3,(z+4/3

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

I1	21(1) 	21(1)	36(1) 	0	0 	11(1)

I2	37(1) 	37(1)	32(1) 	0	0 	19(1)

Fe1	41(1) 	41(1)	14(1) 	0	0 	21(1)

C1	76(7) 	110(10)	38(5) 	27(5)	3(4) 	53(7)

C2	92(8) 	99(9)	54(6) 	35(6)	32(6) 	64(7)

Table 5. Hydrogen coordinates [( 104] and isotropic displacement parameters [Å2 ( 103].

Atom 	x	y	z	Ueq	S.o.f.

H1	3323	(660	5656	86	1

H2	6045	(613	5712	89	1