|  | Single Crystal X-Ray Diffraction Service School of Chemistry - University of Southampton Contact: Dr Mark E Light, light@soton.ac.uk, ex 29429 |
| --- | --- |

Table 1. Crystal data and structure refinement details.

Identification code 	2009src0667a

Empirical formula 	C16H22O11

Formula weight 	390.34

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Orthorhombic

Space group 	P212121

Unit cell dimensions	a = 8.3288(2) Å	( = 90°

b = 9.0098(3) Å	( = 90°

c = 25.4028(8) Å	(  = 90°

Volume	1906.25(10) Å3

Z	4

Density (calculated)	1.360 Mg / m3

Absorption coefficient	0.117 mm(1

F(000)	824

Crystal	plate; colourless

Crystal size	0.17 ( 0.12 ( 0.03 mm3

( range for data collection	2.92 ( 27.48°

Index ranges	(10 ( h ( 10, (11 ( k ( 11, (32 ( l ( 31

Reflections collected	17255

Independent reflections	2507 [Rint = 0.0519]

Completeness to ( = 27.48°	99.8 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.9965 and 0.9805

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	2507 / 0 / 249

Goodness-of-fit on F2	1.121

Final R indices [F2 > 2((F2)]	R1 = 0.0445, wR2 = 0.0854

R indices (all data)	R1 = 0.0532, wR2 = 0.0903

Largest diff. peak and hole	0.235 and (0.207 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit ). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: Sheldrick, G. M. SADABS - Bruker Nonius area detector scaling and absorption correction - V2.10 Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: Cameron - A Molecular Graphics Package. (D. M. Watkin, L. Pearce and C. K. Prout, Chemical Crystallography Laboratory, University of Oxford, 1993).

Special details:

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C1	2283(3)	6171(3)	9318(1)	22(1)	1

C2	1032(3)	4960(3)	9274(1)	21(1)	1

C3	34(3)	5225(3)	8780(1)	20(1)	1

C4	1118(3)	5284(3)	8302(1)	20(1)	1

C5	2386(3)	6474(3)	8404(1)	23(1)	1

C6	3375(3)	6010(4)	9794(1)	25(1)	1

C7	2924(3)	6244(3)	10716(1)	23(1)	1

C8	1659(4)	6358(4)	11130(1)	29(1)	1

C9	1240(4)	2362(3)	9485(1)	24(1)	1

C10	2317(4)	1044(3)	9424(1)	27(1)	1

C11	(2466(4)	4161(4)	9013(1)	27(1)	1

C12	(3526(4)	2841(4)	8955(1)	42(1)	1

C13	475(3)	5088(3)	7387(1)	23(1)	1

C14	(392(4)	5852(4)	6952(1)	30(1)	1

C15	4132(4)	7757(4)	7824(1)	29(1)	1

C16	5332(4)	7515(4)	7397(1)	46(1)	1

O1	3297(2)	6157(2)	8861(1)	24(1)	1

O2	2269(2)	6071(2)	10234(1)	26(1)	1

O3	4353(2)	6306(2)	10787(1)	27(1)	1

O4	1869(2)	3551(2)	9229(1)	22(1)	1

O5	9(3)	2404(2)	9731(1)	35(1)	1

O6	(1125(2)	4044(2)	8705(1)	23(1)	1

O7	(2703(2)	5202(2)	9299(1)	31(1)	1

O8	188(2)	5768(2)	7857(1)	24(1)	1

O9	1313(3)	4020(3)	7341(1)	39(1)	1

O10	3478(3)	6433(2)	7977(1)	28(1)	1

O11	3782(3)	8912(3)	8026(1)	42(1)	1

Table 3. Bond lengths [Å] and angles [°].

C1(O1	1.435(3)

C1(C2	1.513(4)

C1(C6	1.521(4)

C1(H1	1.0000

C2(O4	1.453(3)

C2(C3	1.526(4)

C2(H2	1.0000

C3(O6	1.449(3)

C3(C4	1.513(3)

C3(H3	1.0000

C4(O8	1.438(3)

C4(C5	1.527(4)

C4(H4	1.0000

C5(O1	1.415(3)

C5(O10	1.416(3)

C5(H5	1.0000

C6(O2	1.450(3)

C6(H6A	0.9900

C6(H6B	0.9900

C7(O3	1.205(3)

C7(O2	1.349(3)

C7(C8	1.492(4)

C8(H8A	0.9800

C8(H8B	0.9800

C8(H8C	0.9800

C9(O5	1.202(4)

C9(O4	1.358(3)

C9(C10	1.496(4)

C10(H10A	0.9800

C10(H10B	0.9800

C10(H10C	0.9800

C11(O7	1.203(4)

C11(O6	1.368(3)

C11(C12	1.489(4)

C12(H12A	0.9800

C12(H12B	0.9800

C12(H12C	0.9800

C13(O9	1.194(3)

C13(O8	1.363(3)

C13(C14	1.489(4)

C14(H14A	0.9800

C14(H14B	0.9800

C14(H14C	0.9800

C15(O11	1.196(4)

C15(O10	1.368(4)

C15(C16	1.492(4)

C16(H16A	0.9800

C16(H16B	0.9800

C16(H16C	0.9800

O1(C1(C2	109.9(2)

O1(C1(C6	106.9(2)

C2(C1(C6	113.6(2)

O1(C1(H1	108.8

C2(C1(H1	108.8

C6(C1(H1	108.8

O4(C2(C1	107.8(2)

O4(C2(C3	109.5(2)

C1(C2(C3	108.8(2)

O4(C2(H2	110.2

C1(C2(H2	110.2

C3(C2(H2	110.2

O6(C3(C4	108.5(2)

O6(C3(C2	110.9(2)

C4(C3(C2	109.9(2)

O6(C3(H3	109.2

C4(C3(H3	109.2

C2(C3(H3	109.2

O8(C4(C3	108.6(2)

O8(C4(C5	107.0(2)

C3(C4(C5	107.5(2)

O8(C4(H4	111.2

C3(C4(H4	111.2

C5(C4(H4	111.2

O1(C5(O10	106.2(2)

O1(C5(C4	111.6(2)

O10(C5(C4	107.2(2)

O1(C5(H5	110.6

O10(C5(H5	110.6

C4(C5(H5	110.6

O2(C6(C1	103.3(2)

O2(C6(H6A	111.1

C1(C6(H6A	111.1

O2(C6(H6B	111.1

C1(C6(H6B	111.1

H6A(C6(H6B	109.1

O3(C7(O2	122.7(3)

O3(C7(C8	126.1(3)

O2(C7(C8	111.2(2)

C7(C8(H8A	109.5

C7(C8(H8B	109.5

H8A(C8(H8B	109.5

C7(C8(H8C	109.5

H8A(C8(H8C	109.5

H8B(C8(H8C	109.5

O5(C9(O4	123.6(3)

O5(C9(C10	126.2(3)

O4(C9(C10	110.2(2)

C9(C10(H10A	109.5

C9(C10(H10B	109.5

H10A(C10(H10B	109.5

C9(C10(H10C	109.5

H10A(C10(H10C	109.5

H10B(C10(H10C	109.5

O7(C11(O6	122.7(3)

O7(C11(C12	125.8(3)

O6(C11(C12	111.5(3)

C11(C12(H12A	109.5

C11(C12(H12B	109.5

H12A(C12(H12B	109.5

C11(C12(H12C	109.5

H12A(C12(H12C	109.5

H12B(C12(H12C	109.5

O9(C13(O8	123.4(3)

O9(C13(C14	125.6(3)

O8(C13(C14	111.0(2)

C13(C14(H14A	109.5

C13(C14(H14B	109.5

H14A(C14(H14B	109.5

C13(C14(H14C	109.5

H14A(C14(H14C	109.5

H14B(C14(H14C	109.5

O11(C15(O10	122.7(3)

O11(C15(C16	127.1(3)

O10(C15(C16	110.3(3)

C15(C16(H16A	109.5

C15(C16(H16B	109.5

H16A(C16(H16B	109.5

C15(C16(H16C	109.5

H16A(C16(H16C	109.5

H16B(C16(H16C	109.5

C5(O1(C1	110.23(19)

C7(O2(C6	116.5(2)

C9(O4(C2	117.8(2)

C11(O6(C3	114.3(2)

C13(O8(C4	117.2(2)

C15(O10(C5	116.8(2)

Symmetry transformations used to generate equivalent atoms:

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C1	23(1) 	24(1)	17(1) 	(2(1)	2(1) 	(1(1)

C2	22(1) 	23(1)	17(1) 	(1(1)	2(1) 	(1(1)

C3	22(1) 	21(1)	18(1) 	(2(1)	1(1) 	(2(1)

C4	21(1) 	24(1)	15(1) 	0(1)	(1(1) 	1(1)

C5	26(1) 	23(1)	19(1) 	1(1)	2(1) 	(1(1)

C6	23(1) 	33(2)	20(1) 	(2(1)	2(1) 	(2(1)

C7	29(2) 	19(1)	21(1) 	1(1)	(4(1) 	(1(1)

C8	32(2) 	36(2)	21(1) 	1(1)	0(1) 	3(1)

C9	28(2) 	24(1)	22(1) 	3(1)	(4(1) 	(4(1)

C10	29(2) 	23(1)	28(2) 	0(1)	(3(1) 	(4(1)

C11	23(1) 	36(2)	23(1) 	2(1)	(1(1) 	(3(1)

C12	41(2) 	49(2)	37(2) 	(4(2)	7(2) 	(21(2)

C13	27(1) 	24(1)	18(1) 	(1(1)	2(1) 	(5(1)

C14	35(2) 	35(2)	19(1) 	2(1)	(1(1) 	2(2)

C15	30(2) 	35(2)	23(1) 	4(1)	(2(1) 	(10(1)

C16	47(2) 	59(2)	32(2) 	(3(2)	15(2) 	(22(2)

O1	22(1) 	32(1)	19(1) 	1(1)	1(1) 	(2(1)

O2	23(1) 	38(1)	17(1) 	(2(1)	1(1) 	(3(1)

O3	25(1) 	34(1)	23(1) 	(3(1)	(4(1) 	1(1)

O4	24(1) 	21(1)	22(1) 	2(1)	1(1) 	1(1)

O5	34(1) 	32(1)	39(1) 	8(1)	16(1) 	(2(1)

O6	23(1) 	25(1)	21(1) 	(2(1)	2(1) 	(5(1)

O7	26(1) 	35(1)	32(1) 	(1(1)	7(1) 	1(1)

O8	29(1) 	27(1)	17(1) 	2(1)	0(1) 	2(1)

O9	58(2) 	37(1)	22(1) 	(3(1)	0(1) 	16(1)

O10	31(1) 	28(1)	23(1) 	(1(1)	9(1) 	(7(1)

O11	43(1) 	31(1)	51(1) 	6(1)	7(1) 	(7(1)

Thermal ellipsoids drawn at the 50% probability level.

# Text boxes

# Single Crystal X-Ray Diffraction Service

School of Chemistry - University of Southampton

Contact: Dr Mark E Light, light@soton.ac.uk, ex 29429