Crystal data and details of data collection and refinement for:

(1) 92CAR011

(2) 92CAR018

(3) 92CAR027

---------------------------------------------------------------------------

Compound 1        Compound 2        Compound 3

---------------------------------------------------------------------------

Formula                 [Pt(C22H18N4)].   [Pt(C24H26N4)].    [Pt(C22H22N4)]

2(ClO4)           2(ClO4). 0.5H2O    2(ClO4)

M.W.                    732.39            773.49             736.42

Crystal system          Monoclinic        Triclinic          Monoclinic

a/�                     8.397(3)          8.365(2)           13.876(9)

b/�                     27.420(8)         12.065(5)          14.172(9)

c/�                     10.898(4)         14.319(9)          27.722(5)

a/o                     90                94.73(1)           90

b/o                     96.92(1)          92.95(1)           103.83(2)

g/o                     90                94.99(2)           90

V/�3                    2490.94           1432.28            5293.50

q range for cell/o      1.5-25            1.5-25             1.5-25

Space group             P21/c             P-1                P21/c

Z                       4                 2                  8

Dc/gcm-3                1.953             1.793              1.848

F(000)                  1416              758                2864

m(Mo-Ka)/cm-1           57.6              51.9               56.1

T/K                     298               298                298

Crystal size/mm3        0.50x0.08x0.06    0.45x0.20x0.12     0.50x0.15x0.07

q range for data/o      2.4-28.5          2.3-28.8           2.3-29.5

hmin, hmax              -8,10             -10,8              -9,18

kmin, kmax              -24,35            -15,7              -15,19

lmin, lmax              -12,14            -16,19             -37,37

Total data measured     8993              4627               22200

Total unique            3212              4207               8223

Rint                    0.0443            0.0381             0.0524

Total observed          2820              3119               6616

Significance test       Fo>3s(Fo)         Fo>3s(Fo)          Fo>3s(Fo)

Absorption correction

factors, min, max     0.939,1.191       0.909,1.048        0.888,1.412

No. of parameters       353               434                664

rmin-rmax/e�-3          -0.80,0.82        -0.50,1.10         -1.40,1.80

(D/s)max                0.194             0.551              0.026

Weighting scheme        unit weight       unit weight        unit weight

R                       0.0302            0.0341             0.0466

wR                      0.0322            0.0405             0.0555

---------------------------------------------------------------------------

Notes:

(1) Treatment of the H atoms: In all three compounds, the ring H's were allowed to ride on their parent carbons (C-H=0.96A), and a common Uiso was refined for all in each compound. The methyl H's were ignored.

(2) Structures solved (Patterson + difference Fourier) by SHELX-S (G.M. Sheldrick, Univ. of Gottingen, 1986); and refined (full-matrix least-squares) by SHELX-80 (G.M. Sheldrick, Univ. of Gottingen, 1980); Empirical absorption correction by DIFABS (N. Walker and D. Stuart, Acta Cryst., 1983, A39, 158-166) adapted for FAST geometry by A. Karaulov, Univ. of Cardiff, 1990); Figures drawn by SNOOPI (K. Davies, Univ. of Oxford, 1983).

(3) All calculations made on a T800 transputer hosted by an IBM/AT personal computer.