|  | University of Southampton · Department of Chemistry # EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	02src392    (301-365/1)

Empirical formula 	C9H15Cl2F4N4O3P3

Formula weight 	467.06

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Orthorhombic

Space group 	P212121

Unit cell dimensions	a = 8.2682(2) Å	 = 90°

b = 13.1798(4) Å	 = 90°

c = 16.1482(5) Å	  = 90°

Volume	1759.72(9) Å3

Z	4

Density (calculated)	1.763 Mg / m3

Absorption coefficient	0.700 mm1

F(000)	944

Crystal	plate; colourless

Crystal size	0.24  0.12  0.03 mm3

 range for data collection	2.96  27.50°

Index ranges	10  h  9, 14  k  17, 19  l  20

Reflections collected	10491

Independent reflections	3955 [Rint = 0.0425]

Completeness to  = 27.50°	99.3 %

Absorption correction	Semiempirical from equivalents

Max. and min. transmission	0.9793 and 0.8499

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	3955 / 0 / 228

Goodness-of-fit on F2	0.918

Final R indices [F2 > 2(F2)]	R1 = 0.0322, wR2 = 0.0746

R indices (all data)	R1 = 0.0408, wR2 = 0.0789

Absolute structure parameter	0.03(6)

Extinction coefficient	0.0013(6)

Largest diff. peak and hole	0.319 and 0.321 e Å3

Diffractometer: Enraf Nonius KappaCCD area detector ( scans and  scans to fill Ewald sphere). Data collection and cell

refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography,

part A, pp. 307326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing,

Acta Cryst. A51 (1995) 3337; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421426). Program used to solve structure:

SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467473). Program used to refine structure: SHELXL97 (G. M. Sheldrick

(1997), University of Göttingen, Germany).

Further information:  http://www.soton.ac.uk/~xservice/strat.htm

Special details:

From MeOH.

Meso structure; P1 = S, P2 = R. P1-P2 = 2.737, P2-P3 = 2.763, P1-P3 = 2.784, max deviation = 0.074 (N1).

Table 2. Atomic coordinates [ 104], equivalent isotropic displacement parameters [Å2  103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C1	9687(3)	2462(2)	8903(2)	18(1)	1

C2	8775(3)	3379(2)	9262(2)	17(1)	1

C3	7071(3)	3568(2)	8916(2)	17(1)	1

C4	6858(3)	3772(2)	8000(2)	17(1)	1

C5	13264(4)	5910(3)	9439(2)	36(1)	1

C6	12569(4)	6478(3)	10181(2)	32(1)	1

C7	10741(4)	6389(2)	10062(2)	30(1)	1

C8	10541(4)	6536(2)	9127(2)	26(1)	1

C9	14108(3)	5590(2)	6677(2)	24(1)	1

N1	10091(2)	3481(1)	7345(1)	14(1)	1

N2	10447(3)	5530(2)	7430(1)	17(1)	1

N3	12780(2)	4285(2)	8047(1)	18(1)	1

N4	12009(3)	6032(2)	8795(1)	22(1)	1

O1	11316(2)	2720(1)	8682(1)	18(1)	1

O2	7741(2)	4665(1)	7762(1)	18(1)	1

O3	13490(2)	6020(1)	7439(1)	21(1)	1

F1	9651(2)	4242(1)	9177(1)	21(1)	1

F2	8589(2)	3242(1)	10100(1)	25(1)	1

F3	6432(2)	4352(1)	9352(1)	27(1)	1

F4	6179(2)	2731(1)	9095(1)	27(1)	1

P1	11711(1)	3330(1)	7859(1)	14(1)	1

P2	9363(1)	4585(1)	7245(1)	14(1)	1

P3	12122(1)	5425(1)	7925(1)	16(1)	1

Cl1	13116(1)	2323(1)	7269(1)	21(1)	1

Cl2	8538(1)	4710(1)	6079(1)	24(1)	1

Table 3. Bond lengths [Å] and angles [°].

C1O1	1.435(3)

C1C2	1.538(3)

C1H1A	0.9900

C1H1B	0.9900

C2F1	1.356(3)

C2F2	1.372(3)

C2C3	1.536(3)

C3F4	1.359(3)

C3F3	1.358(3)

C3C4	1.513(4)

C4O2	1.438(3)

C4H4A	0.9900

C4H4B	0.9900

C5N4	1.478(4)

C5C6	1.525(4)

C5H5A	0.9900

C5H5B	0.9900

C6C7	1.528(4)

C6H6A	0.9900

C6H6B	0.9900

C7C8	1.532(4)

C7H7A	0.9900

C7H7B	0.9900

C8N4	1.484(4)

C8H8A	0.9900

C8H8B	0.9900

C9O3	1.448(3)

C9H9A	0.9800

C9H9B	0.9800

C9H9C	0.9800

N1P2	1.584(2)

N1P1	1.589(2)

N2P2	1.563(2)

N2P3	1.605(2)

N3P1	1.567(2)

N3P3	1.610(2)

N4P3	1.618(2)

O1P1	1.5871(18)

O2P2	1.5835(18)

O3P3	1.5842(18)

P1Cl1	2.0048(8)

P2Cl2	2.0089(9)

O1C1C2	111.6(2)

O1C1H1A	109.3

C2C1H1A	109.3

O1C1H1B	109.3

C2C1H1B	109.3

H1AC1H1B	108.0

F1C2F2	105.64(19)

F1C2C3	108.5(2)

F2C2C3	106.1(2)

F1C2C1	111.0(2)

F2C2C1	108.8(2)

C3C2C1	116.1(2)

F4C3F3	107.22(19)

F4C3C4	106.8(2)

F3C3C4	109.1(2)

F4C3C2	106.77(19)

F3C3C2	106.9(2)

C4C3C2	119.5(2)

O2C4C3	110.3(2)

O2C4H4A	109.6

C3C4H4A	109.6

O2C4H4B	109.6

C3C4H4B	109.6

H4AC4H4B	108.1

N4C5C6	103.6(2)

N4C5H5A	111.0

C6C5H5A	111.0

N4C5H5B	111.0

C6C5H5B	111.0

H5AC5H5B	109.0

C5C6C7	103.7(2)

C5C6H6A	111.0

C7C6H6A	111.0

C5C6H6B	111.0

C7C6H6B	111.0

H6AC6H6B	109.0

C6C7C8	102.7(3)

C6C7H7A	111.2

C8C7H7A	111.2

C6C7H7B	111.2

C8C7H7B	111.2

H7AC7H7B	109.1

N4C8C7	102.2(2)

N4C8H8A	111.3

C7C8H8A	111.3

N4C8H8B	111.3

C7C8H8B	111.3

H8AC8H8B	109.2

O3C9H9A	109.5

O3C9H9B	109.5

H9AC9H9B	109.5

O3C9H9C	109.5

H9AC9H9C	109.5

H9BC9H9C	109.5

P2N1P1	119.25(13)

P2N2P3	121.45(13)

P1N3P3	122.38(13)

C8N4C5	111.6(2)

C8N4P3	125.58(19)

C5N4P3	121.11(19)

C1O1P1	121.49(15)

C4O2P2	121.07(15)

C9O3P3	118.66(16)

N3P1O1	111.17(11)

N3P1N1	118.43(11)

O1P1N1	109.08(10)

N3P1Cl1	107.27(8)

O1P1Cl1	100.48(7)

N1P1Cl1	108.86(8)

N2P2N1	119.66(11)

N2P2O2	109.39(11)

N1P2O2	109.22(10)

N2P2Cl2	107.99(8)

N1P2Cl2	107.44(8)

O2P2Cl2	101.60(7)

O3P3N2	109.05(11)

O3P3N3	106.31(10)

N2P3N3	115.62(11)

O3P3N4	103.10(11)

N2P3N4	109.88(12)

N3P3N4	112.03(12)

Symmetry transformations used to generate equivalent atoms:

Table 4. Anisotropic displacement parameters [Å2 103]. The anisotropic displacement

factor exponent takes the form: 2 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C1	20(1) 	16(1)	19(1) 	3(1)	3(1) 	2(1)

C2	20(1) 	18(1)	12(1) 	0(1)	1(1) 	4(1)

C3	14(1) 	19(1)	18(1) 	1(1)	3(1) 	2(1)

C4	11(1) 	20(1)	19(1) 	0(1)	1(1) 	2(1)

C5	24(2) 	53(2)	31(2) 	18(1)	2(1) 	3(2)

C6	27(2) 	44(2)	25(2) 	12(1)	0(1) 	2(1)

C7	31(2) 	36(2)	22(1) 	2(1)	1(1) 	3(1)

C8	31(2) 	24(1)	22(1) 	1(1)	1(1) 	10(1)

C9	24(1) 	31(2)	19(1) 	0(1)	7(1) 	0(1)

N1	14(1) 	14(1)	13(1) 	0(1)	2(1) 	1(1)

N2	17(1) 	14(1)	19(1) 	4(1)	1(1) 	1(1)

N3	12(1) 	19(1)	23(1) 	0(1)	1(1) 	1(1)

N4	18(1) 	27(1)	22(1) 	4(1)	1(1) 	0(1)

O1	15(1) 	20(1)	20(1) 	5(1)	0(1) 	1(1)

O2	15(1) 	18(1)	21(1) 	3(1)	3(1) 	2(1)

O3	22(1) 	18(1)	22(1) 	2(1)	7(1) 	5(1)

F1	20(1) 	18(1)	23(1) 	2(1)	2(1) 	3(1)

F2	31(1) 	33(1)	12(1) 	2(1)	2(1) 	4(1)

F3	25(1) 	34(1)	21(1) 	6(1)	3(1) 	9(1)

F4	21(1) 	33(1)	27(1) 	5(1)	5(1) 	10(1)

P1	13(1) 	14(1)	16(1) 	0(1)	1(1) 	2(1)

P2	12(1) 	17(1)	14(1) 	2(1)	0(1) 	2(1)

P3	14(1) 	15(1)	18(1) 	1(1)	1(1) 	2(1)

Cl1	19(1) 	20(1)	25(1) 	4(1)	2(1) 	5(1)

Cl2	26(1) 	32(1)	15(1) 	4(1)	4(1) 	4(1)

Table 5. Torsion angles [°].

O1C1C2F1	8.5(3)

O1C1C2F2	107.4(2)

O1C1C2C3	133.0(2)

F1C2C3F4	173.29(18)

F2C2C3F4	60.2(2)

C1C2C3F4	60.9(3)

F1C2C3F3	58.8(2)

F2C2C3F3	54.3(2)

C1C2C3F3	175.4(2)

F1C2C3C4	65.6(3)

F2C2C3C4	178.7(2)

C1C2C3C4	60.2(3)

F4C3C4O2	178.67(18)

F3C3C4O2	63.1(2)

C2C3C4O2	60.2(3)

N4C5C6C7	28.5(3)

C5C6C7C8	40.2(3)

C6C7C8N4	35.5(3)

C7C8N4C5	18.5(3)

C7C8N4P3	146.6(2)

C6C5N4C8	6.2(3)

C6C5N4P3	172.0(2)

C2C1O1P1	77.3(2)

C3C4O2P2	106.3(2)

P3N3P1O1	113.33(15)

P3N3P1N1	14.1(2)

P3N3P1Cl1	137.73(13)

C1O1P1N3	127.39(18)

C1O1P1N1	5.0(2)

C1O1P1Cl1	119.32(17)

P2N1P1N3	16.12(19)

P2N1P1O1	112.33(14)

P2N1P1Cl1	138.91(11)

P3N2P2N1	15.1(2)

P3N2P2O2	111.94(15)

P3N2P2Cl2	138.28(12)

P1N1P2N2	16.75(19)

P1N1P2O2	110.35(14)

P1N1P2Cl2	140.22(11)

C4O2P2N2	153.21(17)

C4O2P2N1	20.5(2)

C4O2P2Cl2	92.80(17)

C9O3P3N2	73.1(2)

C9O3P3N3	52.2(2)

C9O3P3N4	170.20(19)

P2N2P3O3	131.88(14)

P2N2P3N3	12.2(2)

P2N2P3N4	115.80(16)

P1N3P3O3	133.05(15)

P1N3P3N2	11.9(2)

P1N3P3N4	115.04(16)

C8N4P3O3	121.2(2)

C5N4P3O3	75.0(2)

C8N4P3N2	5.0(3)

C5N4P3N2	168.8(2)

C8N4P3N3	124.9(2)

C5N4P3N3	38.9(3)

Symmetry transformations used to generate equivalent atoms: