|  | University of Southampton · Department of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	02src556

Empirical formula 	C29H38I2O11PZn

Formula weight 	912.73

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Triclinic

Space group 	P(1

Unit cell dimensions	a = 11.7172(2) Å	( = 69.7750(10)°

b = 12.5417(2) Å	( = 69.7460(10)°

c = 13.7674(2) Å	(  = 70.6080(10)°

Volume	1728.45(5) Å3

Z	2

Density (calculated)	1.754 Mg / m3

Absorption coefficient	2.597 mm(1

F(000)	902

Crystal	block; yellow

Crystal size	0.40 ( 0.25 ( 0.20 mm3

( range for data collection	3.09 ( 27.48°

Index ranges	(15 ( h ( 15, (16 ( k ( 16, (17 ( l ( 17

Reflections collected	25558

Independent reflections	7839 [Rint = 0.0546]

Completeness to ( = 27.48°	98.8 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.6247 and 0.4231

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	7839 / 0 / 408

Goodness-of-fit on F2	1.024

Final R indices [F2 > 2((F2)]	R1 = 0.0419, wR2 = 0.1043

R indices (all data)	R1 = 0.0517, wR2 = 0.1107

Extinction coefficient	0.0008(3)

Largest diff. peak and hole	1.984 and (1.724 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing, Acta Cryst. A51 (1995) 33(37; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421(426). Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: Cameron - A Molecular Graphics Package. (D. M. Watkin, L. Pearce and C. K. Prout, Chemical Crystallography Laboratory, University of Oxford, 1993).

Special details:

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C1	3372(3)	5050(3)	8129(3)	16(1)	1

C2	4413(3)	4469(3)	7461(3)	18(1)	1

C3	5981(4)	4579(4)	5780(3)	28(1)	1

C4	4917(4)	3261(3)	7759(3)	22(1)	1

C5	4307(4)	2623(3)	8735(3)	25(1)	1

C6	5951(5)	882(4)	8576(4)	40(1)	1

C7	3229(4)	3153(3)	9399(3)	24(1)	1

C8	2767(3)	4350(3)	9092(3)	19(1)	1

C9	1133(4)	4287(4)	10728(3)	31(1)	1

C10	1795(3)	7247(3)	8752(3)	18(1)	1

C11	2195(3)	7048(3)	9674(3)	19(1)	1

C12	3835(4)	6173(4)	10563(4)	39(1)	1

C13	1441(4)	7521(3)	10518(3)	26(1)	1

C14	246(4)	8217(3)	10461(3)	27(1)	1

C15	(1695(5)	9320(5)	11376(4)	46(1)	1

C16	(192(4)	8441(3)	9581(3)	24(1)	1

C17	579(3)	7943(3)	8746(3)	20(1)	1

C18	(940(4)	8960(4)	7711(3)	36(1)	1

C19	2197(3)	6988(3)	6589(3)	16(1)	1

C20	2099(3)	8128(3)	5895(3)	19(1)	1

C21	2216(4)	10090(3)	5564(4)	32(1)	1

C22	1630(3)	8446(3)	5006(3)	23(1)	1

C23	1217(3)	7645(3)	4824(3)	21(1)	1

C24	267(4)	7255(4)	3734(4)	36(1)	1

C25	1202(3)	6540(3)	5526(3)	20(1)	1

C26	1689(3)	6225(3)	6412(3)	18(1)	1

C27	1242(4)	4331(3)	6983(3)	28(1)	1

C28	4644(7)	9001(6)	7831(7)	79(2)	1

C29	5349(11)	8241(8)	8445(8)	105(3)	1

O1	4910(2)	5147(2)	6481(2)	21(1)	1

O2	4720(3)	1436(2)	9109(3)	37(1)	1

O3	1698(2)	4920(2)	9682(2)	24(1)	1

O4	3371(2)	6360(2)	9668(2)	24(1)	1

O5	(427(3)	8646(3)	11339(2)	43(1)	1

O6	167(2)	8090(2)	7885(2)	25(1)	1

O7	2441(3)	8892(2)	6172(2)	24(1)	1

O8	804(3)	8021(3)	3912(2)	31(1)	1

O9	1648(3)	5186(2)	7161(2)	25(1)	1

O10	4036(2)	7112(2)	7331(2)	20(1)	1

O11	5356(4)	8909(3)	6643(3)	44(1)	1

P1	2892(1)	6623(1)	7677(1)	15(1)	1

Zn1	5519(1)	7391(1)	6247(1)	24(1)	1

I1	5536(1)	8070(1)	4255(1)	26(1)	1

I2	7639(1)	6139(1)	6590(1)	46(1)	1

Table 3. Bond lengths [Å] and angles [°].

C1(C2	1.400(5)

C1(C8	1.410(5)

C1(P1	1.803(3)

C2(O1	1.369(4)

C2(C4	1.399(5)

C3(O1	1.434(4)

C4(C5	1.388(5)

C5(O2	1.372(5)

C5(C7	1.391(6)

C6(O2	1.434(6)

C7(C8	1.381(5)

C8(O3	1.358(4)

C9(O3	1.429(4)

C10(C17	1.404(5)

C10(C11	1.418(5)

C10(P1	1.809(4)

C11(O4	1.360(4)

C11(C13	1.378(5)

C12(O4	1.433(5)

C13(C14	1.395(6)

C14(O5	1.372(5)

C14(C16	1.381(6)

C15(O5	1.438(5)

C16(C17	1.390(5)

C17(O6	1.363(4)

C18(O6	1.424(5)

C19(C26	1.403(5)

C19(C20	1.412(5)

C19(P1	1.800(3)

C20(O7	1.356(4)

C20(C22	1.393(5)

C21(O7	1.431(4)

C22(C23	1.372(6)

C23(O8	1.377(4)

C23(C25	1.391(5)

C24(O8	1.431(5)

C25(C26	1.402(5)

C26(O9	1.357(4)

C27(O9	1.426(4)

C28(C29	1.307(11)

C28(O11	1.584(9)

O10(P1	1.517(3)

O10(Zn1	1.902(2)

O11(Zn1	2.088(3)

Zn1(I2	2.5619(5)

Zn1(I1	2.5704(5)

C2(C1(C8	117.0(3)

C2(C1(P1	117.6(3)

C8(C1(P1	125.3(3)

O1(C2(C4	121.1(3)

O1(C2(C1	116.3(3)

C4(C2(C1	122.6(3)

C5(C4(C2	117.6(3)

O2(C5(C7	115.5(3)

O2(C5(C4	122.6(4)

C7(C5(C4	121.9(3)

C8(C7(C5	119.2(3)

O3(C8(C7	122.4(3)

O3(C8(C1	116.1(3)

C7(C8(C1	121.6(3)

C17(C10(C11	116.4(3)

C17(C10(P1	125.6(3)

C11(C10(P1	117.9(3)

O4(C11(C13	122.5(3)

O4(C11(C10	115.4(3)

C13(C11(C10	122.1(3)

C11(C13(C14	118.8(3)

O5(C14(C16	124.2(4)

O5(C14(C13	114.2(3)

C16(C14(C13	121.6(3)

C14(C16(C17	118.6(3)

O6(C17(C16	120.9(3)

O6(C17(C10	116.7(3)

C16(C17(C10	122.4(3)

C26(C19(C20	117.4(3)

C26(C19(P1	124.0(3)

C20(C19(P1	118.5(3)

O7(C20(C22	122.8(3)

O7(C20(C19	115.9(3)

C22(C20(C19	121.2(3)

C23(C22(C20	119.2(3)

C22(C23(O8	115.4(3)

C22(C23(C25	122.0(3)

O8(C23(C25	122.7(3)

C23(C25(C26	118.3(3)

O9(C26(C25	121.6(3)

O9(C26(C19	116.8(3)

C25(C26(C19	121.6(3)

C29(C28(O11	106.8(7)

C2(O1(C3	117.7(3)

C5(O2(C6	117.8(3)

C8(O3(C9	118.5(3)

C11(O4(C12	117.4(3)

C14(O5(C15	118.1(3)

C17(O6(C18	119.8(3)

C20(O7(C21	117.6(3)

C23(O8(C24	117.4(3)

C26(O9(C27	119.5(3)

P1(O10(Zn1	146.73(16)

C28(O11(Zn1	118.3(3)

O10(P1(C19	111.79(15)

O10(P1(C1	108.39(15)

C19(P1(C1	108.33(16)

O10(P1(C10	106.47(15)

C19(P1(C10	110.50(16)

C1(P1(C10	111.36(16)

O10(Zn1(O11	91.58(13)

O10(Zn1(I2	118.34(8)

O11(Zn1(I2	101.72(11)

O10(Zn1(I1	120.56(8)

O11(Zn1(I1	104.86(9)

I2(Zn1(I1	113.425(19)

Symmetry transformations used to generate equivalent atoms:

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C1	15(2) 	17(2)	18(2) 	(3(1)	(10(1) 	(3(1)

C2	17(2) 	22(2)	18(2) 	(4(1)	(8(1) 	(5(1)

C3	27(2) 	28(2)	22(2) 	(10(2)	2(2) 	(5(2)

C4	21(2) 	23(2)	23(2) 	(8(2)	(8(1) 	(2(1)

C5	27(2) 	20(2)	30(2) 	(2(2)	(15(2) 	(5(2)

C6	44(3) 	18(2)	45(3) 	(5(2)	(13(2) 	6(2)

C7	25(2) 	23(2)	22(2) 	1(2)	(7(2) 	(9(2)

C8	16(2) 	22(2)	19(2) 	(1(1)	(9(1) 	(6(1)

C9	25(2) 	38(2)	20(2) 	1(2)	0(2) 	(9(2)

C10	16(2) 	20(2)	17(2) 	(5(1)	(3(1) 	(4(1)

C11	18(2) 	20(2)	19(2) 	(2(1)	(7(1) 	(6(1)

C12	30(2) 	55(3)	39(2) 	(22(2)	(24(2) 	5(2)

C13	31(2) 	28(2)	20(2) 	(5(2)	(12(2) 	(3(2)

C14	28(2) 	27(2)	18(2) 	(9(2)	(2(2) 	2(2)

C15	35(3) 	52(3)	30(2) 	(18(2)	0(2) 	15(2)

C16	20(2) 	22(2)	22(2) 	(3(2)	(4(1) 	0(1)

C17	21(2) 	19(2)	17(2) 	0(1)	(6(1) 	(5(1)

C18	24(2) 	45(2)	26(2) 	(5(2)	(12(2) 	8(2)

C19	14(2) 	19(2)	14(2) 	(4(1)	(3(1) 	(1(1)

C20	18(2) 	20(2)	18(2) 	(5(1)	(5(1) 	(4(1)

C21	32(2) 	16(2)	46(2) 	2(2)	(15(2) 	(7(2)

C22	22(2) 	23(2)	18(2) 	1(1)	(8(1) 	(2(1)

C23	18(2) 	27(2)	12(2) 	(3(1)	(6(1) 	1(1)

C24	38(2) 	48(3)	30(2) 	(12(2)	(23(2) 	(4(2)

C25	17(2) 	25(2)	21(2) 	(8(1)	(8(1) 	(2(1)

C26	13(2) 	19(2)	17(2) 	(3(1)	(6(1) 	0(1)

C27	29(2) 	22(2)	37(2) 	(5(2)	(13(2) 	(11(2)

C28	58(4) 	40(3)	129(7) 	(23(4)	(11(4) 	(11(3)

C29	145(9) 	90(6)	122(8) 	(39(6)	(67(7) 	(35(6)

O1	20(1) 	21(1)	16(1) 	(6(1)	(1(1) 	(1(1)

O2	38(2) 	20(1)	39(2) 	(1(1)	(10(1) 	1(1)

O3	19(1) 	24(1)	21(1) 	(2(1)	0(1) 	(7(1)

O4	21(1) 	32(1)	22(1) 	(12(1)	(12(1) 	0(1)

O5	39(2) 	48(2)	24(2) 	(15(1)	(7(1) 	16(2)

O6	16(1) 	34(1)	24(1) 	(7(1)	(11(1) 	3(1)

O7	28(1) 	18(1)	28(1) 	(1(1)	(10(1) 	(8(1)

O8	36(2) 	36(2)	21(1) 	(3(1)	(18(1) 	(4(1)

O9	31(2) 	22(1)	27(1) 	3(1)	(19(1) 	(12(1)

O10	19(1) 	23(1)	19(1) 	(6(1)	(3(1) 	(7(1)

O11	76(3) 	41(2)	30(2) 	1(1)	(21(2) 	(36(2)

P1	13(1) 	17(1)	14(1) 	(3(1)	(4(1) 	(4(1)

Zn1	18(1) 	35(1)	19(1) 	(4(1)	(4(1) 	(10(1)

I1	31(1) 	30(1)	19(1) 	(5(1)	(6(1) 	(11(1)

I2	19(1) 	72(1)	46(1) 	(20(1)	(13(1) 	0(1)