|  | University of Southampton · Department of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	02src656

Empirical formula 	C3H8BrNPd

Formula weight 	244.41

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P21/n

Unit cell dimensions	a = 5.9865(2) Å	( = 90°

b = 11.5083(4) Å	( = 98.2870(10)°

c = 9.1055(3) Å	(  = 90°

Volume	620.77(4) Å3

Z	4

Density (calculated)	2.615 Mg / m3

Absorption coefficient	9.291 mm(1

F(000)	456

Crystal	plate; colourless

Crystal size	0.12 ( 0.08 ( 0.01 mm3

( range for data collection	3.54 ( 27.47°

Index ranges	(7 ( h ( 7, (14 ( k ( 14, (11 ( l ( 11

Reflections collected	9208

Independent reflections	1417 [Rint = 0.0490]

Completeness to ( = 27.47°	99.8 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.9128 and 0.4019

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	1417 / 0 / 57

Goodness-of-fit on F2	1.114

Final R indices [F2 > 2((F2)]	R1 = 0.0335, wR2 = 0.0874

R indices (all data)	R1 = 0.0344, wR2 = 0.0883

Extinction coefficient	0.0080(11)

Largest diff. peak and hole	1.719 and (1.390 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing, Acta Cryst. A51 (1995) 33(37; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421(426). Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: Cameron - A Molecular Graphics Package. (D. M. Watkin, L. Pearce and C. K. Prout, Chemical Crystallography Laboratory, University of Oxford, 1993).

Special details:

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

N1	1696(7)	3581(3)	9113(4)	24(1)	1

C1	(2369(8)	5880(5)	6265(6)	30(1)	1

C2	(2583(9)	4731(5)	5872(6)	36(1)	1

C3	(2966(9)	3916(5)	6925(6)	36(1)	1

Pd1	(19(1)	4880(1)	7713(1)	18(1)	1

Br1	2778(1)	6429(1)	8607(1)	26(1)	1

Table 3. Bond lengths [Å] and angles [°].

N1(Pd1	2.130(4)

N1(H1A	0.9100

N1(H1B	0.9100

N1(H1C	0.9100

C1(C2	1.371(8)

C1(Pd1	2.123(5)

C1(H1A	0.9500

C1(H1B	0.9500

C2(C3	1.384(8)

C2(Pd1	2.110(5)

C2(H2	0.9500

C3(Pd1	2.120(5)

C3(H3A	0.9500

C3(H3B	0.9500

Pd1(Br1	2.4999(5)

Pd1(N1(H1A	109.5

Pd1(N1(H1B	109.5

H1A(N1(H1B	109.5

Pd1(N1(H1C	109.5

H1A(N1(H1C	109.5

H1B(N1(H1C	109.5

C2(C1(Pd1	70.6(3)

C2(C1(H1A	120.0

Pd1(C1(H1A	72.3

C2(C1(H1B	120.0

Pd1(C1(H1B	129.5

H1A(C1(H1B	120.0

C1(C2(C3	119.5(5)

C1(C2(Pd1	71.6(3)

C3(C2(Pd1	71.3(3)

C1(C2(H2	120.3

C3(C2(H2	120.3

Pd1(C2(H2	129.1

C2(C3(Pd1	70.5(3)

C2(C3(H3A	120.0

Pd1(C3(H3A	72.4

C2(C3(H3B	120.0

Pd1(C3(H3B	129.4

H3A(C3(H3B	120.0

C2(Pd1(C3	38.2(2)

C2(Pd1(C1	37.8(2)

C3(Pd1(C1	68.2(2)

C2(Pd1(N1	130.64(19)

C3(Pd1(N1	98.12(19)

C1(Pd1(N1	166.23(18)

C2(Pd1(Br1	133.86(16)

C3(Pd1(Br1	165.71(17)

C1(Pd1(Br1	99.71(15)

N1(Pd1(Br1	93.60(11)

Symmetry transformations used to generate equivalent atoms:

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

N1	26(2) 	25(2)	20(2) 	2(1)	2(2) 	2(1)

C1	25(2) 	35(3)	29(2) 	8(2)	(4(2) 	5(2)

C2	32(3) 	46(3)	28(3) 	(3(2)	(3(2) 	(4(2)

C3	32(3) 	41(3)	31(3) 	1(2)	(10(2) 	(15(2)

Pd1	18(1) 	20(1)	15(1) 	(1(1)	3(1) 	1(1)

Br1	25(1) 	26(1)	27(1) 	1(1)	3(1) 	(4(1)