|  | University of Southampton · Department of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	03src0403

Empirical formula 	C12H12.50N0.50O

Formula weight 	179.73

Temperature 	293(2) K

Wavelength 	0.71073 Å

Crystal system 	Orthorhombic

Space group 	P212121

Unit cell dimensions	a = 8.2378(5) Å	( = 90°

b = 9.2872(5) Å	( = 90°

c = 25.4354(13) Å	(  = 90°

Volume	1945.96(19) Å3

Z	8

Density (calculated)	1.227 Mg / m3

Absorption coefficient	0.077 mm(1

F(000)	768

Crystal	prism; colourless

Crystal size	0.60 ( 0.15 ( 0.10 mm3

( range for data collection	2.95 ( 27.48°

Index ranges	(10 ( h ( 10, (12 ( k ( 10, (32 ( l ( 32

Reflections collected	13136

Independent reflections	3904 [Rint = 0.0626]

Completeness to ( = 27.48°	94.8 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.9923 and 0.9551

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	3904 / 0 / 245

Goodness-of-fit on F2	1.013

Final R indices [F2 > 2((F2)]	R1 = 0.0630, wR2 = 0.1707

R indices (all data)	R1 = 0.0980, wR2 = 0.1934

Absolute structure parameter	1(2)

Extinction coefficient	0.019(6)

Largest diff. peak and hole	0.292 and (0.246 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing, Acta Cryst. A51 (1995) 33(37; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421(426). Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: Cameron - A Molecular Graphics Package. (D. M. Watkin, L. Pearce and C. K. Prout, Chemical Crystallography Laboratory, University of Oxford, 1993).

Special details:

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C1	8686(4)	8678(3)	1604(1)	49(1)	1

C2	9135(4)	8841(4)	2152(1)	66(1)	1

C3	10572(7)	9757(5)	2238(2)	110(2)	1

C4	11024(7)	10733(8)	1867(2)	138(3)	1

C5	10756(5)	10419(4)	1332(2)	84(1)	1

C6	9473(4)	9396(3)	1218(1)	55(1)	1

C7	7398(4)	7638(3)	1472(1)	47(1)	1

C8	5801(4)	9277(3)	893(1)	50(1)	1

C9	5883(4)	10469(3)	1283(1)	50(1)	1

C10	5413(4)	10283(4)	1792(1)	62(1)	1

C11	5454(5)	11464(5)	2150(2)	84(1)	1

C12	5850(6)	12817(5)	1946(2)	86(1)	1

C13	6481(8)	12977(5)	1453(2)	101(2)	1

C14	6361(5)	11840(3)	1096(1)	67(1)	1

C15	5864(3)	6688(3)	729(1)	46(1)	1

C16	6952(4)	6167(4)	363(1)	55(1)	1

C17	6547(4)	4975(4)	71(1)	65(1)	1

C18	5052(4)	4344(4)	145(1)	62(1)	1

C19	3955(4)	4852(3)	511(1)	53(1)	1

C20	2364(5)	4075(4)	591(2)	76(1)	1

C21	1211(6)	4845(8)	940(2)	139(2)	1

C22	1851(6)	5676(6)	1349(2)	111(2)	1

C23	3218(4)	6643(4)	1220(1)	65(1)	1

C24	4350(3)	6067(3)	812(1)	47(1)	1

N1	6370(3)	7927(2)	1042(1)	44(1)	1

O1	7265(3)	6502(2)	1709(1)	69(1)	1

O2	5206(3)	9452(2)	466(1)	74(1)	1

Table 3. Bond lengths [Å] and angles [°].

C1(C6	1.351(4)

C1(C2	1.451(4)

C1(C7	1.473(4)

C2(C3	1.473(6)

C2(H2A	0.9700

C2(H2B	0.9700

C3(C4	1.361(7)

C3(H3A	0.9700

C3(H3B	0.9700

C4(C5	1.408(6)

C4(H4A	0.9700

C4(H4B	0.9700

C5(C6	1.450(5)

C5(H5A	0.9700

C5(H5B	0.9700

C6(H6	0.9300

C7(O1	1.219(3)

C7(N1	1.411(3)

C8(O2	1.201(3)

C8(N1	1.391(4)

C8(C9	1.489(4)

C9(C10	1.362(4)

C9(C14	1.414(4)

C10(C11	1.427(5)

C10(H10	0.9300

C11(C12	1.397(6)

C11(H11	0.9300

C12(C13	1.366(6)

C12(H12	0.9300

C13(C14	1.397(5)

C13(H13	0.9300

C14(H14	0.9300

C15(C16	1.380(4)

C15(C24	1.390(4)

C15(N1	1.459(3)

C16(C17	1.374(4)

C16(H16	0.9300

C17(C18	1.377(5)

C17(H17	0.9300

C18(C19	1.380(5)

C18(H18	0.9300

C19(C24	1.402(4)

C19(C20	1.510(5)

C20(C21	1.483(7)

C20(H20A	0.9700

C20(H20B	0.9700

C21(C22	1.400(7)

C21(H21A	0.9700

C21(H21B	0.9700

C22(C23	1.477(6)

C22(H22A	0.9700

C22(H22B	0.9700

C23(C24	1.494(4)

C23(H23A	0.9700

C23(H23B	0.9700

C6(C1(C2	121.5(3)

C6(C1(C7	120.4(2)

C2(C1(C7	118.0(3)

C1(C2(C3	114.0(3)

C1(C2(H2A	108.7

C3(C2(H2A	108.7

C1(C2(H2B	108.7

C3(C2(H2B	108.7

H2A(C2(H2B	107.6

C4(C3(C2	120.1(3)

C4(C3(H3A	107.3

C2(C3(H3A	107.3

C4(C3(H3B	107.3

C2(C3(H3B	107.3

H3A(C3(H3B	106.9

C3(C4(C5	119.2(5)

C3(C4(H4A	107.5

C5(C4(H4A	107.5

C3(C4(H4B	107.5

C5(C4(H4B	107.5

H4A(C4(H4B	107.0

C4(C5(C6	116.3(4)

C4(C5(H5A	108.2

C6(C5(H5A	108.2

C4(C5(H5B	108.2

C6(C5(H5B	108.2

H5A(C5(H5B	107.4

C1(C6(C5	121.9(3)

C1(C6(H6	119.0

C5(C6(H6	119.0

O1(C7(N1	119.6(3)

O1(C7(C1	121.4(3)

N1(C7(C1	118.9(2)

O2(C8(N1	120.4(3)

O2(C8(C9	121.3(3)

N1(C8(C9	118.2(2)

C10(C9(C14	120.9(3)

C10(C9(C8	121.7(3)

C14(C9(C8	117.3(3)

C9(C10(C11	120.1(3)

C9(C10(H10	119.9

C11(C10(H10	119.9

C12(C11(C10	117.4(3)

C12(C11(H11	121.3

C10(C11(H11	121.3

C13(C12(C11	121.8(4)

C13(C12(H12	119.1

C11(C12(H12	119.1

C12(C13(C14	119.2(4)

C12(C13(H13	120.4

C14(C13(H13	120.4

C13(C14(C9	118.8(3)

C13(C14(H14	120.6

C9(C14(H14	120.6

C16(C15(C24	122.6(3)

C16(C15(N1	117.3(3)

C24(C15(N1	120.0(3)

C17(C16(C15	119.4(3)

C17(C16(H16	120.3

C15(C16(H16	120.3

C16(C17(C18	119.0(3)

C16(C17(H17	120.5

C18(C17(H17	120.5

C17(C18(C19	122.2(3)

C17(C18(H18	118.9

C19(C18(H18	118.9

C18(C19(C24	119.5(3)

C18(C19(C20	119.7(3)

C24(C19(C20	120.8(3)

C21(C20(C19	114.0(3)

C21(C20(H20A	108.8

C19(C20(H20A	108.8

C21(C20(H20B	108.8

C19(C20(H20B	108.8

H20A(C20(H20B	107.6

C22(C21(C20	118.0(4)

C22(C21(H21A	107.8

C20(C21(H21A	107.8

C22(C21(H21B	107.8

C20(C21(H21B	107.8

H21A(C21(H21B	107.1

C21(C22(C23	117.2(4)

C21(C22(H22A	108.0

C23(C22(H22A	108.0

C21(C22(H22B	108.0

C23(C22(H22B	108.0

H22A(C22(H22B	107.2

C22(C23(C24	114.4(3)

C22(C23(H23A	108.7

C24(C23(H23A	108.7

C22(C23(H23B	108.7

C24(C23(H23B	108.7

H23A(C23(H23B	107.6

C15(C24(C19	117.3(3)

C15(C24(C23	121.1(3)

C19(C24(C23	121.5(3)

C8(N1(C7	125.9(2)

C8(N1(C15	117.8(2)

C7(N1(C15	116.3(2)

Symmetry transformations used to generate equivalent atoms:

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C1	49(2) 	40(2)	57(2) 	(5(1)	(9(1) 	2(1)

C2	69(2) 	66(2)	62(2) 	(5(2)	(20(2) 	2(2)

C3	133(4) 	91(3)	106(3) 	(21(3)	(73(3) 	(2(3)

C4	107(4) 	191(6)	115(4) 	(65(4)	24(3) 	(93(4)

C5	55(2) 	73(3)	124(3) 	(29(2)	15(2) 	(19(2)

C6	50(2) 	53(2)	64(2) 	(5(2)	(2(1) 	(7(2)

C7	53(2) 	41(2)	48(1) 	0(1)	(5(1) 	(3(1)

C8	52(2) 	44(2)	53(2) 	4(1)	(8(1) 	(4(1)

C9	51(2) 	36(2)	63(2) 	0(1)	(10(1) 	5(1)

C10	63(2) 	54(2)	68(2) 	(5(2)	4(2) 	(2(2)

C11	90(3) 	79(3)	84(2) 	(25(2)	17(2) 	3(2)

C12	87(3) 	66(3)	106(3) 	(27(2)	(3(2) 	2(2)

C13	143(4) 	49(2)	112(3) 	(14(2)	2(3) 	(1(3)

C14	90(2) 	37(2)	75(2) 	5(1)	(9(2) 	7(2)

C15	50(2) 	40(2)	48(1) 	(2(1)	(8(1) 	(4(1)

C16	49(2) 	62(2)	55(2) 	(4(1)	(1(1) 	(2(2)

C17	69(2) 	70(2)	55(2) 	(14(2)	5(1) 	5(2)

C18	78(2) 	51(2)	56(2) 	(13(1)	(11(2) 	(6(2)

C19	54(2) 	46(2)	60(2) 	0(1)	(12(1) 	(8(2)

C20	73(2) 	65(2)	88(2) 	(3(2)	(14(2) 	(23(2)

C21	71(3) 	180(6)	167(5) 	(52(5)	26(3) 	(57(4)

C22	80(3) 	91(3)	162(4) 	(24(3)	47(3) 	(18(3)

C23	58(2) 	56(2)	81(2) 	(8(2)	9(2) 	0(2)

C24	46(1) 	41(2)	53(1) 	1(1)	(7(1) 	(1(1)

N1	50(1) 	34(1)	49(1) 	(1(1)	(9(1) 	(4(1)

O1	90(2) 	47(1)	69(1) 	14(1)	(23(1) 	(12(1)

O2	98(2) 	56(2)	67(1) 	3(1)	(32(1) 	2(1)

Table 5. Torsion angles [°].

C6(C1(C2(C3	(4.3(5)

C7(C1(C2(C3	172.3(3)

C1(C2(C3(C4	22.2(7)

C2(C3(C4(C5	(32.9(9)

C3(C4(C5(C6	24.1(9)

C2(C1(C6(C5	(3.0(5)

C7(C1(C6(C5	(179.5(3)

C4(C5(C6(C1	(6.3(6)

C6(C1(C7(O1	140.1(3)

C2(C1(C7(O1	(36.5(4)

C6(C1(C7(N1	(35.7(4)

C2(C1(C7(N1	147.6(3)

O2(C8(C9(C10	131.9(3)

N1(C8(C9(C10	(45.4(4)

O2(C8(C9(C14	(43.6(4)

N1(C8(C9(C14	139.1(3)

C14(C9(C10(C11	(2.3(5)

C8(C9(C10(C11	(177.7(3)

C9(C10(C11(C12	5.6(6)

C10(C11(C12(C13	(12.6(7)

C11(C12(C13(C14	16.1(7)

C12(C13(C14(C9	(12.2(7)

C10(C9(C14(C13	5.6(6)

C8(C9(C14(C13	(178.8(4)

C24(C15(C16(C17	(1.0(5)

N1(C15(C16(C17	178.1(3)

C15(C16(C17(C18	1.1(5)

C16(C17(C18(C19	(1.3(5)

C17(C18(C19(C24	1.3(5)

C17(C18(C19(C20	(177.3(3)

C18(C19(C20(C21	(171.9(4)

C24(C19(C20(C21	9.5(5)

C19(C20(C21(C22	(32.5(7)

C20(C21(C22(C23	46.3(8)

C21(C22(C23(C24	(34.5(7)

C16(C15(C24(C19	0.9(4)

N1(C15(C24(C19	(178.1(2)

C16(C15(C24(C23	178.7(3)

N1(C15(C24(C23	(0.3(4)

C18(C19(C24(C15	(1.1(4)

C20(C19(C24(C15	177.5(3)

C18(C19(C24(C23	(178.9(3)

C20(C19(C24(C23	(0.3(4)

C22(C23(C24(C15	(165.9(4)

C22(C23(C24(C19	11.8(5)

O2(C8(N1(C7	165.1(3)

C9(C8(N1(C7	(17.6(4)

O2(C8(N1(C15	(15.1(4)

C9(C8(N1(C15	162.2(2)

O1(C7(N1(C8	147.5(3)

C1(C7(N1(C8	(36.6(4)

O1(C7(N1(C15	(32.3(4)

C1(C7(N1(C15	143.6(3)

C16(C15(N1(C8	100.0(3)

C24(C15(N1(C8	(80.9(3)

C16(C15(N1(C7	(80.1(3)

C24(C15(N1(C7	98.9(3)

Symmetry transformations used to generate equivalent atoms: