|  | University of Southampton · Department of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	03src0410

Empirical formula 	C7H6O4S3

Formula weight 	250.30

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P21/c

Unit cell dimensions	a = 13.1537(7) Å	( = 90°

b = 9.3992(4) Å	( = 103.221(2)°

c = 8.0242(3) Å	(  = 90°

Volume	965.77(8) Å3

Z	4

Density (calculated)	1.721 Mg / m3

Absorption coefficient	0.750 mm(1

F(000)	512

Crystal	block; yellow

Crystal size	0.14 ( 0.10 ( 0.08 mm3

( range for data collection	3.18 ( 27.49°

Index ranges	(17 ( h ( 15, (10 ( k ( 11, (10 ( l ( 10

Reflections collected	9676

Independent reflections	2195 [Rint = 0.0494]

Completeness to ( = 27.49°	99.1 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.9425 and 0.9023

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	2195 / 0 / 130

Goodness-of-fit on F2	1.061

Final R indices [F2 > 2((F2)]	R1 = 0.0283, wR2 = 0.0709

R indices (all data)	R1 = 0.0309, wR2 = 0.0728

Extinction coefficient	0.008(2)

Largest diff. peak and hole	0.323 and (0.315 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing, Acta Cryst. A51 (1995) 33(37; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421(426). Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: Cameron - A Molecular Graphics Package. (D. M. Watkin, L. Pearce and C. K. Prout, Chemical Crystallography Laboratory, University of Oxford, 1993).

Special details:

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C1	4517(1)	7593(2)	1015(2)	17(1)	1

C2	2641(1)	7545(2)	1550(2)	17(1)	1

C3	1569(1)	8030(2)	1644(2)	18(1)	1

C4	598(1)	9818(2)	2607(2)	24(1)	1

C5	2927(1)	6166(2)	1529(2)	17(1)	1

C6	2298(1)	4919(2)	1885(2)	18(1)	1

C7	1918(1)	2512(2)	1200(2)	26(1)	1

O1	790(1)	7362(1)	1063(2)	30(1)	1

O2	1605(1)	9284(1)	2417(1)	21(1)	1

O3	1820(1)	4897(1)	2991(2)	24(1)	1

O4	2397(1)	3840(1)	857(1)	22(1)	1

S1	3565(1)	8800(1)	1292(1)	18(1)	1

S2	4160(1)	5833(1)	1198(1)	19(1)	1

S3	5644(1)	8039(1)	609(1)	22(1)	1

Table 3. Bond lengths [Å] and angles [°].

C1(S3	1.6434(15)

C1(S2	1.7349(15)

C1(S1	1.7410(15)

C2(C5	1.351(2)

C2(C3	1.500(2)

C2(S1	1.7400(15)

C3(O1	1.2012(19)

C3(O2	1.3281(19)

C4(O2	1.4572(18)

C4(H4A	0.9800

C4(H4B	0.9800

C4(H4C	0.9800

C5(C6	1.499(2)

C5(S2	1.7307(16)

C6(O3	1.2000(19)

C6(O4	1.3318(19)

C7(O4	1.4526(19)

C7(H7A	0.9800

C7(H7B	0.9800

C7(H7C	0.9800

S3(C1(S2	122.28(9)

S3(C1(S1	124.52(9)

S2(C1(S1	113.20(8)

C5(C2(C3	123.99(13)

C5(C2(S1	116.44(11)

C3(C2(S1	119.39(11)

O1(C3(O2	125.58(14)

O1(C3(C2	123.40(14)

O2(C3(C2	111.02(13)

O2(C4(H4A	109.5

O2(C4(H4B	109.5

H4A(C4(H4B	109.5

O2(C4(H4C	109.5

H4A(C4(H4C	109.5

H4B(C4(H4C	109.5

C2(C5(C6	125.52(14)

C2(C5(S2	116.62(11)

C6(C5(S2	117.72(11)

O3(C6(O4	125.96(14)

O3(C6(C5	124.00(14)

O4(C6(C5	109.96(13)

O4(C7(H7A	109.5

O4(C7(H7B	109.5

H7A(C7(H7B	109.5

O4(C7(H7C	109.5

H7A(C7(H7C	109.5

H7B(C7(H7C	109.5

C3(O2(C4	114.72(12)

C6(O4(C7	115.40(12)

C2(S1(C1	96.65(7)

C5(S2(C1	97.03(7)

Symmetry transformations used to generate equivalent atoms:

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C1	15(1) 	20(1)	16(1) 	2(1)	2(1) 	(1(1)

C2	13(1) 	18(1)	20(1) 	0(1)	3(1) 	(2(1)

C3	15(1) 	17(1)	22(1) 	2(1)	3(1) 	0(1)

C4	17(1) 	25(1)	33(1) 	1(1)	11(1) 	5(1)

C5	14(1) 	18(1)	19(1) 	0(1)	3(1) 	(1(1)

C6	12(1) 	17(1)	23(1) 	1(1)	1(1) 	0(1)

C7	27(1) 	16(1)	34(1) 	(1(1)	6(1) 	(6(1)

O1	14(1) 	26(1)	48(1) 	(7(1)	3(1) 	(1(1)

O2	14(1) 	18(1)	32(1) 	(3(1)	9(1) 	0(1)

O3	20(1) 	22(1)	33(1) 	0(1)	12(1) 	(3(1)

O4	23(1) 	16(1)	27(1) 	(2(1)	8(1) 	(4(1)

S1	14(1) 	15(1)	25(1) 	1(1)	5(1) 	(1(1)

S2	15(1) 	16(1)	26(1) 	1(1)	7(1) 	0(1)

S3	16(1) 	24(1)	28(1) 	0(1)	9(1) 	(3(1)