|  | University of Southampton · Department of Chemistry EPSRC National Crystallography Service |  |
| --- | --- | --- |

Table 1. Crystal data and structure refinement.

Identification code 	02src649

Empirical formula 	C26H20FeN2O2

Formula weight 	448.29

Temperature 	120(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P21/c

Unit cell dimensions	a = 13.0933(5) Å	( = 90°

b = 10.3440(4) Å	( = 111.319(2)°

c = 15.4112(7) Å	(  = 90°

Volume	1944.42(14) Å3

Z	4

Density (calculated)	1.531 Mg / m3

Absorption coefficient	0.803 mm(1

F(000)	928

Crystal	plate; dark

Crystal size	0.50 ( 0.28 ( 0.12 mm3

( range for data collection	3.34 ( 27.49°

Index ranges	(14 ( h ( 17, (13 ( k ( 13, (20 ( l ( 18

Reflections collected	16057

Independent reflections	4424 [Rint = 0.0534]

Completeness to ( = 27.49°	99.2 %

Absorption correction	Semi(empirical from equivalents

Max. and min. transmission	0.9097 and 0.6895

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	4424 / 0 / 281

Goodness-of-fit on F2	1.027

Final R indices [F2 > 2((F2)]	R1 = 0.0358, wR2 = 0.0844

R indices (all data)	R1 = 0.0511, wR2 = 0.0920

Extinction coefficient	0.0000(5)

Largest diff. peak and hole	0.462 and (0.555 e Å(3

Diffractometer: Nonius KappaCCD area detector (( scans and ( scans to fill asymmetric unit sphere). Cell determination: DirAx (Duisenberg, A.J.M.(1992). J. Appl. Cryst. 25, 92-96.) Data collection: Collect (Collect: Data collection software, R. Hooft, Nonius B.V., 1998). Data reduction and cell refinement: Denzo (Z. Otwinowski & W. Minor, Methods in Enzymology (1997) Vol. 276: Macromolecular Crystallography, part A, pp. 307(326; C. W. Carter, Jr. & R. M. Sweet, Eds., Academic Press). Absorption correction: SORTAV (R. H. Blessing, Acta Cryst. A51 (1995) 33(37; R. H. Blessing, J. Appl. Cryst. 30 (1997) 421(426). Structure solution: SHELXS97 (G. M. Sheldrick, Acta Cryst. (1990) A46 467(473). Structure refinement: SHELXL97 (G. M. Sheldrick (1997), University of Göttingen, Germany). Graphics: Cameron - A Molecular Graphics Package. (D. M. Watkin, L. Pearce and C. K. Prout, Chemical Crystallography Laboratory, University of Oxford, 1993).

Special details:

Table 2. Atomic coordinates [( 104], equivalent isotropic displacement parameters [Å2 ( 103] and site occupancy factors. Ueq is defined as one third of the trace of the orthogonalized Uij tensor.

Atom 	x	y	z	Ueq	S.o.f.

C1	5218(1)	7247(2)	3096(1)	18(1)	1

C2	4403(1)	6354(2)	3162(1)	20(1)	1

C3	3563(2)	7090(2)	3302(1)	23(1)	1

C4	3824(2)	8423(2)	3306(1)	23(1)	1

C5	4836(1)	8522(2)	3176(1)	19(1)	1

C6	6208(1)	6879(2)	2947(1)	18(1)	1

C7	7038(1)	7662(2)	2993(1)	19(1)	1

C8	8025(2)	7137(2)	2886(1)	19(1)	1

C9	9019(1)	7982(2)	3115(1)	18(1)	1

C10	9992(2)	9739(2)	3875(1)	25(1)	1

C11	10865(2)	9457(2)	3601(1)	24(1)	1

C12	10780(2)	8392(2)	3040(1)	25(1)	1

C13	9853(2)	7621(2)	2804(1)	20(1)	1

C14	3800(2)	7371(2)	754(1)	19(1)	1

C15	2991(2)	6510(2)	865(1)	22(1)	1

C16	2197(2)	7268(2)	1059(1)	24(1)	1

C17	2496(2)	8593(2)	1070(1)	23(1)	1

C18	3481(2)	8657(2)	891(1)	21(1)	1

C19	4782(1)	6951(2)	610(1)	19(1)	1

C20	5614(2)	7708(2)	610(1)	20(1)	1

C21	6569(2)	7154(2)	469(1)	20(1)	1

C22	7534(2)	8025(2)	579(1)	19(1)	1

C23	8461(2)	9898(2)	1133(1)	27(1)	1

C24	9312(2)	9550(2)	849(1)	26(1)	1

C25	9244(2)	8387(2)	394(1)	25(1)	1

C26	8341(2)	7601(2)	256(1)	22(1)	1

N1	9073(1)	9035(1)	3638(1)	22(1)	1

N2	7574(1)	9162(1)	1004(1)	23(1)	1

O1	8078(1)	6017(1)	2635(1)	26(1)	1

O2	6623(1)	6013(1)	268(1)	25(1)	1

Fe1	3711(1)	7582(1)	2061(1)	17(1)	1

Table 3. Bond lengths [Å] and angles [°].

C1(C5	1.432(2)

C1(C2	1.443(2)

C1(C6	1.447(2)

C1(Fe1	2.0660(17)

C2(C3	1.416(3)

C2(Fe1	2.0484(17)

C2(H2	0.9500

C3(C4	1.420(3)

C3(Fe1	2.0543(18)

C3(H3	0.9500

C4(C5	1.413(3)

C4(Fe1	2.0619(17)

C4(H4	0.9500

C5(Fe1	2.0559(17)

C5(H5	0.9500

C6(C7	1.338(2)

C6(H6	0.9500

C7(C8	1.464(3)

C7(H7	0.9500

C8(O1	1.232(2)

C8(C9	1.499(3)

C9(N1	1.341(2)

C9(C13	1.395(2)

C10(N1	1.340(2)

C10(C11	1.386(3)

C10(H10	0.9500

C11(C12	1.380(3)

C11(H11	0.9500

C12(C13	1.386(3)

C12(H12	0.9500

C13(H13	0.9500

C14(C18	1.433(2)

C14(C15	1.440(3)

C14(C19	1.449(3)

C14(Fe1	2.0708(18)

C15(C16	1.419(3)

C15(Fe1	2.0626(17)

C15(H15	0.9500

C16(C17	1.424(3)

C16(Fe1	2.0474(18)

C16(H16	0.9500

C17(C18	1.415(3)

C17(Fe1	2.0471(18)

C17(H17	0.9500

C18(Fe1	2.0461(17)

C18(H18	0.9500

C19(C20	1.342(3)

C19(H19	0.9500

C20(C21	1.462(3)

C20(H20	0.9500

C21(O2	1.228(2)

C21(C22	1.511(3)

C22(N2	1.338(2)

C22(C26	1.392(3)

C23(N2	1.342(2)

C23(C24	1.384(3)

C23(H23	0.9500

C24(C25	1.379(3)

C24(H24	0.9500

C25(C26	1.386(3)

C25(H25	0.9500

C26(H26	0.9500

C5(C1(C2	107.05(16)

C5(C1(C6	128.13(16)

C2(C1(C6	124.80(16)

C5(C1(Fe1	69.30(10)

C2(C1(Fe1	68.81(10)

C6(C1(Fe1	125.52(12)

C3(C2(C1	107.53(16)

C3(C2(Fe1	70.03(10)

C1(C2(Fe1	70.12(10)

C3(C2(H2	126.2

C1(C2(H2	126.2

Fe1(C2(H2	125.2

C2(C3(C4	108.90(16)

C2(C3(Fe1	69.58(10)

C4(C3(Fe1	70.10(10)

C2(C3(H3	125.6

C4(C3(H3	125.6

Fe1(C3(H3	126.3

C5(C4(C3	107.82(16)

C5(C4(Fe1	69.70(10)

C3(C4(Fe1	69.52(10)

C5(C4(H4	126.1

C3(C4(H4	126.1

Fe1(C4(H4	126.3

C4(C5(C1	108.69(15)

C4(C5(Fe1	70.16(10)

C1(C5(Fe1	70.06(10)

C4(C5(H5	125.7

C1(C5(H5	125.7

Fe1(C5(H5	125.7

C7(C6(C1	126.15(16)

C7(C6(H6	116.9

C1(C6(H6	116.9

C6(C7(C8	120.16(16)

C6(C7(H7	119.9

C8(C7(H7	119.9

O1(C8(C7	122.49(16)

O1(C8(C9	118.63(16)

C7(C8(C9	118.86(15)

N1(C9(C13	123.17(16)

N1(C9(C8	117.81(16)

C13(C9(C8	118.99(16)

N1(C10(C11	124.14(17)

N1(C10(H10	117.9

C11(C10(H10	117.9

C12(C11(C10	118.14(17)

C12(C11(H11	120.9

C10(C11(H11	120.9

C11(C12(C13	119.18(17)

C11(C12(H12	120.4

C13(C12(H12	120.4

C12(C13(C9	118.46(17)

C12(C13(H13	120.8

C9(C13(H13	120.8

C18(C14(C15	106.91(16)

C18(C14(C19	128.57(16)

C15(C14(C19	124.33(16)

C18(C14(Fe1	68.70(10)

C15(C14(Fe1	69.31(10)

C19(C14(Fe1	123.22(12)

C16(C15(C14	108.01(16)

C16(C15(Fe1	69.23(10)

C14(C15(Fe1	69.92(10)

C16(C15(H15	126.0

C14(C15(H15	126.0

Fe1(C15(H15	126.4

C15(C16(C17	108.43(16)

C15(C16(Fe1	70.39(10)

C17(C16(Fe1	69.65(10)

C15(C16(H16	125.8

C17(C16(H16	125.8

Fe1(C16(H16	125.8

C18(C17(C16	107.96(16)

C18(C17(Fe1	69.74(10)

C16(C17(Fe1	69.67(10)

C18(C17(H17	126.0

C16(C17(H17	126.0

Fe1(C17(H17	126.1

C17(C18(C14	108.68(16)

C17(C18(Fe1	69.82(10)

C14(C18(Fe1	70.56(10)

C17(C18(H18	125.7

C14(C18(H18	125.7

Fe1(C18(H18	125.5

C20(C19(C14	126.23(17)

C20(C19(H19	116.9

C14(C19(H19	116.9

C19(C20(C21	120.63(17)

C19(C20(H20	119.7

C21(C20(H20	119.7

O2(C21(C20	123.03(17)

O2(C21(C22	118.63(17)

C20(C21(C22	118.34(16)

N2(C22(C26	123.49(17)

N2(C22(C21	117.54(16)

C26(C22(C21	118.96(16)

N2(C23(C24	123.96(17)

N2(C23(H23	118.0

C24(C23(H23	118.0

C25(C24(C23	118.48(18)

C25(C24(H24	120.8

C23(C24(H24	120.8

C24(C25(C26	118.90(18)

C24(C25(H25	120.6

C26(C25(H25	120.6

C25(C26(C22	118.46(17)

C25(C26(H26	120.8

C22(C26(H26	120.8

C10(N1(C9	116.85(16)

C23(N2(C22	116.69(16)

C18(Fe1(C17	40.44(7)

C18(Fe1(C16	68.22(7)

C17(Fe1(C16	40.69(7)

C18(Fe1(C2	161.16(7)

C17(Fe1(C2	157.63(8)

C16(Fe1(C2	122.84(8)

C18(Fe1(C3	157.15(8)

C17(Fe1(C3	120.71(8)

C16(Fe1(C3	105.70(8)

C2(Fe1(C3	40.39(7)

C18(Fe1(C5	108.08(7)

C17(Fe1(C5	120.52(7)

C16(Fe1(C5	155.26(7)

C2(Fe1(C5	68.56(7)

C3(Fe1(C5	67.71(7)

C18(Fe1(C4	121.87(7)

C17(Fe1(C4	104.59(7)

C16(Fe1(C4	119.45(8)

C2(Fe1(C4	68.32(7)

C3(Fe1(C4	40.38(7)

C5(Fe1(C4	40.14(7)

C18(Fe1(C15	68.36(7)

C17(Fe1(C15	68.25(7)

C16(Fe1(C15	40.38(7)

C2(Fe1(C15	109.15(7)

C3(Fe1(C15	122.16(8)

C5(Fe1(C15	163.11(7)

C4(Fe1(C15	156.04(8)

C18(Fe1(C1	124.38(7)

C17(Fe1(C1	157.88(7)

C16(Fe1(C1	161.19(8)

C2(Fe1(C1	41.06(7)

C3(Fe1(C1	68.08(7)

C5(Fe1(C1	40.64(7)

C4(Fe1(C1	68.10(7)

C15(Fe1(C1	126.69(7)

C18(Fe1(C14	40.73(7)

C17(Fe1(C14	68.37(7)

C16(Fe1(C14	68.33(7)

C2(Fe1(C14	125.18(7)

C3(Fe1(C14	159.51(7)

C5(Fe1(C14	125.85(7)

C4(Fe1(C14	159.82(7)

C15(Fe1(C14	40.78(7)

C1(Fe1(C14	110.93(7)

Symmetry transformations used to generate equivalent atoms:

Table 4. Anisotropic displacement parameters [Å2( 103]. The anisotropic displacement

factor exponent takes the form: (2( 2[h2a*2U11 + ... + 2 h k a* b* U12 ].

Atom	U11	U22	U33	U23	U13	U12

C1	14(1) 	25(1)	15(1) 	1(1)	4(1) 	1(1)

C2	17(1) 	23(1)	21(1) 	2(1)	7(1) 	0(1)

C3	17(1) 	33(1)	20(1) 	4(1)	9(1) 	0(1)

C4	22(1) 	29(1)	16(1) 	(3(1)	7(1) 	4(1)

C5	18(1) 	22(1)	17(1) 	(1(1)	5(1) 	(1(1)

C6	16(1) 	21(1)	14(1) 	1(1)	4(1) 	2(1)

C7	16(1) 	21(1)	20(1) 	0(1)	6(1) 	1(1)

C8	18(1) 	23(1)	17(1) 	2(1)	7(1) 	0(1)

C9	17(1) 	21(1)	16(1) 	4(1)	6(1) 	1(1)

C10	26(1) 	25(1)	25(1) 	(2(1)	11(1) 	(6(1)

C11	18(1) 	27(1)	26(1) 	5(1)	6(1) 	(6(1)

C12	17(1) 	30(1)	30(1) 	4(1)	12(1) 	1(1)

C13	18(1) 	23(1)	22(1) 	1(1)	8(1) 	2(1)

C14	16(1) 	24(1)	15(1) 	(1(1)	2(1) 	(2(1)

C15	19(1) 	24(1)	21(1) 	(4(1)	4(1) 	(2(1)

C16	13(1) 	33(1)	24(1) 	(2(1)	4(1) 	(3(1)

C17	16(1) 	28(1)	22(1) 	(1(1)	3(1) 	5(1)

C18	21(1) 	23(1)	16(1) 	2(1)	3(1) 	1(1)

C19	19(1) 	23(1)	14(1) 	(2(1)	4(1) 	2(1)

C20	19(1) 	23(1)	17(1) 	(3(1)	5(1) 	1(1)

C21	19(1) 	26(1)	14(1) 	0(1)	5(1) 	2(1)

C22	18(1) 	23(1)	16(1) 	3(1)	6(1) 	2(1)

C23	23(1) 	24(1)	33(1) 	(3(1)	10(1) 	(1(1)

C24	19(1) 	30(1)	29(1) 	6(1)	7(1) 	(1(1)

C25	21(1) 	34(1)	22(1) 	6(1)	11(1) 	5(1)

C26	22(1) 	28(1)	17(1) 	1(1)	7(1) 	3(1)

N1	20(1) 	25(1)	23(1) 	0(1)	11(1) 	(4(1)

N2	20(1) 	24(1)	26(1) 	0(1)	9(1) 	1(1)

O1	23(1) 	22(1)	36(1) 	(6(1)	15(1) 	(2(1)

O2	24(1) 	23(1)	30(1) 	(4(1)	11(1) 	1(1)

Fe1	13(1) 	20(1)	17(1) 	0(1)	5(1) 	0(1)